## Slide 1
Irradiation test setup @CSNS
Irradiated in 80 MeV proton beam at China Spallation Neutron Source (CSNS) in April 2024
2 sensors placed at each test point
  1 IV/CV tested + 1 new
Aluminum foil pieces placed at each point to calibrate irradiation fluence
Irradiated IV change
With bias of -50V, leakage current increases from ∼ 10 pA to ∼ 1nA after irradiated. The magnitude of leakage current is proportional to the irradiation fluence
Irradiation Tolerance Evaluation
Time over Threshold (ToT) versus Threshold
ToT and noise rate as a function of the threshold reference for all tested samples different voltages and irradiation fluence. Results are shown for chips settings at room temperature.
Time over Threshold (ToT) is correlated with the energy of a signal
An increase in ToT leads to an increase in the depletion voltage
Under an irradiation fluence of , the chip can still maintain normal operation.
Inflection Point of S-curve for pixels
Inflection point of the S-curve as a function of charge injection for different irradiated chips. Results are shown for HV = -10V settings at room temperature
Show the noise level of the pixel
Systematic right-shift of inflection point distribution with increased fluence
An increase in the irradiation fluence leads to a reduction in pixel uniformity
The COFFEE2 chip demonstrated excellent irradiation tolerance, confirming the resilience of the 55nm HV-CMOS process. It remained fully functional with only minor performance degradation up to an accumulated fluence of 10¹⁴ 𝑛ₑq/cm². The observed degradation primarily manifested as a slight shift in the S-curve inflection point and a minor broadening of its distribution; nevertheless, the overall performance was well maintained. Furthermore, it was found that applying a higher bias voltage improved charge collection efficiency and increased the depletion depth, which consequently helped recover performance parameters.
Future work involves more detailed test including radioactive source test and test beam measurement.
Irradiation study of COFFEE2, the first 55nm
High Voltage CMOS sensor prototype
Tianyu Shi1,2, Mingjie Feng1,2, Yiming Li1, Jianchun Wang1, Zhiyu Xiang3, Zijun Xu1, Xuhao Yuan1, Cheng Zeng1,2, Hui Zhang1
1Institute of High Energy Physics, CAS, Beijing, China 2University of Chinese Academy of Sciences 3Central South University
To meet the increasingly demanding requirements of future tracking detectors for the CEPC and LHCb Upgrade II, advanced detector technologies with enhanced hit density processing capabilities and enhanced radiation tolerance are essential. To study the sensor performance and electronic response in the next generation process of High Voltage CMOS (HV-CMOS), the sensor chip called COFFEE2, the first prototype for process and circuit module in a 55 nm
Irradiation Test
Introduction
The 2025 International Workshop on the High Energy Circular Electron Positron Collider (CEPC2025）
Email: shity@ihep.ac.cn
One pixel
Summary & Outlook
Process Features
Laser response
AM-241 response
Chip Response to Charge Injection(a); ToT vs. Thershold in different Irradiation fluence (b);
ToT vs. Threshold in different bias voltage(c)
High-Voltage Technology, is designed and tested. A comprehensive irradiation tolerance testing campaign was conducted on the COFFEE2 chip. Utilizing the KIT pixel array, which boasts a fully integrated readout system, this work presents the first irradiation tolerance study of the 55 nm High-Voltage CMOS process.
Deep n-well - P substrate junction as collection electrode
Triple-well process: N-well/P-well/Deep n-well
P-type substrate resistivity: 10·cm
Guard ring: one inner N-well ring, with two P-well outer rings
Substrate breakdown Voltage > 50V with frontside HV bias
More design details:
  Z. Chen et al., Feasibility study of CMOS sensors in 55 nm process for tracking, Nuclear Instruments and Methods in Physics Research A 1069 (2024) 169905.
  H. Zhang, et al., High voltage monolithic pixel sensor in 55 nm technology, JINST 20 (2025) 03, C03023
Pixel electronics (25 μm 25 μm )
  Sensor diode
  Charge Sensitive Amplifier (CSA)
  CR filter
  Comparator
  RAM and tune DAC
  Output stages
Work principle
  Charge collected by pixel n-well
  Converted to voltage signal by Charge Sensitive Amplifier
  Analog voltage pulse shaped and converted to digital signal by comparator
  Output stage generates current
  Current is sent via address line to the transimpedance amplifier outside matrix
  Address lines have constant potential – no cross talk
Genesys2 FPGA Board
  Translates commands from the PC into the precise low-level digital protocol
GECCO Control Readout Board
  It integrates power delivery and controls and supplies all required electrical potentials for testing the chip
Carrier Board (with wire-bonded COFFEE2 chip)
Signal Generator
  Provide charge injection to the chip through the GECCO board
IV test results of COFFEE2 in different irradiation fluence
(a)
(b)
(c)
Main array
Passive
Sensor diode
KIT array
KIT Pixel Electronics
Bench test setup
H. Zhang, et al. High voltage monolithic pixel sensor in 55nm technology
JINST 20 (2025) 03, C03023
Fluence [neq/cm2] | 3.2 × 1011 | 4.9× 1012 | 5.7 × 1013 | 1.6 × 1014 | 1.3 × 1015
Temperature | Room temperature |  |  |  | -28°C
Test box
Dry air
Cooling water
Peltier
Graphite
sheets
Sensor
Main results
0.57 nA
0.59 nA
0.65 nA
1.06 nA
ToT
Charge Injection
SFOut
Digital Output
The inflection Point of S-curve (a); The distribution of inflection point in bias voltage of -10V(b),-20V(c),-30V(d);
(a)
(b)
(d)
(c)