## Slide 1
Progress of the High Field Magnet R&D
for Next-generation High Energy Accelerators
Qingjin XU
Institute of High Energy Physics,
Chinese Academy of Sciences
10 Nov 2025
The 2025 International Workshop on the High Energy Circular Electron Positron Collider (CEPC2025), Guangzhou, 6-10 Nov 2025

## Slide 2
Roadmap of the High Field Magnet R&D at IHEP
2
Challenges: Stress control, quench protection, field quality control,……
2018-2021, 12.47T @4.2K
NbTi + Nb3Sn
2021-2025 16T @ 4.2K
CEPC-SPPC
FCC
NEXT-GENERATION PARTICLE ACCELERATORS

## Slide 3
Development of the Model Dipole LPF3
Latest design: Target field：10 T (LTS) + 6 T (HTS) at 4.2 K
3
AP: 75 mm
75 mm
3
LTS: Nb3Sn common coils with shell-based structure, aperture: 2* 78 mm
HTS: ReBCO racetracks, stacked tapes with MI insulation, aperture: 16*24 mm2
HFM team @ IHEP-CAS

## Slide 4
Development of the Model Dipole LPF3
LPF3-U 磁体组装完成
2024.11.22
Nb3Sn coils reached 9.8 T, 98 % of the design value.
Coupling between HTS & LTS caused difficulties to the training of LTS
Most of quenches occured in the inner Nb3Sn coils.
LTS still have potential for performance improvement. More R&D needed on training tests……
Main challenges: The LTS coils are strongly coupled with the HTS coils in magnetic field and stress during LTS training. the HTS induced current enhance the field strength and stress of the adjacent LTS coils, and the frequent training quench of LTS cause irreversible degradation of the HTS coils.
Common-coil dipole with 78-mm gap
4
Test of the LPF3-U magnet at 4.2 K Nov. 2024 to Jan. 2025

## Slide 5
Development of the Model Dipole LPF3
The HTS coils subjected to several excitation tests in both self-field and 9 T background field, with a maximum excitation current of 2.5 kA (115 % of the design current) in 9 T background field, but generally degraded along with the training of LTS coils, and provided a magnetic field significantly below the design value with long delay.
5
1st HTS test with 9 T BG field
HTS Stand-alone test @77 K
Training of LTS coils
1st HTS test with 9 T BG field
LTS training
HTS Test after assembly @77 K
2nd HTS test with 9 T field
3rd HTS test with 9 T field
2nd HTS test with 9 T BG field
3rd HTS test with 9 T BG field
Test of the LPF3-U magnet at 4.2 K Nov. 2024 to Jan. 2025

## Slide 6
Development of the Model Dipole LPF3
Disassembly of the magnet and HTS coils in Jan 2025
After disassembly, Serious damage of the outer HTS coils observed: conductor delamination, damage of layer insulation..., caused by strong coupling (between LTS and HTS) induced electromagnetic forces during the training of LTS
After testing, the coil surface is not flat
Delamination
Damage in interturn between layers
Damage of layer insulation
6

## Slide 7
Development of the Model Dipole LPF3
Refabrication of the new HTS coils in Spring 2025
To reduce time delay of field, the layer insulation in the coil was replaced from stainless steel to G10
To reduce the impact of LTS quench to HTS, high-purity copper and HTS tapes were deployed around the HTS coil
7

## Slide 8
Development of the Model Dipole LPF3
Refabrication and test of the new HTS coils in Summer 2025
HTS stand alone: 2159 A, 7.6 T in the aperture@ 4.2 K
Maximum field on the coil (calculated): ~10 T
Performance limited by a power failure: current discharged in 1 s
Power failure at 2159 A damaged 1 of 6 HTS coils
Resistive voltage appeared in #5 coil from ~800 A;
bypassing #5 coil for the following tests
8

## Slide 9
Development of the Model Dipole LPF3
Refabrication and test of the new HTS coils in Summer 2025
5 HTS coils 1st powering with LTS: unexpected current ripple triggered the quench protection circuit, then #3 HTS coil quenched, and LTS was triggered after 1.355 s. After that, #2 HTS coil also quenched. HTS coils current decay: ~2.7 s
1st HTS powering with Nb3Sn at 4.2 K,
Quench at HTS 2049 A & LTS 5550 A (bypassing #5 HTS coil)
Voltage and current variations during the quench
9

## Slide 10
Development of the Model Dipole LPF3
10
2nd HTS powering with Nb3Sn at 4.2K
Quench at HTS 1959 A & LTS 6130 A (bypassing #5 HTS coil)
Field map within the aperture. The highest field in the HTS coil ~16.2T (calculated)
Dipole field along the major axis
Refabrication and test of the new HTS coils in Summer 2025
2nd powering with LTS: #3 HTS coil quench at 1959A, and after 0.4156s, the LTS quench detection system triggered. The current decay time of HTS is 1.3 s, and LTS is 0.7718 s;
Voltage and current variations during the quench

## Slide 11
Development of the Model Dipole LPF3
Refabrication and test of the new HTS coils in Summer 2025
Power failure damaged coil (#5 coil) during the stand-alone test: conductor partially burned at the coil end
Quench at 14 T damaged coil (#3 coil) during powering with Nb3Sn coils: conductor burned at the bending section
New ReBCO coils to be fabricated and tested again by the end of this year
11
#3 coil inner
#5 coil
#3 coil outer

## Slide 12
IBS Technology: Status and Outlook
12

## Slide 13
In 2024, the Jc of long wires has been increased to 105 A/cm2 @ 4.2 K, 10 T by optimizing fabrication process
IBS Technology: Status and Outlook
13
100m long, 7-core Ba122 tapes are fabricated by rolling process, and the Jc is continuously improving.
8倍
Ic >300A, Jc >105 A/cm2
Powder-In-Tube 122 tapes: Long length

## Slide 14
IBS Technology: Status and Outlook
In 15~17K, when the transmission current of iron-based superconductor is 14-179A, the corresponding NZPV value is 0.4– 7cm/s
14
Quench propagation study of the IBS tapes and coils

## Slide 15
IBS Technology: Status and Outlook
Ic of Φ34mm-17 turns-DPC reached 49 A at 4.2 K and 35 T
The First IBS Solenoid Coil at 35 T background field
15
2024 Supercond. Sci. Technol. 37 015001
Fabricated a series-connected IBS coil consisting of six DP coils and tested at 35T background field

## Slide 16
IBS Technology: Status and Outlook
Development of the first 7-kA class IBS transposed cable
16

## Slide 17
Lucio Rossi - HiLumi LHC to the CERN guides - Globe 26 February 2019
Q1
Q2a
Q2b
Q3
CP
D1
DFX
DFM
Connection to LHC (UL)
Service gallery (UR)
TAXS
Crab cavities
UA Gallery
Q4
Collimators
TAXN
Service cavern
SC Links
D2
O. Brüning @ HL-LHC Annual meeting in Geneva, 29th September 2025
Development of the CCT magnets for HL-LHC
17

## Slide 18
Development of the CCT magnets for HL-LHC
18

## Slide 19
Development of the CCT magnets for HL-LHC
Performance Test at CERN
All the delivered magnets have been successfully tested at CERN.
All the tested magnets reached the design target: field strength, field quality, operating stability…
19

## Slide 20
Summary
Long-term advanced high field magnet R&D is ongoing for future high-energy accelerators at IHEP-CAS
High Field model dipoles (LTS+HTS) are being developed at IHEP-CAS. ReBCO coils stand alone reached beyond 7 T dipole field in the aperture, beyond 14 T dipole field with Nb3Sn coils, but quench protection issue still to be solved
Significant improvement in Je of IBS tape achieved in May 2025, IBS coil Ic reached 49 A at 35 T. 7kA class IBS transposed cable successfully developed
Delivery of all HL-LHC CCT magnets expected to be completed by 2025. Continuous collaboration with CERN on HFM is expected for the next years
20
Thanks for your attention!