## Slide 1
Ping Chen
Xi’an Institute of Optics and Precision Mechanics
Chinese Academy of Sciences (XIOPM-CAS)
R&D on Photodetectors
chenping1@opt.ac.cn
25/07/2025
On behalf of the XIOPM Photodetector Group

## Slide 2
Outline
Introduction
Overview of MCP detectors
MCP detector characteristics
Prototypes and applications
Future plans

## Slide 3
Preface
2013.03-2015.02 Master &PhD student at XIOPM
Large aperture MCP-PMT simulations
Just getting to know MCP-PMTs
Learnt a lot from the collaboration meetings held very two months
Inspired a lot
MCP
Proposed and Patented by Yifang Wang et. al

## Slide 4
Supervised by Pierre Lebercq
Optimized 4.6-cell RF gun
Preface
2015.03-2016.02 CAS-CNRS joint PhD at LAL
RF gun simulations
La vie est bellle

## Slide 5
Preface
2017.02- Working at XIOPM
MCPs, MCP-PMTs, Imaging Intensifier, Hybrid photodetectors
2024.06- Joined in CERN DRD4 recommend by Guy Wilkinson
Development of Photon Detectors and Particle Identification Techniques
Working Package 2 (vacuum photodetectors ) leaded by Imad Laktineh

## Slide 6
Outlines
Outline
Introduction
Overview of MCP detectors
MCP detector characteristics
Prototypes and applications
Future plans

## Slide 7
Photomultiplier tubes (PMTs)
PMTs are the most common photodetectors in particle and nuclear detection
Single photon sensitive
High gain and low noise
Large sensitive area
Sensitive to scintillation light and Cherenkov light
Hamamatsu Handbook
Construction and Operation Principle of dynode PMTs

## Slide 8
PMT
SiPM
SiPM
Hamamatsu website
The signal-to-noise ratio of PMT is better than that of SiPM especially for few
photon detections.
Photomultiplier tubes (PMTs)

## Slide 9
J. Pe˜na-RodrÅLıguez. DRD4 meeting 2025 (BUW)
Assessment of 6 × 6mm2 SiPMs (Hamamatsu, Broadcom, OnSemi)
before/after neutron irradiation at the ˇReˇz Cyclotron (7 samples)
SiPM dark current increases drastically with the irradiation dose
Loss of the SiPM photon resolution after irradiation (Φ > 3×108neq/cm2)
SiPM radiation resistance assessment by J. Pe˜na-RodrÅLıguez
MCP-PMT radiation resistance assessment by Photonis
Photomultiplier tubes (PMTs)

## Slide 10
Microchannel plate (MCP)
MCP is an excellent secondary electron emission multiplier
Two-dimensional array of glass capillaries (channels with ~2-25 μm diameter) bundled in parallel in a MCP plate
Sensitive to electrons, ions, UV light
Able to detect soft or hard X-rays, neutrons etc if coated with proper photocathode like CsI, Au, CsTe or doped with proper material like B, Li for neutron detection and Pb for hard X-ray…
Construction and Operation Principle of MCPs

## Slide 11
Microchannel plate (MCP) detectors
MCP-PMTs
2-stage MCPs
Single photon sensitive
Fast timing resolution
<30 ps for single P.E. , <10 ps for multi P.Es
photon
electron
PC
MCP
anode
signal
electron cloud
< 10-5pa
Image intensifier
Usually one-stage MCP for high spatial resolution
Replace anode with phosphor screen for imaging
High spatial resolution
< 8 μm viewed with naked eye, < 20 μm with CMOS
Position sensitive MCP detectors
Replace single anode with position sensitive anodes
Anodes could be WSZ, resistive strip line, cross strip, pixelated chip…
photon
electron
PC
MCP
Pixelated
anode
electro cloud
image

## Slide 12
PMT applications
Large aperture PMTs
Small PMTs and MCP detectors
Large coverage for rare instances
Neutrino, comic rays, dark matter…
PID, TOF
Space satellites for particle or photon detection
Lidar
Fluorescence lifetime measurements…

## Slide 13
Outlines
Outline
Introduction
Overview of MCP detectors
MCP detector characteristics
Prototypes and applications
Future plans

## Slide 14
photon
electron
PC
MCP
anode
signal
electron cloud
< 10-5pa
Photocathode sensitivity
Response wavelength
Quantum efficiency
Collection efficiency
Detection efficiency
Gain
Current gain, pulse gain
Dynamic range
Time resolution
Position resolution
Counting rate
Maximum output current
Recovery time
Rise time, Transit time, TTS
Pulse width, fall time, after pulse,
Late pulse
Magnetic field effects
Radiation resistance
Lifetime
PMT characteristics

## Slide 15
Gain
Determined by the secondary electron emission yield, L/D, basis angle, supply voltage, resistance
Vary with different input intensities
because of limited maximum output charge.
Single P.E. gain could be one magnitude higher than the current gain
channel
Counting
Single photoelectron spectrum
Gain
Supply voltage
Gain 1.2e7
Input current
1 pA
2 pA
3 pA
4.3 pA

## Slide 16
Time performance
Photocathode
MCP
Electron trajectories
Delayed pulses worsen time performance, which caused by the electron backscattering on the MCP input surface
Ref. Albert Lehmann, Status/Limitations of MCP-PMT Performance
Larger open area ratio could minimize
late pulses

## Slide 17
Time performance
input
output
Impedance mismatch
input
output
TTS could deteriorate as it becomes saturated
impedance matched
The waveform is usually not perfect because of impedance mismatch between the metal anode and the coaxial line.

## Slide 18
Lifetime
Both photocathode sensitivity
and MCP gain decrease as
illuminated for a long time.
Photocathode QE decreases
more significantly at longer
wavelengths.
QE could decrease by 80%
while gain decreases by less
than 20% for an integrated
output current of 39 mC/cm2 .

## Slide 19
Lifetime
Coated Al2O3 layer by ALD technique and optimized the electron scrubbing volume to improve the lifetime.
Lifetime increased from 373 mC/cm2
to 11000 mC/cm2 as increase the
thickness of the ALD-layer from 1 nm
to 6 nm.
Lifetime increased from 117 mC/cm2
to 373 mC/cm2 as increase the scrubbing volume from 0.43 µA·h/cm2 to 0.75 µA·h/cm2.
Lifetime increased more than 400 times.

## Slide 20
Lifetime
Gain
HV(-V)
Dark current (nA）
HV(-V)
Wavelength(nm)
Spectral response(mA/W)
Pre-test
Post-test
Pre-test
Post-test
Pre-test
Post-test
Lifetime
No degradation in photocathode and MCP, dark current decreased.
Continue to optimize the ALD and scrubbing processes.
The increase in gain may be due to the multiplication from both the ALD layer and the MCP, which requires further study.

## Slide 21
Rate capability
LD driven by a pulse generator
10 ns pulse width
~3500 photons/cm2/pulse
Measurement setup
Counting rate of ALD-MCP PMT
3 MHz@4e3 gain
600 kHz@2e4 gain
50 kHz@3e5 gain
15 kHz@1e6 gain
52.5 MHz for single P.E @ 1e6 gain

## Slide 22
Saturation recovery behaviors
0 nm
1 nm
4.5 nm
6 nm
Measurement setup
MCP-PMTs with different thickness of ALD films were operated at 1E5 gain.
Illuminated by LD at rates of 10 Hz for phase (1) and (3), 500 kHz for phase (2).
The MCP without the ALD layer appears to exhibit superlinearity and a long recovery time.
saturated
Longer recovery time for thicker ALD-layer
Recovery of the MCP with the ALD layer of 1 nm is fast.
Further research will be conducted to confirm the phenomena and causes.

## Slide 23
Saturation recovery behaviors
Heavier saturation, longer recovery time.
A higher supply voltage appears to be more effective in the recovery of the ALD-MCP.
The super-linearity can be lower for none ALD-MCP.

## Slide 24
Magnetic field effects
To figure out how magnetic field decreases gain, electron trajectories in the MCP channel under the magnetic fields are simulated with CST program.
Electrons move in a spiral under the influence of a magnetic field.
Shorter accelerating distance, lower striking energy.

## Slide 25
Fewer secondary electrons are emitted when primary electrons strike the MCP with lower energy.
Magnetic field effects

## Slide 26
Magnetic field effects
The number of electron collisions with the MCP channel increases and then decreases.
Gain is the result of the combined effect of the number of collisions and the collision energy.

## Slide 27
Outlines
Outline
Introduction
Overview of MCP detectors
MCP detector characteristics
Prototypes and applications
Future plans

## Slide 28
Solar-blind MCP-PMT for fast X-ray detections
MCP-PMT prototypes and applications
Photocathode : CsTe
Peak wavelength：250 nm
Gain＞1E6
Rise time: ＜350 ps
TTS @ SPE：＜50 ps
Solar-blind MCP-PMT+BaF2
Better than 1 ns time resolution for X-ray detection.
The fast and slow components of BaF2 fluorescence have difference wavelengths.
The CsTe cathode is mainly sensitive to the fast component of BaF2.
Spectrum response of CsTe MCP-PMT
BaF2 fluorescence
x-ray pulses detection in DCI laser fusion experiment

## Slide 29
Gated MCP-PMT for neutron detection in strong γ rays
MCP-PMT prototypes and applications
Neutron yield and spectrum detection are key
to optimize the nuclear fusion experiment.
The intensity of the γ rays produced together
with neutron is about 5 orders of magnitude
higher than that of neutrons.
gamma
neutron
The MCP-PMT with a gating function is developed.
Photoelectron trajectory is controlled by the electric field between the photocathode and the gating electrode.

## Slide 30
Gated MCP-PMT for neutron detection in strong γ rays
MCP-PMT prototypes and applications
Photocathode : bialkali
Gain:＞1E6
Rise time: ＜350 ps
Gating response time: ＜5 ns
Gating width: 5 ns ~10 ms
Gating noise: ＜ ±2 mV
Gated PMT
Gated PMT
Liquid
scintillator
nTOF
nTOF
No gating
saturated
DCI laser fusion facility
Gating ON
neutron
Single neutron sensitive

## Slide 31
MCP-PMT prototypes and applications
More than 30 gated MCP-PMTs were delivered to the DCI laser nuclear fusion exp.
for neutron yield detection.
About 500 gated MCP-PMTs are set to be delivered before the end of 2026 for the the neutron energy spectrum detection.

## Slide 32
MCP-PMT prototypes and applications
Large current MCP-PMT for strong radiation detection
100ns
250mA
Photocathode : bialkali
Gain:＞1E4
Maximum output current: ＞250 nA @100ns
Nonlinearity ＜ 5%
Time resolution (FWHM) : ＜ 1ns

## Slide 33
Outlines
Outline
Introduction
Overview of MCP detectors
MCP detector characteristics
Prototypes and applications
Future plans

## Slide 34
Position sensitive Hybrid MCP detectors
photon
electron
PC
MCP
Pixelated
anode
electro cloud
image
MCP + Chip anode
Expected performance
Single photon/x-ray/UV/ ion/ electron sensitive
＜50 ps timing resolution
＜20 µm spatial resolution
  Chip 1
  Sensitive to electrons with nearly 0 eV
  70 × 70, 20 μm is ready
  Ceramic base is being fabricated
  Hybrid MCP-PMT based the chip is expected in Sep.
  1.3k ×1.3k, 10 μm is expected in Sep.
  Output frequency 200 Hz
  Chip 2
  Sensitive to electrons with nearly 0 eV
  400 × 400，10 μm is expected end of 2025
  Time resolution ∽50 ps
  Counting mode output

## Slide 35
Large dynamic Hybrid MCP detectors
photon
electron
PC
MCP
Large dynamic chip anode
electro cloud
Gain: 103 ~104
One-stage MCP
Large dynamic chip
/ multi channel readout with
tens of gain

## Slide 36
Improve photocathode QE
  Micro-Nano gratings
  Micro-nano gratings, with subwavelength periodic structures, could boost photoelectric conversion efficiency by manipulating light-photocathode interactions and charge carrier dynamics.
  Dielectric gratings (e.g., SiO₂/TiO₂) create photonic bandgaps via Bragg scattering, forcing light to reflect multiple times within the photocathode.
  Localized surface plasmons
When light interacts with metallic nanostructures (such as nanoparticles, nanorods, or nanogratings) on the photocathode surface, it excites localized surface plasmons.
The electromagnetic field could be enhanced dramatically.
localized surface plasmons can modify the density of states near the material's surface, reducing the energy barrier for electron emission and promoting the escape of photoexcited electrons

## Slide 37
New photocathode material
  Can survive in atmosphere
  Can survive in atmosphere
  High QE
AI-assisted design of new materials

## Slide 38
Thank you for your attention！