## Slide 1
Fast Luminosity Monitor
Fast luminosity diamond monitor for CEPC
8.3 × 1034/cm2s at HZ operation modes
1 × 1036/cm2s at Z-pole operation modes
Event rate ~100 kHz @Z
The CEPC instant luminosity is designed for 8.3 × 1034/cm2s and 1.9 × 1036/cm2s at the HZ and Z-pole operation modes (50MW plan), at center of mass energies of √s = 240 and 91 GeV, respectively.
Simulation of event rate on Diamond slab region (by Yilun Wang)

## Slide 2
Fabrication of Diamond sensors
Two prototype microstrip diamond sensor has been successfully fabricated at NJU
Pitch of 1.0 mm (featuring 0.9 mm wide electrodes and 0.1 mm gaps) on 10 mm×10 mm diamond
Pitch of 1.35 mm (featuring 1.2 mm wide electrodes and 0.15 mm gaps) on 6 mm×6 mm diamond
Microscopy images of the electrodes
Test PCBs are being fabricated in preparation for radiation source signal characterization
Post-litho development