## Slide 1
R&D on the fast GAGG for LHCb upgrade II
The 26th Research Institute of China Electronics Technology Group Corporation (SIPAT)
Henan Normal University October 31, 2025
Xiong Xiao, Jingjing Qu, Pengfei Han, Yuchong Ding*
on behalf of the ECAL China Group

## Slide 2
Outline
1. Background
2. Crystal Growth and Characterization
3. Beam Testing Results
4. Conclusions and Next Work

## Slide 3
1.Background: ECAL at LHCb
The LHCb experiment is designed for heavy flavor physics at the LHC.
Electromagnetic calorimeter (ECAL)
is a key component of LHCb
ECAL is crucial for key physics goals of LHCb, such as:
  CP violation
  Lepton flavour universality

## Slide 4
1.Background: Motivation to LHCb ECAL upgrade
We are here
LHC will operate as High-Luminosity LHC (HL-LHC) after its long shutdown 3 (LS3).
Luminosity will increase from to
Challenges to LHCb ECAL:
  Higher occupancy
  Higher radiation dose
An upgrade of the ECAL is essential!

## Slide 5
1.Background: LHCb ECAL upgrade plan
ECAL upgrade is planned in two phases:
LS3 enhancement (2026 – 2029)
Upgrade II (2034 – 2035)
SpaCal-W with GAGG fibre

## Slide 6
1.Background: SpaCal-W modules for LHCb ECAL upgrade
For both upgrade phases, the innermost modules of LHCb ECAL will be replaced
with spaghetti calorimeter (SpaCal) modules with tungsten (W) absorbers
  Polystyrene fibres, single-sided PMT readout
  Energy resolution:
  Time resolution:
  Radiation hardness up to
  GAGG fibres, dual-sided PMT readout
  Energy resolution:
  Time resolution:
  Radiation hardness up to
LS3 enhancement
(2026 – 2029)
Upgrade II
(2034 – 2035)

## Slide 7
1.Background: Requirements of GAGG scintillator
GAGG scintillator is the most promising material, but current commercial GAGG has scintillation decay time > 40 ns.
L. Y. ~ 45,000 MeV-1
𝜏𝑑,𝑒𝑓𝑓 ＞ 40 ns
ρ ~ 6.67 g/cm3
Zeff ~ 54
*Kei Kamada, Takanori Endo, Kusuke Tsutumi, et al. Cryst. Growth Des. 2011, 11, 4484–4490.
Material Advances, 2022, 3, 6842
R&D to produce large-size and homogeneous fast GAGG:
  Decay time < 10 ns
  Size > Φ50 mm × 110mm

## Slide 8
2.Crystal Growth and Characterization: Stage goals
Results of GAGG in 2024: 𝜏𝑑,𝑒𝑓𝑓 ~ 20 ns, Size ~ Φ42mm×100mm
R&D stage goals of 2025: 𝜏𝑑,𝑒𝑓𝑓 ≤ 15 ns, Size ≥ Φ45mm×110mm
Abbreviations: 𝜏𝑑,𝑒𝑓𝑓 (Decay Time), size (ingot size)
2024.01
2024.12

## Slide 9
2.Crystal Growth and Characterization: Accelerate the decay
Non-radiative Recombination Centers
Increase Mg ions Doping Concentration
How to accelerate the decay time ? The effect of scintillation quenching
The concentration of Mg2+ ions becomes higher and higher from sample PL1 to PL6
Material Advances, 2022, 3, 6842

## Slide 10
2.Crystal Growth and Characterization: Crystal improvement
The fastest decay time of GAGG reached ~5 ns.
Inclusions
Crack
Inclusions
Φ42 mm×100 mm
Cracks & Inclusions existed.
Only a length of ~50 mm is usable.

## Slide 11
2.Crystal Growth and Characterization: Crystal improvement
Improve the crystal quality: ① by decreasing the crystal diameter
The crystal shape has defects.
Cannot cut optical fiber with dimensions of
1mm x 1mm x 100mm.
Φ35 mm×110 mm

## Slide 12
2.Crystal Growth and Characterization: Crystal improvement
Φ45 mm×110 mm 𝜏𝑑,𝑒𝑓𝑓 ＜ 15 ns
Improve the crystal quality: ② by optimizing thermal filed of the crystal growth system

## Slide 13
Definition of sample positions from an ingot
We have produced 22 ingots and take samples from them during 2025
  Sample size: 2 mm×2 mm×3 mm
  Surface treatment: polished with all sides
  Fiber produce: 1mm x 1mm x 100mm
top
middle
tail
GAGG samples
Ingot and sample pictures
#57
2.Crystal Growth and Characterization: Sample Prepare

## Slide 14
Dual testing ensures both R&D efficiency and the reliability of test results, the test results from PKU are consistent with those from CERN.
Decay time (TCSPC with X-ray)
Light yield
Decay time (TCSPC with X-ray)
Light yield
PKU
CERN
2.Crystal Growth and Characterization: Test Systems

## Slide 15
2.Crystal Growth and Characterization: L.Y. & Decay time
The Latest Test results:
  ＜15 ns
  light yield: ＞11000 MeV-1
  Our group have developed an inorganic scintillator that with both fast decay time and high light yield for the first time.
  The non-uniformity of the ingot is ~40%.
and L.Y. for SIPAT GAGG samples from #59 ingot

## Slide 16
#52
Sample part |  | Light yield*3（photon/MeV） | τd,eff（ns）*3
Top | Before annealing*1 | 16,456.25 | 12.50
 | After annealing*2 | 20,302.33 | 14.33
 | Increase rate | +23.37% | +14.64%
Middle | Before annealing | 14,234.00 | 10.25
 | After annealing | 19,139.66 | 15.33
 | Increase rate | +34.46% | +49.59%
Tail | Before annealing | 13,447.00 | 10.25
 | After annealing | 16,029.33 | 12.00
 | Increase rate | +19.20% | +17.07%
Sample H1-H3/M1-M3/T1-T3
annealing in air atmosphere
*1 average value of sample 1-3
*2 average value of sample 4-10
*3 measured by PKU and THU
Annealing in air atmosphere
After annealing in air atmosphere, the light yield was increased, the non-uniformity is ~20%is
While the decay time became longer
2.Crystal Growth and Characterization: Annealing Experiment

## Slide 17
2.Crystal Growth and Characterization: L.Y. & Decay time
By increasing the Mg2+ doping level to quench the scintillation
  Ingot in Nov. 2024: 𝜏𝑑,𝑒𝑓𝑓 ~ 24 ns for top samples and 𝜏𝑑,𝑒𝑓𝑓 ~ 12 ns for tail samples
  Ingot in Jun. 2025: 𝜏𝑑,𝑒𝑓𝑓 reached ~ 10 ns for tail samples with light yield ~11000 MeV-1
Latest batch delivered in June & July 2025
Note: the is measured with X-ray, and the light yield is calculated with Gaussian fitting.
Correlation of and L.Y. for SIAPT GAGG samples
10 ns
2025
2024

## Slide 18
3.Beam Testing Results: The SpaCal-W prototype
GAGG fibres
back
front
back
front
In the first half of 2025, We produced 8 ingots, two of which were used to produce fibers and incorporating to the prototype with two cells.
  The is approximately 10 ns for the front 5 cm of fibers and less than 15 ns for the back 10 cm section.
  The prototype incorporating these fibers was characterized during the SPS test beam in September 2025.
SpaCal-W Prototype
SpaCal-W Prototype with two cells incorporating fibers from new batches

## Slide 19
Time resolution at 3°+3°:
Front only:
  Improvement of time resolution, as expected from measurements done in the lab.
  With R9880U: below 20 ps after 60 GeV
Front & Back:
  The analysis is still ongoing!
Time resolution for prototype
Preliminary
3.Beam Testing Results: Time resolution

## Slide 20
3.Beam Testing Results: Energy resolution
Energy resolution at 3°+3°: (4x4 cells)
  Sampling term: 10.6±0.2 %
  Constant term: ~2 %
Energy resolution for prototype
Preliminary
Preliminary
Energy resolution for prototype
Energy resolution at 3°+3°: (4x4 cells)
  Sampling term: 10. 2 %
  Constant term: ~2 %
2024
2025

## Slide 21
4.Conclusions and Next Work
Conclusions:
  The stage goals have been reached in 2025, 𝜏𝑑,𝑒𝑓𝑓 ≤ 15 ns, Size ≥ Φ45 mm×110 mm.
  GAGG Crystals with a decay time of less than 15 ns can be grown stably, meet the requirements of optical fibers and applicable to other fields.
  With beam test at 2025, the time resolution improved significantly (＜20 ps).
Next work:
  Improve the inhomogeneity of the ingot to ≤20%.
  Increase the ingot size at least to reach Φ50 mm×110 mm, to increase the yield of fibers.
  Furtherly accelerate the decay time to sub-10 ns for entire ingot.

## Slide 22
Acknowledgments
The crystals were characterized by both Zhenwei Yang's group at PKU and Etiennette's group at CERN.
Ming Zeng’s group at THU provided valuable technical advice and student support.
Beam testing was conducted at both CERN and DESY, with thanks to the LHCb ECAL Upgrade II group.

## Slide 23
Thanks for Your Attention!