## Slide 1: Performance Study of the MOSS Chip for the ITS3 Detector
Zijun Zhao(zijun.zhao@cern.ch)
The 11th China LHC Physics Conference
Nov 1st, 2025

## Slide 2: Outline
Overview of ITS3 and MOSS
The functional test of MOSS
  test setup
  test content and results
Summary and prospect
2021 |  |  |  |  |  |  |  |  |  |  |  | 2022 |  |  |  |  |  |  |  |  |  |  |  | 2023 |  |  |  |  |  |  |  |  |  |  |  | 2024 |  |  |  |  |  |  |  |  |  |  |  | 2025 |  |  |  |  |  |  |  |  |  |  | 
Q1 |  |  | Q2 |  |  | Q3 |  |  | Q4 |  |  | Q1 |  |  | Q2 |  |  | Q3 |  |  | Q4 |  |  | Q1 |  |  | Q2 |  |  | Q3 |  |  | Q4 |  |  | Q1 |  |  | Q2 |  |  | Q3 |  |  | Q4 |  |  | Q1 |  |  | Q2 |  |  | Q3 |  |  | Q4 |  | 
J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D
2026 |  |  |  |  |  |  |  |  |  |  | 
Q1 |  |  | Q2 |  |  | Q3 |  |  | Q4 |  | 
J | F | M | A | M | J | J | A | S | O | N | D
ER1 chip design(MOSS MOST)
ER2 chip design(MOSAIX)
ER3 Final chip design
ER1 Chip test
ER2 Chip test

## Slide 3: Overview of ITS3
ALCIE Detector
ITS(Inner tracking system)
ITS3:replace the innermost three barrels
ITS2:
  7 layers: 3 inner barrel(IB) and 4 outer barrel (OB)
ITS3(Upgrade)：
  Advanced Silicon Chips (65nm CMOS MAPS) for the IB
  Fabricated with stitching
  reduce the material budget to 0.09% X0 per layer (ITS2: 0.36% X0 )
  More close to beam pipe (2.5 mm)
  required radiation tolerance :10 kGy of TID and of NIEL
  Power density < 40
ITS3 TDR :CERN-LHCC-2024-003

## Slide 4: Overview of MOSS (MOnolithic Stitched Sensor)
wafer
MOSS chip in carrier board
First Generation Stitching Sensor
  Stitching allows the manufacture of chips larger than the maximum design reticle size.
  Wafer scale (14 x 259 ), 6.72 million pixels in one chip.
One chip consists of an LEC ,10 x RSUs, and a REC.
  Allows control and readout the whole chip via LEC.
  RSUs are divided into top and bottom half units with different pitches and pixel numbers.
  Each half unit have 4 regions, they have different frontend variants.
MOSS Architecture
The frontend variants of the RSU

## Slide 5: Setup of MOSS test system
based on three different types of boards
A carrier board
  access to all features of the chip via 560-pin connectors on perimeter
  four connectors (on long edge) correspond to the chip’s four quadrants, each with five independent half-units.
  the fifth connector (on LEC) operates the chip as two halves via the stitched backbone.
Five Proximity cards
  connect the carrier board to automation module.
Five Automation modules
  steer the proximity board and interface the sensor control and readout with a computer.
The concept for the Lab test system
Lab test
Beam test
(baby)MOSS
Scintillator + PMT
ALPIDE
The concept for the Beam test system
Telescope setup based on three parts:
A (baby)MOSS DUT
Six ALPIDE reference planes
  act as a reference telescope to precisely reconstruct the tracks
Two Scintillator + PMT
  form a trigger system — they ensure that data acquisition only occurs when a particle actually crosses the setup.

## Slide 6: Functional test order
This order!
PowerOn scan:sequential powering of the chip with current monitoring at every step
Register and Shift-register scans:test all applicable (shift)registers with known bit patterns → 7680 registers in 1 MOSS
DAC scan:verification of the in-chip DACs (linearity, etc ...)
Digital and Analogue scans:repeated (#25) digital or analogue (with max possible charge) injections in every pixel
  Dead pixels: 0 hits, Noisy pixels: > 25 hits, Inefficient pixels: 0<hits<25
Threshold scan:repeated analogue pulsing with a test charge sweep in every pixel
Fake-hit rate scan:readout of multiple chip events to detect noisy pixels (default: 100000 readout frames, noisy pixel frequency > 0.01)
(We power, control, and read out the MOSS chip via the long edge.)
Main objective: yield and pixel performance
(Totally 79 MOSS chips were tested)
Photograph of a real test system

## Slide 7: Test result of PowerOn scan
Pre-Clock
De-asserting
reset
Set IRESET+ kick bandgaps
Interlock enable e
PowerOn sequence
Totally 1370 HUs passed the tested, monitor the current distribution during different term.
Means of AVDD, DVDD and IOVDD are 5.47 mA, 5.92 mA and 0.034 mA after power-on.
  Low power consumption under static conditions (Top/Bottom region ~14 )
PSUB -1.2V
Clocked
(The voltage of AVDD, DVDD and IOVDD are 1.2V, 1.2V and 1.8V.)

## Slide 8: Test result of Register and ShiftRegister scan
Register and Shift-register scans:test all applicable (shift)registers with known bit patterns → 7680 registers in 1 MOSS
Test result of Register scan
Test result of ShiftRegister scan
A total of 5600 regions were tested.Only 0.14% (8 regions) failed the Register scan.
  Errors are limited to single regions and caused by minor periphery defects rather than slow-control communication.
Among the 5592 successfully tested regions, only 0.11% (6 regions) failed the Shift Register scan.
  These failures are minor and won’t affect future sensor designs.

## Slide 9: Test result of DAC scan
DAC scan content:
tuning the bandgap reference voltages to achieve stable and accurate bias references.
all on-chip DACs (8 per region, 640 per chip) are scanned across their full range, verifies the linearity and bias range of the in-pixel front-end circuitry.
The average values are close to the target values of 10.2 µA and 0.4 V for Iref and Vref , respectively.
The spread is small enough (FWHM less than 5%) to provide reliable biasing references across regions and chips.
Few outliers wouldn’t affect chip operation, as they can be compensated by adjusting the corresponding DAC settings.
In general, linearity stays within 3 DAC counts over the 256 settings (8-bit DACs).
A region passes this test if all DACs perform within predefined ranges, ensuring that reliable biasing conditions establish within the operational range. In total, 0.65% of regions did not meet this criterion.

## Slide 10: Test results of Analogue/Digital scan
Digital and Analogue scans:Signals are repeatedly injected (#25) separately into both the digital and analog front-ends of the pixels to verify signal propagation, ensuring that data packets can be successfully read out and transmitted to the acquisition system.
Dead pixel
Pixels are classified into four categories:
  Dead pixels: 0 hits, Noisy pixels: > 25 hits, Inefficient pixels: 0<hits<25, good pixels: hits = 25 hits
The right plot shows the distribution of dead pixel in all tested top region 0, with other regions showing nearly identical behavior. In most regions, the number of dead pixels is very low or zero.
Regions with more than 1% faulty pixels are classified as failing test, which corresponds to 0.6% of all tested regions.(8.1% regions masked)
Distribution of dead pixels in each region

## Slide 11: Test result of Threshold scan
Threshold scan:repeated inject analogue pulsing (each step repeated 25 times) with a test charge sweep (VPULSEH ranging from 0 to 70) in each pixel
Example of S-curves from the threshold scan of 1 HU (all pixels)
region-average threshold, threshold RMS and average noise for all the tested regions with 22.5 µm pixel pitch and standard front-end implementation
From the S-curves, the derivative of the s-curve is a Gaussion distribution:
  = pixel threshold
  = pixel noise
For the 22.5 pixel pitch and standard front-end implementation, the threshold is 25.2 DAC and noise is 2 DAC
1 VPULSEH DAC corresponds to about 8

## Slide 12: Test result of FakeHitRate scan
Fake-hit rate scan:readout of multiple chip events without any external charge inject to detect noisy pixels (default: 100000 readout frames, noisy pixel frequency > 0.01)
Hit map scatter plot
In most cases, no noisy pixels are identified. Masking certain excessively firing pixels (those that cannot be reset, etc.) can significantly improve the fake-hit rate.
some regions still fail to meet the ITS3 fake-hit rate requirement (）, even with a relatively high average threshold of 200 .
Regions with more than 1% faulty pixels, either excessively noisy or with undetermined thresholds, are classified as failing the test, corresponding to 0.33% of the tested regions.
(In both Threshold scan and FHR scan)
fake-hit rate for all regions with 22.5 µm pixel pitch and standard front-end implementation

## Slide 13: Yield result
The largest yield loss occurs during the powering test due to shorts in the power network from the new metal stack, which is expected to be mitigated in the next chip submission.
Yield loss in the matrix readout can result from issues in the simplistic readout architecture used in this prototype. Since these issues were anticipated in the chip design, they can be excluded.
Overall, about 76% of regions pass the full verification considering all issues, and 85% when excluding the expected readout architecture limitations. In other words, yield loss observed in functional tests is less than 2%.
Half-unit yield as a function of wafer position. No specific patterns are apparent.

## Slide 14: Test result of LEC(Left End Cap)
control, configuration and readout via LEC power supply via Long edge
The final ITS3 chips are expected to rely exclusively on readout via the Left End-Cap, it is important to characterize the response of MOSS half-units through the LEC interface.
Repeated several tests with HU steered and readout via LEC. (LECPoweron scan, LECRegister, LECThreshold scan and LECFakeHitRate scan. The test logic are the same)
Out of 78 chips tested via LEC, one addition issue was found(in LECRegister scan), resulting in 21 additional regions (about 0.7%) being flagged as faulty.
In pixel matrix performance tests(LECThreshold and LECFakeHitRate scan), the measurements were consistent across both two readout schemes.

## Slide 15: Beam test results
Threshold range meeting ITS3 requirements:
  Top region 0: 110~220
  Bottom region 0:100~175
When Threshold~160, the spatial resolution of bottom region 0 is about 4.5 um, the average cluster size is about 1.2 pixels, meet the requirement of ITS3.

## Slide 16: Beam test results with irradiated
22.5 um pitch
18.0 um pitch
After irradiation, the operational margin shows varying degrees of degradation. For example, in the 22.5 µm pitch (top region 0), it reduces from 110 to less than 50.
Ionizing radiation has no significant effect on the spatial resolution or the average cluster size.
Non-ionizing irradiation slightly degrades spatial resolution (~0.3 µm) at low thresholds because it introduces defects in the sensor bulk, reducing charge collection efficiency and cluster size.

## Slide 17: Summary and prospect
ITS3 — a bent wafer-scale monolithic pixel detector
MOSS — the first stitching sensor produced in the ER1 phase.
  Functional test completed!
  demonstrates promising performance and yield for upgrade.
  pave the way for further optimizations and the development of the final chip design.
MOSAIX — the second-generation stitching chip produced in the ER2 phase.
  Larger-scale stitching, fully powered by the end-cap, and an advanced front-end circuit ,etc.
  already in the tape-out stage and will be delivered and tested in early 2026.

## Slide 18
Backup

## Slide 19: front-end circuit

## Slide 20: ITS3 and ASIC design general requirements