## Slide 1: CEPC Silicon Tracker Detector Module
Xuhao Yuan
2025-07-11

## Slide 2: TDR design
Overall design
  Sensor tiling, spatial constraints (bonds), protection
  Geometric coverage, gaps
  Stave size, mounting, power/readout paths
  Radiation length, including epoxies
  Reference datum
Taking ITK Barrel as the example

## Slide 3: Main mechanical & thermal issues
Mechanical
Mechanical simulation of module and stave (with epoxies and realistic interfaces)
  Stress concentrators, fracture points, stiffness required in 3D
  Stave modal analysis
  Radiation length
Prototypes of module & stave
  Module level
  Sensor packing, protection (sensor, bonds), spatial requirements
  Hybrid dimensions, data path, trace routing density
  Manipulability, stiffness, handling
  Power/grounding, nearby components
  Electrical consequence, chemical compatibility of putting materials in contact with silicon chips
  How to handle during construction and testing, how to store
  Stave level
  Structure, core designs, mechanical/thermal interfaces
  Module arrangement, placement process, reference datum
  Manipulability, required stiffness, handling procedures
  Attachment of data flex, power flex
  Module replacement scheme
  Manufacturable, bondable, testable
Thermal
Cooling requirements
  All heat loads (including power dissipation in cables)
  btw CO2 set point and CMOS temperature
  across CMOS
  CMOS operating temperature, dew point
  Total cooling power for cooling plant
Prototypes of module & stave -> may be the same one as mechanical
  Efficacy of different thermal path designs using different core designs and different interface materials
  and , with full thermal load
  Realistic mockup of power dissipation from distribution
  Effect of different number of cooling tubes, tube run
  Internal condensation on tube
  Thermal contraction in stave at -30℃, establish fracture limit
Thermal simulation of module and stave
  and , thermal runaway margin
  Thermal contraction in stave at -30℃
  CTE mismatch stresses on sensors
  Internal stresses (on epoxy, thermal/mechanical layers), fracture limit
  Optimal location for temperature monitoring

## Slide 4: Outline
Stave design & prototype R&D
ITK Module design & prototype R&D

## Slide 5: Bare stave
CMOS chips with 2x2 cm2, more uniform heating area (~200 mW/cm2)
Comparing with traditional foam-sandwich structure
Structure foam-> Evonik Rohacell 51 IG (0.051g/cm3)
Thermal foam -> Allcomp K-9 carbon foam (0.2g/cm3, ~35W/m.K)
Looking for carbon fiber honey comb (CF-HC) + two carbon fiber (CF) facing
  Large size HC reduce bare stave density, but with high stiffness
0.04g/cm3
Carbon fiber -> K13C2U high-modulus carbon fibers in EX1515 epoxy matrix (45 gsm, 0.1? mm THINCK)

## Slide 6: CF-CFHC-CF structure
bare stave size ~ 1 400 x 120 mm2
center active area~ 1 200 x 120 mm2
Two AL End-of-Stave (EOS) for mounting in future test
3 Ti tube bury inside, with OD 2.2 mm, thickness 0.15 mm

## Slide 7: Material preparation
Contract signed in April
Carbon fiber facing + honey comb + Ti tube with VCR connector ready in weeks
Jigs for honey comb ready by April
2cm CFHC (3mm THCK)
M40J
CF facing ready by May
M40J

## Slide 8: Ti tube status
First 3 Ti tube ready in May
ID ~2.2 mm, Thickness ~ 0.15 mm, Total length ~ 1 400 mm
NOT VCR connector yet, local machine-shop made connector => to be updated next time
Laser welding for Ti tube <-> steel connector, sealing with He gas
0.15 MPa gas test in water, no bobble in water for 5min => will modified in future

## Slide 9: Bare stave production
x2

## Slide 10: Numbers
Cabon fiber faces x2 | 118 g x2 | Thk 0.5 mm; Thinner faces ~0.15 mm next time
Cabon honey comb | 23.2 g | ThK 3 mm
Adhesive film | 38.9 g | BERGQUIST GAP FILLER TGF 4500CVO for CMS IT
End of stave | 76 g x2 | Carbon fiber to be used next time
Ti tube | 33.33 g x3 | Thinner/finer size next time
Edging | 10.5 g | NO need all; Ultem inserts
Paint | 4.5 g | NO need
Total | 566.67 g | Goal: ~400 g
Further M/T tests to do soon

## Slide 11: Module mockup preparation
Dummy chips v0 received by end of Match
Size as COFFEE => CAN BE modified in the next iteration
Fiducial marks + wire bonding pads. Thermal circuits to be added in the next iteration
Dummy hybrid v0 received last week
199.14 mm x 30.27 mm x 0.3 mm
With wire bonding pad and fiducial marks
Thermal circuit will be added in the next version to simulate the heat dissipation
1st dummy hybrid
Next version hybrid with heating pad

## Slide 12: Mechanical mockup producing
Jigs-based assembly. Using gantry for high precision in future
Chips positioning according to D-shape pins, with vacuum fixing

## Slide 13: Mechanical prototype
The first mechanical prototype produced
Also with wire bonding tests: Two layers of the chips are both bonded => looks good
To-do next
Modules with thermal power
Stave level assembly

## Slide 14: Summary
Testing mockup produced for stave/modules
Future plan listed in P3~P4