## Slide 1: CZT Detectors for MeV Astronomy
Ming Zeng, Xutao Zheng, Hao Chang, Jiahuan Zhu
Tsinghua University
MeV Mission Workshop @IHEP: Preparing Next-Generation Astrophysics in the MeV Window 2025-09-17

## Slide 2: News about MASS-Cube
MASS-Cube
The first MASS-Cube payload was launched on Sep. 5th, 2025
Equipped with 4 pixelated CZT detectors, 2×2×1.5 cm3 each
Now on debugging and testing
Demonstrate pixelated CZT in space, increase Technology Readiness Level to TRL 6 - 7
Act as the pathfinder for MASS, MeVGRO, and also other CZT missions

## Slide 3: The room temperature semiconductor: CdZnTe
~ kV/cm
Severe hole capture
Electron capture
Single-polarity charge sensing technique, e.g. Frisch grid, coplanar, pixelated anode
Depth sensing technique and charge loss correction
Transport properties at 300K (A. Meuris et al. 2023)
3D CZT
Improve resistivity
Reduce polarization effect
Improve
CZT
CZT

## Slide 4: Readout and event reconstruction
CZT
Planar cathode
Pixelated anode
-HV
Waveform (QCathode, t0)
XY position, QAnode, t
The anode pixel provides the x and y positions
The z position is derived from the cathode/anode charge ratio and/or the drift time
Planar cathode
Pixelated anode
The "Small-Pixel Effect" governed by the Shockley-Ramo theorem.

## Slide 5: Readout and event reconstruction
CZT
Planar cathode
Pixelated anode
-HV
Waveform (QCathode, t0)
XY position, QAnode, t
The anode pixel provides the x and y positions
The z position is derived from the cathode/anode charge ratio and/or the drift time
Depth reconstruction and depth correction of charge loss are the keys to achieve excellent energy resolution
Drift time

## Slide 6: 3D position sensitive pixelated CZT detectors
CZT unit from Redlen
2×2×1.5 cm3
4 cm available
11×11 pixels
Pixel pitch = 1.72 mm
Planar cathode
Pixelated anode + Grid
2 cm
1.5 cm
8 cm
1.5 cm
Compared with double-sided strip HPGe
Comparable position resolution
Comparable energy resolution
Needs cryocooler / cryostat
Orthogonal strips
Competing technology pathways, that both long-term supported by the DoE.
Notes: CZT: XY 1.72mm, Z ~ 0.6mm, 0.6% ~ 1% @662 keV
HPGe: XY 1.162mm or 2mm, Z ~ 0.5mm, 0.8% @662 keV

## Slide 7: Readout ASICs for pixelated CZT
VAS_UM2.3/TAT4 (obsolete)
IDEAS, Norway
Analog readout
+
Analog output
||
Amplitude & trigger time
for each pixel
GDS-10 (in production)
IDEAS, Norway
Waveform sampling
QingTai (under development)
Microparity, China
Analog readout
+
Integrated ADC/TDC
||
Fully digital output

## Slide 8: Performance
FWHM ~ 0.6% @662 keV
Hand-hold Compton camera prototype
(Yang et al. 2020)
Depth resolution (FWHM) ~0.6 mm →

## Slide 9: Compton telescope proposals based on (entirely) CZT
TERI
  Pixelated CZT (+ Coded Mask)
  Pixel pitch 1.72 mm
  1.3% (FWHM) @662 keV
  Launched to ISS on 2025.04.21
TERI (Shy et al. 2024)
MeVCube concept design
(Lucchetta et al. 2022)
MeVCube
  Pixelated CZT
  Pixel pitch 2.45 mm
  2.8% (FWHM) @662 keV
  6U CubeSat concept
DTU CubeSat proposal
(Owe et al. 2024)
HKU CubeSat proposal
(Kuijper et al. 2024)

## Slide 10: The MASS mission concept
32×16×2 = 1024 CZT Units (4096 cm2)
See https://doi.org/10.1007/s10686-024-09920-4
Double layer chessboard layout, maximum effective area while improve ARM
MASS-Cube
CubeSat pathfinder, also CubeSat constellation mission

## Slide 11: Expected performance — MASS & single MASS-Cube
20 – 50 times
Solid & Dashed:
Energy within ±2𝜎；Compton scattering angle 0–180◦；
Solid only First two interactions ≥ 5 mm, and any two interactions ≥ 0.3 cm.

## Slide 12: Expected performance — MASS-Cube constellation
Left: MASS vs 16 MASS-Cube, each with 64 CZT units (total 16*64=1024)
Right: Single MASS-Cube with different number of CZT units

## Slide 13: Hardware design of MASS-Cube
CubeSat platform compatibility
  Size: 9.4×9.4×11 cm3 ( ~ 1.1U)
  Weight: ~ 1.7 kg
  Power: ~ 14 W
Pixelated CZT detector
  2×2 CZT array, 16 cm2
  Depth resolution (σ) <1 mm
  Energy resolution <1% @662 keV
  Dead time ~ 160 μs
Anti-coincidence detector
  8 mm GAGG + SiPM
  4 sides and bottom
To verify in-orbit background, the GAGG ACD was not installed on the first MASS-Cube payload

## Slide 14: Hardware design of MASS-Cube

## Slide 15: Spectrum performance
Energy (keV) | CH0 | CH1 | CH2 | CH3
59.5 | 5.64% | 5.41% | 5.04% | 5.44%
122 | 3.70% | 3.50% | 3.11% | 3.11%
511 | 1.08% | 1.26% | 0.98% | 0.95%
662 | 0.82% | 1.03% | 0.74% | 0.69%
1332 | 0.54% | 0.74% | 0.55% | 0.47%
Energy resolution (FWHM) at different energy

## Slide 16: Imaging performance
(Without event filter)

## Slide 17: Imaging performance
before
after
511 keV, point source, on-axis
List-mode MLEM, improve imaging results

## Slide 18: Radiation damage of CZT — irradiation experiment
Proton irradiation experiment setup:
Two 2×2×1 cm3 CZT units were irradiated
During irradiation:
Crystal 1: 1333 V @1 cm HV applied
(= 2000 V @1.5 cm)
Crystal 2: no HV applied
Spectrum test with Na-22 between each irradiation
Bean fluence () | China Space Station () | Polar orbit () | Low inclination orbit ()
 | 49 d | 19 d | 11 d
 | 159 d | 62 d | 36 d
 | 1.3 y | 186 d | 108 d
 | 4.4 y | 1.7 y | 1 y
 | 13.3 y | 5.2 y | 3 y
 | 49 d | 19 d | 11 d
 | 159 d | 62 d | 36 d
 | 1.3 y | 186 d | 108 d
 | 4.4 y | 1.7 y | 1 y
 | 13.3 y | 5.2 y | 3 y
Proton fluence and equivalent on-orbit time for various orbits
Beam setting:
Proton energy: 100 MeV
Beam fluence range: 3×107 ~ 3×109 p / cm2
Beam non-uniformity: < 10%

## Slide 19: Radiation damage of CZT — results
Energy Resolution at Various Proton Fluences
The charge collection efficiency (CCE) of CZT decreases as the proton fluence increases
At proton fluence above 1×109 /cm², a significant degradation in energy resolution was observed
When a 1333 V bias was applied to the crystal, no significant radiation enhancement effect was observed
See https://doi.org/10.1007/s10686-025-09998-4 for more details
Signal Amplitude Depth Distribution at Various Proton Fluences

## Slide 20: Conclusion
We proposed the MASS medium-satellite mission and the MASS-Cube micro-/nano-satellite constellation concept based on pixelated CZT
With years of effort, the first MASS-Cube has been launched to demonstrate pixelated CZT in space
  Preliminary testing in progress
CZT is a room-temperature alternative for HPGe, good for modular design or constellation mission
The design of MASS-Cube could be either the standard unit of a larger mission, or the payload component of a constellation

## Slide 21: Open questions
Improvement of readout and event reconstruction methods for pixelated CZT (depth reconstruction, charge loss correction, XY sub-pixel resolution…)
Mass production of a large number of high quality CZTs and readout ASICs
Calibration method for a large number of pixelated CZTs (totally >100k pixels or >1M voxels)
Radiation damage, annealing, and in-orbit calibration of CZTs (mission lifetime)
Detector material improvement, e.g. Cd0.9Zn0.1Te0.9Se0.1?
Potential to do polarimetry?
…
CZT technique for MeV space missions still challenge!

## Slide 22: Thanks!

## Slide 23
1）Domestic pixel CZT detector (Imdetek) + ASIC chip (IHEP)
CZT detector
22*22*15mm3
121 pixel
Imdetek
CPRE 10-32
32 channels
IHEP
Research progress of CZT detectors developed for MeVGRO in IHEP

## Slide 24
Prototype test results
ASIC Chip and FFE
Linear response
FWHM <2.0% @ 662keV(before 3D correction).

## Slide 25
2）Frisch-grid CZT
size: 5×5×20mm3
I-V
CFG CZT anode readout with discrete component circuit

## Slide 26: Simulated ARM
1 MeV On-axis ARM