## Slide 1: Vacuum System of MAX IV Eshraq Al-Dmour
31st Oct. 2012
Huairou, Beijing
Workshop on Accelerator R&D for Ultimate Storage Rings

## Slide 2: Contents
MAX IV Vacuum system constrains, challenges and considerations.
Vacuum system layout.
NEG coating issues.
Installation.
Conclusion.

## Slide 3
MAX IV Vacuum system constrains, challenges and considerations.
Vacuum system layout.
NEG coating issues.
Installation.
Conclusion.

## Slide 4: Constrains and requirements
Compact lattice.
Closed solid magnet block.
Small aperture of the magnets.
Target pressure with beam.
Removal of the power from SR.
Stable positioning for BPM.

## Slide 5: Vacuum System of MAX IV considerations
Small aperture for the magnets
NEG coating
Copper vacuum chambers
Strict surface preparation
Etching and cleaning process
But w. stable BPM
Welded bellows on
Chambers’ extremities
flexible
Installation difficulties
Careful preparation for installation!
Compact lattice
+
conductance limited tubes
No lumped absorbers nor antechamber
Manufacturing process complication.
Distributed pumping
Distributed absorbers
Beam to FE

## Slide 6
MAX IV Vacuum system constrains, challenges and considerations.
Vacuum system layout.
NEG coating issues.
Installation.
Conclusion.

## Slide 7: The vacuum system layout
The vacuum chamber inside diameter is 22 mm (27 mm in the dummy straight sections), 1mm thickness.
Copper vacuum chambers OFS (resistance to activation cycles).
Areas with St. steel for fast corrector coils.
Distributed cooling.
Distributed pumping all along the chamber length, using NEG coating.
One Lumped absorber per achromat is needed to extract the photon beam to the front ends.
Welded bellows to allow the VC to expand without affecting the BPM position.

## Slide 8
One achromat
The vacuum system layout
BPM
Ion pump location
Absorber location
Beam direction
Sector valve location
VC10
VC1
VC2
VC3
VC4
VC5
VC6
VC7
VC8
VC9

## Slide 9
Distributed cooling
Ribs
Cooling for corrector area
Cooling for corrector area
Welded bellows
Welded bellows
Chamber body
Ribs
Beam direction
General Vacuum chamber geometry

## Slide 10
Vacuum chamber layout and the magnets

## Slide 11
Min. clearance with the iron | 0.5 mm
Min. clearance with the coils | 2 mm
Vacuum chamber layout and the magnets
Cooling rib

## Slide 12
Vacuum chamber layout and the magnets
3D printing for parts of the vacuum chamber made of plastic for the magnets’ suppliers.
Gauges with the outer shape of the magnets by the supplier of the vacuum chambers.

## Slide 13
Location of crotch
Absorber for bending magnet radiation
Fast
corrector
position
Crotch
Absorber
Vacuum chamber for beam extraction
Technologies applied:
  Wire erosion.
  TIG welding.
  E-beam welding
  Bending.
  Brazing.
  Milling.
  Etching.
  Turning.
  Etc..
Beam direction
One vertical corrector removed
Cut in iron for FE pipe to pass

## Slide 14
Thermal and mechanical FEA
Calculations being performed to assure safe design for:
Distributed absorbers.
Bellows RF fingers.
BPM stability.
Crotch absorbers (bending magnet radiation).
Insertion devices absorbers.
Deformation of VC.

## Slide 15
Example: absorber for ID SR.
Thermal and mechanical FEA
Temperature (°C)
Stress (MPa)

## Slide 16
MAX IV Vacuum system constrains, challenges and considerations.
Vacuum system layout.
NEG coating issues.
Installation.
Conclusion.

## Slide 17
NEG coating
Effect on the vacuum system design, manufacturing and installation:
Design consideration:
  e.g. space for the coating cathodes.
Manufacturing consideration:
  e.g. Manufacturing processes should not be contaminating.
  e.g. Wire erosion process.
Surface preparation, etching of copper.
Cleaning procedure, testing and certification of process.
Handling before and after coating and storing.
Installation: activation needs.

## Slide 18
Degreasing:
Ethanol/Acetone soaked rag cleaning,
3. Immersion in detergent solution with solution circulation for 5-20 minutes each tube and ultrasonic agitation
(NGL 17.40 sp Alu III at 15 g/l at 55 °C),
4. Rinsing with demineralised
water and drying with N2.
Etching and passivation:
1. Etching at room temp. for 30 minutes (100 g/l ammonium persulphate solution), rinsing,
2. Passivation at room temperature for 5 minutes (chromic acid solution at 80 g/l + 3 ml of Sulphuric acid 96%), rinsing with water and ethanol, drying.
NEG coating - surface preparation at CERN
2. High-pressure rinsing with demineralised water using rotary nozzle (Kärcher),

## Slide 19
NEG coating: R&D at CERN
Purpose of the R&D:
Test coating for small diameter tubes.
Test coating for bent tubes.
Test coating for chambers with antechamber.
Verifying the effect of etching and cleaning on NEG coating.
Validation of manufacturing processes on NEG coating, e.g. wire erosion.

## Slide 20
NEG coating: R&D at CERN
Bent VC:
Ceramic spacers fixed with two Titanium discs
r=19m
0.65 m
0.65 m
1m
30
Coating clearly visible on ceramic spacers
Coating thickness

## Slide 21
NEG coating: R&D
0.5m
#1
#2
#3
2m
VC-2
0.8m
Solenoid
section:
Chambers:
d25
5
7
d22
3
0.74m
VC with antechamber:

## Slide 22
1st trial
2nd trial
VC with antechamber:
NEG coating: R&D
3rd trial

## Slide 23
MAX IV Vacuum system constrains, challenges and considerations.
Vacuum system layout.
NEG coating issues.
Installation.
Conclusion.

## Slide 24
One achromat should be assembled, baked, activated and placed under vacuum inside the magnet block.
Assembly tables: for assembly of one achromat of 23 m.
Lifting tool: for handling flexible copper tubes (mainly after activation) + free expansion during bakeout, space inside the tunnel?
Heater jackets: for activation of NEG, occupy less space.
Protection for bellows during movement.
Installation

## Slide 25
MAX IV Vacuum system constrains, challenges and considerations.
Vacuum system layout.
NEG coating issues.
Installation.
Conclusion.

## Slide 26
Conclusion
Challenging design: technical solutions supported with FEA and tests…etc.
Challenging manufacturing: varies manufacturing techniques, need of follow up, acceptance tests…etc.
Complication due to NEG coating: extensive testing and inspection is needed.
Careful handing and installation.

## Slide 27
Thanks for your attention
Acknowledgment:
Jonny Ahlbäck, Marek Grabski, ALBA, CERN
MAX IV staff