## Slide 1: Radiation hard SiPM development for CEPC calorimeter
Zhijun Liang
IHEP,CAS
Notes: 重点报告内容：（1）未来5年拟开展的研究工作，包括主要研究方向、关键科学问题与研究内容；（2）研究方案，包括骨干成员之间的分工及合作方式、学科交叉融合研究计划、年度工作计划与目标等；（3）五年预期目标和可能取得的重大突破等。

## Slide 2: SiPM introduction
SiPM--silicon photomultiplier: advantage:
  High resolution
  Single photon counting
The goal is to develop Radiation hard SiPM

## Slide 3: Radiation SiPM application
Astrophysics: Space station scientific experiment (Herd …)
Collider physics: calorimeter application
  CMS timing layer, calorimeter
  CEPC calorimeter and time of flight detector
CMS Calorimeter
CEPC PFA
calorimeter
prototype
GECAM
CMS MIP timing detector

## Slide 4: CEPC ECAL and HCAL: SiPM requirement
 | SiPM for ECAL | SiPM for HCAL/muon | SiPM for Cherenkov
Wavelength | 350 – 600 nm | 350 – 600 nm | 100 nm – 600 nm
Size | 3 mm× 3mm | 3 mm× 3mm | 3 mm× 3mm (position sensitive) Or 1mm× 3mm (conventional)
Pixel size | 6 μm × 6 μm | 50 μm × 50 μm Or 20μm × 20 μm | 50 μm × 50 μm ?
PDE | >= 30% (at 420-480nm) | >= 60% (at ~400nm) | 50% at 420nm Sensitive for 200-300nm?
Number of SiPM | ~1 Million | ~5 Million | ~0.2 Million
  ECAL : Small pixel size (6um*6um), large dynamic range
  HCAL: High PDE Sipm (PDE>60-70%)
  Cherenkov: high PDE for UV light

## Slide 5: SiPM radiation hardness challenge
After 10 year operation of CEPC, fluence is above 1013 neq/cm2
SiPM typically work below 1krad or 109 neq/cm2 fluence
  Performance drop after 1krad or 109 neq/cm2
  In great need to develop radiation hard SiPM
Fluence in ZH run（240GeV）
 | Long term Satellite or Space station application | CEPC requirement
TID does | 100 krad | >100 krad
Fluence | ~1010 neq/cm2 | ~1010 neq/cm2 (Barrel) ~1013 neq/cm2 (Endcap)

## Slide 6: SiPM Radiation hardness
After 1010 neq/cm2 or 10Krad dose
  Signal gain decrease
  Energy resolution decrease
  Dark count increase
SiPM gain VS Dose
SiPM dark count VS Fluence
Energy resolution
before/after irradiation

## Slide 7: SiPM dark count after irradiation
Bulk damage after irradiation  dark count increased
Potential Solution:
  Design a special wafer to isolate the dark current from bulk damage
  Isolate the bulk damage from the device
Special wafer

## Slide 8
Pixel size： 50μm
16 x 16 pixels
      SiPM sample from 1st trial MPW run
Small SiPM
We prototyped a small SiPM design

## Slide 9
SiPM读出板
SiPM layout and process has been validated
Typical SiPM signal
      SiPM sample from 1st trial MPW run
SiPM test system
Found a bug in design
SiPM Leakage current is a bit high in 1st trial run
Pstop and GR design has some issue
Optimized the design for engineering runs

## Slide 10: Leakage current of Sipm after irradiation
First trial of this special wafer idea in LGAD development
Indication that IHEP Sipm has potential to be irradiation hard
  After 2E10 neq/cm2, IHEP SiPM leakage current increased by ~10
  After 2E10 neq/cm2, HKP sipm increase by 2-3 order of magnitude
Tested together with HERD team in CSNS.
1E10 neq/cm2 is the fluence received by HERD in 10 years operation
by Tianyuan Zhang.

## Slide 11
Dedicated SiPM engineering run
SiPM for LACT：
7.6 mm X 7.6 mm
152 x 152 pixels
Pixel size： 50um
Fill factor 64%
anode
cathode
GR
Pixel size 50um
Quenching resistance 200KΩ
SiPM designed for LACT
IHEP SiPM layout
Dedicated radiation hard SiPM run will be submitted next month
  Various SiPM size: 1*1mm, 3*3mm, 5*5mm
  Various Pixel size: 10um ,20um, 50um
Designer: MengZhao Li, Mei Zhao

## Slide 12
Dedicated SiPM engineering run
First trial run wafers received at the end of 2025.
  Validate the doping for poly-silicon quenching resistors
  Validate the mask design
Validating quenching resistors: I-V curve
Engineering run wafers
By Weiyi Sun

## Slide 13: Time line for radiation hard SiPM
2026 :SiPM irradiation hard design engineering run
  1st full engineering run ready in June:
    Two type of radiation hard Sipm
      Normal wafers and Special wafers with bulk damage isolation.
2027: 2nd engineering run (More dedicated optimization for CEPC )
  Integration with ECAL/HCAL/ Cherenkov prototype

## Slide 14: Summary
Development for radiation hard SiPM
  Aim for CEPC and Astrophysics application
Key technology has been validated in ATLAS HGTD detector
  Radiation hard LGAD sensor developed by IHEP team
Status of Radiation SiPM R & D project
  1st MPW small prototype was fabricated and tested.
    Showed good potential to be radiation hard in the tests
  Full engineering run designed
    Received trial run wafers at the end of 2025.
    Expect to get full wafers by middle of 2026.
  Plan to integrate into ECAL and HCAL prototyping in the coming years.

## Slide 15: Some thought about the Cost
One 8 inch cost in production : 16k RMB
Number of 3*3mm SiPM in one wafer (assuming 90% yield): ~3000
Raw Cost of SiPM: ~5 RMB
Assuming packaging of SiPM will double the price
Final cost per Sipm ~10 RMB