## Slide 1: Performance study of SiPM for CEPC HCAL
Yuguang Xie
On behalf of HCAL group
2026.02.11

## Slide 2: Content
SiPM for GS-HCAL
SiPM providers and commercial candidates
SiPM performance
Outlook

## Slide 3: SiPM for GS-HCAL
SiPM requirements
High PDE@400nm(>=45%);
High gain(>= 5e5)
Low noise (<=150kHz/mm^2)
Low cost(<=10 RMB/pcs)
GS emission spectrum
Peak：400 nm
MIP response: ~8 MeV/cm
GS characteristics
Parameters | Unit | BGO | PS | GS（GFO）
Density | g/cm3 | 7.13 | 1.03 | 6.0
Melting point | ℃ | 1050 | ~200 | 1250
Radiation Length, X0 | cm | 1.12 |  | 1.59
Molière radius | cm | 2.23 |  | 2.49
Nuclear interaction length | cm | 22.7 | ~59.5 | 24.2
Zeff | -- | 71.5 | ~5.7 | 56.6
dE/dX | MeV/cm | 8.99 | 2 | 8.0
Emission peak | nm | 480 | 425 | 400
Refractive Index | -- | 2.15 | 1.58 | 1.74
Light yield, LY | ph/MeV | 7500 | 10000 | 1500
Energy resolution, ER | %662keV | 9.5 |  | 23
Decay time | ns | 60, 300 | 0.9, 2.1 | 60, 500
Attenuation length | cm | 1.12 | 210 | >4.0
GS-HCAL unit structure
GS unit size: 40×40×10mm(H)
CEPC-HCAL energy resolution requirement
  BMR: 3%~4%; 2. PFA HCAL: ~30%/⊕6.5%
Feature of GS-HCAL
Large sampling ratio ( Thickness 10mm, density 6.0 g/cm3)
Layer thickness: 28mm,Total layers: 48
One 3×3 mm^2 SiPM
at surface center, 60~100 p.e/MIP
40×40×10mm results

## Slide 4: SiPM providers and commercial candidates
Hamamatsu(HPK,滨淞, for HEP)
Fondazione Bruno Kessler (FBK, for HEP)
ON Semiconductor Corp(OSM,安森美, acquisite Sensl, for HEP）
First Sensor (for HEP)
Capital Photonics Technology (Tianjin) Co., Ltd (CPT,中京光电,北师大, for HEP）
Joinbon Technology Co., Ltd.(Hubei) (JBT,湖北锐光科技有限公司, for HEP)
HiSilicon(HuaWei, 华为海思，for LiDAR)
Xilight Technology (XLT,芯辉科技, for LiDAR)
ADAPS photonics(adaps, 灵明光子， for LiDAR)
SiPM suppliers
HPK-S14160
HPK-S13360
JBT-JSP-TP3050-SMT
CPT-EQR20
SiPMs candidates for GS-HCAL
HPK S14160-3050HS/3015PS
CPT EQR20-3030
。。。

## Slide 5: SiPM performance
GS+HPK S13360-6025CS（IHEP)
Some test results earlier
SiPM signal comparison(IHEP)
SiPM performance comparison (JiFeng Han, SCU)
IV curve
DCR
Single photon linearity
Yellow: HPK (40.7V)
Blue: JBT(27V)
Gray: CPT(32V)
CPT
JBT
Yellow: JBT
Blue: CPT
Yellow: JBT
Blue: CPT

## Slide 6: SiPM sensitivity area comparison
HPK66
HPK33

## Slide 7
FBK66
Sensl33
Sensl66

## Slide 8: 1. Difference among factories, also different cost. 2. Imported SiPMs have better precision and uniformity. It is helpful to reduce noise and improve gain uniformity.
NDL33
NDL66

## Slide 9
SiPM Signal（6mm×6mm）
S14160-6050（HPK）
JSP-TP6050-SMT (JBT)
Some test results with customized single channel PreAmplifier
EQR20-11-6060

## Slide 10
SiPM Signal（3mm×3mm）
EQR20-11-3030 （NDL）
S14160-3050 (HPK)

## Slide 11
Spectrum of dark noise
EQR20-11-3030
EQR20-11-6060
S14160-6050

## Slide 12
DCR

## Slide 13
I-V

## Slide 14
 | NDL EQR20- 3030D-S | HPK S14160-3050HS | HPK S14160-6050HS | NDL EQR20- 6060D-S | JB JSP-TP6050
Active Area / mm2 | 3.00 * 3.00 | 3.00 * 3.00 | 6.00 * 6.00 | 6.24 * 6.24 | 6.00 * 6.00
Pixel Pitch /um | 20 | 50 | 50 | 20 | 50
Microcells | 22500 | 3531 | 14331 | 97344 | 13852
Typical Breakdown Voltage / V | 27.2 | 38 | 38 | 27.2 | 24.6
PDE @ Typical Operate Voltage | 47.8% @ 420nm | 50% @ 450nm | 50% @ 450nm | 47.8% @ 420nm | 35% @ 420nm
Gain | 8.0E5 | 2.5E6 | 2.5E6 | 8.0E5 | 2.1E6
Temperature Coefficient /mV/℃ | 24.8 | 34 | 34 | 24.8 | 34.4
Terminal Capacitance /pF | 57.5 | 500 | 2000 | 397 | 2355
Dark Current/μA | 1.5 | 1.1 | 5.5 | 10.2 | 12.5
SiPM radiation resistance

## Slide 15
 | ΔDCR/DCR | ΔId/Id
NDL EQR20-3030D-S | 1.49 | 0.39
HPK S14160-3050HS | 2.89 | 1.15
DCR_after-DCR_before/DCR_before; I_after-I_before/I_before;
@ After 116 Gy

## Slide 17
About 150 p.e/MIP
KEK electron beam(5GeV) test
5 GeV e response at different thickness GS unit
Single 3*3mm^2 SiPM+GS unit
Beam
ECAL
GS Test
40*40*3 mm3 PS trigger
10*40*3 mm3 PS trigger
GS+SiPM
5GeV, 1.6 kHz

## Slide 18
GS | Reflector | MIP Response (p.e./MIP) |  |  |  | 
 |  | HPK 3050HS | HPK 6050HS | NDL 3030 | NDL 6060 | NDL 3030 with new FEE
BGRI-146 | Teflon | 127.0±0.9 | 408.6±2.7 | 163.4±3.2 | 385.3±5.0 | 104.1±1.0
 | Tyvek | 88.4±1.2 | 426.7±2.9 | 120.3±1.1 | 418.8±8.9 | 95.0±0.6
BGRI-147 | TiO2 | 84.5±0.4 | 417.0±4.6 | 167.4±2.3 | 361.6±9.2 | 106.8±1.6
BGRI-E6 | Teflon | 14.7±1.0 | 153.1±1.4 | 17.2±0.3 | 151.4±1.8 | /
The MIP response of GFO glass coupled with 3*3 mm2 SiPM is around 84.5~127(HPK) and 120~167(NDL) p.e./MIP.
Teflon, Tyvek, and TiO2 coatings are close within 33.4%(HPK3*3), 28.14%(NDL3*3), 4.24%(HPK6*6), 13.66%(NDL6*6)
TiO2 coating can be applied as a reflective layer for the glass in GSHCAL.

## Slide 19
HCAL miniPrototype CERN SPS hadron beamtest
Tow 7-Layer modules, 3*3 GS+SiPM units per layer.
Pi, Mu @ 180 GeV, scan 5/20//50/100/120/150/180 GeV, change +16° and -11° angle.
~110 p.e./MIP for Pi.
Both HPK and CPT SiPMs worked well.
Oblique incidence π
Normal incidence μ
π response at different thickness GS unit
Mu deposited energy

## Slide 20: Outlook
Item | Requirement/Goal | Remark(Ref)
Size (mm) | 3*3/6*6 | 4*4 also optional
Encapsulation | SMD | 
Pixel (um) | 25 ?40? (>20um) | Must to balance DCR
PDE@400nm （%） | >= 50% (60%@420nm?) | now 45%
Gain | >= 5e5 | now 8e5
Dynamic range: | 10~10000 P.E | Depends on pixel size
Dark counting rate(DCR, kHz/mm^2） | <100 | now 150
Terminal capacitance(pF） | <=100 | now 57.5
Temperature coefficient(mV/℃) | <25 | now 24.8
Cost for mass production(RMB/pcs) | <=10 | Now ~20
For the future, two development directions:
Low cost high performance SiPM; Self-develop or cooperate with suppliers
Low noise high gain front-end electronics development (high channel density, low power consumption ASIC).

## Slide 21: Technical consideration
Pixel (um) | 20/25/30um, DR: 10~10000 P.E, (22500 for 20um) ,
PDE@400nm （%） | Increasing depletion layer?
Dark counting rate(DCR） | Add guarding ring like HPK?
Optimize encapsulation | Small rim acceptable(<=1mm per side), reduce cost
Version update | Modification and update based on current product , if have
New design | Aiming at CEPC HCAL requirement, maybe expensive and long lead time