## Slide 1: Progress of triangular carbon fiber beam for ITK
Xiaohui Qian, Jian Wang, Yujie Li, Jiajian Zhang, Qi Yan
IHEP.CAS
202603

## Slide 2
content
Structure of triangular carbon fiber beam
Manufacturing of 500 mm length beam
Manufacturing of 1000 mm length beam
Static mechanical test of 1000 mm length beam

## Slide 3
Structure 1：16.31g
Structure 2：15.54g
Main Beam: 0.4mm：0-0-0-90-0-0-0，layer thickness: 0.05mm, M40J
secondary beam: 0.3mm，Carbon fiber filament, T700
Base glue: epoxy
1000
0.3
0.3
Structure of triangular carbon fiber beam
Main Beam
secondary beam

## Slide 4
Deformation by FEA
Main beam deformation: 17.97um
Total deformation: 20.32um
face load on main beam：20Pa (988X41mm), ~80g, not considering cold plate
Gravity ，density 1840kg/m^3
Fixed support both end side
Buckling coefficient: 39.6
Buckling coefficient: 36.5
Structure 1:
Main beam deformation: 18.63um
Total deformation: 20.02um
Structure 2:

## Slide 5
Triangular beam with cold plate
Carbon fiber felt
Triangular carbon fiber beam
Graphene film
carbon fiber plate
Cooling tube
Carbon fiber felt
Sensor(heat source)
Cold plate
The thickness of each layer film of cold plate is different with the picture.

## Slide 6
Manufacturing of 500mm length beam
Mold design:
Almost the same structure as ALICE’s tracker mold
Cross section
Silicone Rubber Rod
PTFE rods
PTFE rod
Slotted outer mold
ALICE’s tracker mold

## Slide 7
Manufacturing of 500mm length beam
Aluminum Mold
Carbon fiber of Secondary beam can not be continuous——separated into lots of carbon fiber rods

## Slide 8
Products of triangular beam
Failure samples (ALICE method)
Not continuous of CF makes the bonding strength between secondary beam and main beam very weak (<2 mm bonding length)
Main beams and secondary beams hard to be their position
Success samples:
Changing the process of secondary——not in the slots of outer mold——continuous fiber

## Slide 9
Manufacturing of 1000mm length beam
Mold design of Beam:
Main difference: the slots in the mandrel
Length of Beam:1000 mm
Secondary beam length: ~7m
PTFE mandrel
Slotted stainless steel plate
Mandrel and Stainless Steel Outer Mold
mandrel

## Slide 10
Mold
Cold plate mold
Triangular beam mold

## Slide 11
Mold

## Slide 12
Main beam：0/0/0/90/0/0/0，M40J
Secondary beam： Unidirectional Carbon Fiber Tows: T700， 12K
First beam weight: 13.9g
mandrel
Manufacturing of 1000mm length beam
First beam
The carbon fiber thread is manually wound on the mandrel.

## Slide 13
Cross section of cold plate mold
Mold design of cold plate:
The stainless steel mold features two elongated slots for inserting the cooling tubes
Length of plate:1000 mm
Put the different material film in the mold layer by layer
Slote for the cooling tube: OD1.6mm
Manufacturing of 1000mm length beam
cooling tube

## Slide 14
First cold plate
Bended for the thermal coefficient difference between materials

## Slide 15
Carbon fiber direction: 0/0/90/0，stainless steel tube
Carbon fiber direction: 90/90/90/90， stainless steel tube
Carbon fiber direction: 90/90/90/90, Titanium tube
FEA of thermal deformation（load：-100℃）
116mm
17.7mm
-9.2 mm

## Slide 16
Optimizing Laying to change the bending of cold Plate
Carbon fiber direction: 0/0/90/0，
Carbon fiber direction: 90/90/90/90，without Graphene film
Carbon fiber direction: 0/90/90/90， without Graphene film
Carbon fiber direction: 90/90/0/90， without Graphene film
Good quality of the thickness consistency: 0.28±0.02mm
Reduce the bending amplitude
Cold plate manufacturing test of different direction
1
2
4
3

## Slide 17
Assembly of cold plate and triangular beam

## Slide 18
Static mechanical test of triangular beam
Supporting method: fixed and pinned support
Load: concentrated load with standard weight (50g)
Displacement measuring: Dial gauge, resolution 1um, accuracy ±5um
Two Beams: beam1：13.9 g and beam2：15.1 g
standard weights
Dial gauge
Triangular beam
Supporting structure

## Slide 19
Loading progress
Unloading progress
Beam2-fixed supporting
Load: 0~450g
Loading and unloading curves are not matched together
Displacement is not linear as the weight increases
Creeping is obvious under high load

## Slide 20
Fixed boundary:
50g: 37.25 ± 0.96 um
100g: 84.75 ± 2.63 um
150g: 132.50 ± 1.91 um
Pinned boundary:
50g: 80.50 ± 3.42 um
100g: 166.50 ± 8.89 um
150g: 279.00 ± 11.34 um
Beam2 test
Low load for creeping: 0~150g
Creeping also exist: curve is not linear

## Slide 21
FEA of test beam
Fixed boundary
load：50g—concentrated load
Test data：beam1 34.75±2.22 um
beam2 37.25 ± 0.96 um
FEA result(main beam)：36.3um

## Slide 22
FEA of test beam
Fixed boundary
load：50g —concentrated load
Test data：beam1 94.00 ± 3.46 um
beam2 80.50 ± 3.42 um
FEA result(main beam)： 81.49 um

## Slide 23
FEA of beam under the exact sensor weight
Fixed boundary
Sensor weight: 80g——uniformly distributed load
Deformation is ~20um better than that of concentrated load of 50g

## Slide 24
Under 50g load, the result can be matched well between FEA and test results.
The two beams deformation almost the same under the fixed boundary condition
Under pinned boundary condition, Beam1(13.9g) deformation is larger than beam2’(15.1g)
Compare between FEA of test result
Comparison under fixed boundary condition
Comparison under pinned boundary condition
FEA
Beam1 and beam2
FEA
Beam1
Beam2

## Slide 25
Conclusion
Successfully manufactured the 1000mm triangular CF beam
The weight of 1000mm beam is ~15g, and its deformation is about 35um under the 50g concentrated load, 80gjub~20um
FEA result can match well with test results
The beam under high load may be creeping obviously
The mold could be further optimized in future

## Slide 26
Back up

## Slide 27
Loading progress
Unloading progress
Beam1-fixed supporting
Load: 0~450g
Loading and unloading curves are not matched together
Displacement is not linear as the weight increases
Creeping is obvious under high load

## Slide 28
Beam1-固支
荷载：0~150g
线性度一般，最大变形
50g: 34.75±2.22 um
100g: 85.00± 6.32 um
150g: 134.25 ± 1.89 um
50g: 94.00 ± 3.46 um
100g: 224.50 ± 5.74 um
150g: 344.00 ± 14.83 um

## Slide 29
固定支撑
载荷：100g

## Slide 30
固定支撑
载荷：150g

## Slide 31
铰链支撑
载荷：100g

## Slide 32
铰链支撑
载荷：150g

## Slide 33
主梁使用M40J 单层50μm
铺层：0，0，0，90，0，0，0
腹杆使用T700 单层50μm
单向，6层