## Slide 1: Study on SiC Sensor Application in Fast Luminosity Detectors
Xiyuan Zhang1 , Yanpeng Li1,2, Meng Li1,3 , Jiaqi Zhou1,2 , Haoyu Shi1, Dou Wang1, Philip Bambade3, Weimin Song2 and Xin Shi1
1Institute of High Energy Physics, CAS
2Jilin University
3Laboratoire de l'Accélérateur Linéaire (LAL),Centre Scientifique d’Orsay

## Slide 2
Crab waist scheme for CEPC to achieve a very high luminosity (5×1034 cm-2s-1)
  IP beam size very small
  Luminosity sensitive to the stability of beam jitter (like ground motion)
Orbit feedback system at the IP to maintain an optimum collision and maximize the luminosity
Two possible methods for the IP orbit feedback system
Insufficient BPM resolution in the horizontal plane, a luminosity-driven dithering feedback system required
Necessity of the Fast Luminosity Monitor for CEPC
Vertical IP orbit feedback——Beam-beam deflection driven method
Horizontal IP orbit feedback——Luminosity driven method
Based on the measurement of the offset with BPMs upstream and downstream of the IP
  Based on the measurements of the luminosity with a certain frequency dithering
Meng Li from accelerator

## Slide 3
Fast Luminosity Monitor working principle
The fast luminosity monitor based on radiative Bhabha at zero degree
  Very large cross section (127mbarn)
  Bhabha particles produced at the IP are proportional to the luminosity
The low energy Bhabha hit the vacuum chamber downstream of the IP
The detectors put outside the beam pipe measuring the secondary particles to provide the luminosity information
  Number of Bhabha sensitive to the change of luminosity in proportion way (relative luminosity measurement)
  Precision requirement：2% @1khz （Number of detected Bhabha electrons  2500 ）
Meng Li from accelerator

## Slide 4
The position of Fast Luminosity Monitor
  Low-energy scattered electrons are mainly lost at Position 1、2 and 3
  Positions 1 and 3 ：suitable for detector installation
  Position 2 excluded：not feasible for detector installation（ inside the dipole magnet ）
Meng Li from accelerator
355ns

## Slide 5
Simulation workflow in RASER (RAdiation SEmiconductoR)
Simulation of the energy deposition of Bhabha electron events from GEANT4
Simulation of the electrical field & weighting field from DEVSIM
Simulation of the current signal from Calcurrent in RASER (RAdiation SEmiconductoR)
Simulation of the voltage signal from NGSPICE
Shockley–Ramo theorem
Electrical field & weighting field
Independent development
Carrier Drift & Diffusion
Energy deposition
Advantages
Open Source;
Strong expandability;
Easily interact with other software
https://raser.team
Simulate the waveform generated by a single particle in a detector

## Slide 6
Detector Geometry & Layout Optimization
Detector dimension :
  Total Size：1 cm (beam) × 3 cm (vertical)
  Unit size: 5 mm × 5 mm per pixel
  Noise requirement (for precision ): at Position3
                at Position1
Detector layout
  Position1: double detectors - symmetrically on
  inner and outer of beam pipe
  Position3: single detector – on outer side only
Optimal choice：Position 3
  Single sided placed
  Lower noise requirement
  Unaffected by beam-beam deflection and synchrotron
Position 1: Also suggested by accelerator colleagues
  Larger required detector area；Severely affected by background
3cm
1cm

## Slide 7
The Simulation to Estimate the Signal in the Detector
Types of secondary particles detected
  Photon-dominated （ ~87% of detected secondary particles ）
  Electrons ~ 8%
  Others ~ 5%
Detector performance at nominal luminosity （Position3）
  Total Energy deposition：~6 MeV per bunch crossing
  Single-pixel current pulse: ~70 μA, ~3 ns full width

## Slide 8
The Simulation to Estimate the Signal in the Detector
Detector response to luminosity reduction
  Simulation conditions: (nominal) vs.
Observed effects at reduced luminosity
  Fewer signal peaks (events decrease)
  Lower amplitude per peak (weaker individual signals)
Position3

## Slide 9
The Simulation to Estimate the Signal in the Detector
Quantifying Detector Response vs. Luminosity
  RAW SUM：Sum of sampling points exceeding threshold within 1 ms
Key findings
  Liner relationship: RAW SUM proportional to luminosity
  Precision:
    Nominal L0： 2%
    10% L0：～7%
  SuperKEKB experience:
  Even 7% precision feedback reduces beam offsets
  p: pixel number ；s: sampling point （10GHz，1ms）
DOI 10.1088/1748-0221/21/02/T02009

## Slide 10
Silicon carbide
Wide band material Silicon Carbide(SiC) as particle detector material:
Pros:
  Bandgap between silicon and diamond
  Higher saturation velocity and breakdown field
  Larger atomic displacement threshold
     Potentially good radiation hardness
  No dark current increase after irradiation
  High thermal conductivity
     No cooling needs
  No sensitivity to visible light
Cons:
  Different polytypes(3C, 4H, 6H)
  Higher ionization energy
     Smaller signals  LGAD
  Epitaxial-grown limited to ~150μm thickness
Large-area Process
Ionization Energy [eV]
Bandgap[eV]
Breakdown Electric
Voltage [V/cm]
Electron Saturation Velocity [cm/s]
Displacement Energy [eV]
Price
3.6
7.6
13
13-15
30-40
43
3· 105
4· 106
107
2.2· 107
2· 107
0.8· 107
5.5
3.23
1.12
High-cost
Mid-range
low-cost
Mature
Immature
Highly mature
Diamond
SiC
Si

## Slide 11
4H-SiC detector development @ IHEP —— SICAR1_PIN detector
4H-SiC PIN detector structure（1.2 x1.2 mm2）
  Full epitaxial growth including N- active region(50 ) and P++ layer
  Mesa termination + Field plate  reduced field crowding
  Without high temperature ion implantation and high temperature post-annealing
Excellent thermal stability
  Ultra-low leakage current: ~50 pA at RT, ~10 nA at 90°C @300V
  Capacitance temperature stability
    Full depletion voltage ~ 76V
    Full depletion capacitance: ~ 3.5 pF
  CCE（α）：negligible variation
  Ultra fast rise time
https://doi.org/10.1016/j.nima.2025.171178

## Slide 12
4H-SiC detector development @ IHEP —— SICAR1_PIN
FLM for CEPC—Secondary particle fraction
  γ ：87% ； e- ：8%
X-ray radiation hardness up to 2MGy
  Leakage current remains stable
  CCE（β particle）— no degradation
Electron radiation hardness up to 1x1016 e/cm2
  CCE reduction in the range of 10% at 1x1016 e/cm2
[1] https://doi.org/10.48550/arXiv.2603.18547
[2] DOI: 10.1109/TNS.2020.3029730

## Slide 13
Proton irradiation assessment of 4H-SiC PIN from NJU
4H-SiC PIN-NJU（ 1.5 x1.5 mm2 ）
Irradiation source— China Spallation Neutron Source （CSNS）
  Beam energy: 80 MeV protons
  Beam spot size: 20 mm × 20 mm
  Fluence: 1.4e11 p/cm², 2.5e12 p/cm², 7.0e12 p/cm², 7.0e13 p/cm²
NJU

## Slide 14
Proton irradiation assessment of 4H-SiC PIN from NJU
Leakage current decreases with increasing irradiation fluence（Opposite to Si）
C-V curve gradually flattens
  Acceptor defects cause compensation effect on n-type doping
Alpha particle charge collection efficiency (CCE) degrades
  CCE Drops to 30% of 7.0×10¹³ p/cm²

## Slide 15
4H-SiC detector development @ IHEP —— SICAR1_PIN
Time resolution
  90Sr source
  TIA amplifier (UCSC) + 2nd amplifier （PE 15A1008）
  Reference（CH1）：Si-LGAD NDL （35ps）
  Time resolution of 4H-SiC PIN ～21ps

## Slide 16
Beam monitor at BSRF- 4W1A
Simulate CEPC beam at BSRF- 4W1A
  Photon flux：7.5 x1012 Phs/sec/0.1% BW
  X-ray + electron response
  External trigger: 1 Hz, sampling length: 100ns
  Detector output signal closely follows beam current（e-） trend
Electron signal
X ray signal

## Slide 17
4H-SiC detector development @ IHEP —— SICAR1_LGAD
4H-SiC LGAD detector structure（1 x1 mm2）
  Full epitaxial growth including N- active region(50 )
  N+ gain layer and P++ layer
  Mesa termination
  Without high temperature ion implantation and
  high temperature post-annealing
Gain factor calibration with α source
  Gain factor: 2-3 @ 300V
50
[DOI: 10.1109/TNS.2024.3471863]

## Slide 18
4H-SiC detector development @ IHEP —— SICAR1_LGAD
4H-SiC LGAD proton irradiation hardness
  Beam energy: 80 MeV protons;
  Fluence: 1.4e11p/cm2 , 2.5e13p /cm2 , 7.0e13 p/cm2
  CV
    Parallel-plate capacitor-like (2.5e13 p/cm2 ~7e13 p/cm2 )
  IV
    > 1A @300V (No irradiation);
    5 orders of magnitude higher than PIN
    Decreases with increasing fluence; reaches nA level at highest fluence

## Slide 19
4H-SiC detector development @ IHEP —— SICAR1_LGAD
Charge collection vs. irradiation fluence
  CCE degrades with irradiation fluence increasing
  7e13p/cm2 → CCE drops to 57% → Superior to PIN devices（CCE drop to 30%）
[DOI: 10.1109/TNS.2025.3635073]

## Slide 20
4H-SiC detector development @ IHEP —— SICAR3_LGAD
4H-SiC LGAD optimization_SICAR3
  High-temperature (500°C)； high-energy implantation > 1 MV
  High-temperature annealing (1700°C) → Activate carriers and repair defects
  High fabrication complexity and high cost → MPW
SICAR3

## Slide 21
4H-SiC detector development @ IHEP —— SICAR3_LGAD
Leakage current
  PIN：~1 nA at 1000 V without breakdown
  LGAD ：Wafer1～100nA ； Wafer2～200nA； Wafer3～1 Wafer4～4
C-V
  Gain layer fully depleted at 120V ～150V
  Active layer fully depleted at 600V

## Slide 22
4H-SiC detector development @ IHEP —— SICAR3_LGAD
Charge collection of beta @700V ： ~3 fC（PIN）；～40fC （LGAD）
Gain ～ 13 @ 700V

## Slide 23
Summary
Thanks！
  Simulation determines the optimal position and geometry of the SiC-based Fast Luminosity Monitor for CEPC， meeting the 2% precision requirement.
  Simulated detector response vs. luminosity variation demonstrates its capability for real-time luminosity feedback.
  SiC is radiation-hard, for photons and electrons
  SiC LGAD achieves 13× gain factor at 700 V
  .

## Slide 24
Backup：Beam monitor for CSNS
High Energy Proton Experimental Station (HPES)
  China's first 1.6 GeV proton source
  a beam monitoring system to detect the flux of the proton beam
…
…
410ns
Macro pulse period: 40 ms
1 ms
Time
Pulse interval 39 ms
80ns
410ns
Micro pulse period：410ns

## Slide 25
Beam monitor for CSNS
Signal acquisition using a 375 nm laser system
  a signal generator to simulate the pulse period（40ms）
  The charge collection decreases linearly with the laser intensity

## Slide 26
Beam monitor for CSNS
ADC-FPGA co-debugging