## Slide 1
Vadim Grinenko
Tsung-Dao Lee Institute, Shanghai Jiao Tong University, Shanghai
Superconductivity with broken time-reversal symmetry in Sr2RuO4: pros and cons
24 October 2026
The 3rd Workshop on Muon Science Technology and Industry
MELODY2026

## Slide 2: μSR investigations of Sr2RuO4 (main collaborators)
Hubertus Luetkens
PSI Villegen
Rustem Khasanov
PSI Villegen
Hans-Henning
Klauss
TU Dresden
Shreenanda
Ghosh
The Johns Hopkins University
Clifford
W. Hicks
University of
Birmingham
Manfred Sigrist
ETH Zurich
Yoshiteru Maeno
Kyoto University
Naoki Kikugawa
NIMS
Zurab Guguchia
PSI Villegen
Yongwei Li
TDLI, Shangahi
Experiment
Rajib Sarkar
TU Dresden
Theory
Julien Garaud
Institut Denis
Poisson CNRS-UMR
Anton Talkachov, KTH, Shtokholm

## Slide 3: Superconductors with broken time-reversal symmetry
and
Two energetically equivalent states with Δ ≠ Δ*
meaning spontaneously broken Z2 symmetry.
T(Z2) – time reversal symmetry: Δ Δ* ≠ | Δα|eiθ
T
Broken time-reversal symmetry (BTRS) state can be described by two component imaginary order parameter: .
Two different phase transitions → Tc ≠ TBTRS and two different coherence lengths ξU(1) ≠ ξZ2;
Spontaneous current around inhomogeneities and at the domain walls.
https://slideplayer.com/slide/5363094/
At Tc broken U(1)
The fundamental symmetry which spontaneously violates by any superconducting state.
?
?
V (Δ)
Δ*
Δ
0
L.P. Gor’kov, Sov. Sci. Rev. A Phys. 9 (1987) 1;
M. Sigrist and K. Ueda, Rev. Mod. Phys. 63 (1991) 239.
Notes: According to modern theories, the possible ground states that are realized in nature are constrained by the symmetry of the physical system.
This, for example, explains appearance of charge-2e superconductivity: a condensate of electron pairs.
In this case, the number of components of the order parameter equals the number of broken symmetries.
We propose that, in some complex systems, the ground state is defined by the free-energy landscape but not by the symmetry of the system.
This, in particular, may result in new states of matter, including Chiral Quadrupling order with broken time-reversal symmetry and Charge-4e superconductivity.
In these states, the number of components of the order parameter can exceed the number of broken symmetries.

## Slide 4: Superconductors that break time-reversal symmetry (BTRS)
Two-component order parameter |Δ1(2)|eiφ1(2) with double degenerate states:
{|Δ1|, |Δ2|, φ1 – φ2 = θ12} → {|Δ1|, |Δ2|, φ1 – φ2 = -θ12}
The degeneracy is lifted by any perturbation.
Degenerate order parameter
Intrinsically |Δ1| = |Δ2|, θ12 = ±π/2 Tc = TBTRS
Examples: px ± ipy, dxz ± idyz, …
Symmetry-breaking perturbations of the crystal lattice lift the degeneracy.
Non-degenerate or accidentally degenerate order parameter
|Δ1| ≠ |Δ2|, θ12 ≠ 0,π fine tuning for Tc = TBTRS
Examples: s ± is’, s ± id, d ± ig, …
A. Talkachov and E. Babaev Phys. Rev. B 113, 144515 (2026).
V. Grinenko, S. Ghosh et al. Nat. Phys. 17, 748–754 (2021).
BTRS
Δ1 or Δ2
Δ1 or Δ2
Δ1 ± iΔ2
Δ1 ± iΔ2

## Slide 5: What are experimental signatures of BTRS superconductivity?
Generation of spontaneous magnetic fields at domain walls, sample surfaces and around nonmagnetic inhomogeneities. Experiments: µSR, Polar Kerr effect, non-reciprocal effects in transport.
Thermodynamic signature of two phase transitions. Experiments: Specific heat, ultrasound and etc.
Multicomponent superconducting order parameter.
Experiments: several superconducting gaps in STM, ARPES, quantum vortex fractionalization, superconducting domain walls.
Are there examples of multicomponent superconductors?

## Slide 6: UPt3 is a strong candidate for chiral superconductivity
Two anomalies in the specific heat
T. H. Trappmann et al, Phys. Rev. B 43, 13714 (1991).
Kerr effect below Tc
Time-Reversal symmetry breaking
E. R. Schemm et al. Science345,190-193(2014).
Half-quantum vortices in the bulk
P. García-Campos et al., arXiv:2512.03908

## Slide 7: Strong evidence for multicomponent BTRS superconductivity in Ba1-xKxFe2As2
Two anomalies in the specific heat
Muon-spin rotation (µSR)
Time-Reversal symmetry breaking
3-typs of unquantized vortices
Y. Zheng, Q. Hu et al., Science 393, 80-84 (2026)
3-superconducting gaps
Y. Zheng, Q. Hu et al., Science 393, 80-84 (2026)
STM
Scanning SQUID
Q. Z. Zhou et al., arXiv:2408.05902
Y. Iguchi et al. Science 380,1244-1247(2023).
V. Grinenko et al., Nat. Phys. 17, 1254–1259 (2021)
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020).
I. Shipulin et al., Nat Commun 14, 6734 (2023).
Second harmonic generation

## Slide 8: Sr2RuO4 is multiband superconductor
Sr2RuO4 has a complex electronic structure, makes it similar to Fe-based superconductors.
Fermi surface
Crystal structure
C. Hicks, MPI Dresden
Electronic orbitals relevant for conductivity
S. Raghu et al., Journal of Physics: Conference Series 449, 012031 (2013).
What do we know about Sr2RuO4?

## Slide 9: Some experimental evidences for multicomponent order parameter in Sr2RuO4
Polar Kerr effect
J. Xia, A. Kapitulnik et al., PRL (2006)
Enhanced muon spin relaxation rate below Tc → spontaneous magnetic fields
Luke, G. M. et al. Nature 394, 558–561 (1998)
Jump in transverse sound viscosity at Tc, -> indication for 2D order parameter.
C. Lupien, PhD thesis (2002)
S .Ghosh et al., Nat. Physics (2020) , S. Benhabib et al., Nat. Physics (2020)
Altogether these experiments are consistent
with chiral state.
Superconducting diode effect
in ZF
M.S Anwar et al., Commun Phys 6, 290 (2023).
R. Fermin et al., arXiv:2504.19361

## Slide 10: Evidences against chiral superconductivity in Sr2RuO4
Half-quantum vortices are not observed
J. R. Kirtley, et al., Phys. Rev. B 76, 014526 (2007)
C. W. Hicks et al., Phys. Rev. B 81, 214501 (2010)
Absence of edge currents?
Scanning SQUID microscopy
C. W. Hicks et al., Science 344, 283-285 (2014).
A. Steppke, et al., Science 355, eaaf9398 (2017).
Missing kink in Tc under strain
Theory
Experiment
Non-chiral p-wave!?
The reduction of the NMR Knight shift below Tc
A. Pustogow et al., Nature 574, 72 (2019).
J. Jang et al., Science331,186-188(2011).
But Half-Height Magnetization Steps are observed

## Slide 11: The main motivation
Is Sr2RuO4 a chiral (Δx ± iΔy) superconductor?

## Slide 12: How can we distinguish between chiral and non-chiral superconductivity using µSR?
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Tc and TBTRS transitions must split under symmetry breaking uniaxial strain.
(dxz ± idyz)
(100) direction
x
y
Tetragonal
Orthorhombic
(110) direction
Uniaxial pressure
Splitting of Tc and TBTRS is expected for both: chiral and accidentally degenerated orders.
Important demonstration that Tc and TBTRS are related to a different phase transitions.
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Do not split with the hydrostatic pressure and isotropic disorder.
Do split with the hydrostatic pressure and disorder.

## Slide 13: Sr2RuO4 under the (100) strain
Tetragonal
Orthorhombic
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021).
along (100)
Experimental setup for the μSR:
S. Ghosh et al., Review of Scientific Instruments 91, 103902 (2020).
Tc is measured by AC susceptibility.
TBTRS by zero-field µSR.
A. Steppke, et al., Science 355, eaaf9398 (2017).
What is the effect of van Hove on BTRS state?
Can van Hove induce magnetism?

## Slide 14: BTRS superconductivity of Sr2RuO4 under the (100) strain
A. Steppke, et al., Science 355, eaaf9398 (2017).
Relaxation rate, λ (µs-1)
Temperature (K)
AC susceptibility
Tc
TBTRS
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021)
Relaxation rate, λ (µs-1)
Temperature (K)
AC susceptibility
TBTRS
Significant splitting of TBTRS and Tc!
BTRS state exists above van Hove singularity!
Tetragonal
Orthorhombic

## Slide 15: Strain induced SDW phase in Sr2RuO4
A. Steppke, et al., Science 355, eaaf9398 (2017).
Tetragonal
Orthorhombic
An incommensurate SDW phase well above the van Hove singularity with TN ~ 7 K;
van Hove
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021)
Small internal magnetic fields correspond roughly to 0.1 µB (similar to Sr3Ru2O7);
The SDW internal field is 100 times stronger than spontaneous fields due to BTRS superconductivity.

## Slide 16: μSR measurements of Sr2RuO4 under uniaxial strain
Superconducting Tc and TBTRS split by uniaxial strain → two distinct phases!
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021).
SDW state
Elastocaloric effect
YS. Li et al., Nature 607, 276–280 (2022).
SDW phase detected by μSR is confirmed by elastocaloric effect measurements.
M. S. Anwar et al., arXiv:2211.14626v1
Spontaneous superconducting diode effect
Split Tc and TBTRS is confirmed by spontaneous superconducting diode effect measurements.
x
y
Tetragonal
Orthorhombic
Uniaxial strain induces spin density wave order (SDW) above the Lifshitz transition in odd with early theoretical predictions.
Lifshitz transition
What is the evidence from other probes in favor of the μSR phase diagram?
TBTRS
Tc

## Slide 17: How can we distinguish between chiral and non-chiral superconductivity using µSR?
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Do split with the hydrostatic pressure and disorder.
Tc and TBTRS transitions must split under symmetry breaking uniaxial strain.
Do not split with the hydrostatic pressure and isotropic disorder.
(dxz ± idyz)
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Disorder effect on Tc
N. Kikugawa et al., Phys. Rev. B 70, 060508(R) (2004)
At small concentrations the dominant effect of La on Tc is related to a pair breaking effect.
La-doping results in isotropic in-plane disorder without anisotropic internal strain.
La-doping is an ideal tool to study the effect of disorder on Tc and TBTRS

## Slide 18: Time reversal symmetry breaking in Sr2-yLayRuO4
The normal state electronic specific heat is nearly the same for all samples, γn ≈ 40 mJ/mol-K2 -> the DOS are unchanged.
Sharp superconducting transition -> homogeneous suppression of superconductivity by a pair braking effect.
1% of La doping suppresses Tc by 50% as compared with a impurity free Tc0

## Slide 19: Time reversal symmetry breaking in Sr2-yLayRuO4
TBTRS ≈ Tc in La-doped samples;
Together with the splitting between TBTRS and Tc under uniaxial strain.
→ consistent with a chiral superconductivity in Sr2RuO4
TBTRS ≈ Tc
V. Grinenko et al., Nat Commun 12, 3920 (2021).
TBTRS ≈ Tc
Sr1.98La0.02RuO4
Y Li et al., arXiv preprint arXiv:2512.24585
Y Li et al., arXiv preprint arXiv:2512.24585
PSI
ISIS
ISIS

## Slide 20: Theory: Splitting of the Tc and TTRSB under disorder for accidentally degenerated orders
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Do split with the hydrostatic pressure and disorder.
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Fine-tuning is possible that transitions do not split with disorder.
d+ig state
Therefore, additional experiments are needed!
B. Zinkl. & M. Sigrist, arXiv:2009.10089 (2020).
Manfred Sigrist

## Slide 21: How can we distinguish between chiral and non-chiral superconductivity using µSR?
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Do split with the hydrostatic pressure and disorder.
Tc and TBTRS transitions must split under symmetry breaking uniaxial strain.
Do not split with the hydrostatic pressure and isotropic disorder.
(dxz ± idyz)
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Hydrostatic pressure preserves tetragonal symmetry a = b
x
y
Tetragonal
D. Forsythe et al., Phys. Rev. Lett. 89, 166402 (2002)
N. Shirakawa et al., Phys. Rev. B 56, 7890 (1997)
“Fine tuning” is impossible for both disorder and hydrostatic pressure!

## Slide 22: The first μSR measurements of BTRS superconductivity under pressure
TBTRS ≈ Tc due disorder and under hydrostatic pressure
BTRS transition temperature, TBTRS (K)
TBTRS = Tc
Superconducting transition temperature, Tc (K)
V. Grinenko et al., Nat Commun 12, 3920 (2021)
Evidence for two component chiral
superconductivity in Sr2RuO4.
Rustem
Khasanov
Tc
TBTRS
Temperature (K)
Suppression of superconductivity and time-reversal symmetry breaking under pressure.
Tetragonal
Sample +cell
Sample
xLa=0.01
xLa=0.04

## Slide 23: Sr2RuO4 under hydrostatic pressure
Tc
TBTRS
Temperature (K)
TTRSB follows Tc under the hydrostatic pressure.
Rustem
Khasanov
Tetragonal
V. Grinenko et al., Nat Commun 12, 3920 (2021)
Y Li et al., arXiv preprint arXiv:2512.24585
New measurements under higher pressure

## Slide 24: The strength of spontaneous relaxation vs. Tc in Sr2RuO4 for samples with Tc ~ TBTRS.
However, the relaxation should vanish for Tc ~ 1.4 K.
1. The relaxation rate has a minimum in the samples with Tc ≈ 1.45 K.
2. Relaxation is enhanced by superconductivity affecting disorder
neff ≈ n0eff(1 - Tc/Tc0), where Tc0 = 1.45 K.
3. Relaxation is suppressed by the hydrostatic pressure or with La-doping roughly following .
?
Y Li et al., arXiv preprint arXiv:2512.24585
What is the mechanism for muon relaxation in exceptionally clean samples?

## Slide 25: Search for correlation with magnetic impurities
No correlation of the enhanced relaxation rate with typical magnetic impurities;
Scanning transmission electron microscopy (STEM) of clean and disordered samples revealed the dislocation density dislocation density of < 1011 m-2.
Magnetic susceptibility χ(T) for Sr2RuO4 samples

## Slide 26: Possible new phase unrelated to superconductivity with a characteristic temperature of ~1 K
V. Grinenko et al., Nature Physics 17 (6), 748-754 (2021).
R. Khasanov et al., 2026
Transitions splits at zero strain
Relaxation persists in the normal state above Hc2;
For 3 samples T* ~1 K -> new phase;
No TTRSB for samples with Tc > 1.4 K -> too low density of superconductivity affecting impurities.
Two different contributions?

## Slide 27: Tc studies under stress are inconsistent with chiral superconductivity
Inconsistency with ultrasound at least by a factor > 10 assuming Tc = TBTRS!
Ghosh, Nat. Phys. 17,
199 (2021)
Benhabib, Nat. Phys. 17,
194 (2021)
G. Mattoni, et al., Nature Communications 17, 700 (2026).
C. W. Hicks et al., Science 344, 283-285 (2014).
A. Steppke, et al., Science 355, eaaf9398 (2017).
[100] -direction
A. Talkachov, E. Babaev et al., arXiv:2509.19137
The cusp is present only if Tc = TBTRS; even a minor splitting will result in parabolic dependence of Tc on strain along [100] direction!
Can be explained by a non-chiral BTRS state with a d+is state.

## Slide 28: Missing anomaly in the specific heat can be consistent with the 3-component GL model (dx2-y2 + is±)
Y Li et al., accepted npj Quantum Materials (2026)
Anton Talkachov, KTH, Shtokholm

## Slide 29: Summary
Old picture:
ZF-µSR measurements of Sr2RuO4 under uniaxial strain, hydrostatic pressure and with different amounts of disorder previously suggested a chiral order parameter such as .
New results:
The investigated disorder effect on the muon spin relaxation rate is consistent with BTRS superconductivity in Sr2RuO4, where the strength of the relaxation rate in the superconducting state Tc2.
However, in some cases the muon spin relaxation rate is affected by unknown magnetic contributions or a new mechanism for muon relaxation with a characteristic temperature T* ~1 K.
Given the missing kink in the strain dependence of Tc and the lack of a resolvable anomaly in the specific heat at TBTRS under strain, the superconductivity of Sr2RuO4 is non-chiral but still may be consistent with a multicomponent mixed pairing state such as .
Looking for postdocs and PhD students!
vadim.grinenko@sjtu.edu.cn

## Slide 30: Spontaneous magnetic fields in chiral px ± ipy superconductivity
J. R. Kirtley et al., Phys. Rev. B 76, 014526 (2007).
C. Kallin http://www.icmr.ucsb.edu/programs/documents/Kallin.pdf
Spontaneous currents flow along the surfaces, domain boundaries, and crystalline defects.
Chiral superconductivity has similarities with ferromagnetic state → spontaneous bulk magnetization.
Dimensionless
Max Bz ~ 100 G for Sr2RuO4
Furusaki, M. Matsumoto, and M. Sigrist: Phys. Rev. B 64 054514 (2001)
M. Matsumoto and M. Sigrist, J. Phys. Soc. Jpn. 68, 994 (1999)
Distribution of spontaneous fields and currents in one domain (px + ipy )

## Slide 31: Phase of the order parameter GL theory
It is useful to consider the Ginzburg-Landau (GL) theory to describe the Josephson effect.
- expression for supercurrent
If then
Since |ψ|~ 1 in the bulk, one get
With a possible solution:
where f(r) = 1 in 1 and f(r) = 0 in 2.
In zero field and for and are independent on r we can get
For and
- the result depends on the phase difference between left and right and the gradient of the amplitude.
- this adds gradients of the phases
Currents in a superconductor appear spontaneously when there is a variation of phase and amplitude of the order parameter!

## Slide 32: Spontaneous fields in non-chiral pairing states, domain walls
Dipolar structure of the field → the net magnetic flux is zero
domain1
s + id
domain2
s - id
the phase difference between s and d components
A. Benfenati et al., PRB 101, 054507 (2020).
Domain boundary pinned by defects produces dipolar spontaneous fields.
A domain wall stabilized by randomly located pinning centers.
J. Garaud and E. Babaev, PRL 112, 017003 (2014)

## Slide 33: Spontaneous fields in non-chiral pairing states due to inhomogeneity
Spontaneous magnetic in a s+id superconductor
W.-C. Lee, S.-C. Zhang, and C. Wu PRL 102, 217002 (2009)
V. L. Vadimov and M.A. Silaev, PRB 98, 104504 (2018)
Order parameter’s modulus |ψ1|,|ψ2| (s+is state)
Spontaneous magnetic field due to spherical inhomogeneity
Non-chiral superconductivity has similarities with antiferromagnetic state -> the average field is zero.

## Slide 34: Superconductors with broken time reversal symmetry – novel type of magnetism
Phenomenologically, broken time-reversal symmetry results in the appearance of a spontaneous magnetization (m) when a superconductor is cooled below TBTRS.
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020)
V. L. Vadimov and M.A. Silaev, PRB 98, 104504 (2018)
C. Hicks, MPI Dresden
m
Theoretically, spontaneous fields appear around inhomogeneities and at the domain walls (no spontaneous fields in infinite homogeneous superconductor).
The spontaneous fields regardless the structure can be observed in the muon spin rotation/relaxation (μSR) experiments!
A direct observation of the field sources with such probes as scanning SQUID magnetometry is still missing!

## Slide 35: Spontaneous currents in a non-chiral s+is superconductor
J. Garaud and E. Babaev, PRL 112, 017003 (2014); A. Benfenati et al., PRB 101, 054507 (2020)
The spontaneous fields originate from a second term having the Skyrmionic form of CP2 topological charge density. [E. Babaev, L. D. Faddeev, and A. J. Niemi, Phys. Rev. B65, 100512 (2002).]
In 2- band case:
Defect pins
the domain wall
Magnetic field
Phase
B contains products of density gradients and gradients of the phases of the form
, where

## Slide 36: Spontaneous currents in s+is superconductor
J. Garaud and E. Babaev, PRL 112, 017003 (2014); A. Benfenati et al., PRB 101, 054507 (2020)
The fields associated with the magnetic field induced by internal Josephson currents between different bands (in momentum space), in the presence of relative density gradients caused by inhomogeneities.
Without inhomogeneities, spontaneous fields are perfectly compensated (counter-flow) since in momentum space all directions are equivalent, and there is no net current transfer.
The spontaneous fields originate from a second term having the Skyrmionic form of CP2 topological charge density. [E. Babaev, L. D. Faddeev, and A. J. Niemi, Phys. Rev. B65, 100512 (2002).]
Defect pins
the domain wall
Magnetic field
Phase

## Slide 37: Sr2RuO4 is multiband superconductor
Variety of possible superconducting order parameters in Sr2RuO4
Multi-band nature of the Fermi surface results in a possibility of mixed pairing states with the pairing mediated by spin fluctuations, candidates: s+id, d+ig, s+ip
A. T. Rømer, et al., PRL 123, 247001 (2019); PRB 102, 054506 (2020); PRB 104, 064507 (2021);
S. A. Kivelson, et al., npj Quantum Mat. 5, 43 (2020).
dxz+idyz
Alternatively, the orbital degree of freedom can encode chiral order parameters with a pairing originated from local interactions, candidates: d+id.
A. Ramires, and M. Sigrist, Physical Review B (2019). H. G. Suh et al.,Phys. Rev. Research 2, 032023(R) 2020.
A. Ramires, arXiv:2110.10621.
A chiral p-wave is excluded according to the NMR Knight shift measurements:
A. Pustogow et al., Nature 574, 72 (2019).
K. Ishida, et al., J. Phys. Soc. Jpn. 89, 034712 (2020).
A. Chronister et al., PNAS 118 (25) e2025313118 (2021).
The reduction of the NMR Knight shift below Tc
Mixed pairing or chiral
?