## Slide 1
Unconventional superconductivity in topological chiral crystal
School of Physics, East China Normal University
Tian Shang (商恬)
2026.10.24 CSNS

## Slide 2
Outline
SR
otation
elaxation
esonance
spin
muon
Rotation
Resonance
Relaxation
S
R
Topological chiral crystal
Basic principles of SR
Unconventional SC in chiral crystal
Summary
LaRhSi/LaIrSi Adv. Mater. 37, e11385 (2025)
ScIr2-xSix Adv. Mater. 38, e74399 (2026)
Notes: Here, is the out line of my talk. First I will make a short introduction about the topological chiral crystal and the basic principles of muSR technique. Then I will talk about recent work of the muSR study on the two topological chiral crystals, which is LaRhSi/LaIrSi and ScIr2-xSix families. Finally, will be a short symmary.

## Slide 3
SR
otation
elaxation
esonance
spin
muon
An object is chiral if it is non-identical to its mirror image
An achiral object is identical to its mirror image
Topological chiral crystal
A chiral crystal is a crystalline solid whose internal atomic arrangement lacks any symmetry planes, inversion centers, or improper rotation axes
Out of the 230 space groups in crystallography, 65 space groups are chiral
What is chirality?
What is a chiral crystal?
N. Schroter, et al., Science 369, 179 (2020)
Notes: So, what is chirality? If the object is non-identical to its mirror image, then we can say this object is chiral, like our hands. If the object is identical to its mirror image, then it is achiral, like the balloon.
Then, what is a chiral crystal? It is defined as a crystalline solid whose atomic arrangement lacks any symmetry planes, inversion centers, or rotation axes. Out of the 230 space groups, there are 65 chiral space groups. Therefore, there should be many synthesized chiral crystals. Here is a typical example of the crystal structure of PdGa chiral crystal. Indeed, it is not identical to its mirror.

## Slide 4
SR
otation
elaxation
esonance
spin
muon
Combination of structural and electronic chirality triggers the emergence of topological chiral crystals, which exhibit a plethora of exotic quantum phenomena
Topological chiral crystal
Band topology has been widely investigated in chiral crystals
Unconventional SC remains largely unexplored
X. Wu, X. Wang, C. Felser, Riv. Nuovo Cim. 48, 241 (2025)
D. Sanchez, et al., Nature 567, 500 (2019)
M. Hasan, et al., Nat. Rev. Mater. 6, 784 (2021)
N. Schroter, et al., Science 369, 179 (2020)
Notes: Due to the combination of structural and electronic chirality, topological chiral crystals exhibit may exotic quantum phenomena.
For example, Giant helicoid surface Fermi arcs have been experimentally verified in the CoSi family. They also host high-fold fermion excitations at high-symmetry points. They also show a much larger topologically nontrivial energy window than achiral topological materials.
3. Until now, band topology has been widely investigated in the chrial crystals, while the SC, especially the unconventional SC remains largely unexplored.

## Slide 5
SR
otation
elaxation
esonance
spin
muon
Limited number of chiral crystals have been found to show SC
Either conventional or type-I superconductors, or not bulk
LaIrSi and LaRhSi belong to the same group as the well-studied CoSi family
Topological chiral crystal
R. Nakajima, et al., J. Mater. Chem. 12, 12207 (2024)
P213 No.198
Y3Rh4Ge13 I213 No. 199 Tc = 1.45 K
(Ta,Nb)Rh2B2 P31 No. 144 Tc = 6-8 K
(Ta,Nb)Ge2 P6222 No. 180 Tc = 2 K
Mo3Al2C P4132 No. 213 Tc = 9.2 K
Zr5(Pt,Ir)3 P6122 No. 178 Tc = 2.1 K
(Rh,Ir)Ge4 I4122, No. 98 Tc = 1.2-2.5 K
Li2(Pd,Pt)3B P4332, No. 212 Tc = 3-7K
Z. S. Gao, et al., Quant. Front. 1, 3 (2022)
Notes: This is based on the fact that there are quite a limited number of superconducting chiral crystals. Here I list some reported superconducting chiral crystals.
Most of them either behave as a conventional SC or as a type I SC, some of them even lack bulk SC.
LiPdB and LiPtB represent an exception, where spin-triplet SC was realized by increasing the SOC. Recent theoretical work shows a nodal topological SC with dispersionless surface Majorana modes in LiPtB.
The well studied CoSi family belongs to the No.198 chiral space. For this space, some materials have been reported to show SC as well, including the LaRhSi and LaIrSi which we will discuss later.

## Slide 6
Outline
SR
otation
elaxation
esonance
spin
muon
Rotation
Resonance
Relaxation
S
R
Topological chiral crystal
Basic principles of SR
Unconventional SC in chiral crystals
Summary
LaRhSi/LaIrSi Adv. Mater. 37, e11385 (2025)
ScIr2-xSix Adv. Mater. 38, e74399 (2026)
Notes: Before going to the results of our work, I would like to make a short introduction of muSR technique.

## Slide 7
Bext
Bext
SR
otation
elaxation
esonance
spin
muon
Field distribution inside a SC (theory)
Blundell, Contemp. Phys. (1999)
T << Tc
T < Tc
T >Tc
Muons measure the local field distribution in the SC vortex phase
MuSR: basic principles for SC
Second moment of p(B)
B2  -4
Gaussian distribution p(B)
  B21/2  -2  s
Shiroka et al.,NJP (2011)
Muon-spin relaxation in a SC (exp.)
P(t)
Brandt, PRB (2003)
-2 versus T, H
gap value and pairing symmetry
magnetic
penetrate depth
superfluid
density
p-wave
k = 0(kx + iky)
Notes: 7
In case of superconductor, once the sample is cooled with applied magentic field, the superconducting sampe will form the flux line lattice (FLL) in the superconducting state.
Depends on the positions, the amplitude of the magnetic fields is diffenent and therefore, the muSR frequency is different. By analyzing the field distrubtion, we can get the information of the superconducting properties.

## Slide 8
Outline
SR
otation
elaxation
esonance
spin
muon
Rotation
Resonance
Relaxation
S
R
Topological chiral crystal
Basic principles of SR
Unconventional SC in chiral crystals
Summary
LaRhSi/LaIrSi Adv. Mater. 37,e11385 (2025)
ScIr2-xSix Adv. Mater. 38,e74399 (2026)
TaGe2-xAlx
Notes: Now, let’s move to the our first muSR study on the LaRhSi and LaIrSi.

## Slide 9
SR
otation
elaxation
esonance
spin
muon
Cubic B20 structure (P213, no.198)
Both (Rh,Ir)Si and La sublattices are chiral
Only Tc was reported
LaRhSi/LaIrSi family hosts a double-helix chiral structure
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025)
La sublattice
RhSi/IrSi sublattice
LaRhSi (Tc = 4.4 K) and LaIrSi (Tc = 2.1 K)
Bulk SC was first confirmed
Hc2(T) shows multiband feature
H. F. Braun, J. Less-Common Met. 1984, 100, 105 (1984)
B. Chevalier, Solid State Commun. 41, 801 (1982)
Notes: Both LaRhSi and LaIrSi adopt the B20 crystal structure. Unlike the binary CoSi family, in LaRhSi/LaIrSi, both La and RhSi form chiral chains. Therefore, LaRhSi or LaIrSi host a double-helix chiral chain.
Up to now, only the Tc was reported in early 1980s.
We synthesized both LaRhSi and LaIrSi, and characterizes their SC by electrical resistivity and susceptibility. The susceptibility data confirm the bulk Tc at 4.4 and 2.1 K for LaRhSi and LaIrSi, respectively.
In addition, the Hc2(T) data also show multiband feature for both compounds.

## Slide 10
SR
otation
elaxation
esonance
spin
muon
Electronic band structure
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025）
Rh/Ir and La atoms contribute most DOS
Comparable electronic bands near EF
Band splitting is significant in LaIrSi
LaRhSi: ESOC ≈ 37 meV
LaIrSi: ESOC ≈ 207 meV
LaRhSi
LaIrSi
LaRhSi
LaRhSi+SOC
LaIrSi
LaIrSi+SOC
Notes: To compare both compounds, we performed band-structure calculations based on the DFT method. For both compounds, the DOS near EF is dominated by the Rh/Ir(4d or 5d) and La 5d orbitals.
Both LaRhSi and LaIrSi show quite similar band structures near EF.
However, the SOC effect is more significant in LaIrSi than in LaRhSi. For example, the estimated band splitting due to SOC is about 37 meV in LaRhSi, while in LaIrSi, it is about 207 meV, almost 5 times larger in Ir case.
The SOC effect can be clearly seen around the high-symmetry gamma point.

## Slide 11
SR
otation
elaxation
esonance
spin
muon
Topological aspects
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025）
Unconventional fermions with Six-fold and four-fold degeneracy at the high-symmetric R and  point for both compounds
Giant helicoid surface Fermi arcs spanning the entire surface Brillouin zone
Notes: Both LaRhSi and LaIrSi are chiral crystal. Therefore, we expect that both compounds will show some novel topological features. For example, unconventional fermions with six-fold and four-fold degeneracy at high-symmetric R and gamma point.
Both compounds also show giant helicoid fermi arcs spanning the entire surface Brillouni zone, resembling the CoSi family of compounds.

## Slide 12
SR
otation
elaxation
esonance
spin
muon
SR: nodeless to nodal SC
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025）
Relaxation is determined by nuclear moments
TRS is preserved in both compounds
LaRhSi: T-independent sc → fully gapped SC
LaIrSi: strong T dependent sc → nodal SC
Notes: Now we use muSR technique to investigate the SC properties of both compounds. First, we performed the ZF-muSR for both compounds in the superconducting and normal states. For both compounds, the ZF-muSR spectra are almost overlap for both temperatures. This confirm the absence of spontaneous fields in the SC state, and thus TRS is preserved in both compounds. Also both compounds show weak muon-spin relaxation, which is sole determined by nuclear moments.
The TF-muSR measures the magnetic penetrate depth and thus the superfluid density. LaRhSi shows almost temperature-independent superfluid density at low T. While superfluid density is almost linearly temperature dependent in LaIrSi. Therefore, LaRhSi shows fully gapped SC, while LaIrSi shows nodal SC, which confirms the presence of unconventional SC in this family.

## Slide 13
SR
otation
elaxation
esonance
spin
muon
Theory of nodal SC
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025)
Coexistence of SC with chirality-induced multifold fermions may stabilize unconventional pairing symmetry
Considering the isotropic spin-triplet pairing, an effective perturbation model around the R point was constructed:
E0 = A0 + A2k2; 0 is the strength of SOC
A3 represents the C3-wrapping term, implying that the Fermi surfaces are not isotropic but only symmetric under C3
A0 = 0.536 eV, A1 = 0.924 eV·Å, A2 = -14.273 eV·Å2,
A3 = 15 eV·Å2
Notes: In these chiral crystals, coexistence of SC with multifold fermions or unconventional fermions may stabilize unconventional paring symmetry.
Here for LaIrSi, as shown in the figure, we focus on the four Fermi surfaces, which are relatively large and contribute most to the density of states.
Considering the isotropic spin-triplet pairing, we construct an effective perturbation model around R point.
The mixing between spin-singlet (s) and spin-triplet (t ) components is a hallmark of noncentrosymmetric superconductors, where broken inversion symmetry permits such a mixing. It is important to note that previous approaches are based on a topologically trivial Hamiltonian with isotropic Fermi surfaces, while the spin triplet component exhibits significant anisotropy.

## Slide 14
SR
otation
elaxation
esonance
spin
muon
Theory of nodal SC: effective Ginzburg-Landau model
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025）
The gap-nodes region(grey) is nearly invariant with respect to 0 (SOC)
It increases as the A3 term
For LaIrSi, considering the isotropic pairings (s and t), SOC (0), the anisotropic wrapping term (A3), and pairing potential
Superconducting quasiparticle spectrum reads:
For the E+,+ band (where  = +), the condition for nodal-line SC is given by:
Notes: Further, following the Ginzburg-Landau model, we can get the superconducting quasiparticle spectrum.
With some calculations, we obtain the condition for the appearance of nodal-line SC. The Xmin and Xmax are functions of A parameters obtained from band structure fitting.
The gap-node region is nearly invariant with respect to SOC strength. But instead, it increases as the A3 term increases.

## Slide 15
SR
otation
elaxation
esonance
spin
muon
Theory of nodal SC: effective Ginzburg-Landau model
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025)
Gap on the E+,+ band is isotropic due to dominant spin-singlet pairing
Gap on the E-,+ band exhibits nodal lines due to dominant spin-triplet pairing
Gap function of the anisotropic Fermi surface
Fully-gapped
Nodal
s/t ~ 1.5
s/t ~ 0.9
Notes: Based on the above theoretical work, we analyzed the temperature-dependent superfluid density.
For LaRhSi, the spin singlet is dominant, and it behaves as a fully gapped superconductor, while for LaIrSi, the spin triplet is dominant, and it shows a line-node SC. And the superfluid density is almost linearly temperature-dependent.

## Slide 16
SR
otation
elaxation
esonance
spin
muon
Insights for other chiral crystals
Unconventional SC in La(Ir,Rh)Si
T. Shang, et al., Adv. Mater. 37, e11385 (2025)
0 is important, but not as large as preferred
RhGe is a good candidate for unconventional and topological SC (not yet confirmed )
All these superconducting materials adopt a
chiral SP P213 (No. 198)
nodal
nodal
S. Mardanya, et al., Phys. Rev. Mater. 8, L091801 (2024)
Notes: Based on our results from LaRhSi and LaIrSi, we extend the calculations to other superconducting chiral crystals with 198 SG. As shown in this phase diagram, there are two nodal regions. Following this phase diagram, to promote nodal SC or unconventional SC, the SOC strength is not as large as preferred.
For example, the SOC of ReSi is significant, but it is out of the nodal region. Therefore, it should be fully-gapped. By contrast, the RhGe shows moderate SOC, and it is located in the nodal region. Therefore, RhGe is a good candidate for searching for unconventional SC. Unfortunately, no bulk SC has been realized in this material.

## Slide 17
Outline
SR
otation
elaxation
esonance
spin
muon
Rotation
Resonance
Relaxation
S
R
Topological chiral crystal
Basic principles of SR
Unconventional SC in chiral crystals
Summary
LaRhSi/LaIrSi Adv. Mater. 37,e11385 (2025)
ScIr2-xSix Adv. Mater. 38,e74399 (2026)
Notes: Now I will talk about our recent work on another chiral crystal, which is also belongs to the Kagome family. The ScIr2 doped with Si.

## Slide 18
SR
otation
elaxation
esonance
spin
muon
SC in the newly discovered ScIr2-xSix
Unconventional SC in ScIr2-xSix
Two-dome SC was observed in ScIr2-xSix Unconventional?
Ir atoms form a kagome lattice viewed along [111]
Tc is enhanced by Si doping.
K. Xia, et al., Adv. Mater. 38,e74399 (2026)
Z. Zhu, et al., Commun. Mater. 5, 85 (2024)
SCI
SCII
Notes: Recently, the ScIr2-xSix has been found to show very interesting SC properties. ScIr2 has a cubic crystal structure, and Ir atoms form a Kagome lattice viewed along the [111] direction.
The parent ScIr2 shows Tc at 2 K, which increases to close to 4 K by Si doping.
Interestingly, two-dome SC was observed in ScIr2-xSix. The underlying physics is unknow, and this two-dome SC may indicate unconventional SC.

## Slide 19
SR
otation
elaxation
esonance
spin
muon
Origin of two-dome SC
Unconventional SC in ScIr2-xSix
Single-crystal XRD confirms the structure phase transition from high-T cubic to low-T rhombohedral phase (chiral crystal)
Structure phase transition at Ts = 190 K
Ts is quickly suppressed as Si is doped
K. Xia, et al., Adv. Mater. 38,e74399 (2026)
Fd-3m No. 227
R32 No. 155
Centrosymmetric
Noncentrosymmetric
Notes: To investigate this two-dome SC and to search for possible unconventional SC, we synthesized ScIr2-xSix samples
We first measure the resistivity data. Interestingly, the parent compound ScIr2 shows an anomaly around 190 K, which is quickly suppressed by Si doping.
For x > 0.1, no anomaly can be detected.
We performed single-crystal-x-ray diffraction measurements. We found that the anomaly at Ts is attributed to a structural phase transition. Below Ts, the cubic phase changes to the rhombohedral phase.
However, the Kagome lattice remains, which can be viewed along [001] direction. Interestingly, the low-T structure also belongs to the chiral space group. Therefore, ScIr2-xSix is also a chiral crystal.

## Slide 20
SR
otation
elaxation
esonance
spin
muon
Characterization of bulk SC
Unconventional SC in ScIr2-xSix
Bulk SC was confirmed for both compounds
ScIr2: Tc = 1.8 K
ScIr1.82Si0.18: Tc = 3.3 K (nominal ScIr1.75Si0.25)
Cubic (x < 0.1) and rhomb. (x >1)
Two typical samples (x = 0 and 0.25) were chosen for SR study
K. Xia, et al., Adv. Mater. 38,e74399 (2026)
cubic
rhomb.
Notes: To investigate the superconducting pairing of ScIr2-xSix family. The x = 0 and 0.25 was chosen for the muSR studies. The normal Si content was determined as 0.18.
Bulk SC with Tc = 1.8 K and 3.3 K was confirmed by susceptibility measurements.

## Slide 21
SR
otation
elaxation
esonance
spin
muon
SR: nodal SC in ScIr2-xSix family
Unconventional SC in ScIr2-xSix
Both compounds can be best described by a two-band (s+d)-wave model:
ScIr2: 0.8s (0.27meV) + 0.2d (0.32 meV)
ScIr1.82Si0.18: 0.8s (0.60meV) + 0.2d (0.73 meV)
K. Xia, et al., Adv. Mater. 38,e74399 (2026)
Relaxation is determined by nuclear moments
TRS is preserved in both compounds
Notes: First, resembling the LaRhSi and LaIrSi, the ZF-muSR confirms the preserved TRS in ScIr2-xSix family.
The TF-muSR measurements reveal that for both compounds, the temperature-dependent superfluid density is best described by an (s+d)-wave model. The weight of the d component is about 20%.
Therefore, ScIr2-xSix family is also a multigap superconductor. Since at least one band shows superconducting gap nodes, ScIr2-xSix can be classified as an unconventional superconductors.

## Slide 22
SR
otation
elaxation
esonance
spin
muon
Electronic band structure high-T cubic phase
Unconventional SC in ScIr2-xSix
Flat band along -L direction is pushed to EF by SOC (10 meV below EF)
Flat bands are shifted upwards by 300 meV in ScIr1.82Si0.18 (away from EF)
Flat bands and DOS peaks might be responsible for the structural instability in ScIr2
DOS is contributed by Ir-5d and Sc-4d orbitals
Two main bands cross the EF for both compounds
Band splitting due to SOC is significant
ESOC = 275 meV
ScIr2
ScIr2+SOC
ScIr2
Notes: To further understand the unconventional SC in the ScIr2-xSix family, we also performed DFT calculations.
The DOS at the EF is contributed by Ir-5d and Sc-4d orbitals, which suggests possible strong SOC. There are mainly two bands that cross the EF, consistent with the multiband SC in ScIr2-xSix family.
For example, after considering the SOC, band splitting is estimated to be 275 meV along the Gamma-L direction. Also, the SOC further pushes the flat band close to EF, 10meV below EF.
Considering that the flat bands and DOS peaks are located at EF, they might be responsible for the structural instability in the ScIr2-xSix family.

## Slide 23
SR
otation
elaxation
esonance
spin
muon
Electronic band structure low-T rhombohedral phase
Unconventional SC in ScIr2-xSix
Electronic bands are quite similar
The rhombohedral phase lacks an inversion center, the SOC further lifts the degeneracy
Flat band splits into two bands along the -L, resulting in a decrease in DOS
Lower Tc in the first SC dome
ScIr2+SOC
ScIr2+SOC
Flat bands account for most of the DOS at EF, which may explain the unconventional SC in ScIr2-xSix
e.g., electronic correlations
Notes: For the low-T rhombohedral phase, the main features of the band structure are quite similar. However, the low-T phase lacks an inversion center; the SOC further lifts the band degeneracy.
Flat band along the Gamma_L direction was split into two bands, resulting in a decrease of DOS. This may explain the reduced Tc in the first SC dome.
Considering that the flat bands account for most of the DOS at EF, this may explain the unconventional SC in ScIr2-xSix, e.g., the enhanced electronic correlations.

## Slide 24
SR
otation
elaxation
esonance
spin
muon
Unconventional SC in ScIr2-xSix
Ir atoms form a chiral chain
Giant helicoid Fermi arcs
Topological aspects
Dirac point at X point shifts to EF by Si doping
ScIr2+SOC
ScIr1.82Si0.18+SOC
DP splits into two Weyl points with topological charges C = ±1
Multifold fermions with topological charges of C = 3 at  point
Z.-M. Yu, et al., Sci. Bulltet. 67, 375 (2022)
T < Ts
ScIr2+SOC
Notes: Now let’s look at the topological aspects of this family. In the high-T cubic phase, there is a Dirc point at X point. This Dirac point is shifted to EF by Si doping (almost located at EF).
The low-T rhombohedral phase belong to the chiral space group, therefore, ScIr2-xSix can be classified as topological chiral crystal. Du to the lack of an inversion center, the Dirac point splits into two Weyl points
Due to the chiral structure, resembling the other topological chiral crystal, mulifold fermion excitations exit at the high-symmetric gamma point.
In addition, a giant helicoid Fermi arcs were predicted on the surface states as well.

## Slide 25
Conclusions and outlook
SR
otation
elaxation
esonance
spin
muon
µSR is a powerful tool for studying unconventional superconductors, including the TRS breaking effect, superconducting pairings, and SC mechanism
A fully-gapped SC is tuned to a nodal-line SC by turning the ratio of spin-singlet to spin-triplet pairing via the strong SOC in the La(Rh,Ir)Si family.
For ScIr2-xSix, two possible pairing mechanisms have been proposed: conventional electron–phonon coupling and one arising from spin- or charge fluctuations driven by electron correlation. The former results in an s-wave pairing, while the latter leads to various unconventional pairing symmetries (e.g., p-, d-,or f-wave)
The combination of chirality (structural and electronic) and unconventional SC makes superconducting chiral crystals good candidates for investigating topological SC
Our work calls for renewed investigations of unconventional SC in other studied superconductors with a chiral structure

## Slide 26
Paul Scherrer institut (PSI)
Ekaterina Pomjakushina
Dariusz Gawryluk
Hubertus Luetkens
Jonas Krieger
Toni Shiroka
MPI (马普所)
Mukkattu O. Ajeesh
Michael Nicklas
TJU (天津大学)
赵建洲（Jianzhou Zhao)
Acknowledge
SR
otation
elaxation
esonance
spin
muon
ECNU (华东师范大学)
徐杨 (Yang Xu)
詹清峰 (Qingfeng Zhan)
段纯刚 (Chungang Duan)
CityU (香港城市大学)
马均章 (JunZhang Ma)
ZJU (浙江大学)
陈晔 (Ye Chen)
胡伦辉 (Lunhui Hu)
袁辉球 (Huiqiu Yuan)
史明 （Ming Shi）
TUD (多特蒙德工业大学)
Igor Plokhikh
Thank you for your time!

## Slide 27
SR
otation
elaxation
esonance
spin
muon
Materials with kagome lattice exhibit rich quantum phenomena
Unconventional SC in ScIr2-xSix
Unconventional SC and CDW have been observed in the AV3Sb5 family
Magnetic properties are widely studied
Unconventional SC kagome materials are extremely rare
Y. Wang, et al., Nat. Rev. Phys. 5, 635 (2023)
Z. Guguchia, et al., npj quantum Mater. 8, 41 (2023)
Notes: The Kagome materials exhibit very rich quantum phenomena due to their specific band topologies, e.g., flat bands, VHs, topological band crossings, magnetic frustration, and so on. Since there are many studies on Kagome materials, I am not going to discuss all the details.
Among Kagome materials, their magnetic properties are widely studied, e.g., quantum spin liquid, skyrmion.
However, their SC remains largely unexplored, due to limit number of candidate materials. Recently, the unconventional SC and CDW have been well studied in VSb 135 family.

## Slide 28
TRIUMF http://neutron.magnet.fsu.edu/muon_relax.html
Bμ = (2π/γμ) νμ
MuSR: basic principles
SR
otation
elaxation
esonance
spin
muon
SR
谱线
缪子进动频率
正电子探测器
正电子探测器
样品
电子钟
正电子
数量
Notes: 1. How we use the muons to measure the interesting materials?
2. Since muon has its own magnetic moment, we can treat muon as a very sensitive and local magnetic probe. Once the muons hit the samples, it will decay into postive electrons in 2.3 muS. The postive electrons will be counted by detectors.
3. Depends the interaction between muon spin and magnetic moment in the samples, the detected positron will show different asymmetry.
By analysizing the muSR asymmetry, we can get the informaiton of the muon depolarization and therefore the physical properties of the measured samples.

## Slide 29
SR
otation
elaxation
esonance
spin
muon

## Slide 30
Magnetic materials
Mn, Co, Fe-based oxides
Heavy-fermion
Low-dimensional
Quantum Spin Ice/Liquid
Spin glass
Skyrmions
Topological
Rotation
Resonance
Relaxation
S
R
Superconductors
Cuprates
Iron-based
Unconventional SC
Magnetic SC
Topological SC
Semiconductors
organic, inorganic
Chemistry, Soft matter
Material Science
Multiferroic, battery
Magnetic thin films (spin valve)
MuSR: applications
SR
otation
elaxation
esonance
spin
muon

## Slide 31
590 MeV
Advantages of muons
SR
otation
elaxation
esonance
spin
muon
Mass: 105.65 Mev/c2 ~ 207me
Charge: +e/-e
Spin: ½
Moment: 3.18 P ~ 0.005B
Gyromag. Ratio: 851.615 MHz/T
Decay period: 2.2 s
Resolution: 10-3-10-4B~0.01mT
Muons are almost ~100% spin polarized, enabling high resolution
Perfect compensated for NMR and neutron scattering techniques
The energy can be adjusted
keV MeV
surface bulk properties
SR is a very sensitive magnetic probe

## Slide 32
We will be able to do muon experiments in China soon！
SR
otation
elaxation
esonance
spin
muon
Muon sources: MuSR
We are all here now!

## Slide 33
Rashba-type
Saxena. Nature 427, 799 (2004)
lack of inversion symmetry
p(c)  p(-c)
CePt3Si
Noncentrosymmetric SCs
SR
otation
elaxation
esonance
spin
muon
Unconventional/topological SC
E. Bauer et al. al., PRL (2004)
Antisymmetric spin-orbit coupling (ASOC)
allows degeneracy of the Fermi surfaces.
Originates from atomic SOC and the hybridization between orbitals with different parity due to the spatial inversion symmetry breaking
Cooper-pair function allows mixture of single and triplet pairing
Centrosymmetric
Noncentrosymmetric
库伯对
Notes: a, The inner and outer rings (separated for clarity) enclose occupied electron states in momentum space, typical of a normal superconductor. b, When space inversion symmetry is lacking, spins might rotate around the momentum-space surface, clockwise on one side and anticlockwise on the other.
Now I would like to introduce one type of the superconductor, which is non-centrosymmetric superconductor. The NCSC implies the superconductors with the crystal structure without inversion symmetry. For example, the Cet3Si, if we do the inversion operator along c-axis, the crystal structure is not overlap.
Due to the lack of inversion symmetry, the antisymmetric SOC will cause the band splitting. Compared to the normal superconductor, in the momentum space, when space inversion symmetry is lacking, spins might rotate around the momentum-space surface, clockwise on one side and anticlockwise on the other.
Due to the band splitting, the mixture of spin single and spin triplet is allowed in the NCSCs. While in case of centrosymmetric, only the singlet or the triplet is allowed.

## Slide 34
Y. Ōnuki, Physica C (2009)
Hc2 beyond Pauli limit
CeIrSi3
H. Q. Yuan, PRL 97, 017006 (2006)
Li2Pt3B
gap nodes
SR
otation
elaxation
esonance
spin
muon
The mixed pairings yield novel/unconventional SC properties
Unconventional/topological SC
Time-reversal symmetry
breaking
CaPtAs
T. Shang, PRL 124, 207001 (2020)
Notes: Due to the mixed pairings, the NCSCs shows some unconventinal fearutes compared to the CSCs materials.
For example, the upper crystal field Hc2 is exceeding to the Palul limit.
The superconducting gap shows nodal structure
Also in some cases, the superconducting state breaks the time reversal symmetry below the Tc.

## Slide 35
SR
otation
elaxation
esonance
spin
muon
How to realize topological SC?
Route 1: e.g., CuxBi2Se3
Chemical doping in topological insulator
S. Sasaki et al., PRL (2011)
K. Matano, et al., Nat. Phys. (2016)
Route 2: e.g., NbSe2/Bi2Se3
Bilayer of s-wave SC/topological insulator
S. Y. Xu, et al., Nat. Phys. (2014)
Jin-Peng Xu et al., PRL (2015)
Route 3: e.g., -BiPd
Intrinsic SC + nontrivial band topology
Z. Sun, et al., Nat. Commun. (2015)
Y. Li, et al., Adv. Quantum Technol. (2019)
Unconventional/topological SC
Drawbacks: Doping-induced disorder and inhomogeneities
Drawbacks: Complex, difficult to fabricate,
relatively low Tc
Drawbacks: Few candidates, relatively low Tc Advantages: One compound only, “clean” solution
Notes: NCSCs become the ideal platform to search for the possible topological SC in recent years.

## Slide 36
SR
otation
elaxation
esonance
spin
muon
Topological Semimetal family
Unconventional/topological SC
NCSCs become the ideal platform for searching the topological SC
Nocentrosymmetric SCs
Inversion symmetry
Weyl semimetal with SC
Time reversal symmetry
Unconventional/topological SC
Majorana bound states
Hongming Weng, et al., JPCM (2016)

## Slide 37
SR
otation
elaxation
esonance
spin
muon
MuSR: basic principles
Schematic TF µSR experiment
TF-µSR: excellent probe of magnetic fields:  =   B
Schematic LF (ZF) µSR experiment
LF or ZF-µSR: very sensitive to weak internal fields and
useful for studying dynamics
ZF-µSR offers unique advantages (direct study of weak magnetism)
H