## Slide 1
Qisi Wang 王奇思
24.11.2026 | Dongguan
Chinese University of Hong Kong 香港中文大学
Probing the symmetry of altermagnetic interactions
MELODY2026

## Slide 2
Outlook on μSR study of unconventional magnets
Basics of altermagnetism & spectroscopy evidence
Inelastic neutron scattering study of g-wave magnon splitting in α-Fe2O3
Outline

## Slide 3
Yujie Yan
Yuehong Li
Yuetong Wu
Tianren Wang
Ke-Jin Zhou
Jaewon Choi
Mirian
Garcia-Fernandez
Collaborators
Xin Tong
Yu Feng
Wei Luo
Yao Shen
Stefano Agrestini
Yi Lu
Andong Liu
Seoul National University

## Slide 4
Outlook on μSR study of unconventional magnets
Basics of altermagnetism & spectroscopy evidence
Inelastic neutron scattering study of g-wave magnon splitting in α-Fe2O3
Outline

## Slide 5
Unconventional magnetism: spintronics & magnonics
X. Chen, W. Chen, Q. Liu, Q, The rise of unconventional magnetism
“Simplified” picture of altermagnetism
Altermagnets: zero net moment with broken PT & τT symmetry
Exchange spin-split electronic bands & lift the degeneracy of opposite-chirality magnon branches
Notes: A simplified picture to understand difference between AM and AFM: sublattice cannot be related by only translational operation, and certain rotation is needed, if we consider the atomic/ligand environment. This leads to a Q-dependent exchange field that split the spin-up and spin-down electronic bands

## Slide 6
Altermagnet: Opposite-spin sublattices are related by crystal rotation — not by translation or inversion
Zero net moment
Compensated sublattices suppress stray fields
Broken time reversal
Spin-polarized bands and T-odd responses survive
Why it matters
Exchange-scale splitting, THz dynamics, spin currents, no stray field
AM retain AFM compensation while gaining FM-like spin-resolved functionality
Altermagnets (AM): compensated yet spin-split
Jungwirth et al., Altermagnetic spintronics, Nat. Phys. 22, 1012 (2026)
Edelstein effect
Notes: Such spin-splitting yet zero net magnetization of AM lead to unique advantage in the spintronic or magnonic applications. Merit of both FM and AFM.

## Slide 7
The wave label is the lowest even-parity angular harmonic allowed by the altermagnetic spin group
Why bands split
E↑(k) = E↓(Rk)
R connects opposite-spin sublattices
Generic k: Rk ≠ k → finite ΔE(k)
Invariant directions:
Rk = k → nodal degeneracy
d / g / i wave
2 / 4 / 6 nodal surfaces
Repeated crystal rotations force alternating spin sectors.
Symmetry-fixed zeros become nodal lines or planes;
Higher symmetry allowed harmonics generate more nodes.
The angular pattern (of spin-splitting) is a symmetry fingerprint
Electronic band splitting: crystal symmetry selects d-, g-, and i-wave
C. Song et al., Altermagnetic spintronics, Nat. Rev. Mater. 10, 473 (2025)
Notes: Altermagnets are classified by the symmetry of the spln-splitting, which inherits from the crystal crystal.

## Slide 8
Unequal symmetry-related exchange paths (due to ligand environment) lift energy and chirality degeneracy away from nodal planes
Why magnon split in AM
Two circular magnon modes are degenerate in a conventional AFM
Crystal rotation permits inequivalent long-range exchange paths: J10 ≠ J11
Nodal planes exchange the branches and protect degeneracy
Off nodal, energy and chirality split with the same g-wave sign pattern
Liu et al., Chiral Split Magnon in Altermagnetic MnTe, PRL 133, 156702 (2024)
Electronic and magnon splitting share a symmetry origin:
Magnon band splitting: the same symmetry logic

## Slide 9
Sensitivity to multiple correlations – charge, spin, orbital
Element specific
Enhanced cross-sections
X-rays
Dipole / quadrupole spin interactions
Spin-flip RIXS process
C. J. Jia et al., Nat. Commun. 5, 3314 (2014)
Complementary to neutron: smaller crystal or thin films
Resonant Inelastic X-ray Scattering (RIXS)

## Slide 10
L. J. P. Ament et al., Rev. Mod. Phys. 83, 705 (2011)
12 m
41A1 beamline, TPS, Taiwan, China
year
2000
2009
Evolution of RIXS resolution
2025
38 meV @ Ni L-edge
I21 beamline, DIAMND, UK
J. Synchrotron Rad. 29, 563 (2022)
Resonant Inelastic X-ray Scattering (RIXS)
J. Synchrotron Rad. 28, 977 (2021)

## Slide 11
24 K; ΔE = 24 meV
~32 meV magnon; dispersion agrees with INS
φ-dependent CD fits three C₃ domain types
CD is controlled by symmetry and intermediate states
CD amplitude is not a direct measure of g-wave splitting
Takegami et al., Circular Dichroism in RIXS: Probing Altermagnetic Domains in MnTe, PRL 135, 196502 (2025)
RIXS-CD provides a detailed magnetic-domain fingerprint, but not a direct ruler for magnon splitting.
α-MnTe: RIXS-CD distinguishes C3 magnetic domains

## Slide 12
Cr L3 edge; ΔE ≈ 32.5 meV; single-domain microregion
RCD(φ) = A cos(3φ)，|A| = 21.6 ± 1.7%
CD reverses sign between opposite AFM domains
CD → 0 along high-symmetry directions, matching g-wave nodes
Predicted splitting ~22 meV, below the experimental resolution
Biniskos et al., Systematic mapping of altermagnetic magnons by RIXS circular dichroism, Nat. Commun. 16, 9311 (2025)
The evidence is threefold: cos(3φ) azimuthal symmetry, nodal zeros, and domain-sign reversal.
CrSb: RIXS-CD maps g-wave magnon symmetry

## Slide 13
Birefringence rotates CL/CR polarization with depth
Propagation-enabled model reproduces magnetic and orbital CD
CD reverses across Cu L3 edge and survives at 240 K
Nag et al., Circular dichroism in resonant inelastic x-ray scattering from birefringence in CuO, PRR (2025)
RIXS-CD alone does NOT prove intrinsic chirality: model birefringence, propagation, and self-absorption.
NOT always chiral: birefringence-induced RIXS-CD in CuO

## Slide 14
~33 meV magnon; CD along (H,0), not along (H,H)
Predicted splitting ~2.4 meV ≪ Res. ≈ 27 meV;
Zhang, QW*, Yi Lu*, Yao Shen* et al., d-wave altermagnetism revealed by resonant inelastic X-ray scattering ,arXiv:2606.18731
La2O3Mn2Se2: RIXS reveals d-wave altermagnetism
Lieb lattice
Semiconductor
Yao Shen (IOP)

## Slide 15
~33 meV magnon; CD along (H,0), not along (H,H)
Polar scan: d-wave symmetry; CD vanishes > TN ≈ 160 K
Predicted splitting ~2.4 meV ≪ Res. ≈ 27 meV;
ED / RIXS-operator analysis supports [C2∥C4z] symmetry
Zhang, QW*, Yi Lu*, Yao Shen* et al., d-wave altermagnetism revealed by resonant inelastic X-ray scattering ,arXiv:2606.18731
The d-wave pattern & disappearance of CD above TN support altermagnetic symmetry.
La2O3Mn2Se2: RIXS reveals d-wave altermagnetism
Lieb lattice
Semiconductor
Yao Shen (IOP)

## Slide 16
Compare nodal- and off-nodal directions
Off-nodal doublet: ΔE ≈ 2 meV
Alternating J10 / J11 LSWT
Liu et al., Chiral Split Magnon in Altermagnetic MnTe, PRL 133, 156702 (2024)
Symmetric exchange lifts energy and chirality degeneracy in MnTe.
α-MnTe: first INS resolution of magnon splitting

## Slide 17
Sixfold intensity pattern in the 180 meV constant-energy slice
Γ–L splitting: 0.15 r.l.u.
Symmetry-protected direction remains unsplit
J11 ≈ 1.8 meV reproduces the pattern
Bandwidth 180–230 meV;
Singh et al., Chiral Spin-Split Magnons in the Metallic Altermagnet CrSb arXiv:2511.16086 (2025)
CrSb extends INS evidence from insulating to metallic altermagnets
CrSb: spin-split magnons in a metallic altermagnet

## Slide 18
Mch ∝ difference between spin-flip channels
Ω₁ and Ω₂ have opposite signs: direct left / right-handedness
Sign reverses after ±4.2 mT field cooling: switchable chirality
Liu et al., Observation of Switchable Chiral Magnons in an Altermagnet, PRL 136, 236705 (2026)
Evidence advances to opposite handedness and reversible control.
α-MnTe: Polarized INS reads and switches magnon chirality

## Slide 19
Lack of characterization of altermagnetic order parameters from magnon spitting
Key experimental challenges
M. Long et al., Nature 845, 656 (2026)
Quantum oscillation in CrSb

## Slide 20
Outlook on μSR study of unconventional magnets
Basics of altermagnetism & spectroscopy evidence
Inelastic neutron scattering study of g-wave magnon splitting in α-Fe2O3
Outline

## Slide 21
α-Fe2O3: correlated insulator, hexagonal, g-wave candidate
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693
Chemical stability
TN = 950 K >> RT
Large crystal size
Low magnon damping
16 grams
Tianren Wang

## Slide 22
ARCS; T = 50 K; Eᵢ = 150 meV
Off-nodal: 3 meV splitting near 100 meV: J13 / J14
Sun et al., Observation of Chiral Magnon Band Splitting in Altermagnetic Hematite, PRL 135, 186703 (2025)
α-Fe2O3: previous INS resolving 3 meV magnon splitting
Still lack of angular information – order parameter?

## Slide 23
HD neutron spectrometer at CSNS
W. Luo et al., Nucl. Instrum. Methods Phys. Res. A 1046, 167676 (2023)
Xin Tong
Yu Feng
Wei Luo
high energy direct geometry chopper spectrometer

## Slide 24
Spin-wave in the collinear magnetic state of α-Fe2O3
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693
Tianren Wang

## Slide 25
Magnon splitting in α-Fe2O3
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693

## Slide 26
Magnon splitting in α-Fe2O3: AM with inequivalent J13
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693

## Slide 27
Magnon splitting in α-Fe2O3: AM with inequivalent J13
T. Wang et al., arXiv:2609.08693

## Slide 28
Magnon splitting in α-Fe2O3: opposite chirality
T. Wang et al., arXiv:2609.08693
Circular transverse correlation

## Slide 29
Magnon splitting in α-Fe2O3: off-nodal “line”
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693

## Slide 30
Magnon splitting in α-Fe2O3: off-nodal “line”
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693

## Slide 31
Magnon splitting in α-Fe2O3: observed in other BZ
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693

## Slide 32
g-wave chiral altermagnetic magnon splitting in α-Fe2O3
T. Wang, Y. Feng*, J. Choi*, Q.W.* et al., arXiv:2609.08693

## Slide 33
Outlook on μSR study of unconventional magnets
Basics of altermagnetism & spectroscopy evidence
Inelastic neutron scattering study of g-wave magnon splitting in α-Fe2O3
Outline

## Slide 34
Outlook: μSR on altermagnets – high sensitivity to magnetism
Surface or bulk magnetism?
Systems challenging for neutrons

## Slide 35
Outlook: μSR on altermagnets – high sensitivity to magnetism
(Alter)magnetism in RuO2??
d-wave candidate: ARPES, AHE,…
H. Mavani et al., Conditions for Altermagnetism in RuO2, arXiv:2610.07494

## Slide 36
Outlook: μSR on altermagnets – high sensitivity to magnetism
(Alter)magnetism in RuO2??
|MRu| < 4.8(2) × 10−4 μB
DFT prediction |MRu| ~ 0.05 μB
μSR estimation of upper limit:
RuO2 single crystal
From ARTEMIS @ J-PARC
M. Hiraishi et al., PRL 132, 166702 (2024)
d-wave candidate: ARPES, AHE…
RuO2 single crystal

## Slide 37
Outlook: μSR on altermagnets – high sensitivity to magnetism
RuO2 film / TiO2
LE-μSR from μE4 @ PSI
A. Akashdeep et al., APL 128, 022406 (2026)
Magnetism from ~10 nm surface.
Volume fraction is < ~8.5%.
Inhomogeneous, static surface magnetism.
Surface defects, reduced dimensionality, local strain, or non-stoichiometry.
RuO2 film / TiO2
DFT prediction |MRu| ~ 0.05 μB
d-wave candidate: ARPES, AHE…
(Alter)magnetism in RuO2??

## Slide 38
Outlook: μSR on altermagnets – high sensitivity to magnetism
N. P. Bentley et al., PRB 112, 134453 (2025)
V1/3NbSe2 single crystal
From GPS @ SIS
Magnetic structure in V1/3NbSe2?
Simple AFM or double-Q?
(S = 1, V3+)
Simple AFM
Double-Q
Field spectra simulation: compatible with both

## Slide 39
Outlook for α-Fe2O3 (and other candidates)
Symmetry tuning by strain
Sample
Driving screw
MnTe: g- to p-wave (share strain)
CrSb: g- to d-wave (epitaxial strain)
Belashchenko, PRL 134, 086701 (2025)
C. Song et al., Preprint doi.org/10.21203/rs.3.rs-8852675/v1