## Slide 1
Sayani Biswas (ISIS)
MELODY 2026, China
25th October 2026
A “deep” dive into materials with negative muons
μ-
Cu
Sn
Pb
Cu
Cu
Sn
Cu
“Bronze” Sea

## Slide 2
Outline
ISIS Neutron and Muon Source
Muonic X-ray Emission Spectroscopy (μ-XES)
μ- lifetime
Elemental Analysis Techniques using μ-
Liv Yarrow (09:00 tomorrow)
Juliet Spedding (10:00 tomorrow)
Applications of μ-XES
Upgrades @ ISIS

## Slide 3
ISIS Neutron and Muon Source
Diamond Light Source
Target Station 1 (TS1)
Target Station 2 (TS2)
ISIS Neutron and Muon Source
High energy protons
Muon Target

## Slide 4
ISIS Neutron and Muon Source
Target
Station 1
(TS1)
Target
Station 2
(TS2)
C, 45°
10mm
RIKEN-RAL
Muon facility
Currently, we use the MuX
instrument in port 4, for elemental
analysis
Recently, we have also explored the ARGUS instrument in Port 2 for elemental analysis
A. Hillier et al, Phil. Trans. R. Soc. A, 377 (2019)

## Slide 5
A. Berlie et al, ACS Omega, 11, 36 (2026)
Elemental analysis techniques using μ-
µ- @ 70 MeV/c

## Slide 6
A. Berlie et al, ACS Omega, 11, 36 (2026)
Elemental analysis techniques using μ-
Muonic X-ray Emission
Spectroscopy (µ-XES)
MuX (4 HPGe detectors)
μ- beam
ARGUS (192 scintillator detectors)
μ- beam
µ- lifetime
µ- @ 70 MeV/c

## Slide 7
μ-XES Technique
Depth sensitivity:
- beam
Fe
500μm
Zn
500μm
Cu
500μm
Ag
1000μm
A. D. Hillier et al, Microchemical Journal (2016)

## Slide 8
μ-XES Technique
Elemental composition:
Stainless steel (SS-AISI 430)
µ- @ 30 MeV/c
Ratios wrt Fe
μ- beam
Ge6
Ge2
Ge7
Ge8
S. Biswas et al, Heritage Science, 11 (2023) 43

## Slide 9
μ-lifetime Technique
Preliminary Results
µ- @ 70 MeV/c
Li: 2.083(15) µs
Cl: 0.548(1) µs
T. Suzuki et al, Phys. Rev. C 35, 2212 (1987)
Exp: 1.0(2)
Theo: 1.0
Li/Cl ->

## Slide 10
Application of μ-XES
OMF : co-formulation of one or more inorganic fertiliser and one or more materials containing organic carbon (Corg); and nutrients of solely biological origin.
<16% N
Pb : 120 mg/kg dry matter;
Zn < 1200 mg/kg
biuret (C2H5N3O2) : 12 g/kg dry matter
Salmonella and E.coli
Etc.
OMF pellet
Organic component
Inorganic component
Biostimulants
Organic component
Inorganic component
OMF challenges: Nutrients (N, P, K, Mg, S) are strongly bound to the organic component in OMF and this inhibits the easy release of nutrients into soil.
Solution: Addition of biostimulant to OMF.
Biostimulants are made from humic material, seaweed extracts, protein lysates, etc.
Prof. Ruben Sakrabani (PI),
Dr. Parveen Rupani, and Zoe Partington
Funders: Ofwat Innovation Fund, STFC Food Network
Organo-mineral fertiliser (OMF)

## Slide 11
Aim: To assess the influence of biostimulants on nutrient (N, P, K, Mg, S) composition as a slow release fertiliser of OMF pellets using muonic X-ray experiments.
Organo-mineral fertiliser (OMF)
distribution of N, C, P, K was consistent at both depths within each pellet
Pellets having 5% biostimulant by mass showed 6% C -> a slight reduction compared to control whilst others did not show any effect.
Prof. Ruben Sakrabani (PI),
Dr. Parveen Rupani, and Zoe Partington
Funders: Ofwat Innovation Fund, STFC Food Network
Preliminary Results:
Control Pellet: 1% N, 8% C, 0.3% P and 0.7% K by mass
Momenta: 30 and 37 MeV/c
Application of μ-XES

## Slide 12
Upgrades @ ISIS
Setup:
4 HPGe
detectors
8 HPGe
detectors
DAQ:
Hexagons
(4 channels)
R5560SE (128 channels)
Data Analysis Software (EVA):
Element/Isotope identification
Peak fitting
Simulations (SRIM/TRIM
& G4Beamline)
Periodic Table
(Mudirac)
Machine Learning
(element identification
& composition)
https://github.com/ISISMuon/EVA
M. Bjørklund et al., J. Phys. conf. ser., 3222, 012020 (2026)

## Slide 13
Acknowledgements
Adrian D. Hillier
Muon group Leader
Me!
Muon Instrument Scientist
(Feb 2024- present)
Industrial Placement Students
Chendur Chandrasekaran
(July 2025- August 2026)
Matea Bjørklund
(July 2024- July 2025)
PhD student (Oct 2026 - present)
ISIS Technicians
James R. Taylor
Jack Williams
Ashley Lester
Jeremy Moor
…
Scientific Computing
Subindev Devadasan
Patrick Austin
Leandro Liborio
Philip Jones (Warwick U.)
Siddharth Dhanpal
Margaret Duff
Niall Bootland
Hussam Al Daas
Susmita Basak
…
UK & international collaborators
ISIS Muon Group members

## Slide 15
T. Yamazaki et al, Phys. Scr. 11, 133 (1975)
For Cu
(Z = 29)
8
T. Von Egidy et al, Phys. Rev. A 26, 2355 (1982)