## Slide 1: The Rational Synthesis of Next-Generation Core–Shell Adsorbents for Efficient CO2 Capture
N. Asikin Mijan
Senior Lecturer
Department of Chemical Sciences
Faculty of Science and Technology
Universiti Kebangsaan Malaysia
Yolk-shell catalyst
CO2 Captured (Air)

## Slide 2
Detrimental Impact of CO2 Emissions
Scientific sensus hold that greenhouse gas emission are the primary cause of global warming.
CO2 is the major green house gaseous, worldwide 27 billions tonnes of CO2 produced annually
Global warming cause increasing temperatures, increase the number of heatwaves occurring annually causing a lot of death.
Causes higher precipitation led to an increase the frequency of droughts and floods in various local areas.
Attempts to mitigate global warming are currently ongoing on a global political level backed by widespread scientific efforts.

## Slide 3
Currently, a lot of research is being carried out to overcome the problem, such as by utilization of solar energy, biodiesel, green diesel, sustainable aviation fuel (SAF) and others
Overcoming The CO2 Problem By Renewable Energy
Laith K Obeas, G Abdulkareem Alsultan,.., Asikin-Mijan et al.(2025), Fuel Processing Technology, 288 (Green diesel)
N. Asikin-Mijan et al. (2022). Fuel, 325, 124917 (SAF)
Salima Kouider Elouahed, N Asikin-Mijan et al. (2024). Energ. Conv. Mana., 303, 118185 (Biodiesel)

## Slide 4
Renewable fuel – Reduced the CO2 emission
Green diesel combustion properties
Deoxygenation reaction set-up
SO2
CO2
Emission test
[1]
[2]
[3]
GA Alsultan, Asikin Mijan et al. (2021). ACS Omega, 6: 408-415

## Slide 5
Feedstock become limitations for commercialization
CO2-to-Fuel
Audi companies- producing diesel fuel from CO2 and H2O and renewable energy sources (wind or solar or hydro power).
CO2 obtained from biogas plant and CO2 captured directly from air.
Carbon capture, utilization, and storage (CCUS)
Multi-step climate mitigation process that intercepts CO2 emissions directly from industrial

## Slide 6
Carbon capture, utilization, and storage (CCUS)

## Slide 7
To Capture CO2 , we need adsorbent
Adsorption is a reliable process technology since the 1960s for gas separation applications.
Adsorption based separations are achieved by passing the gas mixture (adsorbates) over a solid
(adsorbent)
The main opportunity for CO₂ capture lies in industrial processes that emit flue gases with low CO₂ concentrations

## Slide 8
The Capture Bottleneck & Solution

## Slide 9
CO2 capture adsorbent
M. Nurfarhana, N. Asikin-Mijan et al., 2025. Materials Chemistry and Physics
Syawal Mohd Yusof, N. Asikin-Mijan et al. 2026. Industrial & Engineering Chemistry Research.
M. Nurfarhana, N. Asikin-Mijan et al., 2023. Materials Chemistry and Physics

## Slide 10
Key Criteria for Effective CO₂ Capture Catalysts
Abundance basic sites - Alkaline metal (Mg, Na)
(acidic CO2 molecules bond directly with basic O2- - Mg2+
MgO + CO2 MgCO3
Optimized Pore Structure and Surface Area (Micropores 0.5-0.7 nm)
CO2 molecules size approximately 0.23–0.51 nm (accommodate CO2)
S. Yusof, N. Asikin-Mijan et al. 2026. Industrial & Engineering Chemistry Research.

## Slide 11
Solid adsorbent Yolk-shell structure: Type
The yolk–shell structure consist of a core, a void space, and an outer shell.
Higher specific surface area (porous shell)
The outer shell prevents core agglomeration and act as support (stability)
Movable core ensures full reactant contact hence maximizing mass transfer & active sites

## Slide 12
Aims: CO₂ Gas Adsorption Efficiency in yolk-shell adsorbent

## Slide 13
Targeted CO2 Gas Capture efficiency

## Slide 14
Yolk-shell Synthesis via Spray Pyrolysis
Spray pyrolysis is ideal synthesis process simplicity, cost-effectiveness, and scalability (Jeon et al., 2023)

## Slide 15
Sliced-open yolk-shell Al2O3 particles with NiO composite structures

## Slide 23
Validation of Ni, NiO, Al2O3 phase and porosity
Peaks at 2θ ≈ 37.4° and 44.5° are assigned to cubic NiO (JCPDS 00-47-1049)
Peak at 2θ ≈ 44.5° also indicates metallic Ni (PDF 00-04-0850), confirming partial NiO reduction
Adsorbent also existence of broad peak at 2θ ≈ 64.5° corresponds to γ-Al₂O₃ (JCPDS 00-010-0425), indicating low crystallinity/partial amorphous structure
Both catalyst exhibit Type IV isotherms, confirming mesoporosity, pore size (2-50 nm)
Limitation by BJH method
Pore size distribution within the microporous range (< 1 nm)(existed)
NiO-Al2O3
Sample | N2 adsorption–desorption analysis | 
 | Surface area (m2/g) | Pore size diameter (nm)
NiO-Al2O3 | 142-184 | 5-6
Spike at low relative pressures (P/P₀ < 0.01)

## Slide 25
The overall particle-size range spans erratically from 100-900 nm indicating lack of controlled uniform growth during synthesis

## Slide 26
Solid spheres with fully dense
Partially dense spheres,
Empty shell
Yolk-shell structures.

## Slide 29
C
Cl
O
Al
Ni

## Slide 31
Will Muon Help me?

## Slide 32
History and current acchievement
Start project 2025 (February) – Dr. Watanabe
Obtaining two Malaysian Grants
(1. Sakura Exchange program, 2. GUT grant, 3. GET grant (October 2026)
Optimizing the synthesis process

## Slide 33
Oct-Nov 2026 collaboration – RIKEN JAPAN

## Slide 34
Researchers
Dr. Asma Samsuddin
(UKM)
Mr. Syawal Yusof
(UKM)
Assoc. Dr. Wan Roslan Wan Isahak
(UKM)
Vassanthan
(UKM)
Yolk shell adsorbent
CO2 Captured & Desorption,
Yolk shell adsorbent
Dr. Nurul Asikin Mijan
(UKM)