## Slide 1: Single-Q/Multiple-Q magnetic order and persistent spin dynamics in honeycomb cobalt oxides
Ping Miao
China Spallation Neutron Source (CSNS)
Institute of High Energy Physics
Chinese Academy of Sciences
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)
Y. Gu, W. Xie, P. Miao*, Y. Li* et al., arXiv:2610.27663 (2026)
Notes: 各位老师好，接下来我汇报一下过去一年我的工作情况。

## Slide 2
Honeycomb lattice of Na2Co2TeO6 & Na3Co2SbO6
Na2Co2TeO6 (NCTO)
Na2Co2SbO6 (NCSO)
O
Na
Co
Te
μ
Co
Sb
Na
O
μ
Co-Te
Layer
Co-Sb
Layer

## Slide 3
“Kitaev” or “XXZ” anisotropy?
“Kitaev” anisotropy: the bond-dependent Ising axes are mutually orthogonal.
highly frustrated*
“XXZ-Ising” anisotropy: the bond-dependent Ising axes are 120 degrees apart.
somewhat frustrated*
“XXZ-Heisenberg” anisotropy: easy-plane but still has U(1) symmetry.
not frustrated*
Chun et al., Nat. Phys. 11, 462 (2015)

## Slide 4
Long-range magnetic ordering in NCTO & NCSO
Na2Co2TeO6 (NCTO)
Na2Co2SbO6 (NCSO)
NCTO
NCSO
TN_T
TN_S
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)

## Slide 5
Single-Q or Double-Q magnetic order in NCSO?
Phys. Rev. B 109, L060410 (2024)
Phys. Rev. Mater. 3, 074405 (2019)
q = (1/2, -1/2, 0)
q = (1/2, 1/2, 0)
q =
(1/2, 1/2, 0)
(1/2, -1/2, 0)
+

## Slide 6
Single-Q or Double-Q magnetic order in NCSO?
Y. Gu, W. Xie, P. Miao*, Y. Li* et al., arXiv:2610.27663 (2026)
q = (1/2, 1/2, 0)
q = (1/2, -1/2, 0)
q =
(1/2, 1/2, 0)
(1/2, -1/2, 0)
+

## Slide 7
High-resolution Neutron Diffractometer (TREND)
Specifications:
Applications
Bandwidth (Δλ) @ 5 Hz | 0.1–9.9 Å
Moderator | Decoupled poisoned hydrogen
Neutron beam size | 40(h)×10(w) mm2
Best resolution (Δd/d) | 0.027%
Neutron flux (n/scm2) | ≥5×106
d-range @ 5 Hz | 0.4 – 4.7 Å (BS bank) 0.5 – 5.2 Å (HA bank) 0.6 – 7.1 Å (SEL bank) 1.1 – 11.9 Å (MAL bank) 2.3 – 31.0 Å (LAL bank)
Detecting tiny structural changes that significantly influence properties like superconductivity, colossal magnetoresistivity, multiferroicity, quantum magnetism etc.
Solving complex crystal or magnetic structures in advanced functional materials such as multiferroics, energy storage materials, catalysts, small-molecular medicine etc.
in-situ/operando measurements such as charge-discharge process in batteries, gas-adsorption process in porous materials etc.
Detecting defects in high-quality single crystals
First neutron on July 3, 2024

## Slide 8
High-resolution neutron diffraction on NCSO
Y. Gu, W. Xie, P. Miao*, Y. Li* et al., arXiv:2610.27663 (2026)
Single-Q magnetic order!

## Slide 9
Y. Gu, W. Xie, P. Miao*, Y. Li* et al., arXiv:2610.27663 (2026)
a = 5.36053(2) Å
b = 9.26106(3) Å
c = 5.63282(2) Å
α = 90.0008(4) °
β = 108.5736(2) °
γ = 90.0337(4) °
High-resolution neutron diffraction on NCSO

## Slide 10
Magnetization with uniaxial compression in NCSO
Y. Gu, W. Xie, P. Miao*, Y. Li* et al., arXiv:2610.27663 (2026)

## Slide 11
Single-Q or Triple-Q magnetic order in NCTO?
Phys. Rev. B 103, L180404 (2021)
Phys. Rev. Res. 5, L022045 (2023)
Phys. Rev. Lett. 131, 146702 (2023)
Phys. Rev. Lett. 135, 136701 (2025)
Single Q, Triple Domains
Triple-Q, Single Domain
q = (0,1/2, 0)
q = (1/2, -1/2, 0)
q = (1/2, 0, 0)
q = (0,1/2, 0)
(1/2, 0, 0)
(1/2, -1/2, 0)
+
+
Phys. Rev. B 94, 214416 (2016)
Phys. Rev. B 95, 094424 (2017)

## Slide 12
q = (0,1/2, 0)
(1/2, 0, 0)
(1/2, -1/2, 0)
+
+
Y. Gu, W. Xie, P. Miao*, Y. Li* et al., arXiv:2610.27663 (2026)
High-resolution neutron diffraction on NCTO
Triple-Q magnetic order!

## Slide 13
μSR on NCTO
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)

## Slide 14
μSR on NCTO
α(H) = 1/3 @ LF = 0.01T
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)

## Slide 15
μSR on NCSO
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)

## Slide 16
Initial asymmetries
NCTO
NCSO
TN_T
TN_S
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)

## Slide 17
Stretched exponent & Relaxation rate
A broad distribution of correlation times
Spin fluctuations continue to exist much below TN_S
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)

## Slide 18
Magnetic volume fractions
P. Miao*, Y. Li* et al., Phys. Rev. B 109, 134431(2024)

## Slide 19
Summary
High-resolution neutron diffraction provides unambiguous evidence for Single-Q magnetic order in NCSO and indicate Triple-Q magnetic order in NCTO.
μSR experiments shows that spin dynamics survives deeply into the magnetically ordered states in both NCTO and NCSO. Both systems show a broad distribution of correlation times, which is commonly observed in glassy magnets.

## Slide 20
Thank you for your attention!
miaoping@ihep.ac.cn
+86-769-88931326
Institute of High Energy Physics Chinese Academy of Sciences
Ping MIAO
Notes: 我的报告就到这里，谢谢大家。