## Slide 1
mSR studies of spin dynamics in frustrated rare-earth magnets
Hanjie Guo （郭汉杰）
Songshan Lake Materials Laboratory (SLAB)
2026-10-26
Dongguan
The 3rd Workshop on Muon Science Technology and Industry

## Slide 2: Outline
Quantum spin liquids and the role of muSR
QSL candidates hexaaluminates RE(Zn,Mg)Al11O19
Hidden-order-like state in the Shastry-Sutherland magnet Nd2Be2GeO7

## Slide 3: Quantum Spin Liquids
Introduction
P. W. Anderson
geometric frustration
highly degenerate QSL
No long-range magnetic ordering
No spontaneous breaking of translation or rotation symmetry
conventional spin ordering

## Slide 4: Quantum Spin Liquids
Introduction

## Slide 5: Quantum Spin Liquids
Introduction
Y. Iqbal et al., PRB, 93, 144411 (2016)
Z. Zhu et al., PRL, 120, 207203 (2018)
next nearest neighbor
anisotropy

## Slide 6: Quantum Spin Liquids
Introduction
closely related to SC
potential for quantum computation
adiabatic demagnetization refrigeration

## Slide 7: Quantum Spin Liquids
Introduction
no order parameters
exclude any long-range magnetic ordering, spin freezing, valence bond solid…
spinon fractional excitations
 excitation continua
(ordered magnets may show similar behavior)
muon is very sensitive to magnetic fields!
distinguish between static and dynamic fields
polarized in ZF
inelastic neutron scattering
thermal transport
How to detect? Or what to exclude?
specific heat
susceptibility
neutron diffraction
……

## Slide 8
Hexaaluminates RE(Zn,Mg)Al11O19

## Slide 9: general structural features
Hexaaluminate
~11 Å
well separated quasi-2D; minimize influence from interlayer disorder
large differences in ionic radii no antisite disorder between magnetic and nonmagnetic ions
versatile rare earth ions (RE = La-Tb)
P63/mmc
a = b = 5.586026
c = 21.920176

## Slide 10: PrZnAl11O19 : susceptibility
Hexaaluminate
dc susceptibility:
Curie-Weiss fit (T < 15 K)
qCW ~ -10 K  strong AFM coupling
ac susceptibility：
no spin ordering down to 50 mK
no frequency dependence  no spin freezing
frustration index: f > 10/0.05 = 200
Bu, Guo et al., PRB 106, 134428 (2022)

## Slide 11: PrZnAl11O19 : gapless excitations
Hexaaluminate
 gapless excitation
a ~ 2 (ZF)
gapless AFM: a = 3
gapless FM: a = 3/2
spinon Fermi surface: a = 2/3 or 1
Coulombic QSL: a = 3
Dirac QSL: a = 2 (ZF), a = 1 (fields）

## Slide 12: PrZnAl11O19 : low-E excitations
Hexaaluminate
Pr3+ (J = 4)：non-Kramers ion
D3h  3 singlets, 3 doublets
peak overlaps at 12 meV and 36meV
E ~ 1.5 meV, diffuse, long tail on the high-E side
distinct from Schottky anomaly in HC  correlation effect

## Slide 13: NdZnAl11O19: low-E excitations
Hexaaluminate
NdZnAl11O19: peak width comparable to instrument resolution
exclude disorder-induced peak broadening in PrZnAl11O19

## Slide 14: PrZnAl11O19：enhanced nuclear magnetism
×
ZF-mSR spectra: Gaussian-broaden-Gaussian
both ZF and LF data indicate a static ground state
Hexaaluminate
D has a Gaussian distribution width W

## Slide 15: PrZnAl11O19：enhanced nuclear magnetism
Singlet ground state for the electronic system
intrinsic CEF ground state
local distortions induced by implanted muons
Hexaaluminate
nuclear spin
electronic angular momentum
Two ingredients:
non-Kramers ion, singlet ground state  van Vleck paramagnetism
large hyperfine interaction

## Slide 16: Intrinsic transverse field Ising model
D ~ 0.1 meV
In the frame work of intrinsic transverse-field Ising model
……
Sz: dipole Sx, Sy: multipole
Hexaaluminate
PrMgAl11O19
Cao, Guo et al., Mater. Futures 3, 035201 (2024)
H || c
electron spin resonance (ESR)

## Slide 17: CeMgAl11O19: U(1) Dirac QSL candidate
Hexaaluminate
Very stable Ce3+ state
oxidized Ce4+ on the surface
Ce2Zr2O7
PRL 122, 187201 (2019)

## Slide 18: CeMgAl11O19: U(1) Dirac QSL candidate
specific heat:
gapless excitations
a = 2, Dirac nodes
a = 1, Fermi pocket
ac susceptibility:
magnetic correlations below ~0.2 K
no spin freezing
YbZn2GaO5
PRL 133, 266703 (2024)
Cm = ATa
A(0.25 T)/A(0 T) =
0.041 (exp.) vs. 0.053 (theory)
Cao, Guo et al., Sci. China: PMA 68, 267011 (2025)
Hexaaluminate

## Slide 19: CeMgAl11O19: slow spin dynamics
x = 0.53(3), MHz, D = 9(1) MHz 
out of the fast fluctuation limit for muSR
less than canonical spin glass systems（108 Hz）
 slow collective fluctuations
Hexaaluminate

## Slide 20: NdZnAl11O19: CEF ground state
Cao, Guo et al., PRB 112, 144409 (2025)
AFM dominant
no order down to 50 mK
CEF fitting  Ising dominant anisotropy
Hexaaluminate

## Slide 21: NdZnAl11O19: CEF ground state
Hexaaluminate

## Slide 22: persistent spin fluctuations
n = 85.3(8) MHz << 37 GHz（exchange fluctuation rate）
Hexaaluminate

## Slide 23
NdTa7O19 vs. NdZnAl11O19
K
K
Nat. Mater. 21, 416 (2022)
our work

## Slide 24: ADR performance
JACS 147, 34862 (2025)
Superior ADR performance compared to some Gd-based compounds
Hexaaluminate
0.75
0.5
NdMgAl11O19

## Slide 25
Summary for hexaaluminates
Using muSR, combined with other techniques (specific heat, susceptibility, neutron…), we identify several quantum spin liquid candidates
The versatility of rare earth ions provides a fertile ground for studying different models (intrinsic transverse field Ising model, Ising dominant XXZ model…)
QSLs retain a large amount of magnetic entropy at low temperatures;
small exchange energy scale means a small magnetic field can easily polarize the spin system – remove entropy at low T
 excellent for magnetic cooling

## Slide 26
Hidden-order-like state in the SSL Nd2Be2GeO7

## Slide 27: phase diagram
Nd2Be2GeO7
Shastry-Sutherland lattice
phase diagram based on the Heisenberg model
SOC-induced anisotropy
QSL still exists?
Other exotic phases?
=
PRB 105, L060409 (2022)

## Slide 28: CEF ground state
Nd2Be2GeO7
Liu, Guo et al., under review
Cs point symmetry: up to 15 nonzero
Nd3+: J = 9/2
five Kramers doublets, four transitions at low T
Ei = 53.1 meV
Ei = 25.1 meV

## Slide 29: dimer model
Nd2Be2GeO7
J = 0.106(2) meV
ESR transitions between the singlet and triplet are usually forbidden
Dzyaloshinskii-Moriya (DM) vector along z
Electron spin resonance
 | CEF GS
mx | 0.82
my | 0
mz | 1.55
x
y

## Slide 30: magnetic ordering
Nd2Be2GeO7
coexistence of long-range and short-range magnetic correlations
no spin-glass transition

## Slide 31: hidden order?
Nd2Be2GeO7
thermodynamic phase transition
no order parameter（neutron, muon）
hidden order
magnetic order revealed after field-training
correlation length x ~ 90 Å > 10c
neutron diff.
ZF-mSR
strong quantum fluctuations along c axis
 | CEF GS | neutron diff.
mx | 0.82 | 0.60
my | 0 | 0
mz | 1.55 | 0.66

## Slide 32: spin dynamics
Nd2Be2GeO7
In fast-fluctuating limit, Redfield formula:
l peaks when

## Slide 33: unusual field-enhanced spectral density
Nd2Be2GeO7
Level crossing resonance:
flip-flop transition
nuclear spin
muon spin
quadrupole splitting
PRB 111, 155148 (2025)
Z. Naturforsch. 47a, 371-381 (1992)
Ba6Nd2Ti4O17

## Slide 34: unusual field-enhanced spectral density
Nd2Be2GeO7
spin-flop-like transition when H || c
Hz
n = 2.6(1) GHz
Difference: not static!

## Slide 35: Origin of field-induced order
Nd2Be2GeO7
strong magnetoelastic effect
parameter a is not restored after the field-trained process
0.01% increase  negative pressure effect
Speculation: positive pressure  disordered state
Nd2Be2SiO7, external pressure…

## Slide 36: Summary
Nd2Be2GeO7
hidden-order-like transition
the order parameter after the field-trained process is a magnetic dipole; but the one after ZFC is unresolved
the stabilized AFM phase is dynamic in nature, but the moments fluctuate coherently in the 10-9 s time scale
the ground state is very sensitive to perturbations  resides at the boundary between the long-range ordered and dynamically disordered phases?

## Slide 37
Acknowledgement
PhD Students
Yantao Cao
Andi Liu
Prof. Z.M. Tian
HUST
Prof. P.J. Sun
IOP
Collaborators
Beamtime
Dr. J. S. Gardner
ORNL
Prof. J.K. Zho
GBU
Dr. Koda Akihiro
Dr. Helen Walker
Dr. G. Wood
Dr. Toni Shiroka
Dr. Hubertus Luetkens
Dr. T. Hicken
Dr. J. Krieger

## Slide 38
Thank you for your attention!