## Slide 1
Center for Correlated Matter and School of Physics
Zhejiang University, China
Complementary muon-spin relaxation and neutron scattering studies of heavy fermion materials
Michael Smidman

## Slide 2
Acknowledgements
Zhejiang University
Jinyu Wu
Zhaoyang Shan
Jianwei Shu
Chun Han
Yanan Zhang
Dajun Su
Jiawen Zhang
Yongjun Zhang (Hubei Normal)
Bin Shen (Nanjing University)
Zhentao Wang
Yu Liu
Chao Cao
Yu Song
Frank Steglich
Huiqiu Yuan
ISIS
Adrian Hillier
Devashibhai Adroja
Pascal Manuel
Fabio Orlandi
Christian Balz
Matthias Gutmann
PSI
Toni Shiroka
Shams Sohel Islam
TRIUMF
Gerald Morris
Bassam Hitti
CSNS
Wu Xie

## Slide 3
Outline
Introduction
Magnetic order of quantum critical ferromagnet CeRh6Ge4
(3) Non-collinear ferromagnetism in pressure-induced superconductor Ce5CoGe2
(4) Complex magnetic order in candidate spin-triplet superconductor CeSb2

## Slide 4
Quantum phase transitions in f-electron compounds
Kondo lattice: Regular arrangement of atoms with partially filled 4f/5f electron shells + conduction electrons
Tunable competition between RKKY and Kondo interactions
RKKY interaction
Magnetic exchange
 Long-range magnetic order
Kondo effect
Hybridization between f- and conduction electrons
 Non-magnetic singlet ground state (“quenches” f-electron moment)
Heavy fermions: Charge carriers have large effective masses

## Slide 5
Quantum criticality
A. Schroeder et al., Nature (2000)
J. Custer et al., Nature (2003)
M. D. Mathur et al., Nature (1998)
Pressure
Magnetic fields
Doping
Tune a 2nd order transition to T = 0 by non-thermal control parameters
 Quantum critical point
Governed by quantum not thermal fluctuations
Novel phases of matter, e.g. strange metals, nematicity, unconventional superconductivity

## Slide 6
Neutrons | Muons (μSR)
Diffraction probes average structure | “Local probe” of magnetic fields at stopping site(s)
Magnetic Bragg peak intensity | Very sensitive to small local fields/ordered moments
Probe energy-momentum of magnetic fluctuations | Directly probes dynamics of internal fields
Sensitive to M ⟂ Q | Probes internal fields ⟂ muon spin polarization
Neutrons | Muons (μSR)
Diffraction probes average structure | “Local probe” of magnetic fields at stopping site(s)
 | Very sensitive to small local fields/ordered moments
Probe energy-momentum of magnetic fluctuations | Directly probes dynamics of internal fields
Sensitive to M ⟂ Q | Probes internal fields ⟂ muon spin polarization
φ = 0
φ = π/4
Diffraction probes |Fhkl|2 => cannot determine ‘global phase’
Neutrons + muons: “Complementary”magnetic probes
μSR can sometimes distinguish between different magnetic structures with identical or similar diffraction patterns

## Slide 7
Ferromagnetic quantum criticality?
M. Brando et al., Rev Mod Phys. (2015)
UGe2, ZrZn2, CoS2…
CeAgSb2, Nb1-yFe2+y…
Ni1-xVx, CePd1-xRhx…
URu2-xRexSi2, NixPd1-x…
(Disorder)
Ferromagnetic quantum critical points not generally observed
Theoretically predicted to be prohibited in clean ferromagnetic systems [D. Belitz et al. PRL (1999)]
UGe2
V. Taufor et al. PRL (2010)
V. A. Sidorov et al. PRB (2003)

## Slide 8
Outline
Introduction
Magnetic order of quantum critical ferromagnet CeRh6Ge4
(3) Non-collinear ferromagnetism in pressure-induced superconductor Ce5CoGe2
(4) Complex magnetic order in candidate spin-triplet superconductor CeSb2

## Slide 9
CeRh6Ge4: Clean stoichiometric Kondo ferromagnet
B. Shen et al., Nature 579, 51 (2020)
Triangular lattice of quasi-1D Ce chains
Ferromagnetic transition TC = 2.5 K
ab-plane ordering of reduced Ce-moments
E. Matsuoka et al JPSJ (2015)

## Slide 10
Ferromagnetic quantum critical point in CeRh6Ge4
B. Shen et al., Nature 579, 51 (2020)
Ferromagnetic quantum critical point at pc = 0.8 GPa
Resistivity
ac susceptibility
Heat capacity
ac heat capacity

## Slide 11
B. Shen et al., Nature 579, 51 (2020)
Microscopic nature of magnetic order in CeRh6Ge4?
Ferromagnetic quantum critical point in CeRh6Ge4

## Slide 12
CeRh6Ge4: Powder neutron diffraction
Powder neutron diffraction @WISH (ISIS)
Subtract 4 K data from 0.4 K => no systematic magnetic Bragg peaks
J. W. Shu et al. Phys. Rev. B 104, L140411 (2021)

## Slide 13
CeRh6Ge4: Muon-spin relaxation
J. W. Shu et al. Phys. Rev. B 104, L140411 (2021)
Coherent oscillations in ZF- μSR => Long range magnetic order
3 oscillation frequencies (internal fields)
μSR@MuSR (ISIS)

## Slide 14
CeRh6Ge4: μSR
J. W. Shu et al. Phys. Rev. B 104, L140411 (2021)
μSR@MuSR (ISIS)
Two inequivalent muon stopping sites
Ferromagnetic order along a-axis => Two local fields associated with site s2
All consistent with small moment in-plane ferromagnetic order (~0.15-0.3μB/Ce)
Calculated local fields (FM order, 0.24 μB/Ce)
s1: 87 G
s2: 152 G, 364 G
Fitted values
56 G, 151 G, 405 G

## Slide 15
Outline
Introduction
Magnetic order of quantum critical ferromagnet CeRh6Ge4
(3) Non-collinear ferromagnetism in pressure-induced superconductor Ce5CoGe2
(4) Complex magnetic order in candidate spin-triplet superconductor CeSb2

## Slide 16
Ferromagnetic Kondo lattice Ce5CoGe2
D. J. Sun et al. Phys. Rev. B 110, 144432 (2024)
Orthorhombic crystal structure (Pnma): 4 inequivalent Ce-sites
Ferromagnetic transition at TC = 10.9 K with easy a-axis
Spin glass behavior with freezing temperature Tf = TC

## Slide 17
New scenario for unconventional superconductivity in correlated systems?
Y. N. Zhang et al. National Science Review 13, nwag119 (2026)
TC decreases under pressure
Above 1.2 GPa, new magnetic transition with distinct field response Change from ferromagnetic to antiferromagnetic ground state
Magnetic order suppressed to zero temperature quantum critical point at 3.2 GPa
Superconductivity appears well above the QCP at 6.2 GPa (Tc ~ 0.5 K), shifts to higher temperature with pressure (2 K at 15 GPa)
Distinct scenario for superconductivity in correlated ferromagnets

## Slide 18
Canted ferromagnetism in Ce5CoGe2 at ambient pressure
J. Y. Wu et al. Phys. Rev. B 113, 134431 (2026)
Ambient pressure powder neutron diffraction: k=0 ferromagnetic structure with magnetization along a-axis
Cannot refine with collinear FM structure: magnetic (110) peak demonstrates symmetry allowed c-axis component
Non-collinear ferromagnetic structure with net magnetization along a-axis

## Slide 19
J. Y. Wu et al. Phys. Rev. B 113, 134431 (2026)
μSR on Ce5CoGe2
Coherent oscillations with no evidence for change of magnetic structure with temperature
Weak increase in exponential relaxation rate λ + broad hump in C/T => Slowing down of fluctuations in magnetic phase? Incipient antiferromagnetic fluctuations in ferromagnetic state?
μSR@VMS (PSI)

## Slide 20
Outline
Introduction
Magnetic order of quantum critical ferromagnet CeRh6Ge4
(3) Non-collinear ferromagnetism in pressure-induced superconductor Ce5CoGe2
(4) Complex magnetic order in candidate spin-triplet superconductor CeSb2

## Slide 21
Candidate spin-triplet superconductor CeSb2
Layered orthorhombic structure: 4 nearly square Ce-layers/unit cell (2 bilayers)
(a = 6.28 Å, b = 6.13 Å)
Heavy-fermion superconductivity under pressure: SC dome at QCP?
Hc2 (T) greatly exceeds the Pauli limit + inverted ‘S’-shape: Spin triplet?
Squire et al. PRL 131, 026001 (2023)
Ce
Sb
5.1 Å
4.0 Å

## Slide 22
Candidate spin-triplet superconductor CeSb2
Ambient pressure: Multiple magnetic phases with AFM and FM components below TN = 16 K
Neutron diffraction: Commensurate AFM propagation vector (±1/6, -1, 0) below ~ 10 K
Trainer et al. PRB 104, 205134 (2021)
Zhang et al. Chin. Phys. B 26, 067102 (2017)
Liu et al. JPCM 32 405605 (2020)

## Slide 23
Inelastic neutron scattering measurements of CeSb2
“Rod-like” excitations in [HL] and [HK] planes: No long-range propagation of spin-waves (magnons) along c* axis and along on one in-plane direction (with twinning)
Spin-waves stem from integer Bragg positions:
Direct evidence for quasi-1D ferromagnetic excitations
Inelastic neutron scattering @LET (ISIS)
In-plane excitations
Out-of plane excitations
Z. Y. Shan et al. Phys. Rev. Lett. 134, 116704 (2025)

## Slide 24
Ferromagnetic spin ladder model
Data well described by a ferromagnetic spin ladder model with weak coupling between ladders
= -2.2 meV
= -1.8 meV
= -1.4 meV
= -0.1 meV
= 1.2
What about the magnetic structures?
Z. Y. Shan et al. Phys. Rev. Lett. 134, 116704 (2025)

## Slide 25
Magnetic order of CeSb2
Neutron diffraction @SXD (ISIS), SIKA (ANSTO), TREND (CSNS)…
(Unpublished)
Multiple magnetic propagation vectors with different temperature dependences:
No magnetic Bragg peaks above 11 K, but magnetic order below TN = 16 K?

## Slide 26
Magnetic order of CeSb2
(Unpublished)
Coherent oscillations below 16 K: Long range magnetic order below TN = 16 K
Temperature dependence of internal fields consistent with previously observed transitions with small changes in internal fields
μSR@LAMPF (TRIUMF)
Trainer et al. PRB 104, 205134 (2021)

## Slide 27
Magnetic order of CeSb2
(Unpublished)
Calculated internal fields for pure ferromagnetic model: Site 1 => 296 mT, Site 2 => 196 mT
Fitted values: B2(0) = 204 mT, B3(0) = 248 mT, B4(0) = 256 mT
Besides B1, local fields dominated by ferromagnetic spin ladders
μSR@LAMPF (TRIUMF)

## Slide 28
Summary
Neutron scattering and muon-spin relaxation are powerful complementary tools for probing magnetic structure and dynamics in heavy fermions and other correlated materials
Muon-spin relaxation is particularly useful for probing weak magnetic order often found in proximity to quantum phase transitions and novel quantum phases of matter
Z. Y. Shan et al. Phys. Rev. Lett. 134, 116704 (2025)
B. Shen et al., Nature 579, 51 (2020)
J. W. Shu et al. Phys. Rev. B 104, L140411 (2021)
D. J. Sun et al. Phys. Rev. B 110, 144432 (2024)
Y. N. Zhang et al. National Science Review 13, nwag119 (2026)
J. Y. Wu et al. Phys. Rev. B 113, 134431 (2026)