## Slide 1: Experimental Studies of Electron Emissions and Breakdowns in RF Guns
Wei Gai
For ANL/THU/SLAC collaboration
Symposium Accelerator Physics,
August 15
XinglongShan, Gansu, China

## Slide 2: Breakdown in RF cavities
Extremely complicated physical phenomenon
May involve localized field emission, eddy current, plasma formation, metal
fatigue, crystallographic defects, etc. Has been studied for decades.
Dependence on E, B, Sc, ΔTp, Power flow …
Sets of breakdown experiments are trying to isolate some of the contributing
effects.
Anyway to shed lights on the physics of RF breakdowns?
  Direct Dark current measurement;
  Work function;
  Local heating;
  Laser-triggered RF breakdown
  SEM surfaces
  …….
Provide a controllable and flexible method for breakdown studies.

## Slide 3: An s-band rf photocathode gun: 2 configurations
UV Laser
400 nm, ~ 1 mJ, 0.1 – 3 ps
S-band RF gun
50 – 70 MV/m
cathode
Laser
alignment
Faraday Cup
ICT
Dark Current Measurements
photocathode
Schottky Enabled Photo-electron Emission Measurements
Tsinghua U has an rf gun facility available to study copper surfaces

## Slide 4: Schottky Enabled Photo-electron Emission Measurements
Experimental parameters
  work function of copper = f0 = 4.65 eV
  energy of l=400nm photon = hn= 3.1 eV
  Laser pulse length
    Long = 3 ps
    Short = 0.1 ps
  Laser energy ~1 mJ (measured before laser input window)
  Field (55 – 70 MV/m)
ICT
g
e-
First results
from Tsinghua
Data 2010-10-04
Should not get
photoemission

## Slide 5: Long Laser Pulse (~ 3ps) E=55 MV/m@ injection phase=80  55sin(80)=54
Q(pC)
laser energy (mJ)
photocathode input window
First results
from Tsinghua
Data 2010-10-04
Q I
single photon emission

## Slide 6: Short Laser Pulse (~ 0.1ps) E=50 MV/m@ injection phase=30  50sin(30)=25
First results
from Tsinghua
Data 2010-10-04
Q(pC)
laser energy (mJ)
photocathode input window
Q aI + bI2
multiphoton emission

## Slide 7: Dark Current Measurements
Experimental parameters
  work function of copper = f0 = 4.65 eV
  Field (57– 73 MV/m)
  Note: field could be lowered more but Faraday Cup signal was too weak to measure current
First results
from Tsinghua
S-band RF gun
50 – 70 MV/m
cathode
Faraday Cup

## Slide 8: Fowler Nordheim plot of dark current data
Copper work function Φ0=4.6 eV
Fit: β ~ 130
First results
from Tsinghua
Data 2010-10-04
Field (57– 73 MV/m)

## Slide 9: Summary of the first measurements
Schottky Enabled Photo-electron Emission Measurements
  Schottky enhanced emission observed at all the field levels measured.
    hn =3.1 eV, f0=4.6 eV  DF=1.5eV (Schottky effect required)
    The lowest field 25 MV/m
       (Schottky effect)
       implies b>=60
    note: also observed emission at lower fields, but data was noisy. This implies even larger  exists or lower work functions at some points on cathode.
Dark current measurements
   is 130.
Some possibilities/speculation …
Alternative interpretation of Fowler-Nordhiem plots

## Slide 10: Electron emission
Copper surface
typical picture 
geometric perturbations (b)
Fowler Nordheim Law (RF fields):
High field enhancements (b) can field emission.
Low work function (f0) in small areas can cause field emission.
oxides
alternate picture 
material perturbations (f0)
inclusions
peaks
grain
boundaries
cracks
(suggested by Wuensch and colleagues)
(b, f0, Ae, E0)
IFN

## Slide 11: Field emission enhancement factor
b=130 may be unphysical  h/r ~ 100
fresh surfaces machines to ~10nm roughness
h=10 nm, r=0.1 nm (“a tower of single atoms”)

## Slide 12: β from Fowler-Nordheim plot
Raw Data
  Field emitted current
  E-field on surface
Fit
  Different combinations of b and f0 can fit the same raw data
  Can we find a way to measure what role each effect plays?
(β=5, Φ0 =1.2 eV)???
(β=130, Φ0 =4.66 eV)
Notes: WG: beta=130 is unphysical

## Slide 13: Ae from Fowler-Nordheim plot
Raw Data
  Field emitted current
  E-field on surface
Fit
  Typical fits give areas so small that they are difficult/impossible to measure.
  Does this give us a way to probe
  whether b or f0 dominates?

## Slide 14: Dark current imaging experiment
Dark current is strongly coupled to the RF breakdown phenomenon
Conventional formula of dark current – Flower-Nordheim function [1]
: usually considered to be constant for certain material
and fitted parameter by a series of and ; , can’t be observed [2];
, not physical [3].
With dark current imaging system: direct measurement of and identify dark current emitter

## Slide 15
Wide energy spectrum of dark current causes blurred image
Initial emitter on the cathode
After the solenoid
Experiment results:
To get clear image, need to select dark current with certain energy
Different focusing for different energy
After the solenoid, certain energy
Notes: The four points plots are from PARMELA simulation. The lower right one is from our experiment result without collimator.

## Slide 16
Energy selection by a collimator
RF gun
Solenoid
YAG
Collimator
Smaller the hole, dimmer but clearer the image

## Slide 17
Experiment setup
Gun with mountable
cathode
Solenoid
Collimator
YAG
L-band single cell gun. Maximum E-field 100 MV/m with 2 MW input power.
Three size of collimator: φ 0.02”, φ 0.0135”, φ 0.0075”.

## Slide 18
Experiment results
Edge
Pattern
Edge: E-field is 20% higher than the center, may be further enhanced by the gap
Cathode center
Cathode edge
Pattern: created by sandblasting, 30~40 um roughness (cathode base polished to 1 um)
Φ 0.02”
Φ 0.0135”
Φ 0.0075”
Edge
Pattern ?
Reflection
Edge
Edge

## Slide 19
Laser Triggered Experiment setup (at Tsinghua University)
Laser
Ti:Sapphire, 266 nm UV
1.2 ps pulse duration
1mm2 spot size on the cathode
2 mJ max energy
~5% energy jitter
RF gun
1.6-cell S-band 2856MHz
Solid, demountable cathode
55 MV/m at cathode center with
4.8 MW input power
Oscilloscope
12 GHz bandwidth
50 G/s sample rate

## Slide 20
Comparison of the laser damage on the surface and RF breakdown
Laser damage spot
Average intensity 6 mJ/cm2
In air
Non-uniform distribution causes ablation
White light interferometry
ablation
Ablation spot
melting
500 um
20 um
20 um
SEM of laser damage spot
SEM of breakdown spot
20 um
100 um
500 um

## Slide 21
Normal operation of the gun
laser
<0.5 mJ/cm2, no breakdown
Forward and reflection
RF pickup
Faraday cup
Photoelectron current:
Damped oscillation due to ringing in the data acquisition system

## Slide 22
Laser-triggered RF breakdown
High emission current
Single-BD (>99%) and multi-BD (<1%)
Excitation of 8.6 GHz HOM with collapse of the fundamental mode
Bright spot observed during BD,
damage found at the same position afterward
>10 mJ/cm2, breakdown at almost every RF pulse
Notes: RF breakdown without laser trigger of single-breakdown event (left) and multi-breakdown event (right).
(a-b) The Faraday cup signal in Amperes. (c-d) Normalized FFT amplitude of the pickup signal in different frequency bands as a function of time, including the fundamental mode without breakdown (black line), the fundamental mode with breakdown (blue line), and the 8.6 GHz HOM with breakdown (red line). (e-f) Same signals in (c-d) with a zoom in view around 0 ns. (g-h) Normalized FFT amplitude of the reflection signal, including the fundamental mode without breakdown (blue line) and with breakdown (red line).
Note the possibility of single-BD and multi-BD in red.
The picture was taken by the camera looking through the viewport on the half cell.

## Slide 23
De-convoluting of breakdown current
photoelectron
BD current
photoelectron
BD current
Three stages of BD current: increasing electron emission (20∼50 ns); steady state emission (20∼40 ns); and decreasing emission (20∼30 ns).
Shape varies between pulses due to fluctuation of laser intensities, etc.
Notes: The damped oscillation signal is used as the system function of the whole Faraday cup system.

## Slide 24
Circuit model
18 A BD current in both cells; 3.2 MHz and 0.9 MHz frequency downshift for the half cell and full cell respectively
BD current
Frequency detune are also introduced to both cells after the emission
Notes: RF breakdown with laser trigger of single-breakdown event (left) and multi-breakdown event (right). (a-b) The Faraday cup signal in Amperes. (c-d) Normalized FFT amplitude of the pickup signal in different frequency bands as a function of time, including the fundamental mode without breakdown (black line), the fundamental mode with breakdown (blue line), and the 8.6 GHz HOM with breakdown (red line). (e-f) Normalized FFT amplitude of the reflection signal, including the fundamental mode without breakdown (blue line) and with breakdown (red line).
Note the frequency detune of the half cell is introduced immediately after breakdown and that of the full cell is introduced 200 ns after the breakdown and linearly increased to 0.9 MHz, trying to simulation plasma propagation.

## Slide 25
RF breakdown without the laser trigger
Lower BD current
Single-BD (~30%) and multi-BD (~70%)
Excitation of 8.6 GHz HOM and collapse of the fundamental mode
40~140 ns delay of collapse of the fundamental mode
BD occurred in the half cell, but away from the axis
Notes: There are two special points of this plot.
First, the delay of collapse of fundamental mode and two orders of magnitude lower of BD current imply the breakdown occurred on the half cell but away from the axis.

## Slide 26: Comments on Laser triggered BB study
Controllable RF breakdown in a cavity can be achieved.
For multi-BD, the excitation of the HOM caused by the 2nd BD is always near the end of the fundamental mode collapse
Power flow from the full cell due to unbalanced energy after the 1st BD causes the 2nd BD in the half cell
Summary:
We are attempting to explore parameters inter-dependent for RF breakdown in a cavity, and a few tools have been developed for field emission studies. Hope to have more data and the nature will manifest itself.