## Slide 1: CEPC SRF Working Group Meeting
Jiyuan Zhai
Oct 30, 2015, IHEP

## Slide 2
CEPC-SPPC
50-70 km

## Slide 3
328 pages
260 pages

## Slide 4
258 authors
from 45 institutions
in 9 countries

## Slide 6
CEPC Design – Top Level Parameters
Parameter | Design Goal
Particles | e+, e-
Center of mass energy | 240 GeV
Integrated luminosity (per IP per year) | 250 fb-1
No. of IPs | 2
SPPC Design – Top Level Parameters
6
Parameter | Design Goal
Particles | p, p
Center of mass energy | 70 TeV
Integrated luminosity (per IP per year) | (TBD)
No. of IPs | 2
 one million Higgs from 2 IPs in 10 years

## Slide 7
CEPC Lattice Layout (September 24, 2014)
P.S.
P.S.
P.S.
IP1
IP4
IP3
IP2
D = 17.3 km
½ RF
RF
RF
RF
RF
½ RF
½ RF
½ RF
RF
RF
One RF station:
650 MHz five-cell SRF cavities;
4 cavities/module
12 modules, 10 m each
RF length 120 m
4 IPs, 1038.4 m (944 m) each
4 straights, 849.6 m (944 m) each
8 arcs, 5852.8 m each
C = 54.374 km

## Slide 8
Tunnel Cross Section – SPPC + CEPC Magnets
Drill/Blast Method
6 m

## Slide 9
Tunnel Cross Section – RF Sections
Drill/Blast Method
7.2 m

## Slide 10
Circular Lepton Colliders (K. Oide, RAST, volume 7)

## Slide 11
CEPC Design – Guidelines
Build an underground tunnel for a Higgs factory
Use the same tunnel for a future pp collider:
  The tunnel cross section should be big enough to accommodate an e+e- collider, a booster and a pp collider
  The straight sections should be long enough to accommodate large detectors and complex collimation systems of a pp collider
  It should allow to run both e+e- and pp experiments simultaneously
  Within the budget limit, the tunnel circumference should be made as large as possible
Keep options open for:
  Super Z
  e-p and e-A colliders
  Light source
  FEL
A possible timeline:
  A Preliminary Conceptual Design Report (Pre-CDR) this year
  Get ready for R&D to start in 2016 in the government’s 13th Five-Year Plan (2016-2020)
  Get ready for construction to start in 2021 in the 14th Five-Year Plan (2021-2025)
  Get ready for experiments to start in 2028 in the 15th Five-Year Plan (2026-2030)

## Slide 12
CEPC Design - Baseline
Tunnel circumference: ~54 km
Tunnel size: 6.0 m (LEP tunnel: 3.6 m)
8 arcs and 8 straight sections: 4 straight for IPs and RF, another 4 for RF, injection and beam dump, etc.
A 6 GeV linac on the surface (with the option for an FEL in the future)
A full-energy 120 GeV Booster in the tunnel
A 240 GeV e+e- Collider in the same tunnel underneath the Booster
A single beam pipe for both e+ and e- beams (similar to LEP, CESR)
Synchrotron radiation budget: 50 MW per beam
Two SRF systems:
  Booster: 1.3 GHz 9-cell cavity, similar to the ILC, XFEL, LCLS-II
  Collider: 650 MHz 5-cell cavity, similar to the ADS, PIP-II

## Slide 13
CEPC Design – Main Parameters
Parameter | Unit | Value | Parameter | Unit | Value
Beam energy [E] | GeV | 120 | Circumference [C] | m | 54752
Number of IP[NIP] |  | 2 | SR loss/turn [U0] | GeV | 3.11
Bunch number/beam[nB] |  | 50 (48) | Bunch population [Ne] |  | 3.79E+11
SR power/beam [P] | MW | 51.7 | Beam current [I] | mA | 16.6
Bending radius [r] | m | 6094 | momentum compaction factor [ap] |  | 3.36E-05
Revolution period [T0] | s | 1.83E-04 | Revolution frequency [f0] | Hz | 5475.46
emittance (x/y) | nm | 6.12/0.018 | bIP(x/y) | mm | 800/1.2 (3)
Transverse size (x/y) | mm | 69.97/0.15 | xx,y/IP |  | 0.118/0.083
Bunch length SR [ss.SR] | mm | 2.14 | Bunch length total [ss.tot] | mm | 2.65
Lifetime due to Beamstrahlung | min | 47 | lifetime due to radiative Bhabha scattering [tL] | min | 51
RF voltage [Vrf] | GV | 6.87 | RF frequency [frf] | MHz | 650
Harmonic number [h] |  | 118800 | Synchrotron oscillation tune [ns] |  | 0.18
Energy acceptance RF [h] | % | 5.99 | Damping partition number [Je] |  | 2
Energy spread SR [sd.SR] | % | 0.132 | Energy spread BS [sd.BS] | % | 0.096
Energy spread total [sd.tot] | % | 0.163 | ng |  | 0.23
Transverse damping time [nx] | turns | 78 | Longitudinal damping time [ne] | turns | 39
Hourglass factor | Fh | 0.68 | Luminosity /IP[L] | cm-2s-1 | 2.04E+34

## Slide 14
Main Technical Challenges for CEPC
Common for both CEPC and FCC-ee:
IR optics with appropriate dynamic aperture for off-momentum up to 2%
Machine-detector interface (L* = 1.5 m)
HOM damper for the RF cavity
  High average beam current: 2 x 16.6 mA
  High HOM loss: 2 x 2.3 kW per cavity
Specific to CEPC (due to budget constraint):
Pretzel orbit (single beam pipe)
Low energy injection (6 GeV) to the Booster:
  Earth field effect: bend field ~30 Gs, measured earth field ~0.5  0.03 Gs
 | 40 K to 80 K | 5 K to 8 K | 2 K
HOM heat load distribution | 3% | 0.3% | 0.1%

## Slide 15
CEPC Relative Cost Estimate
26%
19%
12%
12%
10%
10%
4%
2%
2.4%

## Slide 16
Chart: 
| Linac & transport lines | Booster | Magnet | SRF | Cryogenics | Regular electricity | Utilities | Detectors
 | 10 | 43 | 75 | 220 | 25 | 30 | 45 | 15
Relative Power Consumption
9%
16%
5%
10%
6%
48%
2%
3%

## Slide 17
Pretzel Scheme
48 bunches / beam, 96 parasitic collision points (~ 500 m spacing)
Horizontal separation, no off-center orbit in RF section
One pair of electrostatic separators for each arc (green)
One pair of electrostatic separators for P2, P3, P4, P6, P7, P8
H.P. Geng

## Slide 18: Local Double Ring Scheme
One bunch train per beam
No pretzel
Crab waist possible
Cost less than whole double-ring
More bunches for high luminosity Z, W
J. Gao, M. Xiao, M. Koratzinos
Parameters | Value | Unit
Circumference | 54374 | m
Length of one FODO cell | 47.2 | m
Harmonic number | 118800 | 
One bucket length in the ring | 0.46 | m
Bucket number in double beam pipe | 6156 | 
Local double section 10% of the whole ring
120 FODO cells length
1.416km on each side of IP
e-
e+
~3 km (10 μs) macro-bunch
RF

## Slide 19: LDR Time Structure
Parameters | Z | W | H
Beam energy [GeV] | 45 | 80 | 120
Synchrotron radiation power per beam [MW] | 50 | 50 | 50
SR loss/turn U0 [GeV] | 0.062 | 0.6 | 3.01
Beam current I [mA] | 796.8 | 84.03 | 16.62
Bunch population Ne [1011] | 3.09 | 3.65 | 3.61
Bunch number | 2688 | 240 | 48
Bucket interval per bunch | 2 | 25 | 128
Distance between bunches [m] | 0.92 | 11.5 | 58.88
Bunch space time [ns] | 3.1 | 38.3 | 196.3
J. Gao, M. Xiao

## Slide 20: Beam Loading of Bunch Trains
Consider one bunch train of the LDR scheme.
Beam loading is different for different bunches.
Cavity voltage amplitude, synchrotron phase and tune will be modulated periodically.
Accurate analytical calculation difficult because of syn. phase oscillation in the ring. Simulation (KEKB, SLC-DR).
LLRF feedback compensation.
P.B. Wilson, SLAC-PUB-6062
Phasor for injection, gap left to cure instability, bunch trains …

## Slide 21: Beam Loading of Bunch Trains
Rough estimation for H-LDR:
Tb-train = 0.2 μs, Ttrain = 10 μs, Tg = 183 us, Td = 1077 us.
Tb-train and Ttrain << Td, the bunch train can be treated as a macro-bunch.
Tg << Td, the beam induced voltage is same as the equal-spacing, thus the same average beam loading.
Phase difference between the head and tail bunches: 10 deg
Voltage difference between the head and tail bunches: 2.8 MV
D. Boussard, CERN SL / 91-16

## Slide 22: CEPC Top-level Parameters related to SRF System (1)
Parameter | Unit | Main Ring | Booster Injection | Booster Extraction
Beam energy | GeV | 120 | 6 | 120
Circumference | km | 54.752 | 54.752 | 54.752
Luminosity / IP | cm-2s-1 | 2.04E+34 | - | -
Energy loss / turn | GeV | 3.11 | 17.6 keV | 2.81
SR power | MW | 103.42 | 16.2 W | 2.46
Revolution period | s | 1.83E-04 | 1.83E-04 | 1.83E-04
Revolution frequency | kHz | 5.4755 | 5.4755 | 5.4755
Bunch charge | nC | 60.56 | 3.35 | 3.2
Bunch number | - | 100 | 50 | 50
Beam current (total) | mA | 33.2 | 0.92 | 0.87
Bunch spacing | μs | 1.825 | 3.65 | 3.65
Beam spectrum spacing | MHz | 0.55 | 0.274 | 0.274

## Slide 23: CEPC Top-level Parameters related to SRF System (2)
Parameter | Unit | Main Ring | Booster Injection | Booster Extraction
Momentum compaction | - | 3.36E-05 | 7.69E-05 | 7.69E-05
Energy spread | % | 0.1629 | 0.1 (linac) | 0.127
Bunch length | mm | 2.65 | 1.5 (linac) | 2.66
RF voltage | GV | 6.87 | 0.213867 | 5.12
RF frequency | GHz | 0.65 | 1.3 | 1.3
Harmonic number | - | 118800 | 237423 | 237423
Synchrotron tune | - | 0.180 | 0.32076 | 0.32076
Energy acceptance (RF) | % | 5.99 | 17.307 | 2.091
Transverse damping time | turns | 77.05 | 682122 (125 s) | 85.2 (15.56 ms)
Longitudinal damping time | turns | 38.52 | 341219 (62 s) | 42.7 (7.789 ms)
Lifetime Bhabha | min | 51.77 | - | -
Lifetime BS (sim.) | min | 47 | - | -

## Slide 24: CEPC RF Parameters
 | H-PZ | H-LDR | Z-PZW | Z-PZBT | Z-LDR
Beam energy (GeV) | 120 |  | 45 |  | 
SR power per beam (MW) | 50 |  | 0.084 | 13.4 | 50
SR loss / turn U0 (GeV) | 3.11 | 3.01 | 0.06 | 0.06 | 0.06
Luminosity L (cm-2s-1) | 2E34 | 2E34 | 2E32 | 2.3E34 | 7E34?
Bunch charge q (nC) | 60 | 58 | 5 | 22.4 | 50
Average beam current I (mA) | 2 x 16.6 | 2 x 16.6 | 2 x 1.4 | 2 x 223 | 2 x 797
No. of bunches per train nb | 1 | 48 | 1 | 28 | 2688
No. of bunch trains nt | 48 | 1 | 50 | 64 | 1
Cavity voltage Vc (MV) | 17.9 | 17.9 | 6 | ? | ?
RF power per cavity P (kW) | 280 | 280 | 0.22 | 70+17.8+ | 260+143+
Bunch space in train Tt (ns) | / | 196.3 | / | 4.6 | 3.1
Bunch (train) space Tb (μs) | 3.8 | 183 | 3.8 | 2.9 | 183
Max. arrival time diff. Ta (μs) | 2.7 | 170 | 2.7 | 2.7 | 170
Fundamental mode (FM) QL | 2.2E6 | 2.2E6 | < 3E8 | < 2.2E6 | < 2.2E5
Cavity filling time Td (μs) | 1077 | 1077 | >> 1077 | < 1077 | < 107
HOM power per cavity (kW) | 3.5 | 3.5 | 0.025 | 17.8 | 143
HOM CBI Qext limit | 2E6~8E7 | 2E6~8E7 | 5E5~2E7 | 3E3~1E5 | 1E3~3E4

## Slide 25: CEPC SRF System Layout
Total RF module length: 1.4 km
Total RF voltage: 12 GeV
Beam power: 104.5 MW
HOM power: 2 MW
Installed RF power: ~ 160 MW
Installed cryogenics: ~ 100 kW @ 4.5 K
 | Collider | Booster
Modules per section | 12 | 4
Module length | 10 | 12
Cavities per module | 4 | 8
No. of modules | 96 | 32
No. of cavities | 384 | 256
Pretzel Scheme
Two symmetric half sections in each of the eight RF sections.

## Slide 26
scaled from 1.3 GHz cryomodule
Euro-XFEL/ILC/LCLS-II type
Cryomodule Layout
X
X
Enlarge two- phase pipe and chimney.
Omit 5K shield while keep 5K intercept for power coupler.

## Slide 27
CEPC Collider RF Section Configuration
IPs & Pn (n: six parasitic crossing points)
Main Ring module (10 m)
Four 650 MHz 5-cell cavities inside
IP or Pn
FFS (350 m)
or 2 FODO cells (95 m)
One FODO cell (47.2 m)
Half FODO cell (23.6 m)
\\
Pretzel scheme Half RF Section (6 modules, 70 m), 3 module pairs (valve boxes)
DIS
SEP
SEP (Pn)
5λ/2
3λ/2 [(2n+1)λ/2, 2 cav. with one klystron]
λ = 0.461 m
RF length of one module = 29 λ/2 = 6.7 m
For counter-rotating beams, all 5-cell cavity centers must be at nλ/2 from Pn.
Beam time structure various in cavities, modules, RF sections and diff. schemes.

## Slide 28: Main Ring SRF System Design Criteria
qb = 60.6 nC
PSR 100 MW
Vrf 6.87 GeV
U0 = 3.11 GeV
T
frf
Q0
η↑, τBS ↑, σz↓
ρ = 6.1 km
Pcoupler < 300 kW
Ncavity
↓
Eacc
Ncell
R/Q
Impedance T.H.
↑
HOM Power
↓
Vc
Lc
Riris
Ep Bp
↓
↑
↓
HOM QL
QL
G
HOM R/Q, k
↓
Rs
Thin Film
Nmodule
Ncav/module
HOM Damping
WG
Hook
Ferrite
Bulk Nb
Nb3Sn/Nb
Nb/Cu
N-dope
↓
Dynamic Cryo Load
↑
↑
Cavity Shape
Large iris
Low loss
PS Efficiency
↑
Cavity Material
I = 33.2 mA
Nb = 50
Mode Propagate
RF AC < 200 MW
Cryo AC < 20 MW
↓
2 K
4.2 K
↓
↓
f0 = 5.5 kHz
Vc
↓

## Slide 29: Main Parameters of CEPC SRF System
Parameters | CEPC-Collider | CEPC-Booster | LEP2
Cavity Type | 650 MHz 5-cell Nitrogen-dope Nb | 1.3 GHz 9-cell Nitrogen-doped Nb | 352 MHz 4-cell Nb/Cu sputtered
Cavity number | 384 | 256 | 288
Vcav / VRF | 17.9 MV / 6.87 GeV | 20 MV / 5.12 GeV | 12 MV / 3.46 GeV
Eacc (MV/m) | 15.5 | 19.3 | 6 ~ 7.5
Q0 | 4E10 @ 2K | 2E10 @ 2K | 3.2E+9 @ 4.2K
Cryomodule number | 96 (4 cav. / module) | 32 (8 cav. / module) | 72 (4 cav)
RF input power / cav. (kW) | 280 c.w. | 20 | 125 c.w.
RF source number | 192 (800 kW / 2 cav) | 256 (25 kW / cav) | 36 (1.2 MW/8 cav)
HOM power per cavity (kW) and damper type | 3.5 coaxial/waveguide@2 K + ferrite@RT | 0.05 coaxial@2 K + ceramic@80 K | 0.3 W coaxial@4.2 K + ferrite@RT

## Slide 30: Choice of RF Frequency, #Cavity, #Cell, Gradient and Q0
Beam dynamics and instability
HOM power
Cavity size, cost and technology maturity
Coupler power capacity, yield and operational risk
Cryogenic load, operating temperatures
Booster low current and duty factor
Synergy with other projects (XFEL, ILC, LCLS-II, ADS, PIP-II)
…
Example:
Main ring cavity number determined by power coupler capacity (coupler power 280 kW => 384 cavities => 18 MV each)

## Slide 31: High Q0
High Q to save cryogenic power
  650 MHz cavity: bulk niobium operating at 2 K with Q0=4E10 at 15.5 MV/m
  1.3 GHz cavity: bulk niobium operating at 2 K with Q0=2E10 at 19.3 MV/m
New nitrogen-doping and flux expulsion technology for high quality factor SRF cavity might be used to reach these targets.
Need very clean cavity processing/assembly, electro-polishing
Thin film technology (such as Nb3Sn) with higher gradient and Q0 operating at higher temperature will be studied as an alternative.

## Slide 32: 650 MHz 5-cell Cavity
 | internal | Left end half cell | Right end half cell
Riris(mm) | 77.96 | 84.46 | 84.46
Alpha(deg) | 2.24 | 16.727 | 16.39
A(mm) | 94.4 | 92.1 | 91
B(mm) | 94.4 | 92.1 | 91
a(mm) | 20.03 | 13.76 | 13.71
b(mm) | 22.09 | 21.14 | 20.29
L(mm) | 115 | 114 | 113
D(mm) | 206.6 | 206.6 | 206.6
flatness | 2.17% |  | 
coupling | 3.04% |  | 
Ep/Eacc | 2.43 |  | 
Hp/Eacc [mT/(MV/m)] | 4.23 |  | 
Need further shape optimization, especially for the HOM properties

## Slide 33: Cavity Design Parameters
Parameter | Unit | Main Ring | Booster
Cavity frequency | MHz | 650 | 1300
Number of cells | - | 5 | 9
Cavity effective length | m | 1.154 | 1.038
Cavity iris diameter | mm | 156 | 70
Beam tube diameter | mm | 170 | 78
Cell-to-cell coupling | - | 3 % | 1.87 %
R/Q | Ω | 514 | 1036
Geometry factor | Ω | 268 | 270
Epeak/Eacc | - | 2.4 | 2
Bpeak/Eacc | mT/(MV/m) | 4.23 | 4.26
Cavity longitudinal loss factor* k∥ HOM | V/pC | 1.8 | 3.34
Cavity transverse loss factor* k⊥ | V/pC/m | 2.4 | 35.3
Acceptance gradient | MV/m | 20 | 23
Acceptance Q0 at acceptance gradient | - | 4E10 | 2E10
* main ring bunch length 2.65 mm, booster bunch length 2.66 mm

## Slide 34: Status of development of critical components, 650 MHz
Currently Available Cavities:
1-Cell 650 MHz*
1. B9AS-AES-001
2. B9AS-AES-002
3. B9AS-AES-003
4. B9AS-AES-004
5. B9AS-AES-005
6. B9AS-AES-006
5-Cell 650 MHz
1. B9A-AES-007
2. B9A-AES-008
3. B9A-AES-009
4. B9A-AES-010
*VTS Tested
Expected Cavities:
1-Cell 650 MHz
Pavac, Inc.
Three are delivered
and VTS-tested
Two to be delivered
in the end of 2015.
5-Cell 650 MHz
Pavac, Inc.
Five to be delivered
in 2015.
  650 MHz section:

## Slide 35: Status of development of critical components, 650 MHz CMs
11 total cryomodules
3 cavities each (650 MHz, 5-cell)
33 total cavities
No magnets internal to the cryomodule
Approximate length = 3.9 m
4 total cryomodules
6 cavities each (650 MHz, 5-cell)
24 total cavities
No magnets internal to the cryomodule
Approximate length = 9.5 m
Low-Beta Cryomodule
High-Beta Cryomodule
Concept 1 (room temperature strongback)
  Many design features common with the current SSR1 cryomodule design
  Coupler port locations are fixed with respect to the vacuum vessel
  Support system not subject to thermal distortions during cooldown
  To date, unproven
Concept 2 (XFEL-like design)
  Design concepts are direct descendants of the XFEL design
  Could possibly use tooling common to XFEL-like cryomodules
  Coupler positions change during cooldown
  Support pipe can distort during cooldown

## Slide 36: HOM Power Spectrum and Damping
LEP/LHC-type HOM coupler for the kW level power capacity. BNL is developing new kW class coaxial HOM couplers.
KEKB and SuperKEKB ferrite HOM absorbers 20 kW. IHEP 4.5 kW tested.
Waveguide at the cavity beam pipe is also a possible solution for the main ring cavity HOM power extraction.
XFEL/ILC type HOM coupler and absorber can easily handle the booster HOM power. Ceramic HOM absorber at 70 K in the cryomodule beam line.
80 % above cut-off frequency , propagate through cavities and finally absorbed by the two HOM absorbers at room temperature outside the cryomodule.
Each absorber has to damp about 10 kW HOM power, can’t be in the cryogenic region.
LEP2: 300 W / cavity
above cut-off : 200 W

## Slide 37: HOM Heat Load Budget
 | Main Ring | Booster
HOM power / cavity | 3.5 kW | 5.3 W
HOM power / module | 21 kW | 56 W
HOM 2K heat load / module | 13 W (0.6 %) | 5.9 W
HOM 5K heat load / module | 39 W (1.8 %) | 3 W
HOM 80K heat load / module | 390 W (18 %) | 43.8 W
Percent of total cryogenic load | 22 % | 11 %
Main Ring heat load: design upper limit (estimated to have enough margin)
Booster heat load: scaled from ILC TDR (DF 50 % for continuous injection)

## Slide 38: HOM Damping Scheme
LEP2 type
Conservative scheme: two (even one) cavities in one module. Another possible solution is hybrid module with water cooled HOM absorber inside (Carlo Pagani).
Need further study. Critical issue.
Inter-cavity beam pipe (and bellow) diameter will determine the fraction of HOM power propagating out of the cryomodule.
Let most HOMs confine in one cavity and extract them out or let them go through cavities? How much will trap, especially the “grey” zone?

## Slide 39: HOM Impedance of Main Ring 650 MHz Cavity
Large HOM frequency spread from cavity to cavity relaxes the Q requirement
Easy to reach these Q values with HOM couplers on beam tubes for the modes below cut-off frequency
Some modes above cut-off may trap in the cavity and cryomodule
Monopole Mode | f (GHz) | R/Q (Ω) | Qlimit σf = 0 MHz | Qlimit σf = 0.5 MHz | Qlimit σf = 5 MHz
TM011 | 1.173 | 84.8 | 5.1E+5 | 2.9E7 | 5.8E7
TM020 | 1.350 | 5.5 | 6.8E+6 | 3.7E7 | 7.5E7
Dipole Mode | f (GHz) | R/Q (Ω/m) | Qlimit σf = 0 MHz | Qlimit σf = 0.5 MHz | Qlimit σf = 5 MHz
TE111 | 0.824 | 832.2 | 2.3E+4 | 1.2E6 | 2.4E6
TM110 | 0.930 | 681.2 | 2.8E+4 | 1.5E6 | 3.0E6
TE112 | 1.225 | 36.2 | 5.2E+5 | 1.9E6 | 3.7E6
TM111 | 1.440 | 101.5 | 1.9E+5 | 1.0E7 | 2.0E7
cut-off
cut-off

## Slide 40
Feedback system is needed to mitigate multi-bunch instabilities.
Single bunch instability is dominated by the vacuum pips, not the cavity.
HOM Impedance of Booster 1.3 GHz Cavity
* TESLA cavity measurement data
** at 6 GeV.
Note: Booster longitudinal damping time: 62 s @ 6 GeV, 8 ms @ 120 GeV, transverse damping time: 125 s @ 6 GeV, 16 ms @ 120 GeV
Monopole Mode | f (GHz) | R/Q (Ω) | Qmeasured* | σf (MHz) * | ** (ms)
TM011 | 2.450 | 156 | 5.9E4 | 9 | 1500
TM012 | 3.845 | 44 | 2.4E5 | 1 | 472
Dipole Mode | f (GHz) | R/Q (Ω/m) | Qmeasured* | σf (MHz) * |  (ms)
TE111 | 1.739 | 4283 | 3.4E3 | 5 | 218
TM110 | 1.874 | 2293 | 5.0E4 | 1 | 44
TM111 | 2.577 | 4336 | 5.0E4 | 1 | 22
TE121 | 3.087 | 196 | 4.4E4 | 1 | 497
cut-off
cut-off
Notes: 40

## Slide 41: HOM Coupler Design
Monopole modes impedance
Dipole modes impedance
Waveguide HOM coupler
Coaxial HOM coupler

## Slide 42: HOM Absorbers beam test
BPM
7-cell cavity in cryostat
gun
No charge-up of the HOM ceramics observed
HOM heating was less than expected
THBA05

## Slide 43: HOM damping for the BNL4 cavity
Poster: TUPB074
Bellow
HOM damping is challenging with power reaching up to 7 kW in a very broad frequency range to ~30 GHz.
A 3-cell prototype is on order to demonstrate the cavity performance and study HOM damping schemes.
Two potential damping schemes include six coaxial couplers to cover lower frequency part of the HOM spectrum (72% of HOM power below 5 GHz) and three waveguide couplers for the high end of HOM spectrum.

## Slide 44: SOM Damping
Mode | f (MHz) | R/Q (Ω) | Qlimit | Qinput coupler | PSOM (W) | PSOM-res (W)
π/5 | 632.322 | 0.02 | 4.5E+9 | 1.2E+07 | 1.3E-5 | 268.9
2π/5 | 637.099 | 0.00017 | 5.4E+11 | 3.3E+06 | 8.7E-7 | 0.6
3π/5 | 643.139 | 0.341 | 2.6E+8 | 1.7E+06 | 9.31E-3 | 638.9
4π/5 | 648.146 | 0.078 | 1.1E+9 | 1.2E+06 | 2.92E-4 | 105.8
Same Order Modes (SOM, other pass-band modes of operating mode) may drive instabilities or extract RF power from the beam
Input coupler as the natural SOM damper (HOM couplers not work)
Total SOM power quite small for real passband modes frequencies and CEPC bunch spacing.
SOM power 1 kW for resonant excitation. Power dissipated on cavity wall is negligible (~ 0.1 W)

## Slide 45: Power Coupler
Main ring 650 MHz 300 kW coupler:
Booster 1.3 GHz 4 kW coupler:
KEK STF1-type coupler developed by IHEP (test to 800 kW with DF 0.75 % = 6 kW) or TTFIII coupler can be used.
very high power handling capacity
two windows for vacuum safety and cavity clean assembly, effective cooling
very small heat load, simple structure for cost saving, high yield and reliability
Tristan (70 kW) / KEKB (380 kW) / BEPCII (120 kW) type as baseline. KEK cERL injector coupler (one window) as reference.

## Slide 46: Tuner
Total number of tuner for CEPC is 640. Highly reliable and maintainable tuners are required.
Lever end tuner (e.g. Fermilab) for 650 MHz 5-cell cavity (but may interfere with beam tube HOM coupler and rigid line) .
Lever tuner, blade and slide jack all suitable for 1.3 GHz 9-cell cavity.
Two piezo stacks. Motor and piezo maintainable.
I. Gonin, PAC13

## Slide 47: 预研关键技术
增强器流强低，微波功率和低温功耗小，且 1.3 GHz 技术相对成熟。主要挑战为主环高频系统：
高品质因数超导腔（Q0 = 4E10 @ 2K）
高阶模功率引出（PHOM = 3.5 kW / multi-cell cavity）
高功率耦合器（Pin = 280 kW，CW，384个）
低热负荷恒温器（83W @ 2K, 120W @ 5K, 790W @ 80K)
以上指标均挑战当前技术极限，没有国际先例。

## Slide 48: 关键技术：高品质因数超导腔
Q0 | 低温功率（kW@4K） | 低温能耗（MW） | 低温系统相对造价 （亿元） | 场致发射暗电流 IFE上限 (μA)
4.0E+10 | 70 | 15 | 0 | 0
2.0E+10 | 116 | 25 | 10? | 1
1.0E+10 | 177 | 38 | 23? | 3
5.0E+09 | 293 | 64 | 50? | 7
实现高 Q0（低温能耗小）的三个要素（新想法，新工艺）：
极小表面电阻（真空掺氮技术）
磁屏蔽及排出（快速降温技术）
全程超净组装（十级洁净技术）

## Slide 49: A bit of history about N doping
2012
Discovery at FNAL of unprecedented Q values on single cells treated with nitrogen in high temperature furnace
2013
Developed understanding of root of Q improvement and made process controllable and reproducible
Discovered that ‘light doping’ improves quench fields while maintaining the benefit of high Q
2014
Cavity vendors currently being qualified for N doping production process for LCLS-2
R&D continues for further understanding and improvements (quench, B sensitivity)
2015
More than 100 N doped cavity tests with 18 nine cell qualified for the two LCLS-2 prototype cryomodules
LCLS-2 invests in this technology, three partner labs working together FNAL-Cornell-Jlab

## Slide 50: Doping Treatment: small variation from standard protocol, large difference in performance
50
Example from a doping process developed for LCLS-2:
Bulk EP
800 C anneal for 3 hours in vacuum
2 minutes @ 800C nitrogen diffusion
800 C for 6 minutes in vacuum
Vacuum cooling
5 microns EP
Cavity after Equator Welding
EP 140 um
Ethanol Rinse
External 20 um BCP
Short HPR
800C HT Bake
RF Tuning
EP 40 um
Ethanol Rinse
Long HPR
Final Assembly
Long HPR
Helium Tank Welding Procedure
VT Assembly
HPR
HOM Tuning
Ship to DESY
Leak Check
120C bake
XFEL
X

## Slide 51: From single cell R&D to cryomodule ready technology: FNAL, Jlab, Cornell, SLAC together towards record Q >2.7e10 @16MV/m, 2K
<Q>=3.5e10
<Emax>=22.2 MV/m
Emaxmedian=22.8MV/m
It is the highest average Q ever demonstrated in vertical test for 1.3 GHz nine cells at 2K, 16 MV/m in the history of SRF (larger than a factor of two the state of the art)
A.Grassellino et al, IPAC15
See at this conference:
MOPB033
MOPB029
MOBA07
MOBA08

## Slide 52: Recipe optimization: quench fields
Light doping yields to higher quench field than heavy doping
For same length of the doping step, quench field decreases with subsequent ‘anneal’ time (why?)
For same recipe, quench fields are worse in nine cell than single cell cavities
Quench fields are not sparse, they always ‘cluster’ around a value – different N doping levels produce different quench barriers
More severe quench limitation > ~200 ppm concentration
There is a trend – similar to the BCS minimum – for quench fields vs mean free path

## Slide 53: New insights on quench in N doped cavities – magnetic peak field driven
M. Checchin et al, MOPB022
A. Vostrikov et al, MOPB027
Nitride teeth…residual nanonitrides post EP?
Or premature flux entry?

## Slide 54: Recipe optimization: RBCS vs flux sensitivity
RBCS min
RFL max
Larger mean free paths produce best performance…
But it is also interesting to notice the large windows of “unexplored”…

## Slide 55: Is trapped magnetic flux sensitivity much higher for N doped cavities? Depends on the doping level -and the accelerating field
Sensitivity to trapped flux for N doping improves with lighter doping (larger mfp)
Not dramatically higher than standard (especially at higher accelerating fields):
  120C bake ~0.5 nOhm / mGauss
  EP ~0.7
  N dope (best) ~0.9
M. Martinello et al, MOPB015
M. Checchin et al, MOPB020

## Slide 56: Surface post N bake, pre-EP: poorly SC nitrides phases
Flat Nb sample baked at 800C˚
for 2 min with N2 + 6 min annealing
Flat Nb sample baked at 800C˚ for
20 min with N2 + 30 min annealing
Bad (poorly SC) nitride phases that need to be removed via EP correlate with poor performance (pre-EP)
11/1/2015
Grassellino | Performance of N doped cavities
56
Nb [113]+Nb2N [210]+?
Few Nb nitrides-features (Nb2N reflections) in Nb near-surface. Nitride “teeth” go ~0.2 μm deep
Pt layer
~0.2 μm
Y. Trenikhina, MOPB055

## Slide 57: Surface post N bake + EP: only low level of interstitial N left
57
Nitrides
Interstitial nitrogen in Nb
Non-doped
Doped
Depth (um)
No visible Nb nitrides-teeth in near-surface show only Nb reflections
Confirms that root of improvement is from nitrogen as interstitial in the lattice
SIMS measurements show concentration of N one-two order of magnitude larger than background
A. Grassellino et al, MOPB029

## Slide 58: Physics – perceived BCS limit has been overcome
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication)
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)
Anti-Q-slope emerges from the BCS surface resistance decreasing with field
This was thought to be the lowest possible BCS resistance
N doping brings also lower than typical residual resistance <2 nanoOhms (non trapped flux related)

## Slide 59: Field dependence of the penetration depth – a possible explanation for the field dependence of BCS RS?
LEM muSR measurements on 120C bake and doped cavity cutouts revel that the penetration depth in the two cases have opposite field dependences, decreasing with field for N doping: possible origin of Q antislope?
A. Vostrikov et al,
FNAL, MOPB027

## Slide 60: How much nitrogen is needed for optimal performance? The intermediate mean free path
Ba = 25 mT
BCS surface resistance as a function of mean free path
BCP and EP unbaked -> strong screening, clean limit
EP+120C bake-> strongly suppressed m.f.p., gradient of the m.f.p. from the surface, dirty limit
N-doped -> intermediate m.f.p., at the predicted minimum for BCS (previously unexplored)
mfp ~ 2 nm at the surface, increasing deeper
~15 nm - no screening
mfp~40 nm
mfp > 400 nm
Dirty limit (120C bake)
Clean limit (EP, BCP)
Optimal mfp = N doping
Meissner screening profiles for differently treated cutouts (Ba magnetic field applied parallel to sample surface = 25 mT). Allows to directly extract surface mfp

## Slide 61: Milestone: record horizontal fully integrated test @ FNAL N doped nine cell in LCLS-2 vessel >3e10 at 16MV/m, 2K
A. Grassellino et al, MOPB028
N. Solyak et al, MOPB087
G. Wu, THBA06

## Slide 62: Bringing it all together: N-doped dressed cavity in cryomodule environment
9-cell N-doped
fully dressed cavity for LCLS-II with
high power coupler, tuner, HOM couplers in horizontal test
Ambient field
< 4 mG
[see MOBA06, MOP028, THBA06, MOPB087]

## Slide 63: Utilizing new physics for record high Qs – bare 1-cell
Combination of nitrogen doping and efficient flux expulsion =>
Record high Q >1e11 up to 28 MV/m in SRF cavities
A. Romanenko, A. Grassellino, A. C. Crawford, D. A. Sergatskov, and O. Melnychuk, Appl. Phys. Lett. 105, 234103 (2014)
Ambient magnetic fields are fully expelled
1.5K, 1.3GHz 1-cell

## Slide 64: Expelling 190 mG
Q > 2.7e10 at 2K, 16MV/m in
190 (!) mG
ambient field
A. Romanenko, A. Grassellino, A. C. Crawford, D. A. Sergatskov, and O. Melnychuk, Appl. Phys. Lett. 105, 234103 (2014)

## Slide 65: Mechanism#1: Depinning by Thermal Gradient
T = 9.2 K
Superconducting
Normal conducting
T = 8 K
T = 10 K
Cavity exterior
(helium)
fT
Cavity interior
(vacuum)
fT ~ -∇T
Require that fT > Jcφ0 to depin flux
Force component from inner to outer wall is what helps
[S. Posen et al, MOPB104]
Thermal gradient at the superconducting/normal conducting boundary creates a depinning force [J. Appl. Phys. 115, 184903 (2014)]

## Slide 66
R. Eichhorn et al.,
“Thermocurrents and their Role in high Q Cavity Performance”, http://arxiv.org/abs/1411.5285
Geometry of thermocurrents: Highest degree of asymmetry when parts of the cavity are superconducting
Courtesy R. Eichhorn

## Slide 67
Thermocurrent
I
Magnetic field
B
Temperature difference
ΔT
Trapped flux in the sc material
B
Surface resistance
Rres
Correlation confirmed by experiment
How can we validate the thermocurrent hypothesis?
S values
Magnetic field
at the RF surface
B
Argumentation loop closed:
Thermocurrents exist and can significantly deteriorate a otherwise perfectly prepared cavity.

## Slide 68: Impact of the cooldown procedure
Small thermal gradients give better performance
This cavity exceeds LCLS-II spec by a factor of 2
LCLS-II spec adjusted for operation at 4.2 K

## Slide 69: FNAL 650 MHz 单cell腔 (beta=0.9) 垂测结果 （掺氮与标准后处理工艺比较）
CEPC主环腔垂测指标
CEPC主环腔运行指标
PIP-II cavity Bpk/Eacc=3.75
CEPC cavity Bpk/Eacc = 4.2
Alexander Romanenko, FCC Week 2015

## Slide 70: FNAL和JLAB十个1.3 GHz N-doping 9-cell腔 垂直测试结果
CEPC增强器腔运行指标
Alexander Romanenko, FCC Week 2015
LCLS-II 近期已下调 Q0 指标下限，并决定增加一套低温制冷机
（降低项目风险）

## Slide 71: IHEP ILC Cavity R&D
2012
2010
2008
2006
2014
single cell ICHIRO large grain cavity, max. 48 MV/m by EP
single cell low-loss large and fine cavity, max. 40 MV/m by CP
9-cell low-loss, large grain cavity without HOM, 20 MV/m by CP
7-cell & 9-cell low-loss, large grain cavity with HOM, 20 MV/m by EP
9-cell TESLA-like, fine grain cavity with HOM
IHEP-01
IHEP-02T
IHEP-02
IHEP-03
Fine tumbling
Test soon

## Slide 72: Single Cell Test Results
40 MV/m, Q0 = 1.6 x 1010 @ 2K
CBP150μm+BCP200μm(total)
750C 3h, 120C 48h
48 MV/m, Q0 = 1.0 x 1010 @ 2K
CBP90μm+BCP10μm+EP100μm(total)
750C 3h, 120C 48h (12h bake causes high field Q-slope)

## Slide 73: 9-cell Test Results and Limitation
KEK June 2010
JLAB July 2011
FNAL May 2013
IHEP-02 quench defect (detected by second sound and thermometry). The quench location has sharp and deep grain boundary step made during half cell pressing.
A pit on the iris and possible contamination may be the reason of strong field emission of IHEP-01.
By passband mode test, 5 cells of IHEP-01 30 MV/m, 7 cells of IHEP-02 40 MV/m, both Pi modes quench at 20 MV/m in cell#9 300 deg equator.

## Slide 74
August, 31: 59 modules arrived with ~55 modules rf tested (XM-3 excluded)
Cryomodule Test at AMTF
74

## Slide 75
The finished L1 section

## Slide 78: Absolute Peak Gradient Determination
Cavity | Peak Gradient (MV/m) | Limitation
1/TB9AES008 | 32.3 | Quench
2/TB9RI018 | 31.8 | Quench
3/TB9AES010 | ≥ 33 | tbd
4/TB9RI019 | ≥ 33 | tbd
5/TB9ACC016 | ≥ 33 | tbd
6/TB9AES009 | 29.8 | Quench
7/RI027 | ≥ 33 | tbd
8/RI028 | 32.2 | Quench
Peak CM-2 Cavity Gradients with all 8 powered at once:
Sum = 258.1 MV, Average = 32.2 MV/m

## Slide 79
Results: Usable Gradient “As received”
“Missing” 75 cavities? Not included in “as received”, because “retreatment at vendor” necessary before first RF test
re-treat & retest
accept for module
Both vendors well above Spec
RI shows ~ 3MV/m in average more than EZ: a) final EP b) low gradient quenches at EZ
In general, first re-treatment is a standard High-Pressure Rinse (or “special” handling at vendor)
Several cavities with < 20 MV/m accepted, especially if a) limitation = “bd“ + b) no FE
MOPB086

## Slide 80
TTC 2014: Trend of Usable Gradient “As received” increasing?
?

## Slide 81: Cryomodule – Vertical Test comparison: MAX GRADIENT
Ideal case VT:CM = 1:1
individual cavity comparison
(upper limit due to 31 MV/m limit in module test)
we lose between vertical and cryomodule test
average VT: (33.8) 30.5 MV/m (clipped at 31 MV/m) average CT: 28.4 MV/m (includes limit at 31MV/m)
MOPB080

## Slide 82: Vertical Test - Cryomodule comparison IV: Q0-values at ~ 23MV/m
Average Q0-value at ~ 23 MV/m: vertical ~1.3 x 1010 cryomodules ~1.4 x 1010
estimated error of cryomodule Q-value: ~30%

## Slide 83: Installation progress
Headline
first level
  second level
    third level
Notes: Before you start editing the slides of your talk change to the Master Slide view:
Menu button “View” > Slide Master:
Edit the following items:
1. On the Title slide (second master slide)
a) Click to add title of your talk
b) Click to add subtitle (conference, location, name of the speaker, date)
2. On the Slide Master (first master slide)
a) The 1st row in the violet header: Delete the existent text and write the title of your talk into this text field b) The 2 rows in the footer area: Delete the text and write the information regarding your talk (same as on the Title Slide) into this text field.
If you want to use more partner logos position them left beside the DESY logo in the footer area.
Close Master View

## Slide 84: IHEP Cavity Industrialization Study
Press Machine
CMM Machine
Vertical Machining Center
CNC Turning Center
HE-Racing Technology (HERT)
previous IHEP workshop (on campus)
experience in accelerator components
  S-band accelerator tubes
  magnets
  high power input couplers for SRF cavity (ILC 1.3 GHz, 500 MHz …)
Newcomer in SRF cavity
TESLA single cell and 9-cell cavity as the startup
facilities for cavity fabrication, welding and annealing

## Slide 85: HERT New EBW Machine and Furnace
EBW Machine
Vacuum chamber: L 3.3m x W 1m x H 1.3m
Voltage: 60 kV, inside equator weld possible
In commissioning
Furnace
High temperature: 1350 C
Working vacuum: 3.0×10-3 Pa
In commissioning

## Slide 86: TESLA 9-cell cavity

## Slide 87: Cavity and Cryomodule R&D
325 MHz HWR-012
1.3 GHz low-loss large grain 9-cell
1.3 GHz TESLA-like 9-cell
650 MHz beta=0.82 5-cell
Euro-XFEL cryomodules
BEPCII 500MHz spare module
1.3 GHz 9-cell cavity ILC module
325 MHz spoke cavity module (7 cavities)
HOM absorber
325 MHz Spoke-012
Spoke-021
Spoke-040

## Slide 88: Coupler and Tuner R&D
500 MHz
BEPCII spare
1.3 GHz
ILC STF1-type
162.5 MHz
China ADS HWR
325 MHz
China ADS Spoke
Slide-Jack Tuner
Lever Tuner

## Slide 89: SRF Facilities
2K cryogenic plant (1kW@4K)
2K Pumps
8000 m3/h @ 3100 Pa
New vertical test dewar
(ID 800 mm)
EBW machine (60 kV)
(3.3m x 1m x 1.3m)
Vacuum furnace (1350 C) C)
1.3 GHz 5MW klystron
and Marx modulator

## Slide 90: SRF Facilities
CBP (tumbling)
BCP
Ultrasonic
RF Pretuning
Clean Room
Vertical Test Stand
UPW & HPR
Cavity inspection

## Slide 91: 关键技术：高阶模功率引出
 | Main Ring | Booster
HOM power / cavity | 3.5 kW | 5.3 W
HOM power / module | 21 kW | 56 W
HOM 2K heat load / module | 13 W (0.6 %) | 5.9 W
HOM 5K heat load / module | 39 W (1.8 %) | 3 W
HOM 80K heat load / module | 390 W (18 %) | 43.8 W
Percent of total cryogenic load | 22 % | 11 %
主环HOM功率不能在低温吸收，必须引出（同轴线或波导，热负载问题）
低阶模式在多cell腔中的trap问题，高阶传输模式在腔间trap问题
主环650MHz腔引起的束流不稳定性较易抑制（Qext ~ 107）
增强器低能段，1.3GHz腔引起的束流不稳定性增长时间明显短于同步辐射阻尼时间，需采用横向和纵向反馈
从未有过的高频腔HOM设计挑战：
HOM功率高
多cell腔
多腔恒温器
低热负载

## Slide 92
增强器主耦合器技术相对成熟
主环主耦合器的主要技术难点：
大功率容量（连续波300 kW）
双窗结构（真空安全及腔洁净需要）
极低热负荷
结构简单以降低成本
高成品率及高可靠性
关键技术：高功率耦合器
从未有过的功率耦合器设计、工艺和质量控制挑战

## Slide 93: CEPC SRF R&D Plan
CEPC R&D & Engineering Design (2016-2020, 5 yrs.)
SRF Prototype R&D (2016-2019, 4 yrs.)
SRF Pre-Production R&D (2019-2022, 4 yrs.)
CEPC Construction (2021-2027, 7 yrs.)
 |  | 2015 |  |  |  |  |  |  |  | 2020 |  | 2027 |  |  |  |  |  |  |  |  |  | 
CEPC Pre-studies (2013-2015)
SRF Pre-study
SRF Production and Installation (2023-2027, 5 yrs.)
Production
Booster SRF in three years (2023-2025):
test two 1300 MHz cavities per week
test one cryomodule per month
Main ring SRF in four years (2023-2026):
test two 650 MHz cavities per week
test two cryomodules per month
New SRF lab and infrastructure on IHEP site
R&D Phase 2
Demonstrate robustness of fabrication and assembly processes of cryomodule and its components.
R&D Phase 1
Components prototyping & performance demonstration
Large scale SRF lab on CEPC site and in industry
HOM damping scheme
high Q0 single cell cavity

## Slide 94: 关键技术研发阶段
高品质因数超导高频腔。设计并研制8个超导高频腔（包括主环腔和增强器腔各4个，及相应的液氦槽）。研究氮掺杂及电抛光技术，优化表面处理工艺，达到垂直测试指标：主环650 MHz腔加速梯度20 MV/m，品质因数4E10；增强器1.3 GHz腔加速梯度23 MV/m，品质因数2E10。
大功率主耦合器；设计并研制8个主耦合器（包括主环耦合器和增强器耦合器各4个），建立测试装置，测试主耦合器性能，达到设计指标：双陶瓷窗，热负载小，主环耦合器通过650 MHz连续波功率300 kW，增强器耦合器通过1.3 GHz峰值功率20 kW（平均4 kW）。
大功率高次模耦合器及吸收器。研究和设计高效且经济的高次模功率引出及吸收方案，研制可通过1 kW功率、热负载小的主环腔高次模耦合器，研制可通过10 kW功率的主环腔高次模吸收器，建造测试平台，测试性能。
设计研发可靠的频率调谐器和低电平控制系统。
针对每种腔型，各建造一个水平测试低温恒温器（含2个腔），测试关键部件集成性能，达到加速器运行指标：主环650 MHz腔加速梯度15.5 MV/m，品质因数4E10；增强器1.3 GHz腔加速梯度19.3 MV/m，品质因数2E10。

## Slide 95: 产业化准备阶段
制造并测试30个1.3 GHz超导腔及40个650MHz超导腔（CEPC超导腔总量的10 %），实现90 %的成品率目标，其中大部分装入低温恒温器样机。培养未来大规模生产的供应商并进行资格预审，并最终选择选择两到三个符合条件的供应商。
制造3个完整的主环低温恒温器样机和2个完整的增强器低温恒温器样机（包括16组增强器超导腔、主耦合器、高次模耦合器和吸收器、调谐器等和12组主环超导腔、主耦合器、高次模耦合器和吸收器、调谐器等），并进行低温高功率测试，达到加速器运行指标：主环650 MHz腔加速梯度15.5 MV/m，品质因数4E10；增强器1.3 GHz腔加速梯度19.3 MV/m，品质因数2E10。
分别连接3个主环低温恒温器和2个增强器低温恒温器，进行束流实验，尤其是对主环的高次模引出、吸收及热负荷性能进行检验。
超导高频研发队伍需要在产业化准备阶段结束时达到约200个全职员工，为大规模生产、测试和安装做好准备。

## Slide 96: 超导实验室基础设施建设
2019年之前须建立一个大规模的超导实验室（包括超导高频及超导磁铁），面积10000平米，用于支撑预研、产业化准备及大规模生产阶段的研制、组装和测试。
实验室最终需要具备的生产和测试能力：每周垂直测试两个主环超导腔和两个增强器超导腔，每月组装并测试一个增强器低温恒温器和两个主环低温恒温器。
实验大厅将在一宽大整体场房内集中安装和试验各类超导设备，能够完成各种类型、大批量超导腔的制造、表面处理、洁净总装、垂直测试、水平高功率试验等，具备低温液氦循环制冷和微波功率源设施，可以同时在线高功率试验四组12米长的超导腔低温恒温器，并同时保证大厅内4个垂直测试进行。
此过程中需要学习和借鉴国外超导实验室基础设施建设及超导加速器产业化的成功经验。