## Slide 1: CEPC Cavity High Q R&D
沙鹏，刘振超，翟纪元，刘柏奇，王牧源，戴劲，米正辉，王光伟，孙毅
20151030

## Slide 2: Content
Introduction
1.3GHz cavity
650MHz Beta=0.82 cavity
650MHz Beta=1 cavity
Vacuum system for N2 injection of vacuum furnace at IHEP

## Slide 3: CEPC cavity requirement
Frequency: 650MHz
Gradient: 15.5MV/m
High Q0>4x1010@2K
HOMs power damping
(several kilo watts)
Low loss factor
No trapped mode
Parameters | CEPC-Collider | CEPC-Booster
Cavity Type | 650 MHz 5-cell Nitrogen-doped Nb | 1.3 GHz 9-cell Nitrogen-doped Nb
Vcav / VRF | 17.9 MV / 6.87 GeV | 20 MV / 5.12 GeV
Eacc (MV/m) | 15.5 | 19.3
Q0 | 4E10 @ 2K | 2E10 @ 2K
Cryomodule number | 96 (4 cav. / module) | 32 (8 cav. / module)
RF coupler power / cav. (kW) | 280 c.w. | 20
RF source number | 192 (800 kW / 2 cav.) | 256 (25 kW / cav.)
HOM power / cav. (kW) | 3.5 | 0.005
HOM damper | coaxial/waveguide@2K + ferrite @ RT | coupler @ 2K + ceramic @ 80K

## Slide 4: N-doping and fast cooldown

## Slide 5: Fermilab 650 MHz single cell (beta=0.9) VT （N-dopingVS. Standard post-process）
CEPC主环腔垂测指标
CEPC主环腔运行指标
PIP-II cavity Bpk/Eacc=3.75
CEPC cavity Bpk/Eacc = 4.2
Alexander Romanenko, FCC Week 2015

## Slide 6: FNAL和JLAB十个1.3 GHz N-doping 9-cell腔 水平测试结果
CEPC增强器腔运行指标
Alexander Romanenko, FCC Week 2015

## Slide 7: HPR, Vertical test for 1.3GHz cavity
HPR
leakage detecting
Injection of Liquid He

## Slide 8: Test results (before N-doping)
2015.06.04, Vertical test before N-doping at IHEP.
Eacc=17MV/m@Q0=1.6e10, Quench at 17MV/m.

## Slide 9: N-Doping of 1.3GHz Cavity
2015.07.09-11, N-Doping + Plasma Cleaning at PKU
Induction heating Chamber
Maintain 10min
（7.5E-4 Pa）
Heating to 800° (7min）
N-doping 10min
（2.6 Pa）
Maintain 5min
（8.5E-4 Pa）
Cool down

## Slide 10: Doping data
Nitrogen injection 10 minutes
Hydrogen degas 10 minutes
Nitrogen anneal 5 minutes

## Slide 11: Vertical test after N-Doping
20150717, Vertical test after N-Doping
No Q0 improvement.

## Slide 12: Test results for 1.3GHz cavity at FNAL
N-doping + EP

## Slide 13: Doping data of JLAB
FNAL、JLAB、Cornell: 60+ cavities have been N-doping treated, the same procedure with any minor changes of N2 injection.

## Slide 14: The reason
N-doping parameters? (Temperature Vs time, Pressure VS time)
Plasma cleaning worse than EP (foreign labs).

## Slide 15: 650MHz N-doping单cell腔加工
充分利用现有原材料及备件，加快研制速度
2015年5月5日将材料运至所工厂
2015年7月2日完成整腔焊接
2015年8月10日在宁夏完成超导腔120um BCP 重抛、退火、20umBCP轻抛，准备进行HPR、洁净间组装及垂直测试
2015年10月14日进行了垂测。

## Slide 16: Machining

## Slide 17
真空检漏
垂测探针耦合度校准

## Slide 18: Vertical test preparation

## Slide 19: Vertical test result

## Slide 20: Q0 at low field

## Slide 21: 650MHz single-cell cavity (Beta=1) for CEPC

## Slide 22
The final welding would be finished at next week。

## Slide 23: Vacuum furnace at IHEP
Chamber
Diffusion Pump
Valve

## Slide 24: N2 injection (undergoing)
Chamber
Diffusion pump
MFC
Valve
N2

## Slide 25: N-doping的样片实验
为了搞清楚N-doping的原理，进行铌材样片的表面特性分析非常重要。
已准备与超导腔同步处理的样片12片。
一种说法：铌材中的氢化物使得超导腔的Q值下降，而掺氮后，氮原子可以俘获氢原子，从而提高了Q值。
需要对铌材样片（N-doping前、后）进行两种对比分析：
  利用二次离子质谱(Secondary Ion Mass Spectrometry ，SIMS)测量样片的氮原子密度随深度的分布；
  利用透视电子显微镜（ Transmission electron microscope ，TEM）对聚焦离子束（ Focused Ion beam ，FIB）制备的铌材样片进行电子衍射谱分析，观察铌晶格的变化。

## Slide 26: TEM/FIB实验
中科院宁波材料所有相应的仪器设备，将与其合作完成。
TEM得到的N-doping前后Nb lattice的变化（FNAL）

## Slide 27: SIMS实验
SIMS设备比较少见，还在寻找相关的单位和设备。
SIMS得到的N-doping前后N原子密度的变化（FNAL）
二次离子激发示意图

## Slide 28: Thanks for your attention!