## Slide 1: SPPC High Field Magnets - Preliminary Design Study and R&D Steps
Qingjin XU
On behalf of the SPPC magnet working group
Institute of High Energy Physics (IHEP)
Chinese Academy of Sciences (CAS)
2016.4.28

## Slide 2: Requirements of the SPPC Magnets
Main dipoles
Field strength: 20 Tesla
Aperture diameter: 40~50 mm
Field quality: 10-4 at the 2/3 aperture radius
Outer diameter: 900 mm in a 1.5 m cryostat
Tunnel cross section: 6 m wide and 5.4 m high
6-m Tunnel for CEPC-SPPC. Left: SPPC collider. Right: CEPC collider (bottom) and Booster (top)
SPPC accelerator complex
The CEPC-SPPC ring sited in Qinhuangdao,
50 km and 100 km options .
Refer to CEPC-SPPC Pre-CDR, Mar. 2015: http://cepc.ihep.ac.cn/preCDR/volume.html
SPPC
50/100 km in circumference
C.M. energy 70 TeV or higher
Timeline
Pre-study: 2013-2020
R&D: 2020-2030
Eng. Design: 2030-2035
Construction: 2035-2042
Qinhuangdao

## Slide 3: Why 20-T Dipole Is Difficult ?
Dipole vs Solenoid
Different coil configurations
Limited coil width for dipole
Magnetic shielding
Cost
Martin Wilson
Solenoid
Lucio Rossi
LHC dipole
Dipole
Je – Current density
t – Coil thickness
Je – Current density
t – Coil thickness

## Slide 4: Performance of Superconductors
NbTi:
11 T @ 1.9K
Nb3Sn (Nb3Al)
17 T @ 4.2 K
500 A/mm2
WHOLE WIRE critical current density of main superconductors @ 4.2 K
Peter Lee

## Slide 5: R&D History of Nb3Sn Dipole Magnets
HTS
NbTi
Nb3Sn
(no bore)
(no bore)
20 T
IHEP
LBNL(RD3C)
(Two 35 mm bore)
Results achieved with Nb3Sn dipole technology test
16 T achieved with block type configuration (HD1 @ LBNL, 2003)
15 T achieved with common coil configuration (RD3 @ LBNL, 2001)
Results achieved with accelerator level field quality and bore
14 T achieved with block type configuration (HD2 @ LBNL, 2007)
13 T achieved with Cos-theta configuration (D20 @LBNL, 1997)
(LHC NbTi dipole 8.3 T)
(Single bore)
D.R. Dietderich, A. Godeke, Cryogenics 48, (2008)

## Slide 6: Challenges and R&D Focus of the 20-T Accelerator Magnets
Jc and cost of Superconductors: Based on the present Jc level, thousands of tons of Nb3Sn and HTS superconductors are needed to fabricate SPPC magnets. Significant increase of Jc and reduction of cost of superconductors are expected.
HTS coils for accelerator magnets, especially tape conductors: field quality (current distribution, magnetization effect,…), quench protection and fabrication method.
Magnetic force in superconducting coils at 20 T: F ̴ B2. And both Nb3Sn and HTS superconductors are strain sensitive! Needs innovative strain management for superconducting coils.

## Slide 7: Design Study of SPPC Dipole Magnets
Chart: 
| 0 | 30 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300 | 330 | 360 | 390 | 420 | 450 | 480 | 510 | 540 | 570 | 600 | 630 | 660 | 690 | 720 | 750 | 780 | 810 | 840 | 870 | 900 | 930 | 960 | 990 | 1020 | 1050 | 1080 | 1110 | 1140 | 1170 | 1200 | 1230 | 1260 | 1290 | 1320 | 1350 | 1380 | 1410 | 1440 | 1470 | 1500
b3 | -0.39506 | -0.16327 | -0.0029767 | 0.080907 | 0.18246 | 0.3156 | 0.439 | 0.5482 | 0.66092 | 0.78202 | 0.90267 | 1.0279 | 1.1648 | 1.3206 | 1.5091 | 1.7498 | 2.0946 | 2.6288 | 3.5771 | 5.2487 | 5.7841 | -5.7987 | -44.674 | -68.098 | -33.263 | 46.267 | 104.97 | 92.844 | -10.311 | -47.905 | -30.782 | -15.193 | -7.0212 | -3.3196 | -1.658 | -0.87994 | -0.49435 | -0.29205 | -0.18021 | -0.11545 | -0.076387 | -0.05198 | -0.036248 | -0.025827 | -0.018755 | -0.013853 | -0.01039 | -0.0078993 | -0.0060811 | -0.0047347 | -0.0037247
b5 | 0.65047 | 0.63445 | 0.61856 | 0.60411 | 0.58834 | 0.57153 | 0.55626 | 0.54083 | 0.52531 | 0.51043 | 0.49419 | 0.479 | 0.46378 | 0.44851 | 0.43298 | 0.41904 | 0.40531 | 0.38867 | 0.3786 | 0.36235 | 0.20873 | -0.53251 | -4.2528 | -4.9148 | 0.75387 | 9.2111 | 9.8532 | 10.795 | 2.2384 | 1.501 | 0.5939 | 0.16091 | 0.048947 | 0.016093 | 0.0056422 | 0.0021176 | 0.00085143 | 0.00036553 | 0.00016666 | 8.0217e-05 | 4.0525e-05 | 2.1376e-05 | 1.1719e-05 | 6.6496e-06 | 3.8919e-06 | 2.3424e-06 | 1.446e-06 | 9.1333e-07 | 5.8915e-07 | 3.8739e-07 | 2.5923e-07
b7 | -0.22665 | -0.23626 | -0.24758 | -0.259 | -0.27031 | -0.28164 | -0.2928 | -0.3039 | -0.31497 | -0.32618 | -0.33686 | -0.34786 | -0.35868 | -0.36961 | -0.38036 | -0.39051 | -0.40017 | -0.41225 | -0.42338 | -0.43247 | -0.44817 | -0.52327 | -1.2989 | -1.178 | -0.45591 | 0.65702 | -0.043029 | 0.29947 | -0.30842 | -0.062959 | -0.036257 | -0.0045847 | -0.00045843 | -6.5972e-05 | -1.4417e-05 | -3.924e-06 | -1.1927e-06 | -3.9146e-07 | -1.3723e-07 | -5.1049e-08 | -2.0095e-08 | -8.2992e-09 | -3.5846e-09 | -1.6598e-09 | -7.6064e-10 | -3.7496e-10 | -1.929e-10 | -9.8611e-11 | -7.1372e-11 | -1.3994e-11 | -4.2101e-11
a2 | -1.1192 | -1.0202 | -0.8741 | -0.77335 | -0.73424 | -0.75942 | -0.86529 | -1.0855 | -1.4598 | -2.0196 | -2.8128 | -3.9196 | -5.4435 | -7.5269 | -10.39 | -14.351 | -19.871 | -27.503 | -37.464 | -47.747 | -51.105 | -43.953 | -50.387 | -145.19 | -275.55 | -306.33 | -145.78 | 144.42 | 327.96 | 268.94 | 175.29 | 104.93 | 61.661 | 37.113 | 23.241 | 15.171 | 10.288 | 7.2145 | 5.2078 | 3.8542 | 2.9147 | 2.2458 | 1.7591 | 1.398 | 1.1253 | 0.9163 | 0.75382 | 0.62594 | 0.52416 | 0.44231 | 0.37589
a4 | -0.8716 | -0.90035 | -0.93672 | -0.97346 | -1.0108 | -1.0487 | -1.0869 | -1.1254 | -1.1637 | -1.2028 | -1.2414 | -1.2804 | -1.319 | -1.3578 | -1.3958 | -1.4314 | -1.4642 | -1.4952 | -1.5293 | -1.6163 | -1.8603 | -3.7839 | -11.221 | -24.239 | -33.011 | -25.068 | 0.16219 | 25.63 | 37.024 | 12.95 | 2.8588 | 0.061841 | -0.23637 | -0.14871 | -0.074522 | -0.036319 | -0.018131 | -0.0094114 | -0.0050941 | -0.0028701 | -0.0016778 | -0.0010142 | -0.00063167 | -0.00040417 | -0.00026495 | -0.00017751 | -0.0001213 | -8.4384e-05 | -5.9669e-05 | -4.2826e-05 | -3.1161e-05
a6 | 0.72944 | 0.7265 | 0.72279 | 0.71915 | 0.7153 | 0.71099 | 0.70752 | 0.70353 | 0.69948 | 0.69478 | 0.69118 | 0.68679 | 0.68241 | 0.67799 | 0.67377 | 0.66895 | 0.6641 | 0.66009 | 0.65533 | 0.64722 | 0.62069 | 0.40548 | -0.95309 | -3.0827 | -4.0809 | -2.769 | -0.86304 | -1.1226 | 0.21362 | -0.77316 | -0.22862 | -0.042185 | -0.0051362 | -0.00035434 | 6.6143e-05 | 5.039e-05 | 2.2979e-05 | 9.7271e-06 | 4.145e-06 | 1.8215e-06 | 8.3132e-07 | 3.9451e-07 | 1.9445e-07 | 9.9283e-08 | 5.239e-08 | 2.8495e-08 | 1.5916e-08 | 9.1718e-09 | 5.3922e-09 | 3.2638e-09 | 1.9977e-09
Integrated bn/an | Value (10-4)
b3 | 0.14
b5 | 1.42
b7 | -0.40
a2 | -0.29
a4 | -1.81
a6 | 0.03
Q. Xu, K. Zhang, C. Wang et. al., 20-T Dipole Magnet with Common Coil Configuration: Main Characteristics and Challenges, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016，4000404
With common coil configuration
20-T dipole magnet with common coil configuration two Φ50 mm beam pipes; load line 80% @ 1.9 K
Q. Xu, K. Zhang, C. Wang et al.

## Slide 8: Design Study of SPPC Dipole Magnets
Lorentz force per aperture:
Fmag_x=23.4 MN/m
Fmag_y=2.38 MN/m
Stress in coil after excitation
Stress in shell after excitation
K. Zhang et. al., 2-D Mechanical Design Study of a 20-T Two-in-One Common-Coil Dipole Magnet for High-Energy Accelerators, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016, 4003705
D.R. Dietderich, A. Godeke / Cryogenics 48 (2008) 331–340
Direction of Magnetic force
K. Zhang, Q. Xu, C. Wang et al.
With common coil configuration

## Slide 9: R&D Steps for SPPC Dipole Magnets
a
b
c
1st step ongoing
Fabrication of 15-T Nb3Sn and Nb3Sn+HTS subscale magnets, to test the stress management method for Nb3Sn & HTS coils and the quench protection method for HTS coils;
By the end of 2018.
2nd step
Fabrication of 15-T Nb3Sn and Nb3Sn+HTS operational field dipole magnet with two Φ50 mm beam pipes and 10-4 field quality, to test the field optimization method for HTS coils;
To be funded.
3rd step
Fabrication of the 20-T magnet with Nb3Sn+HTS or only one of them, if we can get significant progress on the performance of Nb3Sn or HTS superconductors, i.e., their Jc level is 3~6 times increased or even more, and the cost is significantly reduced.
Q. Xu, K. Zhang, C. Wang et. al., 20-T Dipole Magnet with Common Coil Configuration: Main Characteristics and Challenges, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016，4000404
Q. Xu, K. Zhang, C. Wang et al.
With common coil configuration

## Slide 10: R&D Steps for SPPC Dipole Magnets
Cos-theta dipole
Highest efficiency, complicated ends with hard-way bending
Common coil dipole
Simplest structure with large bending radius, lower efficiency
Canted cos-theta dipole
Lowest stress level in coil, lowest efficiency
Efficiency, field quality, stress management, fabrication method…
Block type dipole
Simpler structure with hard-way bending, lower efficiency
Comparison of different coil configurations

## Slide 11: R&D Steps for SPPC Dipole Magnets
Different coil configurations for 20-T dipole magnet
Left: Common coil
Right: Cos-theta
Common coil
Cos-theta
Coil ends
Common coil
Cos-theta
C. Wang et al.
Common coil vs Cos-theta
Comparison of different coil configurations

## Slide 12: R&D Steps for SPPC Dipole Magnets
Super High Jc Nb3Sn
Over-pressure HTS Bi-2212
HTS YBCO Jc estimation
Magnet field Vs. Conductor Jc
Principle: increase of Nb3Sn pinning force at high field through grain refinement: Jc(12 T, 4.2K) from 3.5 kA/mm2 @ 100+ nm to 9.6 kA/mm2 @ 35 nm !
X. Xu et al, Appl. Phys. Lett. 104 082602 & ASC14
D. C. Larbalestier et al, NATURE MATERIALS DOI: 10.1038/NMAT3887, 2014
D.R. Dietderich, A. Godeke, Cryogenics
48 (2008) 331–340
R&D of advanced superconductors: Nb3Sn & HTS
HTS YBCO cost estimation
And, other materials
like …
Iron-based superconductor?

## Slide 13: Development of Nb3Sn Rutherford Cable
Superconducting Rutherford Cable fabricated by Toly Electric with WST ITER type Nb3Sn strand
Collaboration between WST, Changtong Electric, Toly Electric, and IHEP
Y. Zhu (WST) et al.
Superconducting Rutherford Cable fabricated by Changtong Electric with WST ITER type Nb3Sn strand

## Slide 14: Development of Nb3Sn Rutherford Cable
Pitch length | Filling factor (%) | Ic degradation(%) | Average Ic degradation(%) | 备注
60 | 90.6 | 9.39~16.04 | 12.48~12.67 | 损降最大
45 | 90.7 | 3.84~10.33 | 6.31~7.42 | 损降性能相当
52 | 87.4 | 3.18~10.39 | 6.51~6.76 | 
52 | 83.7 | 0.33~6.2 | 3.13~3.60 | 损降最小
Collaboration between WST, Toly Electric, Changtong Electric and IHEP
Y. Zhu (WST) et al.

## Slide 15
Hastelloy
Substrate
Y2O3
Al2O3
Amorphous Layer
MgO
Seed Layer
CeO2
Cap Layer
(Y,Gd)BCO
Superconducting Layer
Ag
Overlayer
Architecture of type II superconductor from SSTC
Improved performance of SSTC tape at 4.2K
R&D of High Field ReBCO Tape by SSTC
3.3mm tape Ic:
>300A @ 12T, 4.2K
Performance of SSTC tape at 4.2K and 12T
SSTC

## Slide 16
Fabrication of hundred meter level Ф1.0mm strands
4.2K、0T：Jce 920A/mm2，Jc 4400A/mm2。
4.2K、20T:Jce 270A/mm2，Jc 1200A/mm2。
An Over-pressure furnace is ready for heat treatment of strands
（a）
PIT制备Bi-2212线材
（a）
Bi-2212 stands and CICC conductor under development
R&D of Bi-2212 Superconductor by NIN
NIN

## Slide 17
Nb3Sn Bpeak
14.5T @4.2K
Main parameters of the cables
Main parameters of the strands
For per meter of such magnet, the required length of the strand: YBCO: 0.6 Km; Nb3Sn in total: 9.12 Km
Coil configuration in the 1st quadrant
Field distribution in the cross section of the magnet
Strand | diam. | cu/sc | RRR | Tref | Bref | Jc@ BrTr | dJc/dB
IHEPWCJC | 0.82 | 1 | 100 | 4.2 | 12 | 2400 | 400
IHEPWYBCO | - | - | - | 4.2 | 12 | 1020 | 40
I=358A (YBCO)
I=9930A(Nb3Sn)
Main field: 14.6T
YBCO Bpeak
14.7T @4.2K
Cable | Hight | Width-i | Width-o | Ns | Strand | Filament | Insulation
IHEPW1 | 5.8 | 1.5 | 1.5 | 14 | IHEPWCJC | Nb3Sn | 0.15
IHEPW3 | 12 | 1.5 | 1.5 | 29 | IHEPWCJC | Nb3Sn | 0.15
IHEPWYBCO4 | 4 | 0.2 | 0.2 | 1 | IHEPWYBCO | YBCO | 0
Iron yoke OD:
600mm
Clear bore diameter 15mm Inter-aperture spacing 156 mm
To fabricate a 14-T dipole magnet (with two apertures) with HTS and Nb3Sn superconductors, to test the field optimization method of HTS & Nb3Sn coils.
C. Wang, K. Zhang, Q. Xu et al.
Model Magnet Development (2016-2018)

## Slide 18
Racetrack coil
Temperature controller
Vacuum pump
Heating Magnetic Stirrer
Epoxy tank
Container
Preparation for Model Magnet Development
Kai Zhang, Chengtao Wang et al.
Container
Epoxy tank
Air compressor
Booster pump
Shell
support
Bladder
Bladder
Strain
sensor

## Slide 19: Summary
SPPC needs thousands of 20-T level magnets to bend and focus the high energy proton beams .
Present status of the accelerator magnet technology: highest 16 T achieved to demonstrate the Nb3Sn technology but without accelerator level bore and field quality. Present highest operational field for accelerators 8.3 T.
To achieve the challenging 20-T accelerator magnets, a 10~15 years long term R&D is necessary.
A working group is being organized for the 20-T magnet R&D in China, and expecting international collaboration with worldwide labs.
R&D of advanced superconductors and model magnets for SPPC study have been started. Welcome more collaborators to join us!
Much more funding is necessary to carry out the R&D of this critical technology for CEPC-SPPC project.

## Slide 20
Thanks