## Slide 1: 铁基高温超导研究进展
陈仙辉
中国科学技术大学

## Slide 2
铁基超导新材料进展
  FeSe衍生体系
  FeAs基超导材料
  其他
物性与机理研究进展
  门电压技术调控超导电性
  Electronic nematicity
  强关联效应
  C4-symmetry reentrance
潜在强电应用探索
报告内容

## Slide 3
Some typical crystal structure of iron-based SCs
Highest Tc (~55 K) in SmO1-xFeAs
Iron-based superconductors: two categories
FeAs-based and FeSe-based
Fe2+ As3- Fe2+Se2-
Tc=8 K Tc=25 K Tc=38 K Tc=55 K Tc=33-42 K
是否还能获得更高超导转变温度？

## Slide 4
Fe1+xSe
Tc = 8 K
Tc=37
(under pressure)
KxFe2-ySe2 Tc = 31 K
with 245 phase
Solid-state reaction method
Lix(NH2)y(NH3)1-yFe2Se2
Tc = 43 K
Liquid ammonia method
K
Fe
Se
Crystallography of Iron-selenides

## Slide 5: FeSe衍生体系——Single Unit-Cell FeSe film
Q. Y. Wang et al., Chin. Phys. Lett. 29, 037402 (2012)
20.1meV
9.5meV
S. L. He et al., Nature Materials 12, 605(2013)
S. Tan et al., Nature Materials 12,634(2013).
Tc ~ 65K
With possibility of Tc >100K

## Slide 6
Extra Fe and intergrowth of tetragonal and hexagonal phases for Fe1+xSe
In the case of AxFe2Se2, the inter-grown antiferromagnetic insulating phase makes it difficult to study the underlying physics. Superconductors of alkali metal ions and NH3 molecules or organic-molecules intercalated FeSe and single layer or thin film FeSe on SrTiO3 substrate are extremely air-sensitive, which prevents the further investigation of their physical properties.
Therefore, it is urgent to find a stable and accessible FeSe-derived superconductor for physical property measurements so as to study the underlying mechanism of superconductivity, and for understanding
High-Tc SC in single-layer FeSe/SrTiO3
In the heavily electron-doped FeSe-derived SCs: interband scattering or Fermi surface nesting is not a necessary ingredient for the unconventional SC.
Tc in the one-unit-cell FeSe on SrTiO3 substrate can reach as high as ~65 K, largely transcending the bulk Tc of all known iron-based superconductors.
FeSe layer is nearly neutral
Unique behaviors in FeSe-derived superconductors:
Problems for studying in FeSe-derived superconductors

## Slide 7
Steel autoclave
10ml H2O
LiOH·H2O+Fe+Selenourea
Teflon
Stir and dissolve
Seal and heat
Hydrothermal synthesis: new method
Reaction at 160 oC
X. F. Lu and X. H. Chen* et al. PRB (2013)
X. F. Lu and X. H. Chen* et al. Nat. Mater. (2015)
Mild condition synthesis for avoiding Fe vacancy in FeSe layers
for heavily electron-doped FeSe-derived superconductors

## Slide 8
Superconductivity with Tc ≈ 43 K can be observed after annealing under 5 GPa and 150 oC.
FeSe衍生体系——Li0.8Fe0.2OHFeSe
X. F. Lu and X. H. Chen* et al. PRB (2013)
X. F. Lu and X. H. Chen* et al. Nat. Mater.(2015)
High stability in air and homogeneity in FeSe layer provide an outstanding platform for studying superconductivity in FeSe-derived materials.

## Slide 9
A. Iyo et al, J. Am. Chem. Soc. 138, 3410 (2016)
FeAs基超导材料——1144-phase

## Slide 10
C. Wang et al, J. Am. Chem. Soc 138, 2170 (2016)
FeAs基超导材料——ThNFeAs
A New ZrCuSiAs-Type Superconductor

## Slide 11
FeAs基超导材料——(Ca,Pr)/(Ca,La)AsFeAs
H. Yakita et al. JACS 136, 846 (2014)
N. Katayama et al. JPSJ 82, 123702 (2013)

## Slide 12
Y. L. Sun et al, J. Am. Chem. Soc. 134, 12893 (2012)
FeAs基超导材料——Bi2Ti2Fe2As4O

## Slide 13
T. Hanna et al. PRB 84, 024521 (2011)
S. Matsuishi et al. PRB 85, 014512 (2012)
S. Limura et al. Nature Commun. 3: 943 (2013)
M. Hiraishi et al. Nat. Phys. 10, 300 (2014)
LaFeAsO1−xHx
/Sm/Ce/La
FeAs基超导材料——Hydrogen in layered iron arsenides

## Slide 14
铁基超导新材料： YFe2Ge2 和 FeS
J. S. Chen et al, PRL 116, 127001 (2016)
YFe2Ge2
X. F. Lai et al., J. Am. Chem. Soc. 137, 10148 (2015)
FeS

## Slide 15
铁基超导新材料进展
  FeSe衍生体系
  FeAs基超导材料
  其他
物性与机理研究进展
  门电压技术调控超导电性
  Electronic nematicity
  强关联效应
  C4-symmetry reentrance
潜在强电应用探索
报告内容

## Slide 16
TC increases when electrons are injected into the 1-uc FeSe films by the field effect
The insulating STO substrate was used as a back gate.
Qi-Kun Xue et al. PRB 89, 060506(R) (2014)
back gate
Electric-field-tuned superconducting transition of 1-UC FeSe
传统门电压技术很难大幅度改变载流子浓度

## Slide 17
Tc ~ 8 K
Bulk FeSe

## Slide 18
DEME-TFSI@220 K
Thickness: 8 nm
Liquid gating technology
B. Lei and X. H. Chen* et al, PRL (2016)
离子液体门电压调控技术

## Slide 19
B. Lei and X. H. Chen* et al, PRL (2016)
Liquid gating control——High-Tc superconductivity in FeSe flakes
From low-Tc phase to High-Tc phase with a Lifshitz transition
and disappearance of hole pocket
Pairing symmetry is different

## Slide 20
X. H. Niu et al., PRB 92, 060504(R) (2015)
Similarity between highly electron-doped FeSe compounds
What will happen with further increasing electron doping?

## Slide 21
Liquid gating control—— SC-insulator transition in (Li,Fe)OHFeSe
LiClO4/PEO@330 K
Thickness: ~200 nm
B. Lei and X. H. Chen* et al. PRB (2016)

## Slide 22
FeSe thin layer ARPES results
Wen, C. H. P., et al. Nat. Commun. 7:10840 (2016)
Similar SC-insulator transition in K-doped FeSe Thin films

## Slide 23
Phase diagram
反常物性：
Nematic phase
Strong correlation
C4 magnetic phase
. . .
理解反常物理性质将有助于我们进一步理解高温超导电性

## Slide 24
In-plane resistivity anisotropy with applied uniaxial pressure
Watson, M. D., et al. PRB 91.155106 (2015).
Electronic nematicity——Nematic Phase in FeSe
2m66 = ( ρxx /ρ0 − ρyy /ρ0)/(εxx − εyy )

## Slide 25
Observation of orbital order suggests a orbital-driven nematic state in ​FeSe.
S. H. Baek, et al. Nat. Mater. 14, 210 (2015)
Electronic nematicity——Orbital order in FeSe
Orbital-driven vs Spin driven

## Slide 26: The nematic spin fluctuation at high energy scale probed by INS
Q. S. Wang, et al. Nature materials (2015).
Electronic nematicity——A neutron study in FeSe
Support spin driven picture!

## Slide 27
Electron correlation——heavily hole-doped AFe2As2 (A = K, Rb, Cs)
A. F. Wang et al.,
PRB 87, 214509(2013)
CsFe2As2
RbFe2As2
KFe2As2
Z. Zhang et al.,
PRB 91, 024502 (2015)
F. Hardy et al.,
PRL 111,027002 (2013)
γN=98 mJ·mol·K2
γN=127 mJ·mol·K2
γN=184 mJ·mol·K2
Large Sommerfeld coefficients

## Slide 28
Y. P. Wu et al., PRL (2016)
Heavy fermion behavior in AFe2As2 (A = K, Rb, Cs)
d-electron heavy fermion superconductors
NMR experiment suggests that AFe2As2 (A = K, Rb, Cs) are d-electron heavy fermion superconductors

## Slide 29
Electron correlation ——Searching for Mott phase

## Slide 30
C. Ye et al., PRX 5, 021013 (2015)
NaFe1-xCuxAs, x = 0.30
The overall line shape and strong spatial variations of the spectra are strikingly similar to those of lightly doped cuprates close to the parent Mott insulator.
Electron correlation——similarity between insulating FeAs
compound and lightly doped cuprates

## Slide 31
arXiv:1504.05116
Electron correlation ——Searching for Mott phase

## Slide 32
C4-symmetry reentrance in Ba1-xNaxFe2As2
S. Avci et al. Nat. Commun. 5: 3845 (2015)

## Slide 33
orthorhombic-distortion reentrance in Ba1-xKxFe2As2
A. E. Bohmer et al. Nat. Commun. 6: 7911 (2015)

## Slide 34
Complex phase diagram in Ba1-xNaxFe2As2
L. Wang et al. PRB 93, 014514 (2016)

## Slide 35
铁基超导新材料进展
  FeSe衍生体系
  FeAs基超导材料
  其他
物性与机理研究进展
  门电压技术调控超导电性
  Electronic nematicity
  强关联效应
  C4-symmetry reentrance
潜在强电应用探索
报告内容

## Slide 36
Critical current in iron-based superconductors
SmFeAsO0.7F0.25 single crystal
Irradiated SmFeAsO0.8F0.15
single crystal
Jc ~ 2106 A/cm2
Jc ~ 2107 A/cm2
P. J. W. Moll et al. Nat. Mater. (2010)
L. Fang et al. Nat. Commun. (2013)

## Slide 37
Critical current in iron-based superconductors
Pristine and Irradiated
Ba0.6K0.4Fe2As2 single crystal
Pristine, Jc ~ 2106 A/cm2
Irradiated, Jc ~ 5107 A/cm2
L. Fang et al. APL (2012)
FeSe0.5Te0.5-coated conductors
Jc > 106 A/cm2
W. D. Si et al. Nat. Commun. (2012)
铁基超导薄膜带材(FeSe0.5Te0.5 ),在4.2 K 下，30 特斯拉磁场下，超导临界电流仍然高达1105 A/cm2。 很有潜力用于高磁场 MRI和储能等方面。

## Slide 38
Superconductivity with Tc ≈ 43 K can be observed after annealing under 5 GPa and 150 oC.
FeSe衍生体系——Li0.8Fe0.2OHFeSe
X. F. Lu and X. H. Chen* et al. PRB (2013)
X. F. Lu and X. H. Chen* et al. Nat. Mater.(2015)
High stability in air and homogeneity in FeSe layer provide an outstanding platform for studying superconductivity in FeSe-derived materials.

## Slide 39
A summary of ongoing studies
New iron-based superconducting materials:
new FeSe-derived materials
new spacing layer in FeAs-based materials
controllable approaches for higher Tc
…
Physics of correlated electrons:
exploring new phases by liquid gating technique
studying electronic nematicity with multiple probes
understanding complicated electron correlation effect
…
Potential applications:
increasing critical current for power applications
…

## Slide 40
Thank you for your attention!

## Slide 41: FeSe衍生体系——Single Unit-Cell FeSe film
电子掺杂 + 界面电-声子相互作用

## Slide 42
Lifting of the dxz/dyz orbital degenerance caused by the electronic nematicity
Nakayama, K., et al. PRL 113, 237001(2014):.
Electronic nematicity——Band structure in FeSe

## Slide 43
T. Shimojima, et al. PRB 90,121111 (2014).
Strong orbital anisotropy detected by ARPES
Electronic nematicity——Band structure in FeSe

## Slide 44: Superconductors can transform the power grid to deliver abundant, reliable, high-quality power for the 21st century
current state future needs
Performance
10 increase in Jc
 10 reduction in ac loss
Cost
10-100 improvement needed
Materials
Increase operating temperature 2-5

## Slide 45
Liquid gating control——induced SC in insulating FeSe thin film
K. Hanzawa et al., PNAS113, 3986 (2016)
35 K

## Slide 46
Electric-field-induced superconductivity in electrochemically etched
ultrathin FeSe films on SrTiO3 and MgO
J. Shiogai et al. Nature Physics 12, 42 (2016)

## Slide 47: Superconductors: aimed for a Major Role in Energy Delivery
superconductivity
coal
gas
heat
mechanical
motion
electricity
hydro
wind
fuel cells
solar
motors
lighting. heating
refrigeration
information
technology
power grid
transportation
industry
nuclear
fission
production
delivery
use
Increased capacity
Enhanced reliability
Smart distribution
High power density
1/2 size
1/2 weight
1/2 losses

## Slide 48: Key issues for power applications
Overall current density Je of conductor, not just of superconductor
Performance in field
Multiple filaments for AC applications
Anisotropy of Jc with respect to field direction
Cost!
  Conductor itself
  Cooling (AC losses)
Scalability of fabrication
Mechanical
  Strength, bend radius