## Slide 1
高场用铁基超导材料的研究进展
马衍伟
中国科学院电工研究所

## Slide 2: 汇 报 提 纲
铁基超导材料简介
高性能122铁基线带材的制备研究
122铁基线带材的实用化制备进展
结论
1
2
3
4

## Slide 3
111 phase LiFeAs
11 phase FeSe
122 phase AFe2As2
(A=Ba, Sr, Ca)
Main known Fe-based superconductors
M. Rotter, et al., Phys. Rev. Lett. 101, 107006 (2008)
X. C. Wang, et al., Solid State Commun. 148, 538 (2008).
F. C. Hsu, et al., Proc. Natl. Acad. Sci. U.S.A. 105, 14262 (2008).
Tc ~38 K
Tc ~18 K
Tc ~8 K
1111 Phase LnOFeAs
Tc ~55 K
Z. A. Ren et al., Chin. Phys. Lett. 25, 2215 (2008)
Among them, the three phases most relevant for wire applications are 1111, 122, and 11 types with a Tc of 55, 38 and 8 K, respectively.

## Slide 4
铁基超导材料具有很高的上临界场(Hc2)
外推 Hc2( 0 K) 可以超过 200 T, 在20 K可产生 ~ 70 T，在高场磁体方面具有重要潜在应用前景。
Gurevich, Nature Mater. 10 (2011) 255
FBS have Hc2 > 30-70 T at 20-30 K where FBS outperform both MgB2 and Bi-2223.
Material | Tc (K)
Nb47wt%Ti | 9 K
Nb3Sn | 18 K
MgB2 | 33-39 K
Bi-2212 | 75-90 K
Bi-2223 | 108-111 K
REBCO | 90-92 K
Interesting FBS have Tc: 38-55 K >> Nb-Ti and Nb3Sn
Operation at 4K >20T or 10-30 K at >10 T would be very valuable

## Slide 5
 | LTS (NbTi, Nb3Sn) | Cuprates | MgB2 | Iron-based
Tc | 18 K | 110 K | 39 K | 55 K
Hc2 | ~30 T | ~100 T | ~40 T | >100 T
γ | 1 | 5-7 (YBCO) 50-90 (BSCCO) | ~3.5 | 1-2
Critical current density of iron-based single crystals Jc>1 MA/cm2
Comparison between different superconductors

## Slide 6
Fe-based wires potential for high-field applications
Development of high-performance wire conductors is essential
MRI
NMR
To apply superconducting materials to technologies related to magnets, they must be transformed into wires
Merits:
High Hc2 (70T@20K),
Low  (<2)
ITER

## Slide 7
Co doped Ba-122 thin films on bicrystals
Lee et al., APL 95, 212505 (2009).
Katase et al., Nat. Commun. 2, 409 (2011)
YBCO 4.2 K
YBCO 77 K
Jc decreases exponentially with GB angle, however, the critical angle GBs of pnictides is θc = 9o, larger than YBCO (θc~5o) .
Weak link effect, the GBs do not degrade the Jc as heavily as YBCO.
Advantageous GB over cuprates! This is the reason why we can use the PIT method to
make the pnictide wire and tapes, but PIT can not work for YBCO.
Grain boundary behavior in 122-type pnictides

## Slide 8
1111 and 11 wire and tapes: Jc ~ 200 A/cm2 in high fields
The Jc values obtained are still two to three orders of magnitude lower than for the 122 tapes.
1111 wires: how to control fluorine content during sintering.
11 wires: hard to remove excess Fe.
1111 type - Sm[O1-xFx]FeAs
11 type - FeTe1-xSex
Compared to 122 tapes: 105 A/cm2 @ 10 T

## Slide 9
美国弗罗里达强磁场实验室： HIP 4.2K、10T时Jc = ~104 A/cm2
美国橡树岭国家实验室：铜包套、冷压， 4.2K、0T时Jc=2.8  104 A/cm2
日本AIST：银包套，冷压
4.2K、0T时, Jc~105 A/cm2,
20 K, 2.5T, ~104 A/cm2
国外制备铁基超导线的情况 122体系

## Slide 10
日本国立材料研究所：Ag包套、冷压；4.2K、10T时, Jc = 8.9  104 A/cm2
日本东京大学： Ag包套, HIP合成；4.2K，0T时 Jc= 4.8  104 A/cm2
国外制备铁基超导线的情况 122体系

## Slide 11
意大利Genova大学：
4.2K, 0T时 Jc=3  104 A/cm2
4.2K, 0T时 Jc 400 A/cm2
澳大利亚Wollongong大学：
国外制备铁基超导线的情况 11/122 体系
仅有磁化Jc

## Slide 12
－ Simple and scalable process, low cost
Fabrication process for Sr(Ba)1-xKxFe2As2 wires
(Powder-in-tube method )
Iron-based superconducting tapes
Final Product
1. The single phase can easily be obtained.
2. The sintering temperature is low.
122 PIT wires:
800-900oC

## Slide 13
2008年4月，采用传统的粉末装管法，首次研制出新型铁基超导体线材
Supercond. Sci. Technol. 21 (2008) 105024
Tc＝25K
LaOFeAs
SmOFeAs
铁基线材临界电流密度非常低
主要是存在反应层、许多杂相、裂纹等
早期线带材

## Slide 14
Key problems for PIT wires: Low density and weak link
Hysteresis in transport Jc: signature of weak links
Residual cracks and porosity always lead to poor grain connection, so suppress Jc in polycrystalline wires!
A hysteretic phenomenon observed for transport Jc in an increasing and a decreasing field indicated a weak-linked behavior, similar to that of the cuprates.
Ag
Low density: cracks and porosity
Pore
Crack
Good connectivity is desirable!

## Slide 15
Add Sn to improve the grain connectivity. (APL2011)
Large reduction rolling to increase texture. (Physica C 2011, APL 2011)
Hot pressing is effective to enhance the superconducting core density as well as grain alignment. (APL2014)
Rolled
Hot pressed
Planar view
Longitudinal section
Tape axis
Tape axis
Solutions

## Slide 16
Chemical addition has been confirmed as a simple and readily scalable technique for enhancing Jc.
Zn and In additions are effective to enhance the Jc-B of 122/Ag tapes
The additions do not significantly affect the temperature transition Tc, and the Tc decreased only 0.4 K.
the Jc enhancement in In or Zn-added samples may be attributed to the improved phase uniformity as well as the good grain connectivity
Lin et al., Scripta Mater. 112 (2016) 128

## Slide 17
Optimized rolling process for 122/Ag tapes: 3-pass deformation is best
Huang, Physica C, 2016
The width of the tapes and the area of superconducting cores increase with decreasing the rolling pass, but the transport Jc seems close.
We can fabricate tapes with 3 rolling passes to get the uniform and high-Jc 122 tapes.
Ag

## Slide 18
Even for hot pressed multifilamentary 122 wires
At 4.2 K, 10 T
7-core, Jc= 6.1×104 A/cm2,
19-core, Jc= 3.5×104 A/cm2.
The superior Jc can be attributed to higher grain texture and improved densification.
Very High transport Jc were achieved in 122/Ag tapes: Jc > 105 A/cm2 (4.2 K, 10 T)－by hot pressing
First to reach practical level Jc!
Zhang et al., APL 104 (2014) 202601
The threshold for practical application:
Jc=105 A/cm2@10 T
Breakthrough work

## Slide 19
New record transport Jc values were achieved in 122/Ag tapes: Jc ~ 1.0×105 A/cm2 (4.2 K, 14 T)
At 4.2 K and 10 T:
Jc = 1.2×105 A/cm2
Lin et al., Sci. Rep. 4 (2014) 6944
Main challenge:
How to transfer the already achieved high Jc to the large scale required for application.
突破性进展
高性能短样制备是制备均匀长线的基础
--继续保持国际领先优势
--文献报道最高值

## Slide 20
热压提高机制研究
About 154.0
Nearly constant !
The variation tendency of Jc values was qualitatively similar to those of F and RRR values.
The hardness was almost saturated as soon as the hot pressing was applied.
The Jc increase for HP900 tapes was mainly attributed to higher degree of c-axis texture and enhanced grain connectivity (high density).
--高的织构度和致密度

## Slide 21
EBSD images: the orientation mapping of grains
Upper: HP850
Lower: HP900
Inhomogeneous distribution of grain size
A room for the Jc improvement
The dominant orientation is (001) as the expected red color for both tapes, but there is a small (100) orientation for HP850 tapes as the green color.
The large fraction of small misorientation angles between 2–10oC (HP850 tapes 23.3%, HP900 tapes 26.2%).
A useful tool to clarify the grain size, local orientation of the grains and misorientation angles between grains.

## Slide 22
钉扎中心: 晶格缺陷，位错，掺杂纳米粒子
磁通线的钉扎与运动是影响Jc的重要因素！
没有钉扎中心，则没有超导电流。
即使磁通线被钉扎住，热激活，磁通量子隧穿和机械振动会导致磁通线重新分布，从而导致样品的磁化强度发生弛豫。
磁通线
高性能热压122带材的磁通钉扎机制与动力学
Jc (4.2 K, 10 T)~105 A/cm2，Ic(4.2 K, 10 T)~300 A。
Tc~35 K, 超导转变宽度小。
剩余电阻率：RRR=ρ(250 K)/ρ(37 K)=4.81, 表明晶粒连接性较好

## Slide 23
磁通跳跃（<6 K, <1 T）-- 高Jc！
首次在铁基超导线带材中发现磁通跳跃行为。
Ba0.65Na0.35Fe2Fe2As2，Ba0.78K0.28Fe2As2，LiFeAs单晶中同样存在磁通跳跃现象。

## Slide 24
磁通钉扎机制
磁化电流密度非常接近于传输电流密度，表明带材的晶粒性可以忽略。
根据Dew-Hughes模型，约化钉扎力：fp=Ahp(1-h)q，峰值位置：hmax=p/(p+q)=0.22，
表明晶界和位错是主要的钉扎中心，点钉扎也可能起到一定作用。
δl型钉扎, 由于平均自由程的涨落而引起的钉扎。

## Slide 25
高性能Sr122带材超导芯的微观结构（TEM）
高密度位错
晶格缺陷
大量的晶界
大量的晶界和位错作为有效钉扎中心起主要钉扎作用。
Nb-Ti, Nb3Sn和MgB2线材中，晶界有利于钉扎磁通，而且不会阻碍晶间电流，这与热压Sr122带材非常相似。
一些点状晶格缺陷作为点钉扎中心也起到一定的钉扎作用。

## Slide 26
磁弛豫——磁通蠕动行为
磁化强度M和时间t为对数函数关系——热助磁通蠕动。
磁弛豫率很小且随磁场、温度变化不大表明热压Sr122带材的钉扎能力很强，而且Jc随磁场变化不大。
发生从磁通弹性蠕动到塑性蠕动的转变。
Dong et al., JAP 119 (2016) 143906
磁通弛豫率：

## Slide 27
高Jc热压Sr122带材磁通相图
磁通弹性蠕动区域的临界电流密度随磁场变化不大。
在液氦温区，临界电流密度随磁场变化不大，但临界电流密度在液氢温区随磁场升高而迅速减小。
进一步增加钉扎力：i) 减小晶粒大小以增加晶界，ii) 增加点钉扎中心，例如：辐照或纳米粒子掺杂。
Hcross 定义为磁通弹性蠕动到塑性蠕动的转变磁场
Dong et al., JAP, 2016

## Slide 28
Conductor requirements for practical applications
Overall current density JcE of conductor, not just of superconductor
Performance in field
Filamentary architecture essential for AC applications
Anisotropy of JcE with respect to field direction
Cost
  Conductor itself
  Cooling
Scaleability of fabrication
Mechanical
  Strength, bend radius, …..
Conductor shape
  tape or wire
Larbalestier, Nature 414 (2001) 368

## Slide 29: Jc properties at 4.2 K for HP Sr-122/Ag tapes
The Ic in applied magnetic fields is slightly higher in the perpendicular field (Ic┴) than in the parallel field (Ic//).
The anisotropy ratio (Г= Ic⊥/Ic∥) is less than 1.5, quite small, very promising for applications.
Small anisotropy
-- Measured by Dr. S. Awaji
HFLSM, Tohoku Univ.
4.2 K
4.2 K

## Slide 30: Temperature dependence of n value for Sr-122 tapes
-- Measured by Prof. Yang
Univ. of Southampton, UK
n value
At 20 K, the n value was over 30
At 4.2 K, the n value was over 20
-- Measured by Dr. Oguro
HFLSM, Tohoku Univ., JP
Fe-sheathed
Ag-sheathed

## Slide 31: The first strain measurements of Sr-122/Ag tapes
-- Measured by Dr. Kovac
Slovak Academy of Sciences
At 4.2 K, 10 T: Ic >125A
Irreversible strains:
 = 0.25%
Improvement of mechanical property of pnictide wires will be one of the major challenges for high field applications
which seems better than that of Bi-2212/Ag
Next step:
Strain property
Kovac et al., SuST 28 (2015) 035007
The first observation of strain effects on the critical current of 122 wires

## Slide 32: Fabrication of stainless steel/Ag double sheathed Ba122 tapes
NIMS group, Supercond. Sci. Technol. 28 (2015) 012001
Highly mechanical property is expected!
High Jc, but show lower Je

## Slide 33
So far, all high-Jc pnictide wires and tapes were made by using Ag as sheath material
Florida, 2012
NIMS, 2014
IEECAS, 2014
Ag is very expensive
We should find other cheap materials, in order to reduce the cost!
Ag
Ag
Ag
Ag

## Slide 34
Fabrication of Fe-cladded 122 tapes
From an economic point of view, the Fe sheath is more attractive than the Ag sheath in fabricating Sr122/Ba122 tapes for practical applications.
At 4.2 K and 14 T:
Jc = 2.4×104 A/cm2
Fe sheath material
-- by the scalable rolling
Ma , Physica C 516 (2015) 17
-- tape thickness=0.6 mm
Fe

## Slide 35
首次成功制备高性能Cu包套铁基超导带材
--对进一步促进铁基超导材料的实际应用具有重要意义
At 4.2 K, 10 T
Transport Jc:
3.1×104 A/cm2
Engineering Je:
>104 A/cm2
Lin, et al., Sci. Rep. 5 (2015) 11506
优点：既可以降低铁基线带材的制造成本，同时还可保证线带材在使用时的热稳定性。
800oC/30分钟
铜包套

## Slide 36
The HP740/60 tape has a uniform and well connective superconducting phase and only a small amount of diffusion of Cu.
The best transport Jc reaches 3.5×104 A/cm2 at 10 T and keeps 1.6×104 A/cm2 at 26 T.
High Jc in Cu-sheathed Sr-122 tapes at low temperature 740oC
Latest result
At 26 T:
Jc = 1.6×104 A/cm2
Cu
Cu
Cu
Lin, to be published
Je >104 A/cm2

## Slide 37
114-core round wires: Jc=800 A/cm2.
When they are flat rolled into tapes, the Jc grows with the reduction of tape thickness. the Jc =6.3×103 A cm-2 in 0.6 mm thick tapes.
7-core tapes: Jc= 1.5×104 A/cm2.
This Jc degradation can be ascribed to the sausage effect.
Yao et al., JAP 118 (2015) 203909
114 filament
Fe
Fe
Fe
Ag
Ag
Ag
At 4.2 K, 10 T:
率先成功制备了高性能122型铁基超导19和114芯线带材
多芯样品具有更高的磁场特性和较低的交流损耗，对实际应用具有重要意义。

## Slide 38
Higher Jc in Ba-122/Ag tapes was achieved by scalable rolling process
One cycle of ﬂat Rolling + Sintering process
At 4.2 K and 10 T:
Transport Jc = 5.4104 A/cm2
The highest among the rolled iron-based superconducting tapes
Such high Jc value is believed to stem in part from an improvement of grain connectivity by reducing weak links.
The degree of texturing F: ~0.69
Average Hv: ~135
-- thickness=0.3 mm
Dong et al., Scripta Mater. 99 (2015) 33

## Slide 39
The average Jc of this long Sr122/Ag wire is ~ 18400A/cm2
The fluctuations of the Jc is ~5%
The first 11m long Sr-122 tape
Uniform wires can be fabricated
The first long wire-- 11 m
Significant breakthrough!
-- by the scalable rolling process
Ma , Physica C 516 (2015) 17

## Slide 40
OD: 110 mm
ID: 71.5 mm
Turns:152
Fabrication of Sr122 coil using 10 m long Ag-sheathed tape
Length：10 m
Thickness：0.44 mm
Width：3.7 mm
Short tape Ic: ~100 A (4.2 K, 0 T)
Superconducting ratio：9%
7-filamentary
Next step:
1) Increase S ratio;
2) Ag is too soft for winding, to use high strength tape.

## Slide 41
Prospects
122 PIT tapes have achieved the practical level Jc, increasing it further is challenging. Still we are below the film Jc, so there is room for improvement.
We believe that PIT process can be applied industrially to fabricate pnictide wires and tapes, as already demonstrated by the production of Bi-2223 and MgB2 wires.
Already reached practical level Jc at 10 T
Strong promising for high-field applications !
Realization of the first 11 m long-length tape
+
Breakthrough work

## Slide 42
Ultra High In-Field Critical Currents: Ic, min – B
 e.g. Jc > 2105 A/cm2 @ 4.2 K, 10 T
Correspondingly, Jc > 105 A/cm2 @ 4.2K, 28 T
High Jc Round Wires:
 Like Bi-2212, round wire is ideal for high homogeneity magnets – NMR
Low Cost Wires:
 e.g. Cu- or Fe-sheathed wire fabrication, instead of using Ag
High Mechanical Strength Long Wires:
 Tensile, Bending
Summary: Challenges for the next stage R&D

## Slide 43
Thank you for your attention !

## Slide 44
铁基超导体线材的传输性能最新进展
Next goal: 105A/cm2 at 20-30T
4.2K, 10 T
Jc=1.2×105 A/cm2
Latest
电工所