## Slide 1: Development of HV/HR CMOS sensors for the ATLAS ITk
Jian LIU (刘剑)
Shandong University
liuj@hepg.sdu.edu.cn
FCPPL 2017 — Tsinghua Univerisity, Beijing, CHINA 30 Mar 2017

## Slide 2: CPPM / Atlas Chinese Cluster Collaboration
CPPM / ACC collaboration for design and test of Front-End pixel electronics for ATLAS phase II upgrade.
Scientific cooperation supervised by Pr. Xinchou LOU, Dr. Zheng WANG and Pr. Marlon BARBERO, derived from ATLAS CPPM / ACC project (Pr. Shan JIN / Dr. Emmanuel MONNIER).
Co-PhD Jian Liu (SDU – Pr. Meng WANG / CPPM Pr. Marlon BARBERO & Dr. Alexander ROZANOV), defended on May/2016. Postdoc at SDU since Sep/2016.
The last development topics involve:
  The simulation and tests in LFOUNDRY HV/HR CMOS technology. Jian Liu (SDU /CPPM).

## Slide 3: HL-LHC Environment
Fluence at the inner most pixel layer, for an integrated luminosity of 3000 fb-1 over 10 years:
NIEL: ~1.4x1016 neq cm-2
TID: ~770 MRads
The new Inner Tracker should be rad-hard, cope with high occupancy and lower price.
Presently, one possibility for upgrade is to use a hybrid pixel detector concept:
Sensor: thin silicon planar or 3D (reduce drift distance),diamond…
Readout-Out Chip: deep-submicron rad-hard ICs (65nm)=>high granularity=> high resolution, low occupancy
After the Phase II upgrade ~2024,
The HL-LHC will operate at a levelled instantaneous luminosity of 7.5×1034cm-2s-1 .
Total pixel silicon area of ATLAS Inner Tracker (ITk) is ~8.2m2.

## Slide 4: HV/HR CMOS for Phase-II Upgrade
Use cases for the future ITk in 2024:
For inner layers. 25 x 25 µm2 pixel size with in-pixel en/de-coding read out by the FE-65 nm (RD53)  higher granularity.
For outer layers. 50 x 50 µm2 pixel size, full monolithic chip  ease of assembly, two tracks separation.
Main advantages:
Commercial CMOS technology lower price per unit area.
Can be thinned to tens of µm  material budget reduced.
Pixel size can be reduced  improved single point resolution.
1st amplifier in-sensor  capacitively coupled to a specific digital part by gluing (compatible with ATLAS FE-I4, an readout IC for the ATLAS IBL).
See Patrick Pangaud’s talk.

## Slide 5: HV/HR CMOS for Phase-II Upgrade
Explore industry standard CMOS processes as sensors:
Exists in many processes, in particular HV/HR CMOS technologies, such as AMS 0.18 µm HV CMOS, GF 0.13 µm BCDlite and LF 150 nm technology…
Basic requirement is Deep N Well(DNW) high substrate bias voltagedriftrad-hard
Triple-well technology  shielded electronics with HV.
DNW: Light doping
Depletion width:

## Slide 6: HV/HR CMOS architectures
Diode
Amp
Amp
Discri
DC
Bump-bond
AC
Capacitively coupled pixel detector (CCPD)
Diode
Amp
Discri
Sensor (can be read out stand alone) bump bonded or capacitively coupled to digital IC:
Monolithic (depleted CMOS pixel chips including the R/O architecture on-chip):
Focusing on CCPD in this talk.
See Patrick Pangaud’s talk.

## Slide 7: CCPD-LF 150 nm prototype in 2015
LF vA
LF vB
Version A sensor:
Larger DNW, larger input capacitance, electronics isolated with HV.
Version B sensor:
Smaller DNW, smaller input capacitance.
Chip size is 5mm×5mm, 114x24=2736 pixels
Pixel size is 33umx125um
Test transistors are implemented in vA
Test sensors and analog buffer are implemented in vB.

## Slide 8: LF VA under protons: analog scan at -20 ℃
5 MRads
5 MRads
100 MRads
100 MRads
Both the threshold and noise reduced after 100 MRad. The ELT pixels have bigger threshold level than linear feedback pixels.
ELT
L1.5um
L0.9um

## Slide 9: LF VA lab test: tuning of LIN feedback pixels
56 pixels (3.1%) were masked.
Scan
LSBdacL=63, TDAC=7
TH=0.80V, BL=0.75V
Tuning
LSBdacL=63
TH=0.80V, BL=0.75V

## Slide 10: LF CPIX demonstrator
New large demonstrator LF CPIX was submitted on March 2016:
  Pixel size 250 µm × 50 µm (FE-I4 like).
  Consists of three pixel flavors: passive, digital and analog pixel. Some improvements have been brought to them with respect to the characterizations of the LF CCPD prototypes.
  New guard-ring strategy in LF CPIX Ver2 to increase the breakdown voltage and reduce the inactive region.
LF CPIX V1
LF CPIX V2
Test structures

## Slide 11: What we have done by using TCAD
DC: Depletion evaluation depending on the biasing voltage and the resistivity.
DC: Leakage current.
Cdnw
Cpw-dnw
AC: Input capacitance from the Pwell and DNW.
DC: Breakdown voltage in the critical region.
Transient: Charge collection behavior.
Cinter

## Slide 12: Guard-ring strategy of LF CPIX
230
8
4
5.5
19
5.4
3
19
5
20
5
35
8
35
8
35
10
35
10
40
10
40
10
DNW-pixel
PW-pixel
NWring
PWring
g1
g2
g3
g4
g5
g6
g7
8
35
bb
sr
230
8
4
10.5
9
10.4
3
19
5
20
5
35
8
35
8
DNW-pixel
PW-pixel
NWring
PWring
g1
g2
bb
sr
(A) Default: The same size as LF CPIX V1 except for the distance between DNW-pixel and PW-pixel.
(C) Shrunk Nwellring + reduced guardrings: has enough space to avoid the depleted region touching the cutting edge.
(B) Shrunk Nwellring: increase the distance between Nwellring and its neighbor PWs to improve breakdown voltage.
3 scenarios were under simulating. Top side bias with 300um thickness. Backside bias with 100um thickness.
Topside bias: PW-pixel, bb and sr connected to –HV, DNW-pixel and NWring to VDDA, others floating.
Backside bias: backplane connected to –HV, DNW-pixel and NWring to VDDA, others floating.
230
8
4
10.5
9
10.4
3
19
5
20
5
35
8
35
8
35
10
35
10
40
10
40
10
DNW-pixel
PW-pixel
NWring
PWring
g1
g2
g3
g4
g5
g6
g7
8
35
bb
sr

## Slide 13: Leakage current of LF CPIX V1
The DNW-pixel dominates the breakdown for both before and after irradiation.
After irradiation, the BV increases from 90 V to 105 V by simulation.
Top-side bias
Back-side bias
Top-side bias
Back-side bias
Fluence = 0
Fluence = 1e15
The matrix BV is ~76V before irradiation.
The matrix BV is ~100V at 827MRads.
827 MRads
827 MRads after 57 days annealing

## Slide 14: Depletion and e-field of LF CPIX V1 and V2
~100 µm
Pwellring + 2 floating guard-rings + backbias + seal-ring.
The depleted region can not reach the chip edge even with removed 5 outer guard-rings.
Break down voltege changed from 90 to 170 V.
Big un-depleted area between depleted edge and cutting edge  guard-ring reducing is possible  reduced dead region.
V1
V2

## Slide 15: AC simulation for LF CPIX
LF 150 nm technology
Pixel size: 50 µm x 250 µm
Substrate resistivity:
Substrate thickness: 200 µm
3D device
Digital pixel V1
Analog pixel V1
Passive pixel V1
Digital pixel V2
Analog pixel V2
Passive pixel V2
Distance between DNW and guard-ring of V1: 4.86 µm.
DNW size of V1: 237 µm x 37 µm
Distance between DNW and guard-ring of V2: 8 µm.
DNW size of V2: 230 µm x 30 µm

## Slide 16: AC simulation for V1 and V2
Pixel flavor | Digital | Analog | Passive
Cdnw @ - 50 V (fF) | 107 | 107 | 107
Ctotal @ - 50 V (fF) | 308 | 279 | 113
Pixel flavor | Digital | Analog | Passive
Cdnw @ - 50 V (fF) | 79 | 79 | 79
Ctotal @ - 50 V (fF) | 277 | 245 | 86
Capacitance of V2 pixels:
Capacitance of V1 pixels:
Mainly contributed from the Cdnw and the Cdnw-pw.
The capacitances of V2 pixels reduced due to the smaller DNW size.

## Slide 17: Summary
Radiation harness of LF CCPD > 100 MRads and 1015 neqcm-2  an option for the HL-LHC.
The simulations show good agreement with measurements before irradiation, for instance the breakdown voltage and capacitance. The increase of the breakdown voltage with increased radiation dose was also reproduced by the TCAD simulation.
The preliminary test results reveals that the performance of the LF CPIX demonstrator has been improved as expected. More further design and characterization details  Patrick Pangaud’s talk.