## Slide 1
Vcuum system works in 2016
Liu Baiqi, Peng Xiaohua

## Slide 2
RF-Shielded Bellows for Superconducting Accelerator Module
RF-Shielded Bellows using in BEPCII
  Compensate dimensional error
  Microwave shielding
Challenge for Superconducting Accelerator Module
  Cleanliness: class 10
  Low temperature resistance : 1.9K
Work progress
  Finish the technologies reserves on the RE-shielded bellows designing using in normal temperature
  Finish the designing for Low temperature
  Designing the technological process to ensure the class 10 cleanliness

## Slide 3
Technology and mechanism study about N-doping
Technology target for N-doping
  Base on the Doping process successfully applied in FERMI

## Slide 4
Technology and mechanism study about N-doping
N-doping process designing under the vacuum furnace in HE-Racing Technology Co.
  After 3 hours baking at 800℃, close the gate valve and inlet N2 by adjusting the micrometering valve, maintain the vacuum chamber pressure at 3±2Pa
Vacuum
chamber
Valve
Diffusion
pump
N2 inlet
Vacuum
Chamber
(f1.6m×2m)
N2
Micrometering valve
Diffusion
Pump
Gate valve
Diffusion pump
is not clean
for N-doping

## Slide 5
Technology and mechanism study about N-doping
N-doping dedicated Vacuum furnace design
  Non-oil turbo-molecular vacuum unit
  3±2Pa automatic control system
turbo-molecular
vacuum unit
Automatic
Control
system
Vacuum furnace parameter
  Effective size f 250 mm×400 mm (for 1.3GHz single cell)
  ultimate pressure: 8E-4 Pa (900℃); 8E-5 Pa (25℃)
  PLC for temperature, vacuum and N2 inflation

## Slide 6
Technology and mechanism study about N-doping
N-doping mechanism study
  Using molecular dynamics method
  Study the movement process of the gas particles in the Nb lattice
Degassing
800℃
N-doping
800℃
Cooling
down
Impurity gas separates from the Nb lattice
N2 infiltrates into the Nb lattice
Atoms in
Nb Lattice fix
Gas particle
Nb particle

## Slide 7
Thanks！