# Dendritic and eutectic growth in Sb60Ag20Cu20 ternary alloy

## RUAN Ying† & WEI BingBo

Department of Applied Physics, Northwestern Polytechnical University, Xi'an 710072, China

The rapid solidification of Sb60Ag20Cu20 ternary alloy was realized by high undercooling method, and the maximum undercooling is up to 142 K (0.18 TL). Within the wide undercooling range of 40－142 K, the solidified microstructures are composed of (Sb), ( and ( phases. High undercooling enlarges the solute solubility of (Sb) phase, which causes its crystal lattice to expand and its crystal lattice constants to increase. Primary (Sb) phase grows in two modes: at small undercoolings non-faceted dendrite growth is the main growth form; whereas at large undercoolings faceted dendrite growth takes the dominant place. The remarkable difference of crystal structures between (Sb) and ( phases leads to (( + Sb) pseudobinary eutectic hard to form, whereas strips of ( form when the alloy melt reaches the (( + Sb) pseudobinary eutectic line. The cooperative growth of ( and ( phases contributes to the formation of (( + () pseudobinary eutectic easily. In addition, the crystallization route has been determined via microstructural characteristic analysis and DSC experiment.

### high undercooling, ternary eutectic, crystal nucleation, dendrite growth

Rapid crystal growth at high undercooling is a liquid/solid phase transition process deviating far from the equilibrium situation, which has been investigated widely to develop metal solidification mechanism and prepare novel metal materials[1―5]. It has been achieved by means of various containerless techniques, such as glass fluxing technique, drop tube technique and various kinds of levitation techniques[6―8]. Recently more attention has been attracted on the rapid crystal growth of undercooled ternary alloy. Sb-Ag-Cu ternary eutectic alloy system has a low eutectic transition temperature (699 K), whose solidification process involves the competitive nucleation and growth of several solid solutions and intermetallic compounds including faceted and nonfaceted phases.

Faceted and non-faceted growth are two types of crystal growth. Faceted growth is realized by liquid phase atoms depositing on the steps of S/L interface which is flat on an atomic scale.

The authors are grateful to Mr. Dai Fuping and Wang Haipeng for their contribution to experimental work.

Kalb J, Spaepen F, Wuttig M. Atomic force microscopy measurements of crystal nucleation and growth rates in thin films of amorphous Te alloys. Appl Phys Lett, 2004, 84: 5240－5242

Yamauchi I, Kawamura H. Rapid solidification and mechanical alloying of Al-Co-Ag ternary alloys for skeletal silver cobalt synthesis. J Alloys Comp, 2004, 370: 137－143

Rosa C D, Park C, Thomas E L, et al. Microdomain patterns from directional eutectic solidification and epitaxy. Nature, 2000, 405: 433－437

Greven K, Ludwig A, Sahm P R. Time dependent interface stability during rapid solidification. J Appl Phys, 1999, 86: 3682－3687

Conti M. Curvature effects in rapid alloy solidification. Phys Rev E, 2001, 63: 041507－041514

Hermann R, Löser W. Extension of the primary solidification region of Nd2Fe14B by levitation of undercooled melts. J Appl Phys, 1998, 83: 6399－6401

Yao W J, Wei B. Rapid growth of nickel dendrite in highly undercooled Ni-Mo alloys. Sci China Ser E-Eng Mater Sci, 2003, 46(3): 259－267

Leonhardt M, Löser W, Lindenkreuz H G. Phase selection in undercooled peritectic Fe-Mo alloys. Acta Mater, 2002, 50: 725－734

Aoyama T, Paradis P, Ishikawa T, et al. Observation of rapid solidification of deeply undercooled Si melts using electrostatic levitation. Mat Sci Eng A, 2004, 375-377: 460－463

Dukiewicz J, Massalski T B. Search for metallic glasses at eutectic compositions in the Ag-Cu-Ge, Ag-Cu-Sb and Ag-Cu-Sb-Ge systems. Metall Trans A, 1981, 12A: 773－778

Ruan Y, Cao C D, Wei B. Rapid growth of ternary eutectic under high undercooling conditions. Sci China Ser G-Phys Mech Astron, 2004, 47(6): 717－728

Ruan Y, Wang N, Cao C D, et al. Rapid solidification mechanism of Ag60Sb34Cu6 ternary alloy in drop tube. Chin Sci Bull, 2004, 49(17): 1801－1805

Mikheev L V, Chernov A A. Mobility of a diffuse simple crystal-melt interface. J Cryst Growth, 1991, 112: 591－596