## Slide 1: Cavity R&D Facilities
Song JIN
2017. 07. 14
International Review on PAPS RF System

## Slide 2: Content
Cavity optical inspection and local grinding
Tuning equipment
N-doping furnace
Nb3Sn furnace
Nb/Cu coating system

## Slide 3: 1、Cavity optical inspection and local grinding system

## Slide 4: Optical Inspection and Grinding System
High resolution optical camera is a key tool to identify cavity defects. Local grinding is effective repairing tool for a cavity with a few defects.
  Kyoto Camera (CavCam) is one of the most successful and widely used cavity optical inspection systems.
  We will order a CavCam high resolution cavity camera combined with the local defect grinder of the latest version.

## Slide 5: Example Images by Kyoto Camera (IHEP TESLA cavity in KEK STF)
Cat-eyes
Trimming grooves
Etching pits
Undercuts
Weld irregularities
Bumps, scratches
Total: 4 ( 2 > 100 μm)
Diameter: 50 ~ 200 μm
Depth: 50 μm?
harmful or not?
Total: tens of
Diameter: < 200 μm
Depth: ?
Bumps after EP1
Narrow down
Numerous ( < 100 μm)
Material original or deep drawing induced pits,
Enlarged by EP
Weld spatters (very harm full)
Foreign inclusions (most harmful)

## Slide 6: User Interface of Control Software

## Slide 7: Kyoto Camera in the World
KEK
Three IHEP 9-cell cavities inspected by the Kyoto camera in KEK STF.
FNAL
One IHEP 9-cell cavity inspected by the Kyoto camera in FNAL.
DESY
CERN

## Slide 8: Combined CavCam and Local-Grinding Design for IHEP PAPS
Switchable Inspection and Grinding of 650 MHz 1 to 5-cell cavity.
Extendable to 1.3 GHz 1 to 9-cell by changing camera head and grinder head.
1.3 GHz Inspection
1.3 GHz Grinding
650 MHz Inspection or Grinding

## Slide 9: Grinding System

## Slide 10: Main Features of the CavCam System
Inspection and grinding of the equator and iris area
Automated inspection (auto-photo, auto-focus etc.)
Resolution: < 5 μm / pixel
Independent brightness control of each illumination LED
Rotatable cavity and camera cylinder
External driving motor of the grinder
Collision-free of the grinder with proximity sensor
Easy operation and maintaining

## Slide 11
2、Tuning Machine

## Slide 12: Introduction
Tuning machine is the equipment to adjust the frequency, field flatness, eccentricity (straightness) and length of the multi-cell cavities to meet the target specifications.
Fully automatic tuning machine (FATM) is needed for the cavity mass-production at industry. We plan to make a machine for 1.3 GHz TESLA cavity in collaboration with related labs (other fund).
For the first tep, we will make a semi-automatic tuning machine (SATM) for 1.3 GHz TESLA cavity based on the DESY design, which is upgradable to FATM in the near future.

## Slide 13: Fully Automatic Tuning Machine
DESY@Zonon
DESY@RI
FNAL
KEK

## Slide 14
(courtesy of DESY)

## Slide 15: Main Features of the Tuning Machine
Include:
Base Frame
Cavity Supporters and Train
Tuning Frame (vice jaws, sensors and actuators)
Bead-Pull System
Motors Control
Not include (upgrade in the future):
Cavity Alignment Tool (laser)
Eccentricity Measurement Device
Network Analyzer
Software
...

## Slide 16: 3、N-doping furnace

## Slide 17: N-doping effects
Vertical test results of 650 MHz Single-Cell (β=0.92) cavity (courtesy of FNAL)
Vertical test results of 1.3GHz single cell cavity (courtesy of FNAL)

## Slide 18: N-doping furnaces
N-doping Furnace at OTIC
(similar as ours, made by Lanzhou Vacuum）
N-doping Furnace at FNAL（made by T-M VACUUM）

## Slide 19: Main parameters of design
Dimensions：7000L×6000W×3500H（mm）
Total electricity power：300 kW
Heating power：210 kW
Uniform temperature zone：1500*600*600 mm
Max temperature：1200 °C
Max Load: 500 kg
Ultra vacuum：<1e-4 Pa
Cooling：natural cooling with protective gas
Gas Injection ：4 ports for N2, Ar, air and RGA
Mass flow controller: 0.1-100Pa

## Slide 20: Main components of vacuum system
Oil-free pumping system: two COOLVAC10000 CL-V（DN500 ISO-K，N2 pumping speed 10 000l/s) cryo-pumps by Leybold、one roots pump (1200L/S)、one screw pump.
All valves are pneumatic, which automatically shut as power off.
Vacuum pipe is made by stainless steel to keep clean.

## Slide 21: Control system
PLC with Touch screen
Industrial Personal Computer with Labview
Main parameters such as mass flow, will be automatic controlled;
Data can be recorded, stored and transferred by internet
There’s also manual control system, which is independent from computer.

## Slide 22: 4、 Nb3Sn furnace

## Slide 23: Advantages
Niobium cavity coating with Nb3Sn can work at 4.2K, which save much cost than 2K.
Nb3Sn is predicted to have 2 times higher magnetic field limit of niobium.

## Slide 24: Economic benefits
Efficiency of 4.2K to 2K is about 5:1. Take PAPS Cryogenics system for example, the refrigerator (2500W@4.2K ≈ 500W@2K) costs 50 million Chinese Yuan, while the refrigerator (500W@4.2K) costs about 15 million Chinese Yuan.
1W@4.2K needs 300W electricity power. So the electricity power of PAPS cryogenics system (500W@2K) is ~750kW. If 4.2K, it’s ~150kW for 500W@4.2K.

## Slide 25
Schematic of Nb cavity coating with Nb3Sn (courtesy of FNAL)

## Slide 26: Cornell Nb3Sn coating furnace

## Slide 27: Cornell Nb3Sn coating technique

## Slide 28: Schematic of Nb3Sn Coating Furnace
Outer oven
G
Nb
chamber
Thermal sensor
Sn heater
Heat shields
G
TP
  Furnace
    Working area:1000 × Φ 600 mm
    Maximum temperature
      Furnace area:1200℃
      Crucible:1300℃
  Vacuum
    Nb chamber
    Crucible material: Tungsten
    Oil free pumping system
    Ultimate vacuum：<1×10-4 Pa
  Temperature control
    The temperature at Nb chamber can be precisely controlled in the range of 1000~1300℃ with accuracy of ±1℃
Roots
Pumps
Turbo Pumps
Screw
pumps
Screw
pumps
(Oil free)

## Slide 29: 5、Nb/Cu coating system

## Slide 30: Introduction*
* P. Zhang, Status of Nb/Cu, Internal report at IHEP;

## Slide 31: Benefit of Nb/Cu*
* P. Zhang, Status of Nb/Cu, Internal report at IHEP;
Low Cost

## Slide 32
Nb/Cu
Cu substrate
- 1.3GHz (multiple VTs)
- 500MHz (eyes on HEPS HC)
Coating method
- DCMS
- HiPIMS (future)
Approach
- Samples
- Real cavity
SRF Cavity
Cu cavity
Nb thin film
SC

## Slide 33: Thanks！