## Slide 1: CEPC 650MHz Cavity HOM Absorber Research
Fanbo Meng
Accelerator Center, IHEP
2017. 04. 19
CEPC workshop, CCNU, Wuhan

## Slide 2
Outline
Absorbing material selection
Material test
Structure optimization and absorbing efficiency
Brazing experiment
Absorber design method
Cooperation details
1

## Slide 3
Absorbing material selection
Mature ferrite
AlN+SiC composite
HIP material
New ferrite
Selection criterion:
Absorbing capability
Mature technology
Suitable Material：
Mature ferrite
AlN+SiC composite

## Slide 4
7
Material absorbing capability test system
Test method:
DUT
fixture
fixture
Agilent VNA
Cable with N type connector
Test port
DUT port
Use SOLT method to calibrate cable
Use TRL method to calibrate fixture
Use S parameter on DUT port to compute the and of sample with transmission and reflection theory
To select the material, we need a absorbing capability test system.

## Slide 5
Waveguide fixture
Material absorbing capability test system
TRL calibration
T state
R state
L state
Work frequency :
0~5.6GHz
0~9GHz
Coaxial fixture
8.5~18GHz
upgrade
finished
upgrading

## Slide 6
9
Verification of test accuracy:
Chart: 
Chart: 
Test result of air
Chart: 
Chart: 
Material absorbing capability test system

## Slide 7
10
Test results of mature ferrite:
Chart: 
Chart: 
Chart: 
Chart: 
Material absorbing capability test system

## Slide 8
Ideal structure
Optimized structure
The brick shape ferrite will cause impedance mismatch, increasing the reflection
Optimize the special structure and ferrite size to lower the reflection, then increasing the absorbing efficiency
Conclusion:
Base on the same material, optimizing the damper structure is a effective method to make a balance between the fabrication cost and absorbing efficiency
The structure and absorbing efficiency

## Slide 9
11
Brazing experiment
1st experiment:
Check the ferrite property variation after high temperature heating.
Metallization temperature
Brazing experiment

## Slide 10
12
Data change before and after brazing experiment:
u” is more important for microwave absorptivity.
The u” change before and after brazing experiment is less than 5% ( including the test error between two test ).
The brazing process does not change the performance of ferrite obviously.
Brazing experiment
Chart: u''

## Slide 11
Brazing experiment
2nd experiment:
Braze ferrite on the copper plate
Failing brazing
Successful brazing

## Slide 12
频率 （GHz） |  | 
8.5 | 15 | 3.75
11 | 15 | 3.75
频率 （GHz） |  | 
8.5 | 15 | 3.75
11 | 15 | 3.75
High frequency, long wave, low reflection
Loss is proportional to frequency
In Ku band, though the may decrease, the absorbing efficiency will not decrease too much.
50%
Brazing experiment

## Slide 13
15
HOM absorber design method
Optimize the HOM absorber + taper:
Treat the HOM absorber + taper as a matched load
Separately design the HOM absorber + taper
Lower the S11 of this structure
Make the S11 trace around the origin of Smith Chart
Increase the design efficiency
HOM absorber + taper model
S11 in dB
S11 in Smith Chart
1st step

## Slide 14
16
Integral simulation of “cavity + HOM absorber + taper”:
Simulate the real HOM absorbing situation
Focus on monopole and dipole mode above 1.4GHz
Cavity + HOM absorber + taper model
absorber
TM111 mode E field, f=1.456GHz, Ql=56.7
Need further simulation for higher mode
Use the wakefield method to calculate impedance with absorber directly in PIC solver
HOM absorber design method
2nd step

## Slide 15
17
Cooperation details
Some new absorbing materials, such as SiC or AlN
Material test, such as , , thermal conductivity, electric conductivity, outgassing rate
Some new RF structure to increase the absorbing efficiency

## Slide 16
18
Thank you for your attention!!