## Slide 1: Achievement of Stable Pulsed Operation at 36 MV/m in STF-2 Cryomodule at KEK
Kirk
E. Kako, T. Shishido, K. Umemori, T. Kubo, T. Konomi, G. Park, T. Saeki, T. Dohmae, M. Egi, Kirk
T. Matsumoto, T. Miura, T. Takenaka, H. Nakai, Y. Kojima, K. Hara, T. Honma, K. Nakanishi, H. Shimizu
Preliminary version

## Slide 2: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 3: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 4: STF Cryomodules
STF Cavity Package
Proc. in IPAC16
Proc. in IPAC12
Proc. in SRF11
Proc. in SRF09
STF-1 (4 cavities) in 2008
Quantum Beam (2 cavities) in 2012
Capture CM in STF-2 accelerator
S1-Global (4+4 cavities) in 2010
STF-2 (12 cavities) in 2014~
4 cavities per batch

## Slide 5: Brief History for STF-2 Cryomodule
Date | Content
2011 ~ 2013 | V.T. for 12 cavities / RF conditioning for 12 couplers
Jun/2013 | Cleaning up STF tunnel
Jul/2013 ~ Apr/2014 | Cavity string assembly (three times)
Oct/2013 ~ Jan/2014 | Module assembly (CM1/CM2a)
Jul/2014 | Complete certification for High pressure Gas Code
Oct/2014 ~ Dec/2014 | 1st cool-down / low power test
Apr/2015 ~ Jul/2015 | 5MW Klystron / Single waveguide system completed
Jul/2015 ~ Sep/2015 | Coupler conditioning at room temperature
Oct/2015 ~ Dec/2015 | 2nd cool-down / high power test (cavity performance check)
Jan/2016 ~ Jul/2016 | Multi-beam Klystron & Waveguide system completed
Jul/2016 ~ Sep/2016 | Coupler conditioning at room temperature
Sep/2016 ~ Nov/2016 | 3rd cool-down / LFD, Q0 measurement, 8 Cavities Operation & LLRF study
2017 | No plan for cool-down test
F.Y. 2018 | 4th cool-down test (?)
F.Y. 2018 ~ | Beamline construction / Beam operation starts (?)

## Slide 6: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 7
Capture CM
(Two cavities)
CM1 + CM2a
(Twelve cavities)
STF-2 Accelerator Layout
To be constructed
Cold box
Cold box
RF Gun
Chicane
To be constructed
View from upstream
View from downstream
Waveguide system

## Slide 8: Construction of STF-2 Cryomodule
Cavity string
Installation into tunnel
Beampipe connection between cavity strings
Alignment
(laser tracker)
Installation into cryo-vessel
Pumping/leak check
Construction completed after HPG certification
Cryomodule connection

## Slide 9: Complicated situation in CM construction
Three cavity strings (4+4+4=12)
Four cryo-vessels (1/3+1/3+1/3+1/2=1.5)
five support posts (3+2=5)
constructed on ground floor
Four cavities per string
Tunnel hatch for half-size cryomodule
Construction of half-size cryomodule
constructed in tunnel
1/3 cryo-vessel
1/3 cryo-vessel
1/3 cryo-vessel
1/2 cryo-vessel
CM2a was constructed by the same way as S1-Global
1+1/2 cryomodule

## Slide 10: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 11
Summary of Cavity Performance
Not measured in 3rd C.T.
Significantly degraded in 3rd C.T.
Kt for CAV#1 and #8 was never changed!

## Slide 12
Change of Cavity Performance in STF-2
Not measured cavities in 3rd C.T.
Uniformly degraded!
All measured cavities in Capture/STF-2 CMs had performance degradation again!
There maybe some risk for performance degradation in higher gradient operation.
2nd cooldown test
3rd cooldown test
RF conditioning by short pulse should be tried again!

## Slide 13: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 14
Positions of radiation detector
We can move these detectors
to below each cavity
upstream
cavity
downstream
upstream
cavity
downstream

## Slide 15
X-rays measurement
CAV5, 6, 7, and 9 not tested in 3rd cooldown
CAV1 had no x-rays in last V.T.
A little bit higher gradient in 3rd test as resulting from RF conditioning
CAV5, 6, 7, and 9 not reached 31.5 MV/m in 2nd cooldown
CAV10 and 12 not reached 31.5 MV/m in 3rd cooldown
Almost same level between 2nd and 3rd test
Onset Gradient
X-rays @31.5MV/m

## Slide 16
X-rays comparison for both-end cavities
upstream
below CAV1
upstream
below CAV1
below CAV12
downstream
below CAV12
downstream
Same radiation level between 2nd and 3rd cooldown test!

## Slide 17: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 18: Trend graph during the heat load measurement
Measurement cycle: dynamic heat load  detuned heat load  static heat load
Heat load in cavity
Heat load in coupler

## Slide 19: Trend graph during the heat load measurement
We can estimate the heat load from the helium mass flow rate.
The heating around the power coupler did not disappear by the next day.

## Slide 20: Error Estimation in Q0 Measurement
Reproducibility of Static Heat Load
  0.36 [W] on average for 28 times measurements
Distribution of Helium Mass Flow
  3.9% on maximum for every heat load measurement
Stability in Accelerating Gradient for Flat-top of Pulse
  0.05% (very stable)
Stability in RF Duty Factor
  0.85% (stable)
Latent Heat of Vaporization
  Negligible small
Helium Mass Flow Meter
  ±0.3% according to spec. sheet
  Calibrated by heater in STF-2

## Slide 21: Comparison of Q0 – Eacc and X-rays
The both results are contradictory!
Heavy field emission
Cavity #1
Cavity #8
Cavity #2
Cavity #12
Lower Q0 may depend on cooldown rate (@LCWS2016)  Will be tried in next cool-down test
Heater is used as calibration
Q0 is estimated from helium mass flow

## Slide 22: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 23: Result of Lorentz Detuning Measurement
S1-Global
STF-2
Capture CM
The STF cavity has more stiffness than TESLA cavity.
Thicker titanium end plate

## Slide 24: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 25: Performance Degradation
Statistics for cavity performance;
Above 31.5 MV/m: 11 cavities
Degradation: 4 cavities
Three types of performance limit;
One cavity: Quench w/o F.E.
Two cavities: F.E. Quench
One cavity: Quench by enormous heat loss
Three degraded cavities in STF-2 are connected in series.
 Common cause for degradation
Q0 measurement is not done yet in STF-2.
It will start from this autumn.
Statistics for cavity string (four cavities per batch);
Four cavity strings: No degradation
Quantum Beam: Degradation, but around ILC spec.
CM-1b in STF-2: Significant degradation
Heavy F.E. in V.T.
22 cavities in 6 cavity strings

## Slide 26
Cavity string/Beam pipe connection in clean booth
Ion pump
Ion pump
Use of simply local clean booth
  Local clean booth was used for four beampipe connection parts
Exchange of metal valve near cavity string #2
  Metal valve was a little bit bigger, disturbed thermal shield attachment
Extra Argon gas purging at gate valve opened
  Usually, when gate valve opens, both sides should be under vacuum
  but, we had to do Argon gas purging for the both sides
  due to complicated process of cryomodule assembly
Local clean booth
Three degraded cavities in series
A little bit bigger metal valve

## Slide 27: Improvement of clean room items
High quality local clean booth
High quality particle counter
Slow pumping system
Will be introduced in 2017(?)
Many experiences in EU-XFEL
Local clean booth
Local clean booth
Particle counter
Slow pumping unit

## Slide 28: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 29: RF System changed from 2015 to 2016
Single Cavity Operation in 2015
8 Cavities Operation in 2016
Klystron
Waveguide
Circulator
LLRF modules
800kW Klystron
(Distributed RF System)
10MW Multi-beam Klystron

## Slide 30: Too High Forward Power distributed
After optimization of LLRF control, forward power was drastically reduced!
Red: Gradient
Blue: Forward Power
Green: Reflect Power
Bump in RF filling disappeared after parameter optimization!
Max. level changed from 400 to 260kW.
We have never observed strange phenomena in vacuum level during this operation.

## Slide 31: Earthquake? (Unbelievable, but…)
Date | Magnitude | Level in Tsukuba city
11/Mar/2011 14:46 | M7.9 | Level 6
14/Mar/2012 21:05 | M6.1 | Level 4
28/Jan/2013 3:41 | M4.9 | Level 3
20/Sep/2013 2:25 | M5.9 | Level 3
10/Nov/2013 7:37 | M5.5 | Level 4
31/Dec/2013 10:03 | M5.4 | Level 3
16/Sep/2014 12:28 | M5.6 | Level 4
25/May/2015 14:28 | M5.5 | Level 4
12/Sep/2015 5:49 | M5.2 | Level 3
16/May/2016 21:23 | M5.5 | Level 4
27/Jul/2016 23:47 | M5.4 | Level 3
22/Nov/2016 5:59 | M7.4 | Level 4
28/Dec/2016 21:38 | M6.3 | Level 4
1st cooldown test in STF-2 CM
2nd cooldown test in STF-2 CM
3rd cooldown test in STF-2 CM
In E-XFEL, G-shock sensor has been used for cryomodule transportation. Max. recorded shock was 6G! But, they observed no performance change in cryomodule test. In STF, data logging by G-shock sensor may be necessary.

## Slide 32: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 33: Vector-sum Operation with 8 Cavities
Eacc
φ
Eacc @flat-top
Eacc @end
φ @end
Eacc distribution

## Slide 34: Vector-sum Operation with 8 Cavities
30 min
35.9 MV/m
35.7 MV/m
31.8 MV/m
28.3 MV/m
30.6 MV/m
27.3 MV/m
30.1 MV/m
27.8 MV/m
30.9 MV/m ± 0.02 MV/m
46Hz ± 1.8Hz
Each pulse for 8 cavities
Trend graph of Ave. Eacc and Δf
during vector-sum operation
They satisfy the ILC specification!

## Slide 35: Outline
History of STF-2 project
Construction of STF-2 cryomodule
Performance for each item
  Accelerating gradient
  X-rays
  Heat load
  Lorentz detuning
Consideration of degradation
  Last V.T.  2nd Cool-down test
  2nd Cool-down test  3rd Cool-down test
Vector-sum operation @31 MV/m
Summary

## Slide 36: Summary for STF-2 Cryomodule
STF-2 Cryomodule was constructed, installed and tested since 2013
  Cavity string assembly in clean room was completely done
  Construction and alignment work were completely done
  Passed HPC without problem
  Cooldown tests have been done totally three times
2nd cooldown test in F.Y. 2015
  Performance check by single cavity operation
  Eight cavities achieved above 31.5 MV/m
  Three significantly degraded cavities by heavy field emission/enormous heat load
  Necessary for improving quality of local clean booth, pumping system, and assembly work
3rd cooldown test in F.Y. 2016
  Performance check by 8 cavities operation
  “More” degraded cavities during testing cryomodule (first observation in STF)
  Uniformly lower Q0-value, irrespective of field emission (cooldown rate?)
  There maybe some risk for performance degradation in higher gradient operation

## Slide 37: Items in 4th Cooldown Test
Change of cool-down method (like FNAL)
Re-check cavity performance and x-rays including kt
More Precise Heat Load Measurement for Cavity
  Disconnected Capture CM
  Disconnected Q-Magnet
Precise Heat Load Measurement at Power Coupler
Microphonic Measurement during high gradient operation

## Slide 38: Toward next steps…
Waveguide/Circulator system will be added for remaining four cavities
Beamline construction will be done
Beam dump will be constructed
RF Gun / Laser system will be reconstructed
LLRF modules will be more added
DAQ/Monitoring system will be updated
12 (STF-2 CMs) + 2 (Injector CM) Cavities operation will be done
Beam commissioning will be done
Final goal for STF-2

## Slide 39
Thank you very much for your attention!
I will “more” improve my slide in SRF2017.
青磁茶碗 銘馬蝗絆

## Slide 40: Back-up slides

## Slide 41: Performance in Vertical Test
Q0 vs. Eacc Curve
Accelerating Gradient
ILC spec.: 35 MV/m ± 20%
8 cavities in STF-2 CM1 achieved above 35 MV/m
  Average gradient: 36.8 MV/m
After MHI-23, mass-production scheme was used
  Workers, EBW machine, EBW method were changed
HIT-02 achieved around 41 MV/m
  EBW was done in MIRAPRO
TOS-02 (w/o HOM couplers) achieved around 36 MV/m
  EBW was done in TOSEI
MHI-C (mass-production type) achieved around 37 MV/m
Capture CM
STF-2 CM1
STF-2 CM2a
STF-2 CM2b
Average Gradient
Capture CM: 36.5 MV/m
↓
STF-2 CM1: 36.7 MV/m
↓
STF-2 CM2a: 28.0 MV/m
↓
STF-2 CM2b: 29.2 MV/m
Mass-production scheme
Mass-production
scheme

## Slide 42: Accelerating gradient in Last V.T.
9 cavities: > 35 MV/m
11 cavities: > 28 MV/m

## Slide 43
Method of RF Conditioning in 2K
Summary of cavity conditioning time in 2K
Temp. sensor at HOM coupler
Cavity conditioning is done very carefully as monitoring
HOM heating, unusual RF output from HOM, and X-rays.
When heating, unusual output or x-rays appear,
we have to keep the gradient level for a while.
After processing out, we can go to next level.
Conditioning time was too short?
RF parameters in STF-2
QL : 5.0 x 106
Filling time : 900μsec
Flat-top : 800(100)μsec
Total width : 1700μsec

## Slide 44: Various clean booths in DESY
There are totally eight kinds of clean booth in the following figures.
DESY people uses clean booth optimized for each location of cavity/cryomodule.

## Slide 45
Cavity performance in CM1/CM2a
Module # | CM1 |  |  |  |  |  |  |  | CM2a |  |  | 
String # | 1 |  |  |  | 2 |  |  |  | 3 |  |  | 
Cavity # | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Cavity name | MHI-14 | MHI-15 | MHI-17 | MHI-18 | MHI-19 | MHI-20 | MHI-21 | MHI-22 | MHI-24 | MHI-23 | MHI-25 | MHI-26
Eacc @Last V.T. [MV/m] | >36.6 (power limit) | 35.7 (Cell#1 Quench) | >38.4 (power limit) | >36.2 (power limit) | 37.2 (Cell#1 Quench) | >35.1 (power limit) | >38.9 (power limit) | >35.8 (power limit) | >12.0 (admin. stop) | 35.9 (Cell#3 Quench) | 32.3 (Cell#1 Quench) | 31.6 (Cell#1 Quench)
Eacc @2nd cooldown test (short pulse) [MV/m] | >38.6 (admin. stop) | 36.8 (Quench) | 35.2 (Quench) | >36.1 (Pf max.) | 26.6 (Quench) | 20.0 (Quench) | 25.0 (Quench) | >36.2 (admin. stop) | >18.0 (admin. stop) | 33.6 (Quench) | 32.1 (Quench) | 31.5 (Quench)
Eacc @2nd cooldown test (full pulse) [MV/m] | >38.7 (admin. stop) | 36.7 (Quench) | 35.3 (Quench) | >36.3 (admin. stop) | >26.0 (admin. stop) | 16.4 (Quench) | 24.6 (Quench) | >32.3 (admin. stop) | >18.1 (admin. stop) | 34.1 (Quench) | 33.2 (Quench) | 32.4 (Quench)
Eacc @3rd cooldown test (full pulse) [MV/m] | >36.8 (admin. stop) | 36.4 (Quench) | 33.4 (Quench) | 35.428.0 (Quench) |  |  |  | 31.6 (Quench) |  | 31.527.7 (Quench) | 31.5 (Quench) | 30.826.8 (Quench)
モジュール試験では8空洞が31.5 MV/mに到達した。
25 MV/m以上にすると9空洞が到達したことになる。

## Slide 46
Cavity performance in Capture CM
Module # | Capture | 
String # | 1 | 
Cavity # | 1 | 2
Cavity name | MHI-12 | MHI-13
Eacc @Last V.T. [MV/m] | >40.7 (power limit) | 32.2 (Cell#2 Quench, Heavy F.E.)
Eacc in 2012 (600μs) [MV/m] | 35.3 (Quench) | 32.5 (Quench)
Eacc in 2012 (1500μs) [MV/m] | 30.6 (Quench) | 32.2 (Quench)
Eacc in 2016 (1650μs) [MV/m] | 28.7 (Quench) | 29.8 (Quench)
Capture CMについては、31.5 MV/m以上は1空洞で、25 MV/mだと両空洞ともに到達している。

## Slide 47
Radiation Level at Last V.T. in STF-2
※ MHI-14(CAV1)のみ放射線は無かった
※ MHI-24(CAV9)は４回測定したが、状況が改善しなかったためそのままモジュールに組み込んだ

## Slide 48: Comparison of radiation level in STF-2 CM
2nd Cooldown Test in 2015
3rd Cooldown Test in 2016
MAR-781/-782
空洞直下で測定した放射線量の結果(ただしCavity#10以降は固定)。
去年と今年の放射線量の比較を示す。今年は８空洞のみの運転である。
全体的に放射線量に変化は見られない。むしろ若干下がっている。
エージングの効果か、測定場所の微妙な違いによるものか。
ただし、放射線量はQ0測定時のもので、8空洞運転時には評価していない
（空洞性能劣化後の放射線は測定していない）

## Slide 49: Comparison of radiation level in STF-2 CM
2nd Cooldown Test in 2015
3rd Cooldown Test in 2016
MAR-781/-782
空洞直下で測定した放射線量の結果(ただしCavity#10以降は固定)。
去年と今年の放射線量の比較を示す。今年は８空洞のみの運転である。
全体的に放射線量に変化は見られない。むしろ若干下がっている。
エージングの効果か、測定場所の微妙な違いによるものか。
ただし、放射線量はQ0測定時のもので、8空洞運転時には評価していない
（空洞性能劣化後の放射線は測定していない）

## Slide 50: Comparison of radiation level in STF-2 CM
Cavity #1
Cavity #2
Cavity #3
Cavity #4
放射線量は去年と同じかむしろ下がっているように見える
エージングの効果かあるいは測定位置の微妙な違いによるものか

## Slide 51: Comparison of radiation level in STF-2 CM
Cavity #8
Cavity #10
Cavity #11
Cavity #12
放射線量は去年と同じかむしろ下がっているように見える
エージングの効果かあるいは測定位置の微妙な違いによるものか

## Slide 52: Comparison of radiation level in STF-2 CM
Cavity #1
@below CM
Cavity #1
@beampipe
Cavity #12
@below CM
Cavity #12
@beampipe
モジュール両端にある空洞のみビームパイプに取り付けられたモニターでも比較してみたが、去年と特に変わっていなかった。
モジュール両端のモニターの取り付け位置は変わっていないため放射線量も変わっていないものと思われる。

## Slide 53
Neutron/Gamma detectors added later…
upstream
downstream
Radiation center in KEK measured neutron and gamma.
And, they analyzed the energy spectrum by NaI.
The detailed result will be presented in next LCWS/SRF?
Highest sensitivity!
Energy spectrum in 8 cavities operation
T. Sanami / T. Oyama

## Slide 54: Helium Flow to Q0 Estimation
Assumption; Helium temperature (2.0 [K]) estimated from helium gas pressure (3 [kPa])
Volume of Ideal gas per mol: 22.4 [ℓ/mol]
Molecular weight of helium: 4.0 [g/mol]
Latent heat of vaporization: 93.0 [J/mol] = 23.3 [J/g] = 4.2 [J/ℓ]
Observation; Helium flow: 30.0 [m3/h], Helium pressure: 2.99 [kPa], Helium temperature: 1.70 [K],
Helium temperature at mass flow meter: 23 [℃]
Eacc: 28.0, 31.5, 35.0 [MV/m]
Dissipated Heat Load including Static Heat Load (example); 30.0 [m3/h] x 4.2 [J/ℓ] = 35 [W=J/s]
RF Duty Factor: 0.81-0.86 % (from Pulse Analysis) Not constant!
Formula for Q0 Estimation ; Eacc = 30.8 x Sqrt(P0 x Q0)
Contents to be considered; Stability in Static Heat Load: Main Systematic Error
Stability in Accelerating Gradient: To be checked by Pulse Analysis
Precise RF Duty Factor: To be checked by Pulse Analysis
Precise Latent Heat of Vaporization: To be estimated by HEPAK code
† Ohuchi-san estimated Heat Load by HEPAK in STF-1 Cryomodule
‡ Nakai-san got HEPAK recently, and we can use it for this analysis
Helium Pressure in Return Line: Not measured yet, but to be monitored
Specification for Helium Mass Flow Meter: Dependence on Temperature (±0.3%)

## Slide 55: Comparison of Q0 – Eacc Curve in STF-2 CMs
中心値が一様に下がっているように見えるが、放射線量を見るとそれほど出ているようにも見えないので、まだ理解できていない効果があるものと思われる。

## Slide 56: Comparison of Q0 – Eacc Curve in STF-2 CMs
中心値が一様に下がっているように見えるが、放射線量を見るとそれほど出ているようにも見えないので、まだ理解できていない効果があるものと思われる。

## Slide 57: Summary of Static Heat Load
Static Heat Load / module @2K [W] |  |  |  | 
Real Data |  | TDR |  | 
Capture CM | STF-2 CM | SUM | Coupler | Support
10.5 (9.2) | 23.0 | 1.32 | 0.17 | 0.60
※ TDRの数値はVol. 3, Part II, pp.46 にあるTable 3.9より引用
† Static Heat Loadに含まれるものは、サポートポスト、カプラ、マグネットなどである
  TDRとの相違点は、空洞(カプラ)台数、サポートポストの数、4極電磁石、ケーブル本数など
参考値: Static Heat Load / module @2K [W] |  |  |  |  | 
S1-Global | PXFEL 1 | PXFEL 2 | PXFEL 3 | XM-3 | Calculated
7.2 | 9.9 | 5.9 | 6.4 | 6.4 | 2.0
※ S1-Globalの値はS1-Global Reportより、E-XFELの値はSRF2013のプロシーディングより引用
※ STF-2モジュールのStatic heat loadはおおよそ10W程度と予想している（次回冷却試験にて確認）
※ E-XFELの100モジュールの結果は諸事情により開示不可

## Slide 58: Summary of Static Heat Load
Static Heat Load / module @2K [W] |  |  |  | 
Real Data |  | TDR |  | 
Capture CM | STF-2 CM | SUM | Coupler | Support
10.5 (9.2) | 23.0 | 1.32 | 0.17 | 0.60
※ TDRの数値はVol. 3, Part II, pp.46 にあるTable 3.9より引用
† Static Heat Loadに含まれるものは、サポートポスト、カプラ、マグネットなどである
今回の測定と比較できるところ
(HOM absorberは含まれていない)

## Slide 59: Difference in Copper Plating
Module | CM1 |  |  |  |  |  |  |  | CM2a |  |  | 
Coupler # | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Cold coupler |  |  |  |  |  |  |  |  |  |  |  | 
Copper plating [μm] | 20 (inner) | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 25 | 25 | 25 | 25
 | 3 (outer) | 3 | 3 | 3 | 5 | 5 | 5 | 5 | 10 | 10 | 10 | 10
Warm coupler |  |  |  |  |  |  |  |  |  |  |  | 
Copper plating [μm] | 10 (inner) | 10 | 10 | 10 | 20 | 20 | 20 | 20 | 25 | 25 | 25 | 25
 | 10 (outer) | 10 | 10 | 10 | 20 | 20 | 20 | 20 | 25 | 25 | 25 | 25
Gold strike plating
Nickel strike plating
外導体の銅鍍金厚が10μmであるということはp.36に明記されている。

## Slide 60: Temperature Status @Power Coupler
Input Port
Input Flange
Input Anchor
Coupler #8の温度計はノイズがひどいため
精確に測定されていない可能性あり
鍍金厚みの違いははっきり見えなかった

## Slide 61: Simultaneous Operation with 8 Cavities
Run 1
Run 2
Run 3
11/25に行った８空洞同時運転の３回のRunの結果を示す。
それぞれ上から最大加速勾配、平均加速勾配、加速勾配のばらつき、離調周波数、
の８空洞平均である。Run 3が平均加速勾配が最も高いものである。
30 min

## Slide 62: Simultaneous Operation with 8 Cavities
Run 1
Run 2
Run 3
前ページの結果で、平均加速勾配と離調周波数のヒストグラムを取ったものである。
Run 3では、平均加速勾配のふらつきは0.02MV/mで、
離調周波数の平均値は46Hzで、ふらつきは1.8Hzであることがわかる。

## Slide 63
Stiffness of Cavity Sys. 72 kN/mm 22 kN/mm
Lorentz Detuning D f = - 150 Hz D f = - 500 Hz
at flat-top
TTF Cavity
Thick Titanium Baseplate,
Thick Nb Beam Tube & Thick Nb End-cell
STF Baseline Cavity
Cell Taper
13 deg. → 10 deg.
Input Port
f40 → f60
STF Baseline Cavity
TTF Cavity
Magnetic shield
Estimation
at 31.5 MV/m
Beam Tube
f78 → f84

## Slide 64: Specification of Tuner/Piezo in STF-2
Tuner type | Slide-jack
# of Tuner/Piezo | 12
Attachment Position | Center (String 1, 3) / End (String 2)
Frequency range | ~530kHz
Cavity expansion | ~2.2mm
Piezo Max. voltage | 1000V (500V@opr.)
Frequency range | >200Hz
center type
end type
Piezo
Tuner

## Slide 65: Replacement of Piezo in Cryomodule
After this trouble, we replaced Piezo.

## Slide 66: Alignment work for STF-2 CMs
S. Araki
Cat’s eye
Laser tracking system
Courtesy of S. Araki
Stand for cat’s eye near cavity

## Slide 67: Result of cavity alignment
CM1 Horizontal
CM2a Horizontal
CM1 Vertical
CM2a Vertical
ILC spec.
ILC spec.
Alignment result satisfied the ILC specification!
Courtesy of S. Araki
16 points are measured for 8 cavities

## Slide 68: Result of cryomodule alignment
Horizontal
Vertical
ILC spec.
ILC spec.
Courtesy of S. Araki
Alignment result satisfied the ILC specification!
5 points are measured for 5 support posts

## Slide 69: 1+1/2 Gas Return Pipe
Full-size gas return pipe
Half-size gas return pipe

## Slide 70: Construction of STF-2 CM1①
Cavity string installation
Lining two cavity strings on rail
Attachment of thermal shield
Leveling gas return pipe

## Slide 71: Construction of STF-2 CM1②
Q-magnet attachment
(collaboration with FNAL)
Attachment of thermal shield
Carrying cryo-vessels
Installation into cryo-vessel

## Slide 72: Construction of STF-2 CM1③
Putting CM1 along beamline
Putting CM2a along beamline
Connecting CM1 and CM2a
Integrated leak check
Adjustment of position
Construction finished

## Slide 73
Change of Kt in STF
During jointing helium tank after V.T., these cavities in STF-2 were deformed?