## Slide 1
“Ver. 0”
for KEK-IHEP meeting at Beijing
July 15

## Slide 2
Takayuki Kubo and Alex Gurevich
20min
A unified theory of
surface resistance and the residual resistance of SRF cavities at low temperatures
Old Dominion University, Department of Physics and Center for Accelerator Science,
Norfolk, VA 23529, USA
KEK / SOKENDAI
Tsukuba, Japan
#17H04839
Supported by NSF under grant # 100492-010

## Slide 3
Typical behavior of
Nb cavities
Surface resistance of Nb cavity

## Slide 4
Surface resistance of Nb cavity
Mattis-Bardeen
Typical behavior of
Nb cavities
D. C. Mattis and J. Bardeen, Phys. Rev. 111, 412 (1958).

## Slide 5
Surface resistance of Nb cavity
Mattis-Bardeen
Typical behavior of
Nb cavities
Residual
resistance
D. C. Mattis and J. Bardeen, Phys. Rev. 111, 412 (1958).

## Slide 6
To explain this shift,
we have summed different contributions so far
: Mattis-Bardeen surface resistance

## Slide 7
To explain this shift,
we have summed different contributions so far
: Mattis-Bardeen surface resistance
: other than the above
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
: trapped flux contribution
A. Gurevich and G. Ciovati, Phys. Rev. B 87, 054502 (2013).

## Slide 8
To explain this shift,
we have summed different contributions so far
: Mattis-Bardeen surface resistance
: others
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
: trapped flux contribution
A. Gurevich and G. Ciovati, Phys. Rev. B 87, 054502 (2013).

## Slide 9
To explain this shift,
we have summed different contributions so far
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
Rs = RMB +Rflux + …

## Slide 10
Rs = RMB +Rflux + …
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
Today, Rflux can be substantially reduced by cooling down a cavity with a large temperature gradient.
A. Romanenko, et al., Appl. Phys. Lett. 105, 234103 (2014).
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
S. Huang, T. Kubo, and R. Geng, Phys. Rev. Accel. Beams 19, 082001 (2016)

## Slide 11
Rs = RMB +Rflux + …
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
Today, Rflux can be substantially reduced by cooling down a cavity with a large temperature gradient.
A. Romanenko, et al., Appl. Phys. Lett. 105, 234103 (2014).
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
S. Huang, T. Kubo, and R. Geng, Phys. Rev. Accel. Beams 19, 082001 (2016)
Understanding this part is becoming important more and more!

## Slide 12
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
3min
We incorporate these effects based on the BCS theory.

## Slide 13
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
Rs=Runified+Rflux+ …
Runified
We will obtain a theory that unifies RMB and the effects of real material.
3min

## Slide 14
The unified theory will be a basis of microscopic understanding on surface processing technologies:
Provides us with clues to understanding what makes the differences of the low field Rs among

## Slide 15
Provides us with clues to understanding what makes the differences of the low field Rs among
EP only
The unified theory will be a basis of microscopic understanding on surface processing technologies:

## Slide 16
Provides us with clues to understanding what makes the differences of the low field Rs among
EP only
EP + 120℃ baking
The unified theory will be a basis of microscopic understanding on surface processing technologies:

## Slide 17
Provides us with clues to understanding what makes the differences of the low field Rs among
EP only
EP + 120℃ baking
Nitrogen doping
The unified theory will be a basis of microscopic understanding on surface processing technologies:

## Slide 18
Provides us with clues to understanding what makes the differences of the low field Rs among
EP only
EP + 120℃ baking
Nitrogen doping
Nitrogen infusion
Etc
The unified theory will be a basis of microscopic understanding on surface processing technologies:

## Slide 19
Provides us with clues to understanding what makes the differences of the low field Rs among
EP only
EP + 120℃ baking
Nitrogen doping
Nitrogen infusion
Etc
and tells how to engineer the surface to tune Rs
The unified theory will be a basis of microscopic understanding on surface processing technologies:

## Slide 20
Provides us with clues to understanding what makes the differences of the low field Rs among
EP only
EP + 120℃ baking
Nitrogen doping
Nitrogen infusion
Etc
and tells how to engineer the surface to tune Rs
The unified theory will be a basis of microscopic understanding on surface processing technologies:
It should be noted that
we do not propose
“a new BCS” or “new MB”:
we incorporate
the realistic surface and bulk broadening of the gap peaks
based on the BCS theory.

## Slide 21
Overview

## Slide 22
BCS model of
SC with an idealized surface
If we start from
Strategy

## Slide 23
Mattis-Bardeen
If we start from
Strategy
BCS model of
SC with an idealized surface

## Slide 24
Mattis-Bardeen
If we start from
Strategy
BCS model of
SC with an idealized surface

## Slide 25
BCS model of
SC with an idealized surface
Mattis-Bardeen
If we start from
Fails
Strategy

## Slide 26
BCS model of
SC with an idealized surface
Mattis-Bardeen
If we start from
BCS model of
a more realistic SC
We start from
Fails
Strategy

## Slide 27
BCS model of
SC with an idealized surface
Mattis-Bardeen
If we start from
We start from
A theory beyond the Mattis-Bardeen
Fails
Strategy
BCS model of
a more realistic SC

## Slide 28
BCS model of
SC with an idealized surface
Mattis-Bardeen
If we start from
We start from
A theory beyond the Mattis-Bardeen
Fails
Strategy
BCS model of
a more realistic SC
Would contain Rres and
lead us to deeper understanding on Rs

## Slide 29
“More realistic” SC

## Slide 30
bulk superconductor
(e.g., Nb)
“More realistic” SC

## Slide 31
bulk superconductor
(e.g., Nb)
normal conductor with thickness d<<ξ
(e.g., damaged Nb or
metallic sub-oxide with a few nm thickness)
“More realistic” SC

## Slide 32
bulk superconductor
(e.g., Nb)
Proximity
effect
normal conductor with thickness d<<ξ
(e.g., damaged Nb or
metallic sub-oxide with a few nm thickness)
“More realistic” SC

## Slide 33
“More realistic” SC
Main physical parameters

## Slide 34
“More realistic” SC
Main physical parameters
Normal layer thickness

## Slide 35
“More realistic” SC
Main physical parameters
Normal layer thickness
Normal conductance
for N layer
Normal conductance
for SC region

## Slide 36
“More realistic” SC
Main physical parameters
Normal layer thickness
Normal conductance
for N layer
Normal conductance
for SC region
Interface
resistance

## Slide 37
Theoretical tool
We use the quasiclassical theory in the diffusive limit.
Usadel equation

## Slide 38
Theoretical tool
We use the quasiclassical theory in the diffusive limit.
Self-consistency condition
Usadel equation
Boundary conditions
where
K. D. Usadel, Phys. Rev. Lett. 25, 507 (1970).
M. Yu. Kuprianov and V. F. Lukichev, Sov. Phys. JETP 67, 1163 (1988).

## Slide 39
Theoretical tool
We use the quasiclassical theory in the diffusive limit.
Normal and anomalous
Quasiclassical Matsubara Green functions
Self-consistency condition
Usadel equation
Boundary conditions
where
K. D. Usadel, Phys. Rev. Lett. 25, 507 (1970).
M. Yu. Kuprianov and V. F. Lukichev, Sov. Phys. JETP 67, 1163 (1988).
T. Matsubara, Prog. Theor. Phys. 14, 351 (1955).

## Slide 40
Theoretical tool
We use the quasiclassical theory in the diffusive limit.
Normal and anomalous
Quasiclassical Matsubara Green functions
Self-consistency condition
Usadel equation
Boundary conditions
where
Retarded normal and anomalous
Quasiclassical Green functions
K. D. Usadel, Phys. Rev. Lett. 25, 507 (1970).
M. Yu. Kuprianov and V. F. Lukichev, Sov. Phys. JETP 67, 1163 (1988).
T. Matsubara, Prog. Theor. Phys. 14, 351 (1955).

## Slide 41
Theoretical tool
We use the quasiclassical theory in the diffusive limit.
Normal and anomalous
Quasiclassical Matsubara Green functions
Self-consistency condition
Usadel equation
Boundary conditions
where
Retarded normal and anomalous
Quasiclassical Green functions
Physical quantities: Density of states and surface resistance
+2.5min
->5.5min
K. D. Usadel, Phys. Rev. Lett. 25, 507 (1970).
M. Yu. Kuprianov and V. F. Lukichev, Sov. Phys. JETP 67, 1163 (1988).
T. Matsubara, Prog. Theor. Phys. 14, 351 (1955).

## Slide 42
Results

## Slide 43
DOS of Normal conductor
Density of states: n=Re[GR]

## Slide 44
DOS of Normal conductor
DOS of BCS superconductor
Density of states: n=Re[GR]

## Slide 45
BCS
superconductor
Normal
conductor
DOS of
Normal conductor
DOS of
BCS superconductor

## Slide 46
BCS
superconductor
Normal
conductor
?
?
DOS of
Normal conductor
DOS of
BCS superconductor
N-side DOS
S-side DOS

## Slide 47
?
?
Conductance ratio
between N and S
Barrier between N and S
N-side DOS
S-side DOS
The proximity effect depends on the boundary parameters

## Slide 48
N-side
DOS
S-side
DOS
minigap

## Slide 49
N-side
DOS
S-side
DOS
minigap

## Slide 50
N-side
DOS
S-side
DOS
minigap

## Slide 51
(Isolated)
Superconductor
with Γ=0.03
(Isolated)
Normal
conductor
So far, we have neglected the bulk DOS broadening (due to an inlelastic scattering, magnetic impurities, random inhomogeneities of the BCS pairing constant etc).
Further realistic results can be obtained by introducing a finite DOS broadening parameter Γ

## Slide 52
N-side
DOS
S-side
DOS
Γ=0.03
β=10
β=1
β=0.1
+4min
=>9.5min
Minigap with
subgap states

## Slide 53
Surface resistance
Now we can calculate the surface resistance of the proximity coupled NS system taking the minigap induced at the N layer into account.
microwave

## Slide 54
Surface resistance
Quasiparticles
minigap
Quasiparticles
gap
Now we can calculate the surface resistance of the proximity coupled NS system taking the minigap induced at the N layer into account.
microwave

## Slide 55
Surface resistance
Quasiparticles
minigap
Quasiparticles
gap
microwave
General
formula
A. Gurevich, Phys. Rev. Lett.
A. Gurevich, Supercond. Sci. Technol. 30, 034004 (2017).

## Slide 56
Surface resistance
Quasiparticles
minigap
Quasiparticles
gap
microwave
N layer
contribution
Bulk S
contribution
Approximate formula
(for α<<1 and Γ→0)

## Slide 57
Surface resistance
N layer
contribution
Bulk S
contribution
The first term is tiny due to its small thickness and small normal-conductivity.
Approximate formula
(for α<<1 and Γ→0)

## Slide 58
Surface resistance
N layer
contribution
Bulk S
contribution
The first term is tiny due to its small thickness and small normal-conductivity.
As T decreases, the second term decreases rapidly rather than the first term due to its large gap.
Approximate formula
(for α<<1 and Γ→0)

## Slide 59
Surface resistance
Approximate formula
(for α<<1 and Γ→0)
N layer
contribution
Bulk S
contribution
The first term is tiny due to its small thickness and small normal-conductivity.
As T decreases, the second term decreases rapidly rather than the first term due to its large gap.
At a low temperature, the first term becomes dominant, which looks like the residual resistance.

## Slide 60
Surface resistance
N layer
contribution
Bulk S
contribution
We will have
N layer
contribution
Bulk S contribution
Approximate formula
(for α<<1 and Γ→0)

## Slide 61
Surface resistance
N layer
contribution
Bulk S
contribution
We will have
Approximate formula
(for α<<1 and Γ→0)

## Slide 62
Surface resistance
We will have
Approximate formula
(for α<<1 and Γ→0)

## Slide 63
Surface resistance
Approximate formula (for finite Γ)
As the DOS broadening parameter increases, the subgap state contribution pushes up the residual resistance.
pushed up

## Slide 64
Surface resistance: example
α=0.1
Γ=0.03
β=10
β=0.1

## Slide 65
Surface resistance: example
α=0.1
Γ=0.03
β=10
β=0.1
Residual resistance!

## Slide 66
Surface resistance: example
α=0.1
Γ=0.03
β=0.1
In particular, this yields a realistic Rs and

## Slide 67
Surface resistance: example
α=0.1
Γ=0.03
β=0.1
A realistic DOS at the top layer
Note that this is N layer DOS!

## Slide 68
Tune the surface layer
towards higher Q at 2K

## Slide 69
α=0.1
Γ=0.03
β=0.1
β=0.01
β=3
β=10

## Slide 70
α=0.1
Γ=0.03
β=10
β=0.1
β=0.01
β=3
At

## Slide 71
β=10
β=0.1
β=0.01
β=3

## Slide 72
β=10
β=0.1
β=0.01
β=3

## Slide 73
β=10
β=0.1
β=0.01
β=3
A larger β induce a broaden DOS peak, so we have a smaller Rs!
A. Gurevich, Phys. Rev. Lett.
A. Gurevich, Supercond. Sci. Technol. 30, 034004 (2017).

## Slide 74
β=10
β=0.1
β=0.01
β=3
As T decreases, the order changes due to the minigap induced residual resistance

## Slide 75
β=10
β=0.1
β=0.01
β=3
We have the optimum!

## Slide 76
T=2K
Γ=0.03
α
β
We can tune Rs
by varying α and β.

## Slide 77
Γ=0.03
Q=2.2×1010
Q=1.6×1011
Decreases N layer thickness
and increases surface barrier

## Slide 78
Γ=0.03
Q=2.2×1010
Q=1.6×1011
Decreases N layer thickness
and increases surface barrier

## Slide 79
Γ=0.03
Q=2.2×1010
Q=4.1×1010
Q=2.4×1011
Q=1.6×1011
Decreases N layer thickness
and increases surface barrier

## Slide 80
Γ=0.03
Q=2.2×1010
Q=4.1×1010
Q=2.4×1011
Q=1.6×1011
The differences between the 2 curves are analogous to those between ILC recipe and N-dope! Remind the residual resistance (without flux) is known to be smaller in N-doped cavity than ILC recipe.

## Slide 81
Summary
We developed a unified theory of surface resistance and residual resistance
The theory incorporates the effects of the surface normal layer or damaged layer and mechanism which produce finite density of subgap states in the bulk.
The theory incorporates both the conventional MB contribution and the residual resistance.
The NS coupling affects not only residual resistance but also surface resistance at T~2K.
We showed tuning Rs by optimizing the thickness of metallic suboxide layer and the interface resistance.

## Slide 82
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
Runified
Rs
Damaged layer
Metallic sub-oxide
Subgap states
Dielectric losses
etc
Runified
Rs
Tune the surface
based on the unified theory!

## Slide 83
Oct. 2016
@Norfolk
Thanks!