## Slide 1
Progress of high resolution TOF system
Wang Yi
Department of Engineering Physics, Tsinghua University
yiwang@mail.tsinghua.edu.cn

## Slide 2
Abstract:
  Introduction of MRPC
  Introduction of three generation MRPC TOF
  Status of TOF of STAR, CBＭ and SoLID
  Conclusion

## Slide 3
Application in nuclear physics experiments
Application in industry（Muon tomography)
Application in medicine（TOF-PET）
Standard parameters:
Resistivity of glass: ~1012 Ω.cm
Working gas: 90%Freon+5%iso-butane+5% SF6
Time resolution <100ps
Efficiency >95%
Charge: a few PC
Dark current: a few nA
Noise ~1Hz/cm2
Rate <100 Hz/cm2
Large area, low cost
Read out
Read out
Insulator
Carbon
Insulator
Resistive
plate
MRPC application：
MRPC structure
MRPC introduction

## Slide 4
The voltage drop in the gas gap:
Two main ways to improve rate capability:
Reducing bulky resistivity of electrode glass (CBM)
Reducing the avalanche charge (ATLAS)
Other methods:
Reducing the thickness of glass
Warming the detector
The smaller the voltage drop, the higher efficiency and higher rate capability!
How to increase rate of MRPC

## Slide 5
Typical MRPC TOF
RHIC-STAR TOF
Float glass
FAIR-CBM TOF
High rate- low resistive glass
JLab-SoLID TOF
High rate and 20ps resolution

## Slide 6
Key technology
1st generation TOF:
Requirement: Time resolution: <80ps
Rate : <1kHz/cm2
Technology: common glass MRPC+NINOs +HPTDC
Analysis method: TOT slewing correction
2st generation TOF:
Requirement: Time resolution: <80ps
Rate : 30kHz/cm2
Technology: low resistive glass MRPC+PADI +GET4
Analysis method: TOT slewing correction
3st generation TOF:
Requirement: Time resolution: <20ps
Rate : 20kHz/cm2
Technology: low resistive glass MRPC+SCA +ADC
Analysis method: TOT slewing correction
Deep learning+ Neural network

## Slide 7
RHIC-STAR

## Slide 8
STAR-TOF MRPC
8
Long side view

## Slide 9
Glass: ～4×1012.cm
Carbon tape: 500k /
Gas gap: 6×0.22mm
Working gas: 95% F134a+5% iso-butane
Time resolution: 70ps
Efficiency >90%
Rates capability: <500Hz/cm2 !
3cm
6cm
Readout pad
STAR MRPC performance

## Slide 10
10
10
MRPC mass production

## Slide 11
TOF
TOF PID:
 /k ~1.6 GeV/c,
(,k)/p ~ 3.0 GeV/c
PID of STAR-TOF
Nature 473 (2011) 353

## Slide 12
Layout of CBM detector

## Slide 13
13
13
The structure of CBM-TOF wall
CBM-ToF Requirements
Full system time resolution sT ~ 80 ps
Efficiency > 95 %
Rate capability  30 kHz/cm2
Polar angular range 2.5°– 25°
Occupancy < 5 %
Low power electronics
(~100.000 channels)
Free streaming data acquisition
Au+Au, Center, 10AGeV
Simulated with CBM ROOT

## Slide 14
14
Development of low resistive glass
Performance of the glass
Glass mass production
Yield >100m2/month
Aging test with X-ray source
Online test system. The efficiency and time resolution can be obtained by cosmic ray while irradiated by X-rays. 0.1C/cm2 charge is accumulated in 35 days.

## Slide 15
Rate: 70kHz/cm2
Time resolution: 40 ps
Rate capability of high rate MRPC
Even though the rate is 70kHz/cm2, the efficiency is still higher than 90% and the time resolution is about 80ps.
Test results at Nuclotron, Dubna，2013

## Slide 16
Glass: low resistive glass
0.7mm thick, 33cm x 27.6cm
Strip: 27cm x 0.7cm, 0.3cm interval, 32 strips
Gas gap: 8 x 0.25mm, two stacks
Design of strip-MRPC for high rate region
Honey
PCB
Mylar
Graphite
Fish line
Glass
Upper stack
lower stack

## Slide 17
17
High rate test in February 2015 at SPS CERN
13 GeV Ar beam
Flux rate around 1kHz/cm2
Buc-2013
THU-Pad
Buc-Ref
PMT
HD-Ref
THU-Strip
HD-P2
Experimental Setup:
USTC
Up setting
Down setting
Beam test @ SPS Feb 2015

## Slide 18
SPS Nov 2015 THU-DU results
Results of each run
Time resolution from tracking method
Performance of the prototype

## Slide 19
19
Two-dimensional code of MRPC
Producttion website:
http://hepd.ep.tsinghua.edu.cn/CBM_TOF/
Mass production of high rate MRPC

## Slide 20
20
Overview of SoLID
Full exploitation of JLab 12 GeV Upgrade
 A Large Acceptance Detector AND Can Handle High Luminosity (1037-1039)
Take advantage of latest development in detectors , data acquisitions and simulations
Reach ultimate precision for SIDIS (TMDs), PVDIS in high-x region and threshold J/y
5 highly rated experiments approved (+3)
Three SIDIS experiments, one PVDIS, one J/y production (+ three run group experiments)
Strong collaboration (250+ collaborators from 70+ institutes, 13 countries)
Significant international contributions (Chinese collaboration)
Solenoidal Large Intensity Device

## Slide 21
The MRPC is developed for the TOF of SoLID
Main Requirements for TOF:
  /k separation up to 7GeV/c
  Time resolution < 20ps
  Rate capability > 20kHz/cm²
MRPC1
MRPC2
MRPC3
100cm
16cmm
28cm
SoLID-TOF structure
SoLID-TOF super module
SoLID-TOF structure

## Slide 22
Challenge for both MRPC and electronics.
Electronics: Fast amplifier + pulse sampling
New analysis method: take the advantage of the entire waveform
技术路线

## Slide 23
The analysis method is based on the neural network.
Artificial neural network(NN): powerful && widely used in high energy physics
Introduce NN to obtain good time resolution: —— Find out the patterns from the MRPC signal and estimate the particle 1st interaction time more precisely.
First interaction time
Learn from the simulation waveforms
Test with experiment data
Test with simulation data
1
2
新的分析方法能够得到更精确定时

## Slide 24
Determine structure of MRPC
Construct NN
Detector simulation->Pulse shape
Training NN
Input measured pulse-> Timing
Neural network analysis method

## Slide 25
MRPC structure
Avalanche through drifting
Induced current:
Front-end electronics + noise
*F. Wang, et al., A standalone simulation framework of the mrpc detector read out in waveforms, arXiv:1805.02387.
6-gas MRPC
Gap/glass thickness: 0.25/0.7 mm
Gas: 90% C2H2F4, 5% C4H10 and 5% SF6
Cosmic muons: ~ 4GeV
: Townsend coefficient
: Attachment coefficient
Shoot a particle
Drifting & Avalanche
Primary interactions
Original current signal
Electronics
Design the structure
Waveform simulation

## Slide 26
MRPC
Signal
t
Fixed threshold
Source
Simulation dataset :
: first interaction happens
: the signal reach the peak
7 uniformly distributed points along the leading edge
Simulation data

## Slide 27
Multilayer perceptron (MLP)
Input
Output
Activation function: g and h —— tanh
Weights:
“Dropout”: avoid overfitting
Several uniformly distributed points along the leading edge
The length of the leading edge t l
Train/validate/test set: 20/10/10 k
Tensorflow & GPU: GTX 1080 Ti
~ 10 mins for training
Time of the very first interaction:
One NN：Multilayer perception (MLP)

## Slide 28
Recurrent neural networks(RNN): Long Short Term Memory network(LSTM)
Train/validate/test set: 20/10/10 k
Tensorflow & GPU: GTX 1080 Ti
F
I
G
O
f : forget gate: Whether to erase
I : Input gate, whether to write
g: gate gate, How much to write
o: output gate, How much to reveal
The length of the leading edge t l
Several uniformly distributed points along the leading edge
> 30 mins for training
Another NN：LSTM

## Slide 29
Define bias:
Accuracy is good and stable
The best time resolution can reach around 20 ps.
29
Accuracy
Precision
Experiment point
Streamer may happen
Simulation results

## Slide 30
Experiment of the cosmic ray
2 identical MRPC: 6-gap, 0.25mm gap, working at E=109 kV/cm
Oscilloscope bandwidth: 1 GHz
Sampling rate: 10 GS/s
MRPC1
MRPC2
FEE
FEE
FEE
FEE
Oscilloscope
PMT1
PMT2
trigger
Leading edge: 700~800 ps
7~8 points along the edge
Experimental setup

## Slide 31
Compare the waveform
Nearly the same!
Still with differences!
Waveforms of 1 event
1L
1R
2L
2R
Signal waveform

## Slide 32
The 4 waveforms are estimated by the LSTM models separately
Define: for vertical particles
The time resolution of two MRPCs are independent:
With LSTM model, for vertical particles, the time resolution is:
Experimental results

## Slide 33
33
Item | dimension/mm
Honeycomb | 90×265×7.5
Outer PCB | 120×298×0.6
Middle PCB1 | 120×298×1.2
Middle PCB2 | 120×328×1.2
Strip length | 268
Strip width | 7
Mylar | 90×268×0.25
Glass | 80×258×0.5
Carbon | 72×250
Gas gap width | 0.104
Number of gas gap | 32
Design of 3g MRPC for SoLID
Honey comb plate
PCB
Mylar
Carbon electrode
Glass

## Slide 34
Analysis with neural network

## Slide 35
Conclusions
Time of flight system (TOF) based on MRPC technology is widely used and played an important role in modern high energy nuclear physics experiments.
With the increase of accelerator energy and luminosity, many experiments have increasingly demand on the TOF for particle identification to have high resolution TOF under high data rate environment.
New technology such as New material (low resistive glass), New electronics (switched capacitor array (SCA) and precision TDC ) will be used in TOF system. New analysis method such as deep learning technology will play an very important role!

## Slide 36
Thanks for your attention!