## Slide 1: A Brief Introduction to Superconducting Accelerator Magnets
Qingjin Xu
Institute of High Energy Physics,
Chinese Academy of Sciences
2018.12

## Slide 3: Outline
Basic Knowledge of the Superconducting Accelerator Magnets
PRINCIPLES of a Circular Collider
Design of Superconducting Accelerator Magnets
Superconducting Materials for Accelerator Magnets
Case Study: R&D of High Field Magnets for SPPC
Overview of SPPC Design Scope
Design Study of the SPPC Dipole Magnets
R&D Steps and Status

## Slide 4: Outline
Basic Knowledge of the Superconducting Accelerator Magnets
PRINCIPLES of a Circular Collider
Design of Superconducting Accelerator Magnets
Superconducting Materials for Accelerator Magnets
Case Study: R&D of High Field Magnets for SPPC
Overview of SPPC Design Scope
Design Study of the SPPC Dipole Magnets
R&D Steps and Status

## Slide 5: Acknowledgement
The materials of this section are based on USPAS (U.S. Particle Accelerator School) courses:
“Superconducting Accelerator Magnets” by Soren Prestemon (LBNL), Paolo Ferracin and Ezio Todesco (CERN), June 2015
“Superconducting Accelerator Magnets” by Paolo Ferracin (LBNL), Ezio Todesco (CERN), Soren O. Prestemon and Helene Felice (LBNL), January 2012
“Superconducting Accelerator Magnets” by Ramesh Gupta and Animesh Jain (BNL), January 2006
“Applied Electromagnetism: Magnet and RF-Cavity Design” by Mau Lopes and Jeremiah Holzbauer (FNAL), January 2016
Learn more at USPAS website: http://uspas.fnal.gov/materials/materials-table.shtml
and textbooks:
  Martin N. Wilson, "Superconducting Magnets", 1983.
  K.-H. Mess, P. Schmuser, S. Wolff, “Superconducting accelerator magnets”, Singapore: World Scientific, 1996.
  Fred M. Asner, "High Field Superconducting Magnets", 1999.

## Slide 6: PRINCIPLES of a Circular Collider
Colliders: two beams with opposite momentum collide
The arcs: region where the beam is bent
  Dipoles for bending
  Quadrupoles for focusing
  Correctors
Long straight sections (LSS)
  Interaction regions (IR)
    Quadrupoles for strong focusing in interaction point
    Dipoles for beam crossing in two-ring machines
  Regions for other services
    Beam injection (dipole kickers)
    Accelerating structure (RF cavities)
    Beam dump (dipole kickers)
    Beam cleaning (collimators)
A schematic view of a synchrotron
The lay-out of the LHC

## Slide 7: PRINCIPLES of a Circular Collider

## Slide 8: PRINCIPLES of a Circular Collider
Arc

## Slide 9
Design of Superconducting Accelerator Magnets

## Slide 10: Dipole vs. Solenoid
Different coil configurations
Limited coil width for dipole
Magnetic shielding
Cost
Martin Wilson
Solenoid
Lucio Rossi
LHC dipole
Dipole
Je – Current density
t – Coil thickness
Je – Current density
t – Coil thickness

## Slide 11
Cos-theta dipole
Highest efficiency, complicated ends with hard-way bending
Common coil dipole
Simplest structure with large bending radius, lower efficiency
Canted cos-theta dipole
Lowest stress level in coil, lowest efficiency
Efficiency, field quality, stress management, fabrication method…
Block type dipole
Simpler structure with hard-way bending, lower efficiency
Different coil configurations for dipole magnets

## Slide 12: Overview of accelerator dipole magnets
Tevatron
HERA
SSC
RHIC
LHC

## Slide 13: HL-LHC 11 T Dipole Coil
Loading plate
2 mm 316LN
SLS (Selective Laser
Sintering) End Spacers
with “springy legs”
Braided 11-TEX S2-glass
on “open-C” Mica sleeve
ODS (Oxide Dispersion
Strengthened) Cu-alloy
Wedges
Courtesy of D. Mitchell, FNAL
OST RRP-108/127
14.85
Ø0.7

## Slide 14
Support structure based on collars and welded stainless steel shell are also used for quadrupole magnets.
During the collaring operation, 4 keys/rods are inserted at the four mid-planes.
CERN-Oxford Inst. (MQY)
Fermilab (MQXB)
KEK (MQXA)
L. Rossi, [1]
Practical accelerator magnets –
LHC IR quadrupole

## Slide 15: HL-LHC MQXF
Target: 132.6 T/m in 150 mm coil aperture
To be installed in 2023
Q1/Q3
  2 magnets with 4.2 m of magnetic length within 1 cold mass
Q2
  1 magnet of 7.15 m within 1 cold mass, including MCBX (1.2 m)
Different lengths, same design
by E. Todesco

## Slide 16: Field Harmonics
From M. N. Wilson, pg. 28
An ideal cos
A practical winding with one layer and wedges
[from M. N. Wilson, pg. 33]
A practical winding with three layers and no wedges
[from M. N. Wilson, pg. 33]
Artist view of a cos magnet
[from Schmuser]
  Cos: a current density proportional to cos in an annulus - it can be approximated by sectors with uniform current density
Perfect Dipole
Biot-Savart law

## Slide 17: Field Harmonics
  Perfect quadrupole
  Cos2, a current density proportional to cos2 in an annulus- approximated by sectors with uniform current density and wedges
  (Two) intersecting ellipses
    Perfect sextupoles: cos3 or three intersecting ellipses
    Perfect 2n-poles: cosn or n intersecting ellipses
Quadrupole as an ideal cos2
Quadrupole as two intersecting ellipses

## Slide 18: Field Harmonics
Maxwell equations for magnetic field
In absence of charge and magnetized material
If (constant longitudinal field),
then
  and
James Clerk Maxwell,
Scottish
(13 June 1831 – 5 November 1879)
Gauss's law for magnetism
Ampère's circuital law
Cauchy-Riemann conditions

## Slide 19: Field Harmonics
A dipole
A quadrupole
[from P. Schmuser et al, pg. 50]
A sextupole
Each coefficient corresponds to a “pure” multipolar field
The field harmonics are rewritten as (EU notation)

## Slide 20: Field Harmonics
Corrective actions: shaping the iron – the RHIC dipole
    The field in the yoke is larger on the pole
    Drilling holes in the right places, one can reduce saturation of b3 from 40 units to less than 5 units (one order of magnitude), and to correct also b5
Field map in the iron for the RHIC dipole, with and without holes
From R. Gupta, USPAS Houston 2006, Lecture V, slide 12
Correction of b3 variation due to saturation
for the RHIC dipoles, R. Gupta, ibidem

## Slide 21: Electro-magnetic Force
The e.m. forces in a dipole magnet tend to push the coil
- Towards the mid-plane in the vertical-azimuthal direction (Fy , F < 0)
- Outwards in the radial-horizontal direction (Fx , Fr > 0)
Tevatron dipole
HD2

## Slide 22: Practical accelerator magnets – LHC main dipole
Two-in-one configuration
  Both beam pipes are contained within one cold mass
Stainless steel collars are locked by three full-length rods.
Magnetic insert
  It transfers vertical force from the yoke to the collared coils
  It improves field quality
Iron yoke vertically split
  At the end of the welding operation the yoke gap is closed
Stainless steel shell halves are welded around the yoke to provide He containment, a 9 mm sagitta, and to increase rigidity.
MJB Plus, Inc., [2]

## Slide 23: Electro-magnetic Force
LHC dipole at 0 T LHC dipole at 9 T
Usually, in a dipole or quadrupole magnet, the highest stresses are reached at the mid-plane, where all the azimuthal e.m. forces accumulate (over a small area).
Displacement scaling = 50

## Slide 24: Electro-magnetic Force
The e.m. forces in a quadrupole magnet tend to push the coil
Towards the mid-plane in the vertical-azimuthal direction (Fy, F < 0)
Outwards in the radial-horizontal direction (Fx, Fr > 0)
TQ
HQ

## Slide 25: Electro-magnetic Force
In the coil ends the Lorentz forces tend to push the coil Outwards in the longitudinal direction (Fz > 0)
Similarly as for the solenoid, the axial force produces an axial tension in the coil straight section.

## Slide 26: Electro-magnetic Force
Nb-Ti LHC MB (values per aperture)
  Fx = 340 t per meter
    ~300 compact cars
    Precision of coil positioning: 20-50 μm
  Fz = 27 t
    ~weight of the cold mass
Nb3Sn dipole (HD2)
  Fx = 500 t per meter
  Fz = 85 t
  These forces are applied to an object with a cross-section of 150x100 mm !!!
    and by the way, it is brittle

## Slide 27: Support Structures
Collars were implemented for the first time in the Tevatron dipoles.
Since then, they have been used in all but one (RHIC) the accelerator magnets and in most of the R&D magnets.
They are composed by stainless-steel or aluminum laminations few mm thick.
By clamping the coils, the collars provide
  coil pre-stressing;
  rigid support against e.m. forces (it can be self-supporting or not);
  precise cavity (tolerance  20 m).
L. Rossi, [1]
MJB Plus, Inc., [2]
Tevatron
SSC
LHC

## Slide 28: Support Structures
L. Rossi, [4]
Collaring of a dipole magnet
Collaring of a quadrupole magnet

## Slide 29: Support Structures
The purpose of the collar is to pre-compress the coil inside a “rigid” cavity.
  The collar cavity fixes the dimension of the coil.
  Coil geometry is given by the collars.
Coil stress-strain is given by
  coil=(lcoil_0-lcavity)/lcoil_0
  coil=Ecoil
A good knowledge of the coil properties (lcoil_0 and E) is mandatory to predict final coil status.
In addition, collar deformation must be taken into account.
S. Wolff, [3]

## Slide 30: Support Structures
As the collars, iron yoke are made in laminations (several mm thick), with a packing factor > 95%.
Magnetic function
  The yoke contains and enhances the magnetic field.
Structural function
  Except for the cases where the collars are self supporting (i.e. like in Tevatron and HERA dipoles), the yoke is in tight contact with the collar. Therefore, it contributes to increase the rigidity of the coil support structure and limit radial displacement.
Holes/slots are included in the yoke design for
  Correction of saturation effect
  Cooling channel
  Assembly features
  Electrical bus
L. Rossi, [4]

## Slide 31: Support Structures
The cold mass is contained within a shell (or shrinking cylinder).
The shell constitutes a containment structure for the liquid Helium.
It is composed by two half shells of stainless steel welded around the yoke with high tension (about 150 MPa for the LHC dipole).
  With the iron yoke, it contributes to create a rigid boundary to the collared coil.
If necessary, during the welding process, the welding press can impose the desired curvature on the cold mass.
  In the LHC dipole the nominal sagitta is of 9.14 mm.
L. Rossi, [4]

## Slide 32: Support Structures
End plates, applied after shell welding, provide
  axial support to the coil under the action of the longitudinal e.m. forces
    Torque may be applied to end bolts;
  Liquid Helium containment.
L. Rossi, [4]
A. Devred, [5]

## Slide 33: Quench Protection
Quench
Normal zone growth
Detection
Power supply switched off
Protection heaters
Extraction
Quenchback
Trigger protection options
The faster this chain happens the safer is the magnet
Current decay in the magnet
Magnetic energy
Converted to heat by Joule heating

## Slide 34: Quench Protection
In most accelerator magnets, the “natural” resistance growth is insufficient to provide a good protection => Need to enhance the resistance
Method 1:
  Add an external resistor
Method 2:
  Protection heaters mounted on the coils
    Optimized to minimize thermal diffusion time
Method 3:
  Use of couple secondary circuits
    Can be external or internal to the coil
    Quench back
Method 4:
  Coil subdivision
Cold

## Slide 35: Quench Protection
In the LHC main ring, the dipoles are connected in series. The principle is
  to “by-pass” the quenching magnet to avoid dumping all the string energy in one magnet
  To de-excite the rest of the magnets into a dump resistor
Combination of various methods: heaters, dump resistor, diodes

## Slide 36: Superconducting materials
Nb-Ti
Nb3Sn
Critical surfaces

## Slide 37: Superconducting materials
Typical operational conditions (0.85 mm diameter strand)
Cu
Nb3Sn
Nb-Ti
Je ~ 5 A/mm2
I ~ 3 A
B = 2 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 8-9 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 12-13 T

## Slide 38: Superconducting materials
The superconducting materials used in accelerator magnets are
  subdivided in filaments of small diameters
    to reduce magnetic instabilities called flux jumps
    to minimize field distortions due to superconductor magnetization
  twisted together
    to reduce interfilament coupling and AC losses
  embedded in a copper matrix
    to protect the superconductor after a quench
    to reduce magnetic instabilities called flux jumps
NbTi LHC wire (A. Devred, [1])
Nb3Sn bronze-process wire (A. Devred, [1])
NbTi SSC wire (A. Devred, [1])
Nb3Sn PIT process wire (A. Devred, [1])

## Slide 39: Superconducting materials
Flux jumps
  An external magnetic field penetrates in a type-II superconductor in the mixed state through fluxoids.
  If the superconductor is subjected to a thermal disturbance, the local change in Jc produces a motion or “jump” of fluxoids, which is accompanied by power dissipation.
  The stability criteria for a slab in the adiabatic condition
  where a is the half-thickness of the slab, jc is the critical current density [A m-2],  is the density [kg m-3], C is the specific heat [J kg-1], and c is the critical temperature.
  Nb-Ti filament diameters are usually less than 50 µm.
  High conductivity copper reduces instability.

## Slide 40: Superconducting materials
Superconductor magnetization
According to the critical state model, when a filament is in a varying external field, its inner part is shielded by a current distribution in the filament periphery.
The shielding currents are proportional to the amplitude of the applied field and do not decay when the external field is held constant.
  When the filament is fully penetrated, the magnetization M is proportional to Jcrf.
  Field distortions are proportional to rf. LHC filament diameter 6-7 µm; HERA filament diameter 14 µm.
K.-H. Mess, et al., [5], p. 84.

## Slide 41: Superconducting materials
Interfilament coupling
  When a multifilamentary wire is subjected to a time varying magnetic field, current loops are generated between filaments.
  If filaments are straight, large loops are generated, with large currents
    Big losses
  If the strands are magnetically coupled the effective filament size is larger
    Flux jumps
  To reduce these effects, filaments are twisted with a twist pitch of the order of 20-30 times of the wire diameter.
M.N. Wilson, [4], p. 148.

## Slide 42: Superconducting materials

## Slide 43: Superconducting materials
Quench protection
  Superconductors have a very high normal state resistivity. A filament of Nb-Ti, if quenched in free space, could reach very high temperatures in few ms.
  If the filament is embedded in a copper matrix, when a quench occurs, the current redistributes in the low-resistivity matrix and the peak temperature can typically be maintained below 300 K.
  The copper matrix facilitates quench protection: it allows the quench to propagate and it provides time to act on the power circuit.
  In the case of a small volume of superconductor heated beyond the critical temperature (for instance because of a flux jump), the current can flow in the copper for a short moment, allowing the filament to cool-down and recover superconductivity.
    The matrix also helps stabilizing the conductor against flux jumps (dynamic stability).
by L. Bottura

## Slide 44: Summary
Performance of Superconductors: Jc, cost, mechanical behaviors,…
Magnetic force in superconducting coils at high field: F ̴ B2
Field quality: magnetization effect, iron saturation effect, current distribution in tape conductors,…
Quench protection: High stored energy and operating current
Fabrication methods: Strain sensitive superconductors
Challenges of the High Field Superconducting Magnets

## Slide 45: Outline
Basic Knowledge of the Superconducting Accelerator Magnets
PRINCIPLES of a Circular Collider
Design of Superconducting Accelerator Magnets
Superconducting Materials for Accelerator Magnets
Case Study: R&D of High Field Magnets for SPPC
Overview of SPPC Design Scope
Design Study of the SPPC Dipole Magnets
R&D Steps and Status

## Slide 46
IHEP-CAS: Chengtao Wang, Kai Zhang, Zhan Zhang, Shaoqing Wei, Lingling Gong, Da Cheng, Yingzhe Wang, Ershuai Kong, Zhen Zhang, Xiangchen Yang, Quanling Peng, Qing Qin, Yifang Wang,
IEE-CAS: Xianping Zhang, Dongliang Wang, Yanwei Ma
HIPS-CAS: Huajun Liu, Tao Zhao, Yanlan Hu,…
IMP-CAS: Wei Wu, Yu Liang, Wenjie Liang, Lizhen Ma,…
WST: Meng Li, Chao Li, Bo Wu, Yanmin Zhu, Jianwei Liu, Jianfeng Li,…
Toly Electric: Yu Zhao, Hean Liao, Bingxing Lu,…
*The work is supported by the Strategic Priority Research Program of the Chinese Academy of Sciences (CAS) Grant No. XDB25000000, the key research program of CAS Grant No. XDPB01, Hundred Talents Program of CAS and National natural Science Foundation of China Grant No. 11675193, 11575214, 11604335, U1632276.
Team Members & Collaborators
Acknowledgement

## Slide 47
CEPC-SPPC
BTC
IP1
IP3
e+
e-
e+ e- Linac
LTB
CEPC Collider Ring
CEPC Booster
BTC
SPPC ME Booster
SPPC LE Booster
IP4
IP2
SPPC Collider Ring
Proton Linac
SPPC HE Booster
CEPC is an 240-250 GeV Circular Electron Positron Collider, proposed to carry out high precision study on Higgs bosons, which can be upgraded to a 70-150 (Upgrading phase) TeV pp collider SPPC, to study the new physics beyond the Standard Model.
50/100 km in circumference

## Slide 48: SPPC Magnet Design Scope (V201701)
Main dipoles
Field strength: 12~24 (Upgrading) Tesla
Aperture diameter: 40~50 mm
Field quality: 10-4 at the 2/3 aperture radius
Outer diameter: 650-900 mm in a 1.5 m cryostat
Tunnel cross section: 6 m wide and 5.4 m high
6-m Tunnel for CEPC-SPPC
SPPC
100 km in circumference
C.M. energy 70-150 (Upgrading) TeV
Timeline
Pre-study: 2013-2020
R&D: 2020-2030
Eng. Design: 2030-2035
Construction: 2035-2042
Conceptual design of the SPPC 12-T magnet with IBS and common coil configuration
SPPC collider
CEPC collider
CEPC booster

## Slide 49: SPPC Magnet Design Scope
Baseline design
  Tunnel circumference: 100 km
  Dipole magnet field: 12 T, iron-based HTS technology (IBS)
  Center of Mass energy: >70 TeV
  Injector chain: 2.1 TeV
Upgrading phase
  Dipole magnet field: 20 -24T, IBS technology
  Center of Mass energy: >125 TeV
  Injector chain: 4.2 TeV (adding a high-energy booster ring in the main tunnel in the place of the electron ring and booster)
Development of high-field superconducting magnet technology
  Starting to develop HTS magnet technology before applicable IBS wire is available
  ReBCO & Bi-2212 and LTS wires be used for model magnet studies and as options for SPPC: stress management, quench protection, field quality control and fabrication methods
Top priority: reducing cost!
Instead of increasing field
Make IBS the High-Tc and High-Field
“NbTi” superconductor in 10 years!

## Slide 50
Je of IBS: 2016-2025
Chart: Applied Magnetic Field (T)
| 5 | 10 | 15 | 20
REBCO: B ∥ Tape plane | 4599.7996 | 4264.0246 | 3416.6751 | 3085.9004
REBCO: B ⊥ Tape Plane | 3664.9998 | 2919.9995 | 2379.9996 | 1796.1537 | 1447.6924 | 1188.462 | 1034.3652 | 956.923 | 851.8301 | 780.8449 | 719.9995 | 679.4359 | 626.087 | 593.2388 | 563.4783 | 535.3843 | 516.5215 | 469.5647 | 433.0766 | 406.956 | 391.3041 | 367.6926 | 360.0003 | 344.3473 | 328.6954 | 322.3077
Bi-2212: 50 bar OP | 2187.8458 | 2018.5437 | 1897.0961 | 1799.3564 | 1729.1673 | 1666.7736 | 1608.1837 | 1558.7923 | 1516.4066 | 1473.2906 | 1436.5687 | 1398.9095 | 1365.3787
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: High Field MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar | 1379.4097 | 1269.0093 | 1128.2455 | 1107.3276
YBCO B perp ln extrap | 322.2305 | 315.4585 | 296.3443 | 267.862 | 242.7389
YBCO par ln extrap | 3024.7539 | 2573.1471 | 2188.967 | 2051.8662

## Slide 51
Goal：
1) To increase the Jc of iron-based superconductor (IBS) by 10 times, reduce the cost to 20 Rmb/kAm @ 12T & 4.2K, and realize the industrialization of the conductor;
2) To reduce the cost of ReBCO and Bi-2212 conductors to 20 Rmb/kAm @ 12T & 4.2K;
3) Realization and Industrialization of IBS magnets and SRF cavities.
Working groups：1) Fundamental sciences study; 2) IBS conductor R&D; 3) ReBCO conductor R&D; 4) Bi-2212 conductor R&D; 5) Performance evaluation; 6) Magnet and SRF technology.
Domestic Collaboration for HTS R&D
“Applied High Temperature Superconductor Collaboration (AHTSC)” formed in Oct. 2016.
Including 18 institutions and companies in China. Regular meeting every 3 months.

## Slide 52
The 12-T Fe-based Dipole Magnet
Yoke OD
500mm
Strand | diam. | cu/sc | RRR | Tref | Bref | Jc@ BrTr | dJc/dB
IBS | 0.802 | 1 | 200 | 4.2 | 10 | 4000 | 111
Design with expected Je of IBS in 2025
Io=9500A
The required length of the 0.8 mm IBS is 6.1 Km/m
For 100-km SPPC, 3000 tons of IBS is needed
Target cost of IBS: 20 RMB (~2.6 Eur) /kAm @12 T

## Slide 53
The 12-T Fe-based Dipole Magnet
Field quality in the aperture
<3*10-4 within 2/3 bore
(ROXIE simulation results)
Field quality | 2D with Rf= 13.3mm | 3D with Rf= 8/13.3 mm
b3 | 0.45 | 0.79/1.91
b5 | 1.01 | -0.65/-2.24
b7 | 0.46 | 0.08/0.67
b9 | -0.27 | -0.13/-0.22
a2 | 3.53 | -1.00/-2.31
a4 | 0.49 | -0.46/0.69
a6 | 0.33 | 0.26/2.49
a8 | 0.58 | -0.12/0.84
a10 | 2.23 | 0.06/2.18
Flare ends

## Slide 54
R&D of High Field Dipole Magnets
Components and assembly
3d coil layout
NbTi+Nb3Sn, 2*ф10 aperture
All HTS, 2*ф40 aperture
3D magnetic field distribution
Magnetic flux distribution
Nb3Sn+HTS, 2*ф20 aperture
R&D Roadmap for the next 10~15 years

## Slide 55
R&D of High Field Dipole Magnets
The 1st High Field Dipole LPF1: NbTi+Nb3Sn
Cross section of LPF1
Magnetic field distribution
Main parameters of the strands
Strand | diam. (mm) | cu/sc | RRR | Tref (K) | Bref (T) | Jc@ BrTr (A/mm2) | Ic@ BrTr (A)
Nb3Sn | 0.802 | 1 | 200 | 4.2 | 12 | 2700 | 682
NbTi | 0.82 | 1 | 130 | 4.2 | 5 | 2613 | 690

## Slide 56
R&D of High Field Dipole Magnets
Mechanical FEA magnet model
3D CAD configuration of LPF1
Assembly
4.2 K
5,950 A

## Slide 57
R&D of High Field Dipole Magnets
Preloading at room temperature
(Load 1)
Excitation
(Load 3)
Cooling down
(Load 2)
σx
σy
σz
Mises stress
Stress analysis of the coils

## Slide 58
R&D of High Field Dipole Magnets
Preloading at room temperature
(Load 1)
Excitation
(Load 3)
Cooling down
(Load 2)
Displacement Sum
X displacement
Y displacement
Z displacement
17μm
3μm
11μm
17μm
Displacement analysis of the coils

## Slide 59
R&D of High Field Dipole Magnets
Quench protection circuit
Schematic of the quench protection system
MIITs Hot spot temperature
Hot spot temperature vs. MIITs for different cables
Adiabatic analysis

## Slide 60
Thickness (μm) | Resistance （Ω） | Peak power（w/cm^2) | Charge voltage (V) | Max current (A) | Capacitance (mF)
50 | 3.1 | 100 | 341 | 110.07 | 9.67
Magnet inductance
Heat delay
Quench simulation with dump resistor only
Quench simulation with dump resistor and heaters
Quench heater
Current decay
Current decay
Hotspot temp.
Hotspot temp.
Voltage
Resistance
Voltage
Resistance
Temperature distribution
In coil after quench
Temperature distribution
In coil after quench
R&D of High Field Dipole Magnets

## Slide 61
Cabling Coil winding HT VPI Magnet assembly Test
Fabrication of the 1st model dipole magnet (NbTi+Nb3Sn)
Cabling Machine
Rutherford Cable
Coil Winding
Heat Reaction
VPI
Magnet Assembly
VPI Coil Package
Impregnated
Coil
R&D of High Field Dipole Magnets

## Slide 62
10.2 T @ 4.2 K dipole field
in two apertures
(Performance limited by NbTi coils)
Test results of the 1st high-field dipole magnet in China Feb. 2018
Magnet under test @ Hefei
Magnet fabrication @ Beijing
Test system setup @ Hefei
R&D of High Field Dipole Magnets

## Slide 63: Concept of the SPPC 20-T Dipole Magnet
Chart: 
| 0 | 30 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300 | 330 | 360 | 390 | 420 | 450 | 480 | 510 | 540 | 570 | 600 | 630 | 660 | 690 | 720 | 750 | 780 | 810 | 840 | 870 | 900 | 930 | 960 | 990 | 1020 | 1050 | 1080 | 1110 | 1140 | 1170 | 1200 | 1230 | 1260 | 1290 | 1320 | 1350 | 1380 | 1410 | 1440 | 1470 | 1500
b3 | -0.39506 | -0.16327 | -0.0029767 | 0.080907 | 0.18246 | 0.3156 | 0.439 | 0.5482 | 0.66092 | 0.78202 | 0.90267 | 1.0279 | 1.1648 | 1.3206 | 1.5091 | 1.7498 | 2.0946 | 2.6288 | 3.5771 | 5.2487 | 5.7841 | -5.7987 | -44.674 | -68.098 | -33.263 | 46.267 | 104.97 | 92.844 | -10.311 | -47.905 | -30.782 | -15.193 | -7.0212 | -3.3196 | -1.658 | -0.87994 | -0.49435 | -0.29205 | -0.18021 | -0.11545 | -0.076387 | -0.05198 | -0.036248 | -0.025827 | -0.018755 | -0.013853 | -0.01039 | -0.0078993 | -0.0060811 | -0.0047347 | -0.0037247
b5 | 0.65047 | 0.63445 | 0.61856 | 0.60411 | 0.58834 | 0.57153 | 0.55626 | 0.54083 | 0.52531 | 0.51043 | 0.49419 | 0.479 | 0.46378 | 0.44851 | 0.43298 | 0.41904 | 0.40531 | 0.38867 | 0.3786 | 0.36235 | 0.20873 | -0.53251 | -4.2528 | -4.9148 | 0.75387 | 9.2111 | 9.8532 | 10.795 | 2.2384 | 1.501 | 0.5939 | 0.16091 | 0.048947 | 0.016093 | 0.0056422 | 0.0021176 | 0.00085143 | 0.00036553 | 0.00016666 | 8.0217e-05 | 4.0525e-05 | 2.1376e-05 | 1.1719e-05 | 6.6496e-06 | 3.8919e-06 | 2.3424e-06 | 1.446e-06 | 9.1333e-07 | 5.8915e-07 | 3.8739e-07 | 2.5923e-07
b7 | -0.22665 | -0.23626 | -0.24758 | -0.259 | -0.27031 | -0.28164 | -0.2928 | -0.3039 | -0.31497 | -0.32618 | -0.33686 | -0.34786 | -0.35868 | -0.36961 | -0.38036 | -0.39051 | -0.40017 | -0.41225 | -0.42338 | -0.43247 | -0.44817 | -0.52327 | -1.2989 | -1.178 | -0.45591 | 0.65702 | -0.043029 | 0.29947 | -0.30842 | -0.062959 | -0.036257 | -0.0045847 | -0.00045843 | -6.5972e-05 | -1.4417e-05 | -3.924e-06 | -1.1927e-06 | -3.9146e-07 | -1.3723e-07 | -5.1049e-08 | -2.0095e-08 | -8.2992e-09 | -3.5846e-09 | -1.6598e-09 | -7.6064e-10 | -3.7496e-10 | -1.929e-10 | -9.8611e-11 | -7.1372e-11 | -1.3994e-11 | -4.2101e-11
a2 | -1.1192 | -1.0202 | -0.8741 | -0.77335 | -0.73424 | -0.75942 | -0.86529 | -1.0855 | -1.4598 | -2.0196 | -2.8128 | -3.9196 | -5.4435 | -7.5269 | -10.39 | -14.351 | -19.871 | -27.503 | -37.464 | -47.747 | -51.105 | -43.953 | -50.387 | -145.19 | -275.55 | -306.33 | -145.78 | 144.42 | 327.96 | 268.94 | 175.29 | 104.93 | 61.661 | 37.113 | 23.241 | 15.171 | 10.288 | 7.2145 | 5.2078 | 3.8542 | 2.9147 | 2.2458 | 1.7591 | 1.398 | 1.1253 | 0.9163 | 0.75382 | 0.62594 | 0.52416 | 0.44231 | 0.37589
a4 | -0.8716 | -0.90035 | -0.93672 | -0.97346 | -1.0108 | -1.0487 | -1.0869 | -1.1254 | -1.1637 | -1.2028 | -1.2414 | -1.2804 | -1.319 | -1.3578 | -1.3958 | -1.4314 | -1.4642 | -1.4952 | -1.5293 | -1.6163 | -1.8603 | -3.7839 | -11.221 | -24.239 | -33.011 | -25.068 | 0.16219 | 25.63 | 37.024 | 12.95 | 2.8588 | 0.061841 | -0.23637 | -0.14871 | -0.074522 | -0.036319 | -0.018131 | -0.0094114 | -0.0050941 | -0.0028701 | -0.0016778 | -0.0010142 | -0.00063167 | -0.00040417 | -0.00026495 | -0.00017751 | -0.0001213 | -8.4384e-05 | -5.9669e-05 | -4.2826e-05 | -3.1161e-05
a6 | 0.72944 | 0.7265 | 0.72279 | 0.71915 | 0.7153 | 0.71099 | 0.70752 | 0.70353 | 0.69948 | 0.69478 | 0.69118 | 0.68679 | 0.68241 | 0.67799 | 0.67377 | 0.66895 | 0.6641 | 0.66009 | 0.65533 | 0.64722 | 0.62069 | 0.40548 | -0.95309 | -3.0827 | -4.0809 | -2.769 | -0.86304 | -1.1226 | 0.21362 | -0.77316 | -0.22862 | -0.042185 | -0.0051362 | -0.00035434 | 6.6143e-05 | 5.039e-05 | 2.2979e-05 | 9.7271e-06 | 4.145e-06 | 1.8215e-06 | 8.3132e-07 | 3.9451e-07 | 1.9445e-07 | 9.9283e-08 | 5.239e-08 | 2.8495e-08 | 1.5916e-08 | 9.1718e-09 | 5.3922e-09 | 3.2638e-09 | 1.9977e-09
Integrated bn & an | Value (10-4)
b3 | 0.14
b5 | 1.42
b7 | -0.40
a2 | -0.29
a4 | -1.81
a6 | 0.03
Q. Xu et. al., 20-T Dipole Magnet with Common Coil Configuration: Main Characteristics and Challenges, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016，4000404
With common coil configuration
20-T dipole magnet with common coil configuration two Φ50 mm beam pipes; load line 80% @ 1.9 K
Main parameters of the magnet
Integrated field quality

## Slide 64: Concept of the SPPC 20-T Dipole Magnet
Lorentz force per aperture:
Fx=23.4 MN/m ; Fy=2.38 MN/m
Stress distribution after excitation
K. Zhang et. al., 2-D Mechanical Design Study of a 20-T Two-in-One Common-Coil Dipole Magnet for High-Energy Accelerators, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016, 4003705
2D & 3D structure of the 20T dipole magnet
With common coil configuration

## Slide 65: Design Study of the SPPC Dipole Magnets
Different coil configurations for 20-T dipole magnet
Left: Common coil
Right: Cos-theta
Common coil
Cos-theta
Coil ends
Common coil
Cos-theta
Common coil vs Cos-theta
Comparison of different coil configurations

## Slide 66
Precondition (Iron based conductor, ReBCO, Bi-2212)
The Je of the HTS conductors is high enough for accelerator application
The cost is lower than or similar with the LTS conductors
Mechanical performance is qualified
Main challenges of the HTS technology
Field quality control：10-4 field uniformity needed for accelerators
Quench protection：quench propagation speed of HTS conductors is about two orders of magnitude lower than the LTS case
Cable fabrication：how to fabricate high-current cable with tapes?
Coil layout：compact, high efficiency, stress control, …
Advantages of the all-HTS magnet：
Possibility of reducing the cost significantly (Iron based conductor, ReBCO)
Possibility of raising the operation temperature of the magnet（4.2K -> ?K）
All-HTS High Field Magnet?

## Slide 67: Summary
Magnet & CEPC-SPPC: High field magnet technology is the key to the success of the high energy accelerators in future.
SPPC design scope: 12 T IBS magnets to reach 70TeV with 100 km circumference. Upgrading phase: 20~24 T IBS magnets to reach 125~150 TeV.
Strong domestic collaboration for the advanced HTS conductor R&D: Make IBS the High-Tc and High-Field “NbTi” conductor in 10 years!
R&D of high field magnet technology: Starting to develop Nb3Sn+HTS magnet technology before applicable iron-based wire is available: ReBCO & Bi-2212 and LTS wires be used for model magnet studies and as an option for SPPC.

## Slide 68: Questions and Discussions