## Slide 1
Theory of RF Superconductivity: Primer
Takayuki Kubo (KEK & ODU)
Version 2
Dec.11, 2018
https://researchmap.jp/kubotaka/
Web page

## Slide 2
Introduction

## Slide 3
Superconductivity: Meissner effect
T>Tc
There is a “critical temperature Tc“ above which is a normal metal.

## Slide 4
T>Tc
Below Tc, becomes superconducting state
T<Tc
Cool down
Superconductivity: Meissner effect

## Slide 5
T>Tc
There is no magnetic flux inside the superconducting material !!
T<Tc
T<Tc
Cool down
Apply H0
Superconductivity: Meissner effect

## Slide 6
T>Tc
Let us restart from the normal state (T>Tc).
Superconductivity: Meissner effect

## Slide 7
T>Tc
Let us restart from the normal state (T>Tc)
and apply the magnetic field.
T>Tc
Apply H0
Superconductivity: Meissner effect

## Slide 8
T>Tc
Then cool down to T<Tc. We have no magnetic flux in this case too!
T>Tc
Apply H0
T<Tc
Cool down
Superconductivity: Meissner effect

## Slide 9
T>Tc
T>Tc
T<Tc
T<Tc
Apply H0
Cool down
Cool down
Apply H0
Path 1
Path 2
In both the paths, we have no magnetic flux inside!
Meissner effect
Superconductivity: Meissner effect

## Slide 10
Note that
T>Tc
T<Tc
Flux expulsion
This is a separate physical phenomenon associated with superconductivity.
The perfect conductivity (zero DC resistance) can explain the phenomenon shown in Path 1 (Lenz’s law), but cannot explain Path 2:

## Slide 11
T>Tc
Superconductivity: persistent current
Let us consider a ring made from a superconducting material (T>Tc).

## Slide 12
T>Tc
Superconductivity: persistent current
Keep T>Tc and apply the magnetic field.
T>Tc
Apply H0

## Slide 13
T>Tc
Superconductivity: persistent current
Cool down (T<Tc). Flux is excluded from the material. Some flux keep penetrating the hole.
T>Tc
T<Tc
Apply H0
Cool down

## Slide 14
T>Tc
T>Tc
Superconductivity: persistent current
T<Tc
T<Tc
Turn OFF the magnetic field. Since the flux penetrating the hole cannot go beyond the material, it is conserved.
The persistent current supports flux.
Apply H0
Cool down
Turn OFF

## Slide 15
The zero DC resistance is a useful characteristic of superconductivity.
As seen below, under a finite frequency (RF) and a finite temperature, superconducting material exhibits a finite resistance, but its resistance at is still much smaller than normal conductors.
superconducting resonant cavity for
particle accelerators (SRF cavity)
There are other RF applications (e.g., photon detector, quantum computing etc.)

## Slide 16
Superconducting RF Cavity: introduction (1)
Picture of a 1.3GHz single cell elliptical cavity for International Linear Collider, made from ultra pure niobium material.
Cell
Beam pipe

## Slide 17
Superconducting RF Cavity: introduction (2)
Electric field
Particles enter the “cell” through the beam pipe and are accelerated by the electric field parallel to the axis.
The average electric field the particles see during transit is called “Gradient” or “”.

## Slide 18
Superconducting RF Cavity: introduction (2)
Electric field
Magnetic field
Particles enter the “cell” through the beam pipe and are accelerated by the electric field parallel to the axis.
The average electric field the particles see during transit is called “Gradient” or “”.
is proportional to the surface magnetic field , and we can write . Here is a constant defined by a cavity design. So we often use , instead of .
Improving or is one of the most important tasks for SRF researchers.
e.g., mT/(MV/m) for Tesla design cavities

## Slide 19
Superconducting RF Cavity: introduction (3)
Electric field
Magnetic field
The other important parameter is “Quality factor” or “”, which is the ratio of stored energy to dissipation per RF cycle.
is proportional to the inverse of surface resistance (explained below): . Here is a constant defined by a cavity design. So we often use instead of .
Increasing or reducing is also the most important task for us.
e.g., for Tesla design cavities

## Slide 20
Superconducting RF Cavity: introduction (4)
So, performances of cavities are summarized in plots like this.
(or ) and (or ) are
the most important parameters in SRF!!!
want to improve

## Slide 21
When we discuss (or ) and (or ), we encounter the following keywords: superconducting gap, coherence length, Meissner effect, penetration depth, vortex, flux quantum, lower critical field (Hc1), superheating field (Hsh) etc.
The goal of this lecture is to introduce these keywords by using only elementary techniques. (We do NOT use advanced theoretical techniques such as the finite temperature Green’s function.)

## Slide 22
BCS Theory: nut shell
You do not need to follow all the contents in this chapter.
Only , , and macroscopic wavefunction are the important concept in this chapter.

## Slide 23
Boson and Fermion
Two particles
is position or momentum or some other index of states
Particle 1 is
in “a” state.
Particle 2 is
in “b” state.
Let us consider two identical particles. Let us write the state vector as

## Slide 24
Boson and Fermion
Let us consider two identical particles. Let us write the state vector as
Two particles
is position or momentum or some other index of states
Since we cannot distinguish identical particles,
or
Every time we exchange particle 1 and 2, the factor C is multiplied.
Here
Particle 1 is
in “a” state.
Particle 2 is
in “b” state.

## Slide 25
Boson and Fermion
Two particles
is position or momentum or some other index of states
Since we cannot distinguish identical particles,
or
Every time we exchange particle 1 and 2, the factor C is multiplied.
Here
Particle 1 is
in “a” state.
Particle 2 is
in “b” state.
Let us exchange them again
Let us consider two identical particles. Let us write the state vector as

## Slide 26
Boson and Fermion
Two particles
is position or momentum or some other index of states
Since we cannot distinguish identical particles,
or
Every time we exchange particle 1 and 2, the factor C is multiplied.
Here
Particle 1 is
in “a” state.
Particle 2 is
in “b” state.
Let us exchange them again
“C=+1 particle”: Boson
“C= -1 particle” : Fermion
There are two types of particle!
Let us consider two identical particles. Let us write the state vector as

## Slide 27
Boson and Fermion (2)
Let us consider two fermions (e.g., electrons).
If both the particles 1 and 2 are in the “a” state, the wave function is

## Slide 28
Boson and Fermion (2)
Let us consider two fermions (e.g., electrons).
If both the particles 1 and 2 are in the “a” state, the wave function is
Exchanging the two particles, we have
Two fermions cannot occupy the same states.
Pauli’s exclusion principle

## Slide 29
Boson and Fermion (2)
Let us consider two fermions (e.g., electrons).
If both the particles 1 and 2 are in the “a” state, the wave function is
Exchanging the two particles, we have
Two fermions cannot occupy the same states.
Pauli’s exclusion principle
Now consider N fermions.
If two of N fermions occupy the same state “f”, we have
exchange
Pauli’s exclusion principle

## Slide 30
Consider a particle confined in a potential. Suppose we can solve the one-particle Schrodinger equation and know the energy spectrum.
Here we assume the spectrum does not degenerate for simplicity.
Boson and Fermion (3): many particles
1
2
3
4
5

## Slide 31
1
2
3
4
5
1
2
3
4
5
Boson and Fermion (3): many particles
Each level can be dominated by an arbitrary number of particles.
Boson (e.g., photon, 4He)
Fermion (e.g., electron)
Each level can be dominated by 0 or 1 particle (exclusion principle).

## Slide 32
Boson at low temperatures
1
2
3
4
5
What happens in many boson system at low temperatures?

## Slide 33
Boson at low temperatures
1
2
3
4
5
At below a temperature , a macroscopic number of particles “condense” to the ground state: Bose-Einstein condensation (BEC)
1
2
3
4
5
Macroscopic wave function

## Slide 34
Fermion at low temperatures (1)
In contrast to bosons, N() fermions cannot occupy the same state.
Particles are piled up from the ground state.
The highest level occupied when T=0 is called the Fermi energy .
…

## Slide 35
Fermion at low temperatures (2)
…
Let us consider free electron gas.
This corresponds with a number of electrons (the right figure).
We find or
Its momentum is given by where
The particle energy is given by
Since , a total number of states below is a number of lattice inside the sphere with the radius .
is the electron density
Its energy scale is typically eV
The periodic
boundary condition

## Slide 36
Fermion at low temperatures (3): Cooper pair
When an attractive potential exists, no matter how weak, a significant effect sets in: electrons form pairs!
Example of attraction potential:
Electron-phonon interaction
Two electrons in vacuum do not form a pair without a strong attractive force.
When two electrons put on the Fermi sea, however, they make a pair by a weak force, no matter how weak.
The origin of attractive force in the low TC superconductors is the Electron-phonon interaction, but meanwhile you do not need to care about what the origin is.

## Slide 37
Fermi sea
Schrodinger equation
Fermion at low temperatures (4): Cooper pair

## Slide 38
Here we simplifies the electron-electron interaction
Fermion at low temperatures (4): Cooper pair
Then we have
Debye frequency

## Slide 39
Let’s solve
or
We obtain
Self-consistency requires
By using we obtain
Fermion at low temperatures (4): Cooper pair
This is the point! Since ,
We have 2D-like self-consistency equation.

## Slide 40
We examined the very simple case: only two electrons and Fermi sea.
When an attractive potential exists, no matter how weak, electrons form a pair and stabilize energy by E.
Fermion at low temperatures (5): Cooper pair
This pair is a boson!

## Slide 41
We examined the very simple case: only two electrons and Fermi sea.
When an attractive potential exists, no matter how weak, electrons form a pair and stabilize energy by E.
What happens for the many electrons system?
(The BCS theory)
Fermion at low temperatures (5): Cooper pair
Bose-Einstein condensate of pairs!
Macroscopic wave function.
This pair is a boson!
Typical scale of is for SRF materials (e.g., Nb, Nb3Sn). This is much smaller than Fermi energy.
BCS theory

## Slide 42
Fermion at low temperatures (6): Coherence length
Let us calculate the mean square radius of a Cooper pair.
Using the wave function obtained above.
where
and
In BCS theory, the pair wave function (anomalous Green’s function) is given by
Typical scale of is -100 nm for SRF materials (e.g., Nb, Nb3Sn). This is much larger than typical electron-electron distance: Cooper pairs are overlapped.
Coherence length (BCS)

## Slide 43
Meissner state and vortex state
SRF cavities are operated under the Meissner state.
This is the significant difference from superconducting magnet.
Hc2 is NOT important.
Hc1 and Hsh (superheating field) are important in SRF

## Slide 44
: Cooper pair density
Let us write the macroscopic wavefunction of condensate as
London equation and Meissner effect (1)

## Slide 45
: Cooper pair density
Using the momentum operator,
we obtain the current density:
London equation and Meissner effect (1)
Let us write the macroscopic wavefunction of condensate as

## Slide 46
: Cooper pair density
Using the momentum operator,
we obtain the current density:
Here is defined by
London equation and Meissner effect (1)
Let us write the macroscopic wavefunction of condensate as

## Slide 47
rot
Here we used
London equation and Meissner effect (2)

## Slide 48
rot
Maxwell eq.
London equation
Here we used
London equation and Meissner effect (2)

## Slide 49
rot
Maxwell eq.
London equation
In Cartesian coordinate, we have . Since we obtain
Here we used
London equation and Meissner effect (2)
We can easily check the dimension of since , .

## Slide 50
London equation and Meissner effect (3): example
Consider a 1D system
x
y
Superconductor
The London eq. is reduced to
The solution is
We impose
finite : →
: →

## Slide 51
Consider the right figure
x
y
Superconductor
Here .
Homework #1
Calculate the screening current distribution. You can use the Maxwell equation:

## Slide 52
Flux quantization
Let us consider a superconducting ring.
We define “Path C” inside the ring.
Assume the distance between C and the surface is much larger than . Then we have zero current on C due to the Meissner effect.
C

## Slide 53
Flux quantization
Let us consider a superconducting ring.
We define “Path C” inside the ring.
Assume the distance between C and the surface is much larger than . Then we have zero current on C due to the Meissner effect.
C
Remind the formula:
Since j=0, we have
on the path C

## Slide 54
Flux quantization
Let us consider a superconducting ring.
We define “Path C” inside the ring.
Assume the distance between C and the surface is much larger than . Then we have zero current on C due to the Meissner effect.
C
Remind the formula:
Since j=0, we have
on the path C

## Slide 55
Flux quantization
Let us consider a superconducting ring.
We define “Path C” inside the ring.
Assume the distance between C and the surface is much larger than . Then we have zero current on C due to the Meissner effect.
C
Remind the formula:
Since j=0, we have
on the path C
(Remind is the phase of wave function!)

## Slide 56
Flux quantization
Let us consider a superconducting ring.
We define “Path C” inside the ring.
Assume the distance between C and the surface is much larger than . Then we have zero current on C due to the Meissner effect.
C
Remind the formula:
Since j=0, we have
on the path C
(Remind is the phase of wave function!)
Then we find

## Slide 57
Homework #2
Calculate
Check its dimension.
You can easily confirm . Let us remind
You can use

## Slide 58
Vortex (1)
Superconducting
ring containing
Superconductor with
a normal conducting string
containing
hole
Normal string

## Slide 59
Vortex (2): field distribution
C
Remind the formula:

## Slide 60
Vortex (2): field distribution
C
Remind the formula:
Let us integrate both the side along C.

## Slide 61
Vortex (2): field distribution
C
Remind the formula:
Let us integrate both the side along C.
The second term is negligible when . Thus
Here is used.

## Slide 62
Vortex (2): field distribution
C
Remind the formula:
Let us integrate both the side along C.
The second term is negligible when . Thus
Here is used.

## Slide 63
Vortex (3): current distribution

## Slide 64
Vortex (3): current distribution
At , the current density is

## Slide 65
Vortex (3): current distribution
At , the current density is
Kinetic energy of Cooper pair is
Superconductivity is broken when becomes comparable with .
This happens at
The radius of the normal conducting core is
or

## Slide 66
Vortex (4): energy
: Cooper pair density,
: Cooper pair charge,
: superfluid velocity
: Cooper pair mass,
Kinetic energy density of supercurrent around a vortex is

## Slide 67
Vortex (4): energy
: Cooper pair density,
: Cooper pair charge,
: superfluid velocity
: Cooper pair mass,
Kinetic energy density of supercurrent around a vortex is
Total kinetic energy of supercurrent around a vortex is
Length of the vortex

## Slide 68
Vortex (4): energy
: Cooper pair density,
: Cooper pair charge,
: superfluid velocity
: Cooper pair mass,
The energy of the vortex per unit length:
Kinetic energy density of supercurrent around a vortex is
Total kinetic energy of supercurrent around a vortex is
Length of the vortex

## Slide 69
Vortex (5): energy
While the flux quantization permit , we have assumed vortex contains a single flux quantum (n=1). Now we can understand this reason by using this result:
vortices with a single flux quantum is more stable than a single vortex with .

## Slide 70
Lower Critical Field Hc1
When and there are no vortices (),
When and there is a single vortex (with length ),
The lower critical field is where
vortex

## Slide 71
Lower Critical Field Hc1
We can calculate for an arbitrary vortex position. When the vortex is located at , we have (see Appendix)
: applied magnetic field

## Slide 72
Lower Critical Field Hc1
When , we have . This means that a superconductor containing a vortex is unstable.
Vortex state is unstable.
Meissner state is stable.
Vortex position
Meissner state
Vortex state
nm, nm

## Slide 73
Lower Critical Field Hc1
When , we have . This means that a superconductor containing a vortex is unstable.
Vortex state is unstable.
Meissner state is stable.
Vortex position
When , we have . This means that a superconductor containing a vortex is as stable as that without a vortex.
Vortex state is as stable as Meissner state.
Vortex position
Meissner state
Vortex state
Vortex state
Meissner state
nm, nm
nm, nm

## Slide 74
Superheating Field Hsh
Let us consider , where we have .
This means a superconductor containing a vortex is more stable than that without a vortex.
Vortex state is more stable than Meissner state.
Vortex state
Meissner
state
nm, nm

## Slide 75
Superheating Field Hsh
Let us consider , where we have .
This means a superconductor containing a vortex is more stable than that without a vortex.
Vortex state is more stable than Meissner state.
Vortex state
Meissner
state
Meissner state is still “metastable”.
It is not the global minimum but a local minimum.
There is an “energy barrier”.
Energy barrier
nm, nm

## Slide 76
Superheating Field Hsh
When does the Meissner state become completely unstable?
It is when exceeds the superheating field at which the energy barrier disappears: is flat at .
Note here our formulation is not applicable to the vicinity of the vortex core: we have a short distance cutoff . So we examine the condition is flat at instead of . Then
or
nm, nm
Vortex state
Meissner state
(completely unstable)
Here the GL result is used

## Slide 77
Superheating Field Hsh
The above calculation is a rough estimate. To calculate the correct , the pair breaking effect must be taken into account.
At , Ginzburg-Landau theory is available:

## Slide 78
Superheating Field Hsh
The above calculation is a rough estimate. To calculate the correct , the pair breaking effect must be taken into account.
At , Ginzburg-Landau theory is available:
To calculate the correct at , more advanced theoretical techniques (e.g. quasiclassical Green’s function) are necessary.
Here , is the normal density of states at the Fermi energy.

## Slide 79
Q-E curve
170mT
0mT
85mT
of Nb
of Nb
210mT
1.3GHz
elliptical
Nb cavity
Our cavities can regularly exceed , but have never achieved . The ultimate limit of cavities made from bulk material is considered as
Note that when material has a layered structure, theoretical filed limit is pushed up.

## Slide 80
Homework #3
Estimate () of Nb3Sn. You can use mT.
Calculate the corresponding value of for Tesla shape cavity. You can use the relation between the surface magnetic field and gradient: and mT/(MV/m).
Compare it with the record field of Nb cavity, -210mT
Nb3Sn is the candidate for the next generation SRF material. One of the reason is its higher theoretical field limit. To achieve the field comparable to , the multilayer approach is proposed.

## Slide 81
If you are interested in the newest discussion on the high-Eacc SRF cavity, the following review is useful:
T. Kubo, Superconductor Science and Technology 30, 023001 (2017).
This review contains
Superheating field (London, Ginzburg-Landau, Eilenberger eq)
Multilayer coating for a future high-Eacc technology
Bilayer for a future high-Eacc technology (the performances of modern surface processing i.e., N-infusion and baking may also be explained by bilayer structure)
References related to this lecture are also contained in this paper.
* Multilayer coating of SRF cavity was proposed by A. Gurevich in 2006 to push up the theoretical field limit of SRF cavity. [A. Gurevich, Appl. Phys. Lett. 88, 012511 (2006)]

## Slide 82
Surface resistance and
Quality factor

## Slide 83
Conductivity
Suppose the field is switched ON at t=0
The Fourier transform is given by
is introduced to converge the integral

## Slide 84
Conductivity (2)
For a finite temperature, however, Cooper pairs are thermally dissociated, and the normal contribution appears:

## Slide 85
Conductivity (2)
For a finite temperature, however, Cooper pairs are thermally dissociated, and the normal contribution appears:
At , we have the infinite conductivity: zero DC resistance.

## Slide 86
Conductivity (2)
For a finite temperature, however, Cooper pairs are thermally dissociated, and the normal contribution appears:
At , we have the infinite conductivity: zero DC resistance.
At , we have a finite conductance .
The calculation based on the BCS theory (Mattis-Bardeen) leads to
for a dirty limit superconductor at .

## Slide 87
Surface impedance of bulk superconductors
Here we use “engineer notation”

## Slide 88
Surface impedance of bulk superconductors
Here we use “engineer notation”
x
y

## Slide 89
Surface impedance of bulk superconductors
Here we use “engineer notation”
x
y

## Slide 90
Surface impedance of bulk superconductors
Here we use “engineer notation”
x
y

## Slide 91
Surface impedance of bulk superconductors (2)
By using
we can calculate
and

## Slide 92
Surface impedance of bulk superconductors (2)
By using
we can calculate
Here is used.
and

## Slide 93
Quality factor (1)
x
(depth)
y
Let us calculate RF dissipation per unit area and unit time.

## Slide 94
Quality factor (1)
x
(depth)
y
You can confirm that reproduces
Let us calculate RF dissipation per unit area and unit time.
Confirm the dimension of P is given by

## Slide 95
Quality factor (2)
Magnetic field
Inside the cavity, depends on a point of the inner surface:
Here is a point on the inner surface. Since the depth dependence is the same as the last page, we have
The total dissipation in the cavity is
Assume is position independent

## Slide 96
Quality factor (3)
Quality factor is defined by the ratio of stored energy to dissipation per RF cycle:

## Slide 97
Quality factor (3)
Quality factor is defined by the ratio of stored energy to dissipation per RF cycle:
Point on the surface
Point in the cavity volume

## Slide 98
Quality factor (3)
Quality factor is defined by the ratio of stored energy to dissipation per RF cycle:
Point on the surface
Point in the cavity volume

## Slide 99
Quality factor (3)
Quality factor is defined by the ratio of stored energy to dissipation per RF cycle:
Point on the surface
Point in the cavity volume
Here
is known as the geometrical constant.
The dimension of numerator and denominator are and , respectively. So the dimension of (numerator/denominator) is . This should be proportional to typical length scale of cavity, so it is . This is always cancelled out with the factor . Then is a constant that depends on the cavity shape, not on the size.
e.g., for Tesla design cavities

## Slide 100
Homework #4
Confirm the dimension of is given by
Confirm the dimension of and are given by and .
Confirm the dimension of is given by .
Suppose you measured of Tesla shape cavity at T=2K and obtained . What is of your cavity surface? You can use the geometrical constant of Tesla shape cavity G=270 .

## Slide 101
Q-E curve
170mT
0mT
85mT
of Nb
of Nb
210mT
You can see that (or ) depends on the surface field . The field dependent surface resistance is generally seen in SRF cavities. Moreover the curve is drastically changed by materials processing. Physics behind is one of the important research topics in SRF.

## Slide 102
“Flavor” of modern discussion
on the surface resistance of SRF cavities
T. Kubo and A. Gurevich, “Field-dependent surface resistance and engineering optimal surface nano-structuring of SRF cavities”, The 8th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity, INFN, Italy (2018)

## Slide 103
What is the origin of many different Q-E curves?
A. Grassellino, et al.,
Supercond. Sci. Technol. 30, 094004 (2017)
G. Ciovati, J. Appl. Phys. 96, 1591 (2004);
P. Dhakal, et al.,
Phys. Rev. ST Accel. Beams 16, 042001 (2013)
A. Grassellino et al.,
Supercond. Sci. Technol. 26 (2013) 102001
The longstanding mystery in SRF
C. Benvenuti et al., Physica C 351, 421 (2001)
T. Kubo etal., IPAC14, Dresden, Germany (2014), p. 2519, WEPRI022

## Slide 104
Unfortunately, the Mattis-Bardeen’s formula for the weak-field Rs tells you nothing about the shape of Q-E curve.
?
A. Grassellino, et al.,
Supercond. Sci. Technol. 30, 094004 (2017)

## Slide 105
Unfortunately, the Mattis-Bardeen’s formula for the weak-field Rs tells you nothing about the shape of Q-E curve.
  It is valid only at the weak-field limit: the left end of Q-E curve.

## Slide 106
Unfortunately, the Mattis-Bardeen’s formula for the weak-field Rs tells you nothing about the shape of Q-E curve.
  It is valid only at the weak-field limit: the left end of Q-E curve.
  Moreover, effects of material features other than mfp are not taken into account: thus may not be valid even at the weak-field limit.
?
?

## Slide 107
Unfortunately, the Mattis-Bardeen’s formula for the weak-field Rs tells you nothing about the shape of Q-E curve.
  It is valid only at the weak-field limit: the left end of Q-E curve.
  Moreover, effects of material features other than mfp are not taken into account: thus may not be valid even at the weak-field limit.
?
?
Need to develop
a theory of
field dependent Rs including realistic material features.

## Slide 108
Review: Progresses in theory (part 1)
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)

## Slide 109
Review: Progresses in theory (part 1)
DOS
The surface resistance is given by
Here is roughly (when and )
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)

## Slide 110
Idealized BCS DOS
Weak-field limit
Review: Progresses in theory (part 1)
DOS
The surface resistance is given by
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
Here is roughly (when and )

## Slide 111
Idealized BCS DOS
Weak-field limit
Mattis Bardeen’s formula
comes from this DOS
Review: Progresses in theory (part 1)
DOS
The surface resistance is given by
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
Here is roughly (when and )

## Slide 112
Idealized BCS DOS
Weak-field limit
Mattis Bardeen’s formula
comes from this DOS
Review: Progresses in theory (part 1)
DOS
The surface resistance is given by
Broadening of the gap peaks in N(ε) by current was calculated 50 years ago:
K. Maki, Prog. Theor. Phys. 29, 333 (1963).
K. Maki, in Superconductivity, part 2, ed. R.D. Parks, 1967.
Anthore et al., PRL 90, 127001 (2003)
DOS under a dc current
However, we know the DOS is modified under the pair-breaking current.
Experimentally confirmed:
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
Here is roughly (when and )

## Slide 113
Idealized BCS DOS
Weak-field limit
Mattis Bardeen’s formula
comes from this DOS
Review: Progresses in theory (part 1)
DOS
The surface resistance is given by
Under a strong rf current
DOS peaks oscillate (animation)
However, we know the DOS is modified under the pair-breaking current.
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
Here is roughly (when and )

## Slide 114
Idealized BCS DOS
Weak-field limit
Mattis Bardeen’s formula
comes from this DOS
Review: Progresses in theory (part 1)
DOS
The surface resistance is given by
Under a strong rf current
DOS peaks oscillate (animation)
However, we know the DOS is modified under the pair-breaking current.
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
This logarithmic factor
in MB’s formula comes from the sharp peak of the idealized BCS DOS
Here is roughly (when and )

## Slide 115
Idealized BCS DOS
Weak-field limit
Mattis Bardeen’s formula
comes from this DOS
Review: Progresses in theory (part 1)
DOS
The surface resistance is given by
Under a strong rf current
DOS peaks oscillate (animation)
However, we know the DOS is modified under the pair-breaking current.
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
decreases
Here is roughly (when and )

## Slide 116
Review: Progresses in theory (part 1)
Under a strong rf current
DOS peaks oscillate (animation)
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
decreases
Broadening of DOS peaks causes the Q rise
Gap shrinks
This is the ideal QE curve derived from the BCS theory.

## Slide 117
Incorporated effects of pair-breaking mechanisms originating from
realistic material features into Rs at the weak-field limit.
Review: Progresses in theory (part 2)
A. Gurevich and T. Kubo,
Phys. Rev. B 96, 184515 (2017)

## Slide 118
Incorporated effects of pair-breaking mechanisms originating from
realistic material features into Rs at the weak-field limit.
Review: Progresses in theory (part 2)
Subgap states originating from a finite quasiparticle lifetime.
Surface layer of gradually reduced BCS pairing constant.
Proximity coupled thin Normal layer on the surface
Small density of magnetic impurities
A. Gurevich and T. Kubo,
Phys. Rev. B 96, 184515 (2017)

## Slide 119
Incorporated effects of pair-breaking mechanisms originating from
realistic material features into Rs at the weak-field limit.
Review: Progresses in theory (part 2)
Subgap states originating from a finite quasiparticle lifetime.
Surface layer of gradually reduced BCS pairing constant.
Proximity coupled thin Normal layer on the surface
Small density of magnetic impurities
A. Gurevich and T. Kubo,
Phys. Rev. B 96, 184515 (2017)

## Slide 120
Incorporated effects of pair-breaking mechanisms originating from
realistic material features into Rs at the weak-field limit.
Review: Progresses in theory (part 2)
Subgap states originating from a finite quasiparticle lifetime.
Surface layer of gradually reduced BCS pairing constant.
Proximity coupled thin Normal layer on the surface
Small density of magnetic impurities
S
N
Thinner than
A. Gurevich and T. Kubo,
Phys. Rev. B 96, 184515 (2017)

## Slide 121
Incorporated effects of pair-breaking mechanisms originating from
realistic material features into Rs at the weak-field limit.
Review: Progresses in theory (part 2)
Subgap states originating from a finite quasiparticle lifetime.
Surface layer of gradually reduced BCS pairing constant.
Proximity coupled thin Normal layer on the surface
Small density of magnetic impurities
S
N
Thinner than
Magnetic impurities
A. Gurevich and T. Kubo,
Phys. Rev. B 96, 184515 (2017)

## Slide 122
Incorporated effects of pair-breaking mechanisms originating from
realistic material features into Rs at the weak-field limit.
Review: Progresses in theory (part 2)
Subgap states originating from a finite quasiparticle lifetime.
Surface layer of gradually reduced BCS pairing constant.
Proximity coupled thin Normal layer on the surface
Small density of magnetic impurities
S
N
Thinner than
Magnetic impurities
These structures model realistic surfaces of superconducting materials which can contain oxide layers, absorbed impurities or nonstoichiometric composition.
A. Gurevich and T. Kubo,
Phys. Rev. B 96, 184515 (2017)

## Slide 123
The rest of this discussion is in
T. Kubo and A. Gurevich, “Field-dependent surface resistance and engineering optimal surface nano-structuring of SRF cavities”, The 8th International Workshop on Thin Films and New Ideas for Pushing the Limits of RF Superconductivity, INFN, Italy (2018)
If you are interested in the modern discussion of the surface resistance (or Q0) beyond the Mattis-Bardeen surface resistance, see the following papers.
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
A. Gurevich and T. Kubo, Phys. Rev. B 96, 184515 (2017)

## Slide 124
The lecture note will be uploaded on arXiv or somewhere

## Slide 125
Appendix

## Slide 126
Appendix: calculation of G
Here we used the formula
Here S is the boundary of the superconductor:
the surface of material and the rim of a vortex core.

## Slide 127
Appendix: calculation of G
Here S is the boundary of the superconductor:
the plane surface of material () and the rim of a vortex core ().
Core surface
plane surface
Let us decompose and into and .
Here is the contribution from the applied field, and is the associated Screening current.
is the contribution from the vortex, and is the current circulating around the vortex.
Here
is used. This can be confirmed by reminding

## Slide 128
Appendix: calculation of G
Core surface
plane surface
is the contribution from the vortex. Instead of struggling with the boundary condition, we may consider an isolated vortex and isolated image antivortex. So vanished on . Then the 1st and 2nd term vanishes.
is the screening current and is not singular at the core.
Thus the 4th term also vanishes as .