## Slide 1: Hands-on Training (SC Cavity)
Peng SHA (shapeng@ihep.ac.cn),
Chao DONG, Lingxi YE

## Slide 2: School Time Table

## Slide 3: Course Outline
Science Background : Surface resistance
RF Surface Resistance Measurement
Q Measurement of Nb Cavity Loaded with Dielectric
(1) Basic Physics Formulas
(2) Apparatus and Setup
(3) Procedures and Data Analysis

## Slide 4: Surface resistance——Rs
Comparison of Rs between NC and SC cavity
NC Cavity | SC Cavity
1. Conductivity/Resistivity 2. DC resistance 3. Skin depth 4. RF surface resistance | RF surface resistance temperature-dependent term : BCS resistance temperature-independent term : Residual resistance
kB : Boltzmann constant
Δ : Gap energy of Cooper pair

## Slide 5: Surface resistance——Rs
An example of Rs and Q0 of NC and SC cavity
NC Cavity | SC Cavity
Freq. = 1.3 GHz G = 270 Ω Cu (20⁰C) ：σ = 0.58e+8 [1/Ωm] Rs = 9.4 mΩ (δ = 1.8 um) Q0 = G/Rs = 2.9e+4 | Freq. = 1.3 GHz G = 270 Ω Rs = 17 nΩ (δ = 44 nm) Q0 = G/Rs = 1.6e+10
Rs(Cu)/Rs(Nb) = 5.5e+5 Q0(Nb)/Q0(Cu) = 5.5e+5 | 

## Slide 6: RF Rs of Small Sample Measured by Nb Cavity Loaded with Dielectric Sapphire
Freq：4GHz 和 6.9GHz
Mode：TE011 和 TE021
Niobium cavity
Input
antenna
Transmitted antenna
upper cover plate
Filled with sapphire
Fixed input antenna
Phi12mm sample:
In the middle of
lower cover plate
Why choose sapphire?
Loss angle tangent is very small at low temperature,
~10^-8 or ~10^-9 at 4K.

## Slide 7
Principle of RF Rs measurement
i=1, working mode is TE011 (~4GHZ); i=2, working mode is TE021 (~6.9GHz);
(2) is the unloaded Q of the whole cavity for different modes;
(3) 、 are integral value of electromagnetic field of this cavity;
(4) is the loss angle tangent of Sapphire ( f);
(5) is the surface resistance of Nb cavity (Rs f 2 );
(6) is the surface resistance of sample.
Specific experimental steps:
Using Nb sample (same material as cavity, here, = ) to get
S parameters and QL at two modes.
Calculating using S parameter and QL.
Then we can get the value of and . From now, and
can be seen as constants.
After that, if we want to measure other materials, we can just use one stable mode
TE011 . But we can’t get this yet, because sapphire used is not good enough!

## Slide 8
Electromagnetic field simulation of TE011 4GHz
Electric Field
Magnetic Field

## Slide 9: Q Measurement of Nb Cavity Loaded with Dielectric

## Slide 10: Basic Physics Formulas
Cavity stored energy :
Cavity RF loss :
Loaded Q:
(QL is measured by bandwidth of -3dB. )
(1) Coupling constant
(over/under coupling)：
(2) Input coupling:
(3) Monitor coupling:
(4) Unloaded Q of cavity:
(5) External Q:

## Slide 11: Apparatus and Setup
A cryogenic experimental platform
from 300K to ~3.2K.
4.2k, 1.5W
Connecting thermometer
Connecting
Heater
Network Analyzer
Cable

## Slide 12: Apparatus and Setup
Hoisting cold head and top flange,
install cavity on cold dust
2-level
cold head
cold dust

## Slide 13: Apparatus and Setup
Packing well with Heat insulation material

## Slide 14: Apparatus and Setup
Start vacuum pumping. Turn on compressor when vacuum is about 10Pa.

## Slide 15: Apparatus and Setup
5 temperature sensor:
A: level1 cold head
B: Spare
C: Sample cavity
D: heat sink
E: Spare
F: level2 cold head

## Slide 16: Procedures and Data Analysis (10K)
First, getting the value of S11、S21 and QL at different temperatures.
S11 = ? S21 = ? QL = ? Temp of cavity = ?
Frequency : 4GHz (TE011)

## Slide 17
(1) Coupling constant
(over/under coupling)：
(2) Input coupling:
(3) Monitor coupling:
(4) Unloaded Q of cavity:
(5) External Q:
Procedures and Data Analysis (10K)
Second, please calculate the following parameters using the formula in Slide 10.

## Slide 18: Procedures and Data Analysis (3.5K)
First, getting the value of S11、S21 and QL at different temperatures.
S11 = ? S21 = ? QL = ? Temp of cavity = ?
Frequency : 4GHz (TE011)

## Slide 19
(1) Coupling constant
(over/under coupling)：
(2) Input coupling:
(3) Monitor coupling:
(4) Unloaded Q of cavity:
(5) External Q:
Procedures and Data Analysis (3.5K)
Second, please calculate the following parameters using the formula in Slide 10.

## Slide 20: Thanks for your attention!