## Slide 1: Fabrication and Test of HTS Coils
Ning Feipeng, Wang Chengtao
Liu Xuyang, Xie Zongtai
IHEP,CAS, China
2018-12

## Slide 2: Outline
1. Introduction of HTS
2. Fabrication of HTS coils
3. Ic test of HTS short sample and coils

## Slide 3: 1. Introduction of HTS
HTS (High Temperature Superconducting)
  Usually refers to the superconductors with critical temperature greater than 77 K (liquid Nitrogen temperature) .
  Since 1987, very short history.
  Three products: Bi-2223,Bi-2212,YBCO(Yttrium barium copper oxide)
Liquid Nitrogen
Liquid Neon

## Slide 4: Introduction of HTS
YBCO:
  Yttrium Barium Copper Oxide, YBa2Cu3O7 , Tc=90 K, Tape
  produced by coating method (CCC - coated conductor composite): using chemical deposition or physical coating methods coating a layer of YBCO superconducting film on the hastelloy substrate.
Hastelloy
Substrate
Y2O3
Al2O3
Amorphous Layer
MgO
Seed Layer
CeO2
Cap Layer
(Y,Gd)BCO
Superconducting Layer
Ag
Overlayer
Architecture of YBCO superconductor from SSTC
2G HTS:

## Slide 5
1. Introduction of HTS

## Slide 6: 2. Fabrication of HTS coils
Race track double-pancake YBCO coil fabrication.
Winding machine
Stainless steel instead of YBCO

## Slide 7: 3. Ic test of HTS short sample and coils
U (mV) | I (A) | Field(Gs)
U-I table and curve

## Slide 8: Questions 1
Four YBCO tapes, for example, ST-04-E and ST-05-L,
ST-04-E
55 μm
95 μm
ST-05-L
175 μm
350 μm
What is the critical tensile force of each tape?

## Slide 9: Question 2
n value is an important parameter of superconducting materials. What is the n value of the your tested YBCO short sample and coil?
Ec is the quench criteria 1 μV/cm, L is the length of the tape, Ic is the critical current.
The length of the coil is 23.4 m. Give your own understanding of n.

## Slide 10: The hall sensor data