## Slide 1: Recent development of ultra-fast timing detector in Cina and its potential application in CEPC
Zhijun Liang
Institute of High Energy Physics ,
Chinese Academy of Science
CECP workshop 2019

## Slide 2: Timing detector for CEPC
4D tracking for CEPC particle flow reconstruction.
Need a silicon technology with both time and spatial resolution
https://iopscience.iop.org/article/10.1088/1748-0221/11/11/C11040/pdf

## Slide 3: Timing detector for CEPC
ILD-Like, Baseline design
Full silicon
IDEA
For full silicon concept, there is no particle identification
  Need a silicon technology with both time and spatial resolution

## Slide 4: Particle identification for CEPC
K/pi separation for CEPC flavor physics for full silicon concept
  10ps time solution can provide 2~3 sigma K/pi separation at 5~7GeV
Study from Topside
Study from CEPC (by Manqi)

## Slide 5: Low gain Avalance detector (LGAD）
Low-Gain-Avalanche-detector (LGAD)
  Compared to APD and SiPM, LGAD has lower gain (~10)
  high drift velocity, thin active layer ( fast timing)
  High S/B, no self-triggering
LGAD Foundry:
HPK (Japan)
CNM(Spain)
FBK (Italy)…
IHEP-NDL (China)
Prototype of IHEP-NDL LGAD sensors

## Slide 6: LGAD sensor R & D in China： NDL LGAD sensor
  LGAD sensor with Epitaxial layer
    NDL is foundry for SipM. They started at LGAD R & D with IHEP in 2019.
    Three batches LGAD sensor fabricated in 2019.
    Thickness of epitaxial layer: 33um
      epitaxial layer Resistivity: 100 Ohm.cm or 300 Ohm.cm
http://www.ndl-sipm.net/contacteng.html

## Slide 7: IHEP-NDL sensor design
  6 guard ring (floating, no metal contact ) : BV170, BV60
  (new!!) 2 guard ring (with metal contact, can be grounded) : Type 9#, 10#
  Higher breakdown voltage (VBD) with new guard ring design
pad1
pad2
pad3
pad4
2 guard ring design
(new!!)
With metal contact
Can be grounded
6 guard ring design
No Metal contact
Guard ring floating
 | VBD | V_Depleted | Layout | Wafer | Gain
Type 13# (BV170) | ~165V | ~100V | 6GR | 100Ω.cm | 40
Type 12#(BV60) | ~95V | ~40V | 6GR | 300Ω.cm | 40
Type 10# (new!) | ~300V | ~40V | 2GR | 300Ω.cm | 80
Type 9# (new!) | ~250V | ~40V | 2GR | 300Ω.cm | 80

## Slide 8: Beta test
Beta test (collected charge, gain, time resolution)
Electrons by Sr90 Beta source
Single channel board developed by UCSC
Fast amplifier with bandwidth >1GHz
Climate chamber to run at -30C

## Slide 9: IHEP-NDL LGAD sensor performance
New LGAD foundry in China: The Novel Device Laboratory
just start prototyping LGAD sensor early 2019
Two prototype of 2x2 LGAD, 5x5 LGAD
Time resolution is about 30ps
Charge collection: 10~30 fC
30ps
4fC

## Slide 10: 5x5 NDL sensors
Two type of NDL 5x5 sensors are fabricated in Sep 2019
 | VBD | V_Depleted | Layout | Epi layer(33um) resistance | Gain
NDL 5x5 6# | ~250V | ~120V | 2 guard ring | 100Ω.cm | 10~20
NDL 5x5 12# | ~235V | 35V | 2 guard ring | 300Ω.cm | 10~20

## Slide 11: Irradiation hardness requirement
The requirements will change with different MDI design
Total ionization dose(from CDR): ~ 10MRad (100kGy）
Fluence (from CDR): ~1013Neq/cm2

## Slide 12: Irradiation campaign
Irradiation hardness is important for HGTD project
IHEP is responsible for irradiation tests
  Leading total ionization dose (TID) study for sensor and module
    X ray irradiator in IHEP, TID up to 200MRad
  Carried out one irradiation campaign for non-ionization damage
    Collaboration with China atom energy institute (CIAE) for 100MeV proton irradiation
    Fluence up to 4x1015 neq/cm2
100MeV Proton irradiation campaign in CIAE
X ray irradiation in IHEP

## Slide 13: Radiation damage effect for LGAD：Acceptor removal
Radiation damage effect for LGAD
  Acceptor removal
  Interstitials inactivate the doping elements (Boron) via kick-out reactions that produce ion-acceptor complexes
  Reduction of gain, collected charge

## Slide 14: First Results of CIAE irradiation: NDL sensors
Depleted voltage and foot voltage Vs fluence
  Much easier to depleted the LGAD sensor after 1e15 Neq/cm2
  It should be good for CEPC application (1013Neq/cm2 )
  Need more study for LHC application

## Slide 15: Acceptor removal effect
By Tao Yang
P+ doping density decrease after irradiation
  Need more study for LHC application
  It should be good for CEPC application (1013 Neq/cm2 )
CEPC irradiation hardness requirement

## Slide 16: I-V after X ray irradiation :NDL sensor (1)
 | VBD | V_Depleted | Layout | Wafer | Gain
Type 13# (BV170) | ~165V | ~100V | 6GR | 100Ω.cm | 40
Type 12#(BV60) | ~95V | ~40V | 6GR | 300Ω.cm | 40
Type 10# | ~300V | ~40V | 2GR | 300Ω.cm | 40
Type 9# | ~250V | ~40V | 2GR | 300Ω.cm | 80
I_leak is lower after irradiation
  ~ 0.1 nA
I_leak is large at low V_bias
  can improve by adjusting GR
Due to Metal pad in Guard ring?
From
Yunyun

## Slide 17: I-V after X ray irradiation : HPK sensor
Guard Ring current at 100kGy increases
  >= 4 times compared the current at 0Gy.
HPK type 3.2 with UBM
HPK type 3.1 with UBM
From Yunyun

## Slide 18: I-V after X ray irradiation : comparisons
Short summary of leakage current on working point before VBD
  NDL 9# and 10# have the same laytout (2GR design)
  9# has higher p+ dose for gain layer, longer annealing time than type 10#

## Slide 19: Laser test ： timing resolution study
Testing timing response for NDL LGAD sensor with TCT laser system
  Replace the TCT laser with pico-second pulse laser
  pico-second Laser Pulse width : 7ps; wavelength: 1064nm, , Frequency: 20MHz
Evaluate the jitter contribution
  Less than 10ps
  Laser power is larger than MIP
  Try Beta test in next step for more realistic measurement
Wirebond one pixel
to UCSC single channel board
By Yuzhen, Yunyun, Suyu,Liaoshan

## Slide 20: Laser test ： timing resolution study
Preliminary irradiation results
  Time resolution of NDL LGAD is slightly worse after 100kGy

## Slide 21: ASIC for fast timing detector
To design ASIC for fast timing detector
  Need to handle jitter, Time walk (TW) and TDC uncertainty
  record Time of arrival (TOA)and Time over Threshold (TOT)
  Correction for Time walk, precision within 10ps
Time walk correction with TOA and TOT
Reduce capacitance to reduce jitter
From ATLAS

## Slide 22: ATLAS HGTD Module
Full size Module :1 LGAD + 2 ASIC
    15x30 channels
    2cm x 4cm
Existing module
    5x5 channels
    Built by IHEP
bump-bonding
Wire-bonding
HGTD module
Assembled in IHEP
LGAD
ASIC

## Slide 23: HGTD detector Module R & D
IHEP assembled first batch of HGTD modules with ALTIROC1_v2
IHEP modules showed good performance in DESY beam test
  35ps time resolution in module level
HGTD module prototypes assembled in IHEP
IHEP module time resolution
In DESY 2019 test beam
performance
2019 DESY beam test for HGTD modules

## Slide 24: Future 4D LGAD
LGAD we have now
One gain layer per pixel
Relative large dead area
Spatial resolution is not good
LGAD in the future:
Uniform gain layer
Small dead area
Both time and spatial resolution

## Slide 25: Summary
New foundry of ultra-fast LGAD sensor in China
  Novel device lab (NDL) in Beijing Normal university
  30ps time resolution in beam test and beta tests
    ~10ps in jitter term , Landau term dominated
Irradiation hardness of NDL has been tested
  It meets CEPC requirements
Next step:
  Beam test to verify its K/pi separation power

## Slide 26: Low-Gain-Avalanche-detector
Landau Noise term:
  Signal fluctuation due to non-uniform charge deposition
  Minimized by reducing thickness of the sensor (50um)
Time walk
  corrected using the amplitude
  estimate with the time over threshold (TOT).
Jitter
  Need gain to increase S/N
  Need thin detector to decrease trise

## Slide 27: Time resolution vs gain in 5x5 NDL LGAD
Pico-second laser measurement
  The power of the laser is reduced to simulate MIP
  Jitter term can reach 20ps in this laser tests
    PS: Landau term can not be evaluated in laser test

## Slide 28: Inter-pad resistance
Measure the resistance between neighbor pad in 2x2 and 5x5 LGAD
  HPK type 3.2 (5x5) sensors showed good inter-pad isolation after irradiation
  NDL 2x2 sensors :
    6GR design has better Inter-pad resistance than 2GR design after irradiation.
From Yunyun
pad1
pad2
pad3
pad4

## Slide 29: Doping profile Vs Flence
By Tao Yang

## Slide 30: fast readout ASIC R & D
Fast readout ASIC (ALTIROC) R & D is one of the key for HGTD Project
  TDC Time resolution is better than 10ps
  Radiation hard electronics: >200MRad
IHEP is one of key institute in ALTIROC design team
  leading part of ALTIROC2 digital blocks design, will contribute to radiation hard design
  Leading chip emulator development