## Slide 2: SCRF From HEPL to year 2000
“Livingston Plot” from Hasan Padamsee

## Slide 3: First Industrial Production in Japan (1988 – 1995)
The first mass-production of SRF Cavities in the world
SRF Cavity for TRISTAN at KEK
Bulk-Nb - 508MHz - 5-Cell Cavity
32 SRF cavities were fabricated by Mitsubishi and operated in TRISTAN

## Slide 4: Large Scale Production: CEBAF & LEP II
LEP II @ CERN
32 bulk niobium cavities
  Limited to 5 MV/m
  Poor material and inclusions
256 sputtered cavities
  Magnetron-sputtering of Nb on Cu
  Completely done by industry
  Field improved with time
  <Eacc> = 7.8 MV/m (Cryo-limited)
352 MHz, Lact=1.7 m
1.5 GHz, Lact=0.5 m
5-cell cavities
4-cell cavities
CEBAF @ TJNAF
338 bulk niobium cavities
  Produced by industry
  Processed at TJNAF in a dedicated infrastructure

## Slide 5: A great success for LEP II
96 GeV:
Mean Nb/Cu
6.1 MV/m
100 GeV: 3500MV
Mean Nb/Cu
6.9 MV/m
104 GeV: 3666MV
Mean Nb/Cu
7.5 MV/m
design
Accelerating Field Evolution with time
Final energy reach
limited by cryogenic
from G. Geschonke’s Poster for the ITRP visit to DESY

## Slide 6: A great success for CEBAF
Lost Time Totals June'97-May'01
1.5 % in FY 01
0.0 % in FY 01

## Slide 7: TRISTAN SRF from KEK to MHI
KEK 1981
1995

## Slide 8: Lessons from CEBAF, LEP2 and TRISTAN
Use of the best niobium (and copper) allowable in the market at the time
Industrial fabrication of cavity components with high level quality control
Assembly of cavity components by Industry via Electron Beam Welding in clean vacuum
Use of ultra pure water for all intermediate cleaning
Use of close loop chemistry with all parameters specified and controlled
Cavity completion in Class 100 Clean Room
  Final cleaning and drying (UV for bacteria and on line resistivity control)
  Integration of cavity ancillaries in ISO4 clean room
That is
New level on Quality Control

## Slide 9
1.3 GHz multicell cavities

## Slide 10: The TESLA Challenge: SCRF Linear Collider
TESLA Collaboration set up at DESY
1992
9-cell, 1.3 GHz
Eacc = 25 MV/m Cost/MV = LEP/20

## Slide 11: Learning Curve with BCP
3 cavity productions from 4 European industries: Accel, Cerca, Dornier, Zanon
4th production of 30 cavities to define Quality Control for Industrialization
BCP = Buffered Chemical Polishing
Module performance in the TTF LINAC
Improved welding
Niobium quality control
<Eacc> @ Q0  1010
<Eacc> @ Q0  1010
<1997>
<1999>
<2001>

## Slide 12: 3rd cavity production with BCP – TESLA TDR ref.
TESLA 500 specs:
24.3 MV/m @ Q0 = 5  109
Year 2000

## Slide 13: Two major contributions to rise the limits
In-Situ Baking (120-140 °C) from CEA-Saclay (Bernard Visentin)
  Cures Q-drop at High Field
    Formation of a uniform Nb2O5, dielectric, layer on the surface
      Reduction of the normal conducting dissipation from NbO and NbO2
    Diffusion of the high oxygen concentration in the superconducting layer
      Better BCS performances, i.e. lower surface resistance
Electro-polishing (EP) from KEK (Kenji Saito)
  Improves field emission and maximum field
    Much smoother surface, less local field enhancement
      Better cleaning with high pressure water rinsing
      Q-drop cure by in-situ baking more efffective
      High temperature (1400 °C) heat treatment avoidable

## Slide 14: Results on AC70 – 1 (2004)
TESLA 800 specs:
35 MV/m @ Q0 = 5  109
EP at the new DESY plan 800°C annealing 120°C Backing

## Slide 15: European XFEL Cavity Production - 1
At the end of the long prequalification process (TTF, FLASH, ILC,…)
Ettore Zanon, EZ & Research Instruments, RI
were contracted at the end 2010 to produce each
8 Cavities for infrastructure rump/up and qualification
  4 Dummy CVs (DCV), 4 Reference CVs (RCV)
280 XFEL type series cavities (first 8 are PCV)
12 ILC HiGrade cavities
Additional 120 cavities allocated end 2012 to each companiy
Nb & NbTi supplied by DESY
Production precisely following detailed specifications which also include the exact definition of infrastructure to be used (build to print)
Final treatment after main EP: final EP for RI / flash BCP for EZ

## Slide 16: European XFEL Cavity Production - 2
No performance guaranty by the vendors, i.e. the risk of unexpected low gradient or field emission is taken over by XFEL/DESY (responsibility for re-treatment).
Goal: average usable XFEL gradient 23.6 MV/m at Q0=1x1010,
X-Rays <1x10-2mGy/min
First series cavities (PCV) to be delivered end 2012 – begin 2013
All cavities to be delivered till end 2014 – begin 2015
Delivery rate: about 8 CVs/week (4/each vendor)
Supervision of the CV production: DESY & INFN/LASA

## Slide 17: Surface Treatments from Prototypes

## Slide 18: Part of the Cavity Infrastructure at EZ

## Slide 19: E-XFEL experience on cavity production rate
2013
2014
2015
EZ cavity production udated on May 6th, 2015

## Slide 20: E-XFEL: Usable Installed Voltage

## Slide 21: 1.3 GHz E-XFEL cavities «as received»
EZ
RI
EZ
RI
EP
BCP

## Slide 22: As Received Usable Gradient
Include operations spec
  Q0 ≥ 1×1010
  FE threshold (X-ray)
 Usable Gradient

## Slide 23: Final performance: Eacc Total after 313 retreatments performed on 237 of the 831 cavities
Before:
E usable 27.7 ± 7.2 [MV/m]
(RI): E usable 29.0 ± 7.3 [MV/m])
(EZ): E usable 26.4 ± 6.6 [MV/m])
After:
E usable 29.8 ± 5.1 [MV/m]
(RI): E usable 31.2 ± 5.2 [MV/m])
(EZ): E usable 28.6 ± 4.8 [MV/m])
Before:
E max 31.4 ± 6.8 [MV/m]
(RI): E max 33.0 ± 6.5 [MV/m])
(EZ): E max 29.8 ± 6.6 [MV/m])
After:
E max 33.0 ± 4.8 [MV/m]
(RI): E max 34.7 ± 4.4 [MV/m])
(EZ): E max 31.5 ± 4.9 [MV/m])

## Slide 24: Final performance: Q0 Total after 313 retreatments performed on 237 of the 831 cavities
Before:
Q0 @ 23.6 MV/m 1.31 ± 0.26 [1.1010]
(RI): Q0 @ 23.6 MV/m 1.29 ± 0.24 [1.1010])
(EZ): Q0 @ 23.6 MV/m 1.34 ± 0.28 [1.1010])
After:
Q0 @ 23.6 MV/m 1.37 ± 0.25 [1.1010]
(RI): Q0 @ 23.6 MV/m 1.34 ± 0.22 [1.1010])
(EZ): Q0 @ 23.6 MV/m 1.41 ± 0.26 [1.1010])
Before :
Q0 @ 4 MV/m 2.15 ± 0.32 [1.1010]
(RI): Q0 @ 4 MV/m 2.11 ± 0.32 [1.1010])
(EZ): Q0 @ 4 MV/m 2.18 ± 0.32 [1.1010])
After:
Q0 @ 4 MV/m 2.23 ± 0.34 [1.1010]
(RI): Q0 @ 4 MV/m 2.21 ± 0.34 [1.1010])
(EZ): Q0 @ 4 MV/m 2.26 ± 0.33 [1.1010])

## Slide 25: Some Considerations from the E-XFEL
Industry, once trained, is doing as well as the lab behind
but with a better yield
Results obtained are very close to those available at the time of the ITRP: 15 years ago
  Results depend on the technology applied
  The complete cycle in Industry improves the yield, but not dramatically
The option of a second treatment is still mandatory to improve the yield. That’s very expensive
  HPR is usually sufficient, flash BCP can be required, EP is excluded (HT installed)
  Second treatment is improving the yield, both for high field and field emission

## Slide 26: 3rd cavity production with BCP – TESLA TDR ref.
TESLA 500 specs:
24.3 MV/m @ Q0 = 5  109
Year 2000

## Slide 27: High Q - High Gradiend
Since ninties TESLA/ILC pushed for High Gradient
All CW applications are now asking for high Q
With a percent duty cycle the maximum usable gradient is a crucial cost driver
With CW operation cryogenisc is the limiting factor
ElectroPolishing - Zero B Field - Fast Cooldown Nitrogen Doping - Infusion - Large Grain - ……

## Slide 28: The “strange effect” of Nitrogen Doping
High Q0 for CW (FermiLab & JLab)
  For CW operation Cryogenics is a significant cost driver that limits the usable accelerating field
  Once fixed machine energy gain and cavity geometry the dissipated power at cryogenic temperature is directly proportional to (Eacc)2 and inversely to Q0.
  CW needs high Q0 @ moderate field
Q0 vs. Eacc – JLab test 1 & 2 and FNAL
Ari D. Palczewski
A. Grassellino, SRF Materials Workshop 2012
T = 2 K
2

## Slide 29: High Q and High Gradient
Two main research directions to push high Q at high gradients:
  High temperature ( 800C) nitrogen doping
  Low temperature treatments ( ~ 50C-200C) with or without nitrogen
    With increasing importance of cooldown studies/details in the whole temperature range ~300->2K
A possible common matrix that ties it all together: nano - hydrides?
Theoretical advancements and path forward
A. Grassellino et al.

## Slide 30: State of the art (high Q and G @ 1.3 GHz, 2K)
Q > 3 1010 @35 MV/m with N doping
Q > 1 1010 at 49 MV/m (Bpk = 210 mT) with 75/120C bake
A. Grassellino et al.
But: moderate reproducibility and material dependent

## Slide 31: From Pulsed E-XFEL to CW LCLS II
EZ & RI produced all the 1.3 GHz cavities for LCLS II – phase I, including final treatment and Nitrogen doping
All the cryomodules, from XFEL drawing modified for CW, have been produced in China by Wuxi
DOE subscribed the high nominal value for the cavity Qo (as promised by the successful application of the nitrogen doping) but doubled the cryoplant: just in case
Big effort to successfully adopt a technology that was still at the R&D phase
Cavity treatments and criomodule/cryogenics design are going together: deep magnetic igene and fast cool down

## Slide 32: The LCLS-II Challange from SRF2019 (Marc Ross)
CEBAF (94) LEP2 (99) LCLS-II (2021) HE (2026)
Three large CW Superconducting linacs:
Substantial investment in CW SRF
Parameter | CEBAF 1994 | LEP2 1999 | LCLS-II 2021 | LCLS-II-HE 2026
N_cav | 338 | 288 | 280 | 440
E_acc (MV/m) | 7.5 | 7.2 | 18.5 | 20.8
Meters of SRF | 169 | 490 | 296 | 466
E_tot (GeV) | 1.2 | 3.6 | 4.6 | 8.6
<Q0> | 4.0e9 | 3.2e9 | 2.7e10 | 2.7e10
f (MHz) | 1497 | 352 | 1300 | 1300
Temp (K) | 2.08 | 4.5 | 2.0 | 2.0
Heat Load (kW) | 5 | 53 | 3.7 | 7.3
Heat Load kW/GeV | 4.2 | 14.7* | 0.8 | 0.8
* @4.5K. Divide by 3.5 to convert to equivalent load at 2 K, (4.2 for LEP2) |  |  |  | 

## Slide 33: LCLS-II cavity data from SRF2019 (Marc Ross)
16
Vertical Test
Fermilab VT / year
200
100
E_acc
Q0
Testing Complete 07.2019
MOP044 Gonnella
FRCAA3 Gonnella
>19 MV/m
 Pass

## Slide 34: LCLS-II cryomodule data from SRF2019 (Marc Ross)
Typical Performance Summary (F-17, 04.2019)
 | VTS |  |  | CMTF Test |  |  |  | 
Cavity | Eacc* [MV/m] | FE onset | Q0@16MV/m | Max** Gradient [MV/m] | Usable Gradient*** [MV/m] | FE onset [MV/m] | Q0 @16MV/m 2K @ 30 g/s | Material
CAV0540 | 21.4 | none | 2.8E+10 | 20.5 | 20.5 | none | 3.19E+10 | TD 200/900
CAV0530 | 20.6 | 24 | 2.9E+10 | 19 | 17 | none | 2.56E+10 | TD 200/900
CAV0533 | 25 | none | 3.0E+10 | 18.5 | 18.5 | none | 3.22E+10 | TD 200/900
CAV0529 | 19 | none | 3.2E+10 | 18.5 | 18 | none | 3.16E+10 | TD 200/900
CAV0525 | 19.5 | none | 3.3E+10 | 19 | 17 | none | 3.84E+10 | TD 200/900
CAV0535 | 25.7 | none | 3.5E+10 | 19 | 18.5 | none | 3.77E+10 | TD 200/900
CAV0067 | 18.8 | none | 3.4E+10 | 19 | 19 | none | 3.44E+10 | NX-C, 200/975
CAV0517 | 18.8 | none | 3.0E+10 | 10 | 7.1 | 6 | 2.12E+10† | TD 200/900
Average | 21.1 |  | 3.13E+10 | 17.9 | 16.9 |  | 3.16E+10 | 
Total Voltage | 175.2 |  |  | 148.9 | 140.7 |  |  | 
Marc Ross @ SRF2019

## Slide 35: LCLS-II: Usable Gradient
Marc Ross @ SRF2019

## Slide 36: LCLS-II: The effect of Infrastructure
Marc Ross @ SRF2019

## Slide 37: Some open Questions
Marc Ross @ SRF2019

## Slide 38: Doping and the mistery of nano-hydrides
Pre-HF Soak
Post-HF Soak
NL115
3N60
NL115
3N60
NL115
HF 1hr
NL115
HF 1hr
NL115
HF 1hr
NL115
3N60
Nb Nitration Compared to Nb Nitration + HF 1 hr Rinse

## Slide 39: The effect of HF Soaking

## Slide 40: Abaut gas on surfaces ander vacuum

## Slide 41: “as received” materials (cross-section)
ATI -good flux expulsion- Ningxia -bad flux expulsion-
Material that shows good flux expulsion properties
(after annealing at 900C) has larger grain in the “as received” condition
Material with bad
flux expulsion properties shows small grains, many with high level of local misorientation
Band contour map w GBs misorientation
Band contour map w GBs misorientation
Local misorientation map
Local misorientation map
From Martina Martinetto at SRF 2019

## Slide 42: Large Grain Niobium, the DESY experience
Large grain Nb (proposed at JLab)
  Should reduce the material cost by 20-30%
  Should simplify the surface treatments
  Mechanics and PED more delicate
  Results comparable to those with fine grain
A variety of cavity have been built in many labs
Very good results have been obtained in single and multi-cell cavity at different frequency
Large grain
Fine grain
Best Results @ DESY
© Waldemar Singer

## Slide 43: Promissing resulta from Peking University
SRF2017
Efforts for 9-cell cavities at PKU (collaboration with HIT)
Cavity | Nb | Eacc (MV/m) | Q @ Emax | Q @ 16MV/m
PKU1 | FG | 23.0 | 6.0E09 | 1.1E10
PKU2 | LG | 22.4 | 2.2E10 | 2.0E10
PKU3 | FG | 28.6 | 4.0E09 | 7.0E09
PKU4 | LG | 32.6 | 1.0E10 | 1.6E10
Eacc: 32.6MV/m, Q0:1E10 (1.8K)
Reach ILC requirement
Eacc: 22.4 MV/m,
Q0=2E10 @ 20 MV/m, 2K

## Slide 44: Ingot Slicing from LASA experience
CBMM ingot. Ø=480 mm
RRR>300
Wire sawing with oxygen
Protection @Heraeus
25 (x2) 4.675 mm slices
produced:
3D rendering of ingot inner structure
From slices grain boundary pattern.
GB displace but «topological» structure remains nearly unaltered.

## Slide 45: 2 ESS-like LG Cavitie Tested at LASA
December 2016 & October 2019 - Good Q0 but limited by quench

## Slide 46
650 MHz multicell cavities

## Slide 47: INFN, b = 067, ESS cavities as a reference (BCP)
37 out of 38 cavities produced, 14 jacketed
Total of 11 cavities already qualified at DESY
On average, Q0 at 16.7 MV/m at 1.8 1010
Soft multipacting easily processed around 10-12 MV/m as expected
ESS insert at AMTF
Scaling R/Q and frequency to 650 MHZ @ b=1 a Q0 = 3-4 1010 is expected @ 17 MV/m

## Slide 48: The 650 MHz elliptical cavities for PIP-II
LB650
HB650
 | LB650 | HB650
# cavities | 36 | 24
Q0 | 2.3e10 | 3.2e10
Rs (nW) | 8.4 | 8.1
Eacc (MV/m) | 16.7 | 19
Bpk (mT) | 73.7 | 73.9
b = 0.61
b = 0.90

## Slide 49: By next Summer new experience for PIP-II
INFN LB650 RF Design rationales:
Cell coupling kcc optimized assuming TESLA-type cavity as a reference, of the quantity N2/(βkcc), where N is number of cells, β relative velocity. It models field-flatness sensitivity to cell frequency errors.
End Cell frequency tuning achieved by increasing the diameter of the whole terminal cell thus preserving its round shape and symmetry.
Maximize G factor while preserving sidewall angle at 2° avoiding potentially negative value during the cavity field flatness tuning stage.
Achieve a large frequency separation between π and 4/5 π modes.
Single stiffening rings at both end and inner cells, preserving manufacturing quality and tunability with respect to a double stiffener.
INFN LB650 for PIP-II, cold cavity | 
βgeometric | 0.61
Frequency | 650 MHz
Number of cells | 5
Iris diameter | 88 mm
Cell-to-cell coupling, kcc | 0.95 %
Frequency separation π-4π/5 | 0.57 MHz
Eq. diameter - IC | 389.8 mm
Eq. diameter - EC | 392.1 mm
Wall angle – Inner & End cells | 2 °
Effective length (10*Lhc) | 704 mm
Optimum beta βopt | 0.65
Epeak/Eacc @ βopt | 2.40
Bpeak/Eacc @ βopt | 4.48 mT/(MV/m)
R/Q @ βopt | 340 Ω
G @ βopt | 193 Ω
Inner cells stiffening radius | 90 mm
External cells stiffening radius | 90 mm
Wall thickness | 4.2 mm
Longitudinal stiffness | 1.8 kN/mm
Longitudinal frequency sensitivity | 250 kHz/mm
LFD coefficient kext at 40 kN/mm | -1.4 Hz/(MV/m)2
Pressure sensitivity kext at 40 kN/mm | -11 Hz/mbar
Maximum Pressure VM stress at 50 MPa | 2.9 bar
Maximum Displacement VM stress at 50 MPa | 1.5 mm

## Slide 50: EP Qualification on single cell – 5-cell next Spring
Treatment trial
Charge removal: 1200 kC. Avg. removal of 60 mm. 7 hours
Acid chilling if temperature on beam tubes is >25°C
External water cooling during the whole treatment
Continuous measurement of thickness (by US thickness gage placed on cavity wall) and temperature (by thermocouple sensors)
15 V voltage (in the polishing zone of V-I curve)
64 mm avg removal (0.15 mm/min)
51 kHz frequency variation (0.79 kHz/mm)
current is the 30-40 A range
Chart: Removal after 7 hours treatment
| 1 | 2 | 3 | 4 | 5 | 7 | 8 | 9 | 10 | 11
removal | 72.9167 | 78.1667 | 74.75 | 64.5 | 45.0833 | 44.4167 | 80.3333 | 82.0833 | 74.3333 | 94.0833

## Slide 51: Results from FermiLab – 5-cell, b = 0.9
Quench field improved from 20 to 24 MV/m by adding 3um of cold EP
Cavity limited by FE at ~23MV/m, quench field may be higher
Higher Q most likely due to better field compensation
Quench field improvement due to cold EP
2/6 N-doping + 7um EP + xxx cold EP
2/6 N-doping + xxx cold EP
Martina Marinello: private communication

## Slide 52: Some Considerations for the Future
The successful large scale production of SRF components for the European XFEL pushed toward new frontiers
Several labs are investing on R&D to improve accelerating gradient and quality factor
A few very exciting results have been obtained with a reasonable reproducibility
LCLS-II is now the new reference with pros and cons
The results dependence from the bulk material producer and from the production batch is still much to high
Higher Eacc and Qo design parameters need more stable results and completely understood parameters
Deep scientific control on the niobium production is becoming a unavoidable must